## Slide 1: Theoretical Models of Flux Expulsion and Dissipation
Mattia Checchin
15 Nov 2017
TTC Topical Workshop, FNAL

## Slide 2: Trapped flux surface resistance
⇒ temperature-dependent part of the surface resistance
⇒ intrinsic residual resistance
Trapped flux surface resistance
—flux trapping efficiency
—trapped flux sensitivity
—external magnetic field
H. F. Hess et al., Phys. Rev. Lett. 62, 214 (1989)
Cooldown
Pinning points
Trapped vortices

## Slide 3
Flux Trapping Efficiency
——

## Slide 4: Thermodynamic force during cooldown
We can define the thermodynamic force acting on the vortex as:
The Gibbs free energy density defines the stability of vortices in the SC:
Meissner State
Mixed State
Meissner State
Mixed
State

## Slide 5: Critical thermal gradient for expulsion
The minimum thermal gradient needed to expel vortices is the critical thermal gradient :
The pinning force acting against the expulsion is defined in terms of critical current density :
Meissner State
Mixed State
Pinning point

## Slide 6: Statistical definition of trapping efficiency
The probability of expelling vortices with the thermal gradient is
The trapping efficiency is function of :
The trapped field is then:
For TESLA shape

## Slide 7: Comparison with experimental data
Cavity name | 
CBMM | 0.3
ACC002 | 1.6
Cavity name | 
CBMM | 0.3
ACC002 | 1.6
Magnetization measurements1,2 of niobium and niobium films close to show .
The model returns in agreement with the literature values:
M. Martinello, M. Checchin et al., to be published
S. Posen et al., J. Appl. Phys. 119, 213903 (2016)
1 G. Park, C. E. Cunningham and B. Cabrera, Phys. Rev. Lett. 68, 12 (1992)
2 L. H. Allen and J. H. Claassen, Phys. Rev. B 39, 4 (1989)
Lower

## Slide 8
Trapped Flux Sensitivity
——

## Slide 9: Trapped flux sensitivity at 1.3 GHz
Trapped flux sensitivity:
Non-monotonic trend of as a function of mean-free-path
  M. Martinello et al., App. Phys. Lett. 109, 062601 (2016)
  D. Gonnella et al., J. App. Phys. 119, 073904 (2016)
N-doping cavities present higher sensitivity than standard treated cavities
Sensitivity is dependent on the accelerating gradient
  C. Benvenuti et al., Physica C 316, 153 (1999)
  M. Martinello et al., App. Phys. Lett. 109, 062601 (2016)
  D. Hall et al., IPAC 2017

## Slide 10: Sensitivity as a function of frequency
  M. Martinello et al., SRF 2017
  M. Checchin et al., submitted to APL
120 C
EP/BCP
2/6 N-doped
Higher low field sensitivity for higher frequency cavities
2/6 N-doped have higher sensitivity, as expected form 1.3 GHz data
Steeper field dependence for high frequency cavities

## Slide 11: Mean-free-path dependent pinning potential
A vortex treated as a flexible flux line oscillating in the plane
2D pinning (elastic) potential:
  Lorentzian/Parabolic
  Dependent on mfp
  Dependent on distance from pinning center
The pinning center is localized at the depth from the RF surface
Pinning potential
Pinning center

## Slide 12: Motion equation of a vortex
Pinning Center
Pinning Center
The pinning constant is depth-dependent
  flexible vortex line
Multiple pinning centers per flux line can be considered
Solution valid for domain
The motion equation has form:

## Slide 13: Mean-free-path dependence
Pinning
regime
Flux-flow
regime
Small – pinning regime :
  increases with and
Large – flux-flow regime :
  decreases with , independent on
Pinning
  M. Checchin et al., Supercond. Sci. Technol. 30, 034003 (2017)
  M. Martinello et al., App. Phys. Lett. 109, 062601 (2016)

## Slide 14: Frequency dependence
– pinning regime:
– flux-flow regime:
Intermediate :
  the frequency dependence is rather complex!
As increases:
  higher peak value
  peak at lower mfp values
  M. Checchin et al., submitted to APL
Pinning
regime
Flux-flow
regime

## Slide 15: Good agreement between data and models
  M. Checchin et al., Supercond. Sci. Technol. 30, 034003 (2017)
  M. Checchin et al., submitted to APL
  J. I. Gittleman and B. Rosenblum, Phys. Rev. Lett. 16, 734 (1966)
Point-like vortex approach
Flexible vortex line approach
Elastic vortex line approach
  A. Gurevich and G. Ciovati, Phys. Rev. B 87, 054502 (2013)
is not depinning frequency

## Slide 16: Dependence on the pinning center depth
Sensitivity dependent on the pinning site distance from the surface
  Bulk pinning does not affect the vortex oscillation
Pinning
Pinning
Pinning center

## Slide 17: Conclusions
Trapping Efficiency——bulk property:
  Balance of pinning and Gibbs free energy gradient at the interface between Meissner and mixed state
  Well described by a statistical argumentation
  Different type of pinning defects may be present
Trapped Flux Sensitivity——near-surface property:
  Two regimes of dissipation:
    Pinning regime, vortices constrained by pinning
      — increases if and
    Flux-flow regime , vortex motion counteracted by viscosity
      — decreases if , but independent on
  Frequency dependence:
    With same mean-free-path higher frequency cavities show higher sensitivity
    Steeper field dependence of for higher frequencies

## Slide 18
Thank you for your attention

## Slide 19: Distribution of pinning defects
Double distribution of pinning centers (e.g. dislocations + grain boundaries)
finite probability that vortices are not pinned
First plateau defined by the ratio of the two peaks’ area
Complete flux expulsion reached when is larger enough so that

## Slide 20: High T baking effects
After 1000 C
baking
High T baking effects:
Decreases the number of pinning points
  pdf narrowing
Smaller