## Slide 1: Flux Dissipation in Nb3Sn Films
Ryan Porter, Daniel Hall
Cornell University
Supported by:
U.S. DOE award DE-SC0008431.
This works make use of: Center for Bright Beams , NSF Award PHY-1549132

## Slide 2: Outline
Brief introduction
Loss from trapped flux during cooldown
  Ambient fields
  Thermal gradients
Possible flux entry without quench
Temperature “slip”
Conclusions

## Slide 3: Properties of Nb3Sn
Parameter | Niobium | Nb3Sn
Transition temperature | 9.2 K | 18 K
Superheating field | 219 mT | 425 mT
Energy gap Δ/kbTc | 1.8 | 2.2
λ at T = 0 K | 50 nm | 111 nm
ξ at T = 0 K | 22 nm | 4.2 nm
GL parameter κ | 2.3 | 26
Blue: tin
Red: niobium
Higher critical temperature
→ Operation at 4.2 K
Higher superheating field
→ Double the limit of niobium
Lower losses
Higher gradients
~90 MV/m

## Slide 4: Cornell Nb3Sn Program
We have a program at Cornell for creating Nb3Sn coatings
Coat Nb with 2-3 µm of Nb3Sn
  Vaporize tin in high temperature vacuum furnace
Can (currently) coat:
  samples
  single cells (≥ 1.3 GHz)

## Slide 5: Comparison to niobium
20× more efficient than Nb at 4.2 K!
Notes: This is 30 times more efficient than Nb at 4.2 K at useable gradients
This is the first time an “alternative” cavity has beaten niobium at useable gradients

## Slide 6
Losses from trapped magnetic Flux

## Slide 7: Breaking down the Q
0 nΩ
16 nΩ
Trapped flux
Thin film regions
BCS Resistance
Ambient fields
Thermal gradients
Surface resistance at 4.2 K and 10 MV/m

## Slide 8: Breaking down the Q
0 nΩ
16 nΩ
Trapped flux
Thin film regions
BCS Resistance
Ambient fields
Thermal gradients
Surface resistance at 4.2 K and 10 MV/m

## Slide 9: Thermal currents
Nb
Nb3Sn
HOT
COLD
S – Seebeck coefficient
Generated B field
Induced thermocurrent
Cooling in a small thermal gradient will prevent a large amount of trapped flux!

## Slide 10: Measuring losses from trapped flux
Want to characterize losses from trapped flux
  Helmholtz coil during cooldown to ambient magnetic flux
  Adjust cooling rate to change thermal gradient

## Slide 11: Losses from trapped flux

## Slide 12: Sensitivity with field
Notes: Define sensitivity

## Slide 13: Weak Pinning Scenario
A weak pinning model developed by Danilo Liarte and Jim Sethna discussed earlier
  Relevant takeaway:
Flux trapping sensitivity depends linearly with Brf
Flux trapping sensitivity depends on penetration depth
  Penetration depth depends on mean free path
  Could reduce Q-slope!
Notes: BCD 97

## Slide 14
Possible Flux Entry

## Slide 15: Localised quench
Nb3Sn cavities are limited by a quench to ~16MV/m
  Occurs at a thermal defect
What happens, thermally, right at the defect?

## Slide 16: Near quench behavior
Measure temperature of sensor near the quench point as field is increased
Sudden jumps in temperature
Temperature
Max Field
Time

## Slide 17: Near quench behaviour
The sudden nature of these jumps and hysteresis strongly suggests flux entry
2 K

## Slide 18: Jump heights
Jump heights from multiple cooldowns (rescaled so first jump heights are equal)
  Some changes due to calibration
  Quench or re-cool change when jumps occur

## Slide 19: Grain boundary flux penetration
Increasing current across boundary
Power dissipated
Ahmad Sheikhzada and Alex Gurevich
Physical Review B 95, 214507 (2017)
arXiv:1702.02843
Notes: Grain acts as Josephson Junction. Flux expands across whole boundary. Blocks Current.

## Slide 20: What is happening at the surface?
We cut out this region and examined it with microscopy
Nothing suspicious except cliff
  Rough Surface
  Field enhancement
Nb3Sn surface
Nb substrate grain boundary?

## Slide 21: Surface Roughness
Nb3Sn we create is rougher than electropolished Nb
  ~1 µm peak to peak
This causes large enhancement of the surface magnetic field

## Slide 22: Field Enhancement
1% of the surface has surface fields at least 50% higher than for a flat surface
  Possible that flux entry is occurring at a higher magnetic field than accelerating gradient suggests

## Slide 23
Temperature Slip

## Slide 24: Temperature Slip 2 K
Observe temperature “slip”
First seen at 2 K after many quench
Slip occurs at lower field than jump

## Slide 25: Temperature Slip 4.2 K
Seen at 4.2 K before and after quench
Sometimes 2 slips at 4.2 K

## Slide 26: Temperature Slip
Size of slip depends on field when slip occurs
Time of slip depends on filling time/Pf
Change after quench -> flux distribution matters

## Slide 27: Conclusions
Good Q requires shielding from ambient magnetic field and slow cooling rates
Observed jumps in temperature near quench site
  > quantized flux entry likely at grain boundary
Observed temperature slips in areas with high amounts of trapped flux
  > flux rearrangement?

## Slide 28: Acknowledgements
Prof. Matthias Liepe
Prof. Tomas Arias
Prof. David A. Muller
Prof. James P. Sethna
Danilo Liarte
Daniel Hall
Paul Cueva
Nathan Sitaraman
James Maniscalco
James Sears
Greg Kulina
John Kaufman
Holly Conklin
Terri Gruber
with special thanks to
The Cornell Nb3Sn program is primarily supported by the U.S. Department of Energy