## Slide 1
Martina Martinello
TTC Topical Workshop – Pushing Cavity Performance Limits
15 Nov 2017
Frequency dependence of the BCS surface resistance at high fields

## Slide 2: RBCS(Eacc) at 1.3 GHz
From 1.3 GHz data we know that:
RBCS(Eacc) increases in regular niobium cavities (EP, BCP, 120C baking)
RBCS(Eacc) decreases in N-doped niobium cavities
A. Romanenko and A. Grassellino, Appl. Phys. Lett. 102, (2013)
A. Grassellino et al., Supercond. Sci. Technol. 26, 102001 (2013)

## Slide 3: RBCS(Eacc) at 1.3 GHz
A. Romanenko and A. Grassellino, Appl. Phys. Lett. 102, (2013)
A. Grassellino et al., Supercond. Sci. Technol. 26, 102001 (2013)
How do these field dependences change with the frequency?
From 1.3 GHz data we know that:
RBCS(Eacc) increases in regular niobium cavities (EP, BCP, 120C baking)
RBCS(Eacc) decreases in N-doped niobium cavities

## Slide 4: Analyzed Cavities
N-doping
EP/BCP
120C baking
1.3 GHz, 2 K
 | 650 MHz | 1.3 GHz | 2.6 GHz | 3.9 GHz
EP |  |  |  | 
BCP |  |  |  | 
120C baking |  |  |  | 
2/6 N-doping |  |  |  | 

## Slide 5: Data Analysis
For each cavity:
      Mean free path extrapolation: the mfp specifies the impurity content after each treatment
      Surface resistance decomposition:
BCS surface resistance at
: Trapped flux surface resistance
: Intrinsic residual resistance

## Slide 6: Data Analysis
For each cavity:
      Mean free path extrapolation: the mfp specifies the impurity content after each treatment
      Surface resistance decomposition:
BCS surface resistance at
: Trapped flux surface resistance
: Intrinsic residual resistance

## Slide 7: 1a. BCS Surface Resistance (650 MHz and 1.3 GHz)
Rres
Because of the exponential decreasing with T, RBCS at 1.5 K is negligible at low frequencies :
RBCS (2 K) can be calculated as:
1.3 GHz

## Slide 8: 1b. BCS Surface Resistance (2.6 and 3.9 GHz)
Fit of Rs (T) acquired at different Eacc values:
Accurate determination of Rres (Eacc)
At this point RBCS(2K) can be easily calculated:
2.6 GHz
2.6 GHz

## Slide 9: Field Dependence at Different Frequencies
Different thermal treatments were studied at different frequencies:
120 oC baking
BCP and EP
Nitrogen doping (2/6 recipe)

## Slide 10: 1. Normalized for 120 C Baking
T=2 K
T=2 K

## Slide 11: 1. Normalized for 120 C Baking
T=2 K
T=2 K

## Slide 12: 1. Normalized for 120 C Baking
T=2 K
T=2 K

## Slide 13: 1. Normalized for 120 C Baking
T=2 K
T=2 K

## Slide 14: 1. Normalized for 120 C Baking
At low field RBCS follows the w2 trend suggested by the Mattis-Bardeen theory
T=2 K

## Slide 15: Q-factor of 2.6 GHz at high field tends to the one at 1.3 GHz
120C baked cavities
Q-factor of 2.6 GHz cavity converge to the one at 1.3 GHz at high gradients
T=2 K

## Slide 16: Field Dependence at Different Frequencies
Different thermal treatments were studied at different frequencies:
120 oC baking
BCP and EP
Nitrogen doping (2/6 recipe)

## Slide 17: 2. Normalized for EP

## Slide 18: 2. Normalized for EP

## Slide 19: 2. Normalized for EP/BCP

## Slide 20: 2. Normalized for EP/BCP

## Slide 21: Anti Q-slope in BCP’d 3.9 GHz Cavities
T=2 K
anti Q-slope

## Slide 22: Anti Q-slope in BCP’d 3.9 GHz Cavities
T=2 K
anti Q-slope
Data from E-XFEL database
courtesy of V. Gubarev
also published in D. Sertore et al., Proc. of SRF 2015 MOPB077
anti Q-slope

## Slide 23: Field Dependence at Different Frequencies
Different thermal treatments were studied at different frequencies:
120 oC baking
BCP and EP
Nitrogen doping (2/6 recipe)

## Slide 24: 3. Normalized for N-doping
T=2 K

## Slide 25: 3. Normalized for N-doping
T=2 K
T=2 K

## Slide 26: 3. Normalized for N-doping
T=2 K
T=2 K

## Slide 27: 3. Normalized for N-doping
T=2 K
T=2 K

## Slide 28: Unprecedented Medium Field Q0 at 3.9 GHz
Q-factor of N-doped 3.9 GHz comparable to 120 C baked 1.3 GHz cavity at
T=2 K

## Slide 29: Summary on the frequency dependence of RBCS(Eacc)
The physical mechanism underneath the RBCS reversal has a stronger effect at high frequencies
The RBCS reversal, that has been considered the signature of the N-doped treatment, is actually visible also in clean Nb but at high frequency
On the other hand, N-doped cavities at low frequencies do not show the RBCS reversal observed at 1.3 GHz
EP/BCP
N-doping
120C baking

## Slide 30: Frequency Dependence NOT Related to QP Overheating
Current theoretical description of the N-doping phenomenon not in agreement with experimental findings
J. Maniscalco et al. in Proc. of IPAC 2017
Increasing frequency
T=2 K
Increasing frequency

## Slide 31: Non-equilibrium QP distribution enhances superconductivity
T. Kommers and J. Clarke,
Phys. Rev. Lett. 38, 1091 (1977)
1 G.M. Eliashberg, ZhETF Pis. Red. 11, 186 (1970)
2 J.-J. Chang and D. J. Scalapino, Phys. Rev. B 15, 2051 (1977)
3 D. J. Goldie and S. Withington, Supercond. Sci. Technol. 26, 015004 (2013)
The non-equilibrium quasiparticle distribution driven by microwave fields is shown to stimulate the superconductivity1,2,3:
increases with the RF field amplitude (absorbed power)

## Slide 32: Non-equilibrium QP distribution enhances superconductivity
T. Kommers and J. Clarke,
Phys. Rev. Lett. 38, 1091 (1977)
1 G.M. Eliashberg, ZhETF Pis. Red. 11, 186 (1970)
2 J.-J. Chang and D. J. Scalapino, Phys. Rev. B 15, 2051 (1977)
3 D. J. Goldie and S. Withington, Supercond. Sci. Technol. 26, 015004 (2013)
The non-equilibrium quasiparticle distribution driven by microwave fields is shown to stimulate the superconductivity1,2,3:
increases with the RF field amplitude (absorbed power)

## Slide 33: Thermal equilibrium distribution of quasiparticles

## Slide 34: Non-equilibrium distribution of quasiparticles
: electron-phonons inelastic scattering (relaxation) time
: quasi-particles recombination time
,
Condition for non-equilibrium SC:

## Slide 35: Non-equilibrium distribution of quasiparticles
: electron-phonons inelastic scattering (relaxation) time
: quasi-particles recombination time
N-doping (surface treatments in general) may modify and enhancing the non-equilibrium effects
,
Condition for non-equilibrium SC:

## Slide 36: Summary and Open Questions
RBCS(Eacc) shows a strong frequency dependence: high frequencies are favorable to lower RBCS at high field
The decreasing of RBCS(Eacc) can appear also in high-frequencies non-doped cavities and, vice versa, RBCS(Eacc) increases in low frequencies N-doped cavities
Non-equilibrium SC may qualitatively explain the decreasing of the surface resistance as a function of the field and its enhancement at higher frequencies
Can the presence of impurities modify the relaxation and recombination time of QPs? How could we measure it?

## Slide 37
Thank you for your attention!