## Slide 1: Collective weak pinning model of vortex dissipation in SRF cavities
Danilo Liarte,
James Sethna,
Daniel Hall,
Matthias Liepe
Cornell University
TTC Topical Workshop - RF Superconductivity: Pushing Cavity Performance Limits

## Slide 2: Outline
Introduction
Collective weak pinning
Results
Final remarks
a)
b)
c)

## Slide 3: Outline
Introduction
Collective weak pinning
Results
Final remarks
a)
b)
c)

## Slide 4: Gaining insight on trapped flux
Gurevich & Ciovati
PRB 2013

## Slide 5: Sensitivity of to trapped flux
Gonnella et al. J. Appl. Phys. 2016
Dependence on MFP (Gonnella)
Dependence on RF field (Hall)
Hall et al. IPAC 2017

## Slide 6: Outline
Introduction
Collective weak pinning
Results
Final remarks
a)
b)
c)

## Slide 7: fluctuations and collective weak pinning
For , a vortex can bend to find a favorable position in the pinning potential, cutting off the square-root growth of .
accumulated pinning force
Pinning f orces add up randomly; only fluctuations can pin the line.
viscous
Lorentz
pinning
elastic
Magnus
inertial

## Slide 8: fluctuations and collective weak pinning
viscous
Lorentz
pinning
elastic
Magnus
inertial
Pinning force & depinning current…
(cgs units)
A vortex breaks up into segments of size ; each will compete with the Lorentz force.

## Slide 9: Outline
Introduction
Collective weak pinning
Results
Final remarks
a)
b)
c)

## Slide 10: Collective weak pinning at low frequency Derivation and analytical solution
Lorentz
MF pinning
elastic
Solution for Nb3Sn at 20mT RF field and 1mA/µm2 depinning current
for
for

## Slide 11: Collective weak pinning at low frequency ‘Sanity’ tests
Amplitudes in y and z
Curvature radius
at the surface
Pinning length
‘Curvature radius’
at the surface
At 10 MHz
At 1.3GHz
Point-like force, collective weak pinning, BC…
Viscous dissipation term

## Slide 12: Dependence on RF field
The linear behavior is consistent with collective weak pinning (but not accurate)
There is a factor of 100 off in comparison with the experimental results. Viscous dissipation is needed.
DBL, Hall, Liepe, Sethna, in progress
U

## Slide 13: Collective weak pinning at low frequency ‘Sanity’ tests
Estimate density of impurities assuming
experimental value for
Individual
pinning force
Atomic scale

## Slide 14: Collective weak pinning at high frequency Simulated solution
viscous
Lorentz
MF pinning
elastic
At mT
At mT

## Slide 15: Sensitivity of to trapped flux as a function of the RF field
Simulation
Experiment (Hall)
At (black), 2 (red), 3 (blue), and 4mA/µm2 (green)

## Slide 16: Sensitivity of to trapped flux as a function of frequency
Simulation
Experiment (Oseroff)
Analytical curve
Square-root
Plateau

## Slide 17: Outline
Introduction
Collective weak pinning
Results
Final remarks
a)
b)
c)

## Slide 18: Conclusions and future work
Hysteretic losses might explain the dependence of the residual resistance sensitivity to trapped flux on the RF field.
Our approximations are consistent, though we predict dissipations larger than the experimental ones by a factor of about eight.
The collective weak-pinning model predicts three distinct regimes for the dissipation as a function of frequency: linear, square-root, and a plateau.
Simulations with explicit inclusion of impurities.
Large amplitudes, grain boundaries, and mixed (strong and weak pinning) scenarios.
Experimental check: do most trapped vortices lie perpendicular to the interface? (We have assumed vortices that are normally aligned with respect to the interface.)

## Slide 19: Acknowledgments
TTC Topical Workshop Committee, for the invitation.
The Sethna and the Liepe groups in Cornell.
The Center for Bright Beams SRF team.
Prof. Alex Gurevich, for useful consultation.
Financial support from the Center for Bright Beams.
TTC Topical Workshop - RF Superconductivity: Pushing Cavity Performance Limits