## Slide 1: Theoretical calculations of maximum fields in SRF cavities
Danilo Liarte, James Sethna, Daniel Hall, Matthias Liepe
Cornell University
Sam Posen
Fermilab
Mark Transtrum
Brigham Young University
Gianluigi Catelani
Peter Grünberg Institut
TTC Topical Workshop - RF Superconductivity: Pushing Cavity Performance Limits

## Slide 2: Surface energy barrier & vortex entry fields
Bean & Livingston, PRL 1964
DBL, Posen, Transtrum, Catelani, Liepe, Sethna, SUST 2017

## Slide 3: Stability analysis: the superheating field (Hsh)
In high-field applications, SRF cavities operate above Hc1, at the metastable Meissner state.
The Meissner state becomes unstable for fields above Hsh.
Sketch of a type II superconductor phase diagram
Kubo, SUST 2016

## Slide 4: Stability analysis: the superheating field
As a function of k (near Tc)
Ginzburg-Landau theory
As a function of T (at high k):
Eilenberger theory
Transtrum, Catelani, Sethna, PRB 2011
Kramer, PR 1968, etc…
Catelani & Sethna, PRB 2008

## Slide 5: Summary
Anisotropy
Disorder
Laminates
Final considerations

## Slide 6: Summary
Anisotropy
Disorder
Laminates
Final considerations

## Slide 7: Hsh is isotropic (near Tc) for new materials
Ginzburg-Landau theory: rescaling and change of coordinates map anisotropic systems into the isotropic one.
Hsh is isotropic for high-k materials (near Tc, including MgB2).
MgB2 is complicated (Bud’ko & Canfield, Phys. C 2015): two gaps, two distinct anisotropies (see bottom right) conflicting estimates.
DBL, Transtrum, Sethna, PRB 2016
Mass anisotropy
GL parameter

## Slide 8: Summary
Anisotropy
Disorder
Laminates
Final considerations

## Slide 9: Sn depleted regions and Nb3Sn quenches
Muller Group
(CBB)
Thomas Proslier
(Argonne)
A. Godecke: SUST 2006
Can the tin depleted regions (or something else) facilitate vortex nucleation?

## Slide 10: Cavity quenches and reliability
We predict a relation between critical temperature drop, defect sizes, and quench fields that is ‘consistent’ with experiments.
Gaussian disorder model: High-k materials are (almost) as ‘reliable’ to vortex nucleation by disorder as low-k materials.
The proximity to Hsh is dangerous.
DBL, Posen, Transtrum, Catelani, Liepe, Sethna, SUST 2017
Critical temperature profile that allows vortex nucleation in Nb3Sn
Quench field of 77mT

## Slide 11: Summary
Anisotropy
Disorder
Laminates
Final considerations

## Slide 12: Laminates
Kubo’s review (SUST 2016): multilayer coating. Advances in optimizing thickness and materials assessment.
Gurevich’s proposal (Appl. Phys. Lett. 2006): Can we use SIS structures to increase Hsh, and reduce the effects of flux penetration?
Sam Posen (FNAL)
Kubo, SUST 2016
Sam Posen’s simulations (SUST 2017): If there is a mechanism to prevent annihilation after each oscillation, one would expect large losses.

## Slide 13: Summary
Anisotropy
Disorder
Laminates
Final considerations

## Slide 14: Acknowledgments
TTC Topical Workshop Committee, for the invitation.
The Sethna and the Liepe groups in Cornell.
The Center for Bright Beams SRF team.
Prof. Alex Gurevich, for useful consultation.
Financial support from the Center for Bright Beams.
TTC Topical Workshop - RF Superconductivity: Pushing Cavity Performance Limits