## Slide 1
Alexander Romanenko
TTC Topical Meeting
17 Nov 2017
Understanding the Low Field Q Slope in SRF Cavities

## Slide 2: Outline
Low field Q slope
  Manifestation
  Previous studies/models/thoughts
  Importance for ultralow fields applications of high Q SRF cavities
Our recent studies
  Extending the measurement range to very low fields
    Saturation of the Q decrease
  Effect of the oxide growth
  Likely origin

## Slide 3: Low field Q slope
Low field Q slope

## Slide 4: Previous experimental data/studies
G. Ciovati, J. Appl. Phys. 96, 1591 (2004)
B. Visentin, Pushing the Limits 2006
1.37K
2K

## Slide 5: Previous experimental data/studies
The LFQS comes from residual
A. Romanenko and A. Grassellino, Appl. Phys. Lett. 102, 252603 (2013)

## Slide 6: Previous models/thoughts
Halbritter
  NbOx clusters inside the penetration depth
    Should show up in BCS part of Rs
Palmieri
  Two layers with top layer having penetration depth dependent on the rf field amplitude
Weingarten
  Weakly superconducting inclusions transitioning 2x per period
Rs ~ a/B2 + b
Rs ~ a/B2 + b

## Slide 7: Renewed (now practical) importance of the LFQS
A. Romanenko et al, Appl. Phys. Lett. 105, 234103 (2014)
1.3 GHz
1.5K
How will the best cavities we have behave at ultralow fields for various possible applications?
Quantum Computing
Dark sector searches
Gravitational effects
….

## Slide 8: LFQS present after all treatments
A. Grassellino et al, arXiv:1701.06077
Effect on low field Q?

## Slide 9
What is the cause of the low field Q slope and what happens with Q as we decrease the field further?

## Slide 10: Single shot measurements
Q > 1010 cannot be measured using standard network analyzer techniques
Instead -> decays from PLL state with bandpass filtering (10-1000 Hz around resonance) instead
QL=2pft

## Slide 11: Measurements towards quantum regime
T=1.5K
Now measured down to
<N> ~ 1010 photons
Low field Q slope stops below ~ 0.1 MV/m with
Q~3 x 1010
1.3 GHz
A. Romanenko and D. I. Schuster, https://arxiv.org/abs/1705.05982

## Slide 12: Various cavities/treatments investigated
Changes within penetration depth have little effect
Oxide growth/change -> strong increase in very low field dissipation
A. Romanenko and D. I. Schuster, https://arxiv.org/abs/1705.05982

## Slide 13: From 2D resonator world
J. Gao, PhD Thesis, Caltech, 2008
J. Zmuidzinas, Annu. Rev. Condens. Matter Phys. 2012. 3:169–214
Two level systems in the dielectric as a cause
Electric field effect: Martinis et al, Phys. Rev. Lett. 95, 210503 (2005)

## Slide 14: Electric field effect
f = 1.3 GHz, TM010 mode
Electric field amplitude

## Slide 15: Fit to TLS model
A. Romanenko and D. I. Schuster, https://arxiv.org/abs/1705.05982

## Slide 16: Effect of thicker oxide
A. Romanenko and D. I. Schuster, https://arxiv.org/abs/1705.05982
100 nm oxide added

## Slide 17
About 2 nOhms added in the whole range of fields > 0.2 MV/m

## Slide 18: Thicker oxide has a drastic effect at low fields
Nb
Nb2O5
5 nm
Nb
Nb2O5
100 nm
~9 nOhm added at low fields!
A. Romanenko and D. I. Schuster, https://arxiv.org/abs/1705.05982

## Slide 19: Exploring lower temperatures
Demonstration of T = 10 mK and <N> ~ 1 photon high Q in early 2018
Large dilution refrigerator capable of fitting up to 9-cell 1.3 GHz cavities is being installed
Advanced magnetic shielding
Extensive wiring for exploring all possible applications (quantum computing etc)
1 m
Allows to explore fundamental physics of residual resistance of SRF cavities (e.g. hydrides etc could turn SC at low enough T)

## Slide 20: Summary
Low field Q slope saturates below ~0.1 MV/m, Q remains high > 3e10
  Saturation field just below of what was explored in the past
    The key discovery was hiding behind the corner
Growing thicker oxide drastically increases the ultralow field surface resistance
  Much smaller but measurable, almost field-independent change at higher fields – also new, in the past oxide-induced residual resistance was only explored at <5 MV/m
The two above signatures point toward two-level systems in the amorphous Nb2O5 as a likely LFQS origin
Are there even more surprises at lower temperatures?
  Dilution refrigerator measurements upcoming