## Slide 1
Energy Loss from Dielectric Two-Level State (TLS) Defects
Robert McDermott University of Wisconsin
configurational states
eigenstates
general
double-well
potential for
TLS
tunneling D0
asymmetry D
high density of
defects in typical
amorphous dielectrics
DOS

## Slide 2
Anomalous Properties of Glasses at Low-T
Zeller & Pohl, PRB 4, 2029 (1971)
Pohl et al., RMP 74, 991 (2002)

## Slide 3
normalized lineshape function
electric dipole moment ed
driving electric field
Rabi frequency
transition rate
; constant density of defect states
tan d
E
V
Nonlinear Dissipation from Two-Level States (TLS)
See Amorphous Solids: Low-Temperature Properties,
ed. W. A. Phillips (Springer, Berlin, 1981).

## Slide 4: Dielectric Loss at Low Temperature
Huge loss at low power and low temperature!
decreasing microwave drive
approach:
systematic test of the
linear circuit
S21
dielectric under study

## Slide 5: Loss of PECVD Grown Dielectrics
<V2>1/2 (Volts)
tan d
hypothesis: high loss in SiO2 due to OH defects
TLS DOS x (dipole moment)2
Martinis et al., PRL 95, 210503 (2005)

## Slide 6
Candidate Qubit Dielectrics
Search for improved qubit dielectrics continues
a-Si:H has ~ factor 10 lower loss than SiNx
(defects overconstrained from fourfold bond coordination?)
Even in qubits with “simple” single-layer fabrication, lossy native oxides will
limit T1 times (2D transmon data compatible with surface loss)
Crystalline dielectrics should be much better
O’Connell et al., APL 92, 112903 (08)

## Slide 7
Scaling of Dielectric Loss with Device Dimension
total loss
participation ratio
Wenner et al., APL 99, 113513 (2011)

## Slide 8
3D Transmon
Embed qubit in BULK superconducting cavity:
lossy surface oxides make negligible contribution
Couple qubit to cavity via large (mm-scale)
dipole antenna – large vacuum Rabi splitting
despite reduced zero-point fields
Significant improvements in coherence
T1 to ~ 50 ms, T2 ~ 20 ms
Paik et al. PRL 107, 240501 (2011)

## Slide 9
Scaling of Dielectric Loss with Device Dimension
Dial et al., SST 29, 044001 (2016)
Chu et al., APL 109, 112601 (2016)

## Slide 10: SWAP Spectroscopy
Measurement of qubit decay rate (1/T1) as a function of frequency.
T1 suppression due to incoherent
coupling to resonant TLS
g : TLS-qubit coupling
G : TLS decay rate
Barends et al., PRL 111, 080502 (2013)

## Slide 11
Surface Treatment to Suppress TLS Loss
See Kumar et al.,
Origin and Reduction of 1/f Flux Noise
PR Applied 6, 041001 (2016)

## Slide 12: Swap Spectroscopy: Treated vs. Untreated Devices
Treated (B)
Reference (Q0)
Treated (A)
Reference (Q1)

## Slide 13: Swap Spectroscopy: Treated vs. Untreated Devices
Measure T1 over a large range of frequencies
Defects manifest as a Lorentzian peak in the decay rate.
The “T1 dropouts” contribute to the frequency crowding issue for frequency-tunable qubits
2 g2/G is the peak decay rate due to a resonant defect. The plot is the integral of all 2 g2/G > 0.05 MHz, across all measured samples, normalized to a GHz bandwidth.

## Slide 14
Summary
Loss from dielectric TLS a dominant decoherence mechanism
Bigger is better (3D is best), but lossy surfaces still contribute
Interface quality is critical
Some evidence that adsorbates contribute to dielectric loss; possible
approaches to mitigate loss are under investigation