## Slide 1
Investigation of radiation damage effect on advanced materials under different irradiation conditions
C. Accettura1,2, A. Bertarelli1, F. Carra1,A. Lechner1,E. Skordis1, S. Redaelli1, M. Tomut3, M. Beghi2, E. Besozzi2, N. Simos4
1CERN (Switzerland), 2Politecnico of Milan (Italy), 3GSI (Germany), 4BNL (USA)
7th High Power Targetry Workshop, East Lansing (USA) 04.06.2018

## Slide 2: Outline
Introduction
  Beam-matter interaction
  LHC and HL-LHC collimation system
  Expected radiation damage on HL-LHC collimators
  How to mimic this damage in other facilities
Irradiation tests on collimator materials
  Proton irradiation at BNL
  Ion irradiation at GSI
Future tests
Conclusions
Notes: Explain quick summary

## Slide 3: Beam-matter interaction
To investigate material behaviour under irradiation, it is important to consider the irradiation conditions
  High energy density fast interaction dynamic thermo-mechanical response
  Long-term irradiation radiation damage (microstructural changes induced by radiation) – main topic of this presentation
    Atomic displacement caused by charge particle-nucleus interaction (DPA)
    Gas production (H, He)
Consequences of long-term irradiation
  Degradation of thermal and electrical conductivity
  Radiation hardening
  Swelling
  Induced brittleness
Atomic displacement induced by an incident particle

## Slide 4: LHC collimation system
Focus on material for beam intercepting device of LHC, e.g. collimators
The energy stored in the beam is very high even a tiny fraction of it would induced quench in the superconductive magnet
Need of a protection system from unavoidable beam losses
LHC | 362 MJ
HL-LHC | 690 MJ
FCC | 8500 MJ
Actuation system
Jaw Cooling system
Vacuum Vessel
Particle Beam
CFC Jaw Block
~1.2 m
120 t Australian road train
v = 390 km/h
MoGr
MoGr with Mo coating
CuCD

## Slide 5: Molybdenum-carbide graphite
Collimators operate in an extreme environment: thermal shock (accidental beam impact), UHV, radiation, high geometrical stability C-based materials best compromise, but CFC and graphite have poor electrical conductivity for HL-LHC
A new composite material has been developed to enhance electrical conductivity and other properties MoGr baseline for collimators that will be installed in 2020 (LS2).
Powders compaction:
~90-95%vol graphite
~4.5%vol Mo
Ti doping
Sintering:
Mo-C reaction to form carbides
Enhancement of graphitization
Stress-relief treatment:
High temperature, pressure-less
J. Guardia et al., Development and properties of high thermal conductivity molybdenum-carbide-Graphite composites, 2018
 | In-plane | Perpendicular
Electrical conductivity [MS/m] | ~1 | ~0.08
Thermal Conductivity [W/(mK)] | 700 – 900 | ~50
CTE RT÷200 °C [10-6K-1] | 1.7 - 2.7 | 8 - 12
Flexural Strength [MPa] | 60 – 80 | 10 - 12
Specific Heat [J/(gK)] | 0.6 - 0.65 | 
Density [g/cm3] | 2.5 – 2.6 | 

## Slide 6: Thermo-mechanical response
Different successful experiences: HRTM14, HRTM23, HRTM36 thermo-mechanical response of BID materials and benchmarking of numerical simulation
HRTM36: assessment of thermo-mechanical properties of 18 materials, including metallic coatings (Mo, Cu, TiN) on CFC, MoGr, Graphite
Few mm Scratches in impact area impact on electrical conductivity seems acceptable
Dynamic response function of thermo-physical properties important to correlate to radiation damage-induced degradation
HRTM36 rotating barrel
A. Bertarelli et al., Dynamic testing and characterization of advanced materials in a new experiment at CERN HiRadMat facility, IPAC 2018
Impacted Cu and Mo coating on MoGr

## Slide 7: DPA for HL-LHC collimators
FLUKA simulations used to determine the expected DPA level after 12 years of HL-LHC (7 TeV protons)
Displacement Per Atom (DPA) in HL-LHC
(8x1016 protons lost in collimation system)
Material | Primary [DPA] | Secondary [DPA] | Mo coating [DPA]
MoGr | 0.3 | 4·10-4 | 1÷3·10-3
CFC | 0.12 | 1·10-4 | 

## Slide 8: How to mimic 7 TeV protons?
Goal: mimic radiation damage induced by 7 TeV protons in 12y and predict the properties degradation
Find a correlation (empirical and theoretical) between ion-induced and proton-induced radiation damage different facilities involved
EU project within HORIZON 2020
WP17.4 Simulation of irradiation effects and mitigation methods (A. Lechner, CERN-EN/STI)
Radiation damage investigation
GSI beamlines
BNL beamlines
Max 200 MeV protons
~5 MeV/u ions
CERN- HRMT beamlines
Thermo-mechanical response
440 GeV protons
Penetration | Superficial
Gas production | No
Activation | Zero-low ☺
Dose rate | High
GSI ion irradiation:
Notes: Dose rate conservative

## Slide 9: MoGr irradiation
Feb. 2014
mid 2013
July 2014
2016
5th generation
MG 5200-S
(2.65 g/cm3)
Fully molten
7.2%v Mo
46.4%v C-fibers (long+short)
2 annealing cycles:
1150°C
1300°C
4th generation
MG 3110-P
(2.67 g/cm3)
Fully molten
20%v Mo
40%v C-fibers (long+short)
6th generation
MG 6400-U
(2.63 g/cm3)
Fully molten
4.5%v Mo
NO C-fibers
Annealing 1800˚C
MG 6530-Aa
(2.5 g/cm3)
Fully molten
4.5%v Mo
5%v C-fibers (long only)
Annealing 1900°C
MG 6541-Aa
(2.5 g/cm3)
Fully molten
4.5%v Mo
0. %v Ti
5%v C-fibers (short only)
Annealing 1900°C
GSI (238U, 209Bi, 197Au, 152Sm, Ca, C ions)
7th generation
MG 6403-Aa
(g/cm3)
Fully molten
4.5%v Mo
%v Ti
NO C-fibers
mid 2015
E. Quaranta, EuCARD-2 WP11 Annual meeting, CERN 2017
3th generation
MG 1110-E
(3.7 g/cm3)
NOT fully molten
20%v Mo
40%v C-fibers (long+short)
BNL (p+, n)
BNL (p+, n)

## Slide 10: Proton irradiation at BNL
BLIP 2014:
MG1110E
1x1021 p/cm2 200MeV
6x1018 p+n/cm2 118 MeV
MG-1110E exposed to max. fluence of 1x1021 p/cm2
0.3 DPA
N. Simos et al. Radiation damage and thermal shock response of carbon-fiber-reinforced materials to intense high-energy proton beam, 2016
Serious structural degradation, already at 6x1018 p/cm2
Premature failure related to release of internal stresses and/or irradiation-induced transformation of the phase, not to poor graphitization (see XRD below)
Introduction of Ti to stabilize phase
Internal stresses release with pressure-less thermal treatment
BLIP 2016:
MG6530Aa, MG6403Fc, MG6403Ga
2x1020 p/cm2 200MeV
No macroscopic damage after first visual inspection  proof of similar damage threshold of other C/C composites

## Slide 11: Ion irradiation at GSI
C, Ca, Bi, Au, U
4.8 MeV/u-5.9 MeV/u
1x1011-5x1013 ions/cm2
Residual stresses accumulated during sintering lead to deformation starting from ~1x1013 ions/cm2
High temperature post-sintering treatment useful to increase fluence threshold for deformation
Grades with C-fibers suffer less electrical conductivity degradation
High temperature post-sintering treatment useful to increase fluence threshold for deformation (to be further investigated)
MG3110P irradiated with 208Bi at 4.8MeV/u
Electrical resistivity increase for different MoGr grades
MoGr grades:
- MG3110P No post-sintering treatment
- MG6400 PS treatment, no Ti, no fibers
- MG6530 PS treatment, no Ti, long fibers
- MG6541 PS treatment, Ti, short fibers
Notes: The beneficial effect of post-sintering high temperature treatment is confirmed by the test at GSI

## Slide 12: Future tests
New and ‘old’ grades of BID materials (also coated!) under test to reach DPA level ~HL-LHC:
  With high-energy proton at BLIP (CFC, MoGr) done (In the framework of raDIATE collaboration)
  With light ions at GSI (CFC,MoGr,Graphite) August 2018
Mo thin coating deposited on the bulk material (secondary collimators) investigation of thin film properties degradation:
  Adhesion
  Impedance
  CTE
  Thermal conductivity
Courtesy of M. Calviani, CERN EN-STI

## Slide 13: Next GSI irradiation campaign
48Ca, 4.8MeV/u
Φ=5·109 ion/(s·cm2)
f=10Hz, td=5 ms
 | DPA/hour | DPA collimator
Mo coating | ~5·10-5 | 1÷3·10-3
MoGr | ~1·10-3 | 0.3 (primary)
  DPA level in the coating similar to HL-LHC after 60h of irradiation
Sample dimensions: D=10mm, t=1mm
Sample dimensions:
20x2.5x0.1mm
~4·1014 ions/cm2
4 different fluences and different samples
To overcome thin penetration layer: 150μm thick sample for electrical conductivity measurements!

## Slide 14: Next GSI irradiation campaign
Thermo-mechanical simulation of 1mm thick disks (2D, axysymmetric)
Structural analysis
Transient thermal analysis
3h
ΔT~4°C
Tmax~100°C
Maximum stresses (mainly due to clamping) far from material limits

## Slide 15: Conclusions
Radiation damage to graphitic-based materials for HL-LHC Collimators (MoGr, CFC) could be assessed through irradiation tests campaigns under different conditions:
  200 MeV protons at BNL
  ~ 4.8 MeV/u ions at GSI
Several improvements in MoGr were implemented/validated thanks to these campaigns
  High temperature pressure-less thermal treatment to relieve internal stresses
  Ti-addition to stabilize Mo carbide phases
  C-fibers to help counteract electrical resistivity degradation
Ion irradiation at GSI has some drawbacks (no gas production, different dose rate), but it allows to:
  Reach high dpa in short time
  Perform analysis on not-activated sample
New experiment planned at GSI testing collimator materials also with metallic coating
  Evaluation of radiation-induced degradation of thermo-physical, electrical and micro-mechanical properties:
  thermal diffusivity, electrical conductivity, CTE, elastic properties, etc..
Future PIE of thin film metallic coatings irradiated at BNL, fundamental for HL-LHC secondary collimators

## Slide 16
Thank you for the attention!

## Slide 17: Collimator materials
BID material properties:
  High electrical conductivity
  High thermal conductivity
  Low CTE
  High ultimate strength
  UHV compatibility
  Radiation resistance
STRATEGY for new BID:
Graphite/diamond (low density, good thermal properties,..)+ metals (good mechanical properties)

## Slide 18: Coating CTE- Substrate Curvature
Mismatch between bulk and film CTE bending of the sample
Hp: T-independent E
- Optical system drives a 2D pattern of parallel laser beams
- CMOS sensor detects reflected beams
- Beam position function of the substrate-coating curvature

## Slide 19: Impedance measurements
Slide courtesy of N. Biancacci (CERN, BE/ABP)
Our standard method (long coil + IW2D simulations) is not suitable for small samples
Implemented analytical formulas to compute input impedance of a coil, theory known since 50y [1]
Extended to multi-layer in [2]
Allows any permittivity/permeability/conductivity below coil self resonance (neglects parasitic capacitance between wires and wire-substrate)
Successful measurements on BLIP spare samples.

## Slide 20: Microscopic investigation
Focused ion beam: qualitative idea of adhesion, bulk-coating interface

## Slide 21: Thermo-mechanical simulations
Input parameters
Φ=1010 ion/(s·cm2)
Eion=4.8 MeV/u
N=48 u/ion
f=5Hz
td=3.5 ms
Eimpact= Eion·N·Φ·f
Wimpact=
Wimpact=
Wimpact=
Φ=5·109 ion/(s·cm2)
Eion=4.8 MeV/u
N=48 u/ion
f=10Hz
td=5 ms