## Slide 1: Strain Reduction on the SNS Target Using Gas Injection
Wim Blokland, RAD/BST
Yun Liu, RAD/BST
Drew Winder, NTD/ISD
Notes: Abstract: SNS has successfully deployed and demonstrated mercury target Gas Injection Initial Implementation (GI3). Gas injection is expected to increase the performance and durability of target mercury vessels in two ways: (1) by reducing the dynamic stress resulting from the beam energy deposition, and (2) reducing cavitation erosion of the vessel inner wall. The system is operating safely and stably, and initial measurements with GI3 enabled have demonstrated location-dependent peak strain reductions of 10-60% on the mercury vessel. The effect of gas injection on cavitation damage erosion can only be assessed after T18 is sampled and measured in the spring of 2018. This seminar presents the details of the measurements on target T18 made with fiberoptic strain sensors, including some single-mode radiation resistant sensors developed at ORNL.

## Slide 2: Target Lifetime
Target reliability is a key part of SNS reliability and thus user experience
Target modules are expensive to build and dispose of
We want reliable targets that last as long as possible
Gas bubbles can act as shock absorbers to lessen the pressure wave, which reduces stress and influences cavitation behavior

## Slide 3: Gas Injection System
Mercury
Mercury+Gas
Gas is injected in the target into the main mercury supply channels
Sixty 8-micron orifices control the flow
Mercury turbulence shreds the gas to tiny bubbles
Sensors must fit in interstitial space

## Slide 4: Fiber Optic Strain Gauges
Sensors cannot interfere with the leak detection equipment
High bandwidth to measure fast pulse response
Radiation dose of 104 to 107 R before beam and 108 to 109 R/hr in operation
Sensors must be mounted in the ~3mm thick interstitial space between shroud and mercury vessel

## Slide 5: Sensor Installation
  2 thermocouples
  16 commercial MM strain gauges
  8 custom SM strain gauges
Bob Sangrey

## Slide 6: Studies
Pulse on demand:
  First all without gas then with gas injection as it takes hours for the gas to leave the mercury
  Single pulses at different energies (charge)
  Multi-pulse burst for 5 seconds at 600 kW
Gas injection ramp-up while running at 850 kW
Additional studies during production

## Slide 7: Pulse on Demand: Front Middle
Sensor 12
Gas off
Gas on

## Slide 8: Pulse on Demand: Front Middle Side
Beam Power (kW) | Strain Magnitude (me) |  | Strain Reduction (%)
 | Gas injection off | Gas injection on | 
200 | 31.73 | 23.06 | 27.3
400 | 70.06 | 51.50 | 26.5
600 | 118.76 | 70.95 | 40.3
800 | 151.79 | 90.09 | 40.6
1000 | 189.04 | 114.75 | 39.3
1200 | 219.97 | 137.64 | 37.4
Gas Off
Gas On
Gas Off Gas On
Sensor E

## Slide 9: Pulse on Demand: Front Middle of target T19
Sensor B
Sensor B
T19
Second target with gas injection

## Slide 10: Pulse on Demand: Accelerometer
The accelerometer on the target manifold sees a significant reduction while the accelerometer on the piping sees a smaller reduction (noise)
Gas off
Gas on

## Slide 11: Pulse on demand: Multi-pulse burst TC1 temperature
Thermocouples are too far back for a fast response but the sensor has conductive materials and we can not risk the leak detector
  In the future we will use a fiber based temperature sensor
Heat response is the same for gas injection off and on
TC2 is near the mercury inlet and doesn’t see any change during this time scale
TC1 & TC2

## Slide 12: Pulse on demand: Pulse Train
Sensor 12
5 second burst at 600 kW:
slow strain build up (heating)
Individual pulse impacts
Strain due to temperature
Strain due to beam impact
This shows that the sensor response in both gas off and gas on cases is the same!

## Slide 13: Gas Injection Ramp-Up: Back
Ramping the gas injection up during 850 kW beam.
Strain measured during the gas injection ramp up
Sensor 11
Sensor 15
Sensor 13

## Slide 14: Gas Injection Ramp-Up
Correlation between gas and strain
More gas means more reduction in strain
Sensor 11
Sensor 15
Sensor 13

## Slide 15: Gas Injection Ramp-Up: Side
Frequency spectrum changes as gas injection ramps up
Sensor 11

## Slide 16: Gas Injection Ramp-Up: Accelerator return line
More gas means more reduction in acceleration on mercury return line

## Slide 17: Strain measurement of 1.2 MW production beam
Conditions

## Slide 18: Strain profiles of 1.2 MW production beam

## Slide 19: What we want to do with the data over time
We have many GB of data to
  look for:
    Target structure changes
    Sensor attachment failures
    Sensor degradation
  help improve target modeling
We used cluster analysis on T18 during the ugly data Machine Learning contest
  Not much happened during T18
  Subtle target changes might be lost in long waveforms
   looking at preprocessing: e.g. ARMA modeling on T14 MM Data
T18 Clustering Result
400 kW
1000 kW
200 kW
100 kW
Simulation:
Measured : ▪
Cluster Distribution
Recording Index
Simulated and measured strain (T15 sensor 2, up front)

## Slide 20: What we want to do with the data over time
Before event
During event
Event
T14 Data (~4 weeks) from MM
sensors
Example to reduce data and capture relevant information
  ARMA model coefficients over time T14

## Slide 21: So what did we learn?
Strain is reduced and more gas can reduce even more
Temperature of the target not affected
Strange things happen to our
sensors
We can use machine learning to detect changes
T18 Results
(see Y. Liu talk on Thursday)