## Slide 1
Mattia Manzolaro
Design of High Temperature ISOL Targets
Mattia Manzolaro
on behalf of the SPES target group
(A. Andrighetto, S. Corradetti, M. Ballan, A. Monetti, G. Meneghetti, D. Scarpa, M. Rossignoli, F. D’Agostini, F. Borgna)

## Slide 2
SUMMARY
1- Introduction
2- The SPES target
3- Numerical models
4- On-line tests
5- Target material characterization @ HT
6- ISOL targets @ other facilities
7- Conclusions and future developments
Mattia Manzolaro slide 2/46

## Slide 3
SUMMARY
1- Introduction
2- The SPES target
3- Numerical models
4- On-line tests
5- Target material characterization @ HT
6- ISOL targets @ other facilities
7- Conclusions and future developments
Mattia Manzolaro slide 3/46

## Slide 4
1- Introduction: the ISOL (Isotope Separation On Line) technique
production target
transfer line
ion source
mass separator
charge breeder (1+ → n+)
& post accelerator
primary beam driver
high temperature
diffusion
effusion
+
+
+
+
+
high temperature
radiative heat transfer
P
Mattia Manzolaro slide 4/46

## Slide 5
1- Introduction: the SPES facility @ LNL
New infrastructure for:
Cyclotron
ISOL RIB Facility
Application Facility
SPES is: 1) A second generation ISOL RIB Facility (for neutron-rich radioactive ion beams)
2) An interdisciplinary Application Facility (for p,n applications)
Mattia Manzolaro slide 5/46

## Slide 6
1- Introduction: the ISOL RIB (Radioactive Ion Beam) facility
ISOL hall
40 MeV 200 µA primary proton beam
1+ RIB @ LE
to MRMS/HRMS
and n+ RIB @ HE
Mattia Manzolaro slide 6/46

## Slide 7
surface
ion source
SPES
production target
transfer line
proton
beam
1+
extraction electrode
IT = 700 A
IIS = 200 A
1- Introduction: the RIB bunker and the TIS (Target – Ion Source) system
Mattia Manzolaro slide 7/46

## Slide 8
SUMMARY
1- Introduction
2- The SPES target
3- Numerical models
4- On-line tests
5- Target material characterization @ HT
6- ISOL targets @ other facilities
7- Conclusions and future developments
Mattia Manzolaro slide 8/46

## Slide 9
40 MeV, 200 µA
proton beam
window (C)
disc (UCx)
dumper (C)
box (C)
heater (Ta)
2- The SPES target: general architecture and main characteristics
p energy: 40 MeV
p intensity: 200 µA
the whole target system must be operated at extremely high temperature (2000°C and more)
Mattia Manzolaro slide 9/46

## Slide 10
2- The SPES target: general architecture and main characteristics
Mattia Manzolaro slide 10/46

## Slide 11
2- The SPES target: general architecture and main characteristics
welding of thin Ta components for the high temperature target transfer line
Ta sheet (tk = 0.2 mm) rolled and welded for the main body of the heating system (Øe = 50 mm)
Mattia Manzolaro slide 11/46

## Slide 12
2- The SPES target: general architecture and main characteristics
Mattia Manzolaro
before testing
after testing
Endurance tests at high temperature with Joule heating thermal load → 10 kW
(primary proton beam thermal load → 8 kW)
400 testing hours at ≈ 2000 °C → 200 hours at maximum power (10 kW)
80 heating-cooling cycles → 10 with current ramps of 1 s from 0 A to 1300 A (!)
TIS UNIT STILL OPERATIVE !
Mattia Manzolaro slide 12/46

## Slide 13
SUMMARY
1- Introduction
2- The SPES target
3- Numerical models
4- On-line tests
5- Target material characterization @ HT
6- ISOL targets @ other facilities
7- Conclusions and future developments
Mattia Manzolaro slide 13/46

## Slide 14
3- Numerical models: a multiphysics approach
particle-matter interaction
thermal analysis
- thermal conduction
- thermal radiation
electrical conduction
structural analysis
p
q
I
σ
particle physics MonteCarlo simulations (FLUKA)
coupled-field Finite Element simulations (ANSYS)
Mattia Manzolaro slide 14/46

## Slide 15
3- Numerical models: a multiphysics approach
particle-matter interaction
thermal analysis
- thermal conduction
- thermal radiation
electrical conduction
structural analysis
ONE-WAY coupling
temperature distribution (x,y,z)
TWO-WAY coupling
temperature distribution (x,y,z)
Joule heating (x,y,z) – ρ (T)
electrical-thermal Finite Element model
power density (x,y,z)
ONE-WAY coupling
Mattia Manzolaro slide 15/46

## Slide 16
3- Numerical models: the electrical-thermal Finite Element model
directly implemented (electrical-thermal model)
power density tables import
Mattia Manzolaro slide 16/46

## Slide 17
Joule heating thermal load (1300 A) to heat the target during the conditioning phase
> point P1: Ta tube reference temperature
> point P2: C window reference temperature
P1
P2
3- Numerical models: the electrical-thermal Finite Element model
Mattia Manzolaro slide 17/46

## Slide 18
2
3
4
5
7
6
1
8
1.
Target vacuum chamber
2.
Power supply connection
3.
Vacuum turbomolecular pump
4.
Cooling water line
5.
HT pyrometer
6.
LT pyrometer
7.
Kodial viewport (Ta tube)
8.
Kodial viewport (graphite window)
Chart: electrical current (A)
| 600 | 700 | 800 | 900 | 1000 | 1100 | 1200 | 1300
experimental data | 1147 | 1286 | 1417 | 1528 | 1627 | 1718 | 1804 | 1876
FE data | 1148 | 1275 | 1394 | 1507 | 1615 | 1717 | 1815 | 1909
Chart: electrical current (A)
| 600 | 700 | 800 | 900 | 1000 | 1100
experimental data | 899 | 1015 | 1117 | 1212 | 1301 | 1386
FE data | 943 | 1059 | 1168 | 1270 | 1366 | 1457 | 1545 | 1630
3- Numerical models: the electrical-thermal Finite Element model
Joule heating thermal load (1300 A) to heat the target during the conditioning phase
Mattia Manzolaro slide 18/46

## Slide 19
3- Numerical models: the electrical-thermal Finite Element model
Reference: M. Ballan et al., Nucl. Instrum. Methods Phys. Res., Sect. B 376, 28-32 (2016)
Joule heating thermal load (1300 A) to heat the target during the conditioning phase
Mattia Manzolaro slide 19/46

## Slide 20
Proton beam thermal load: 40 MeV, 0.2 mA (≈ 8 kW) (power density input for the Finite Element model calculated by means of particle physics MonteCarlo codes)
3- Numerical models: the electrical-thermal Finite Element model
TEMPERATURE DISTRIBUTION [°C]
Mattia Manzolaro slide 20/46

## Slide 21
3- Numerical models: the electrical-thermal Finite Element model
THERMAL STRESS STATE [Pa]
(induced by temperature gradients)
Proton beam thermal load: 40 MeV, 0.2 mA (≈ 8 kW) (power density input for the Finite Element model calculated by means of particle physics MonteCarlo codes)
Mattia Manzolaro slide 21/46

## Slide 22
3- Numerical models: the electrical-thermal Finite Element model
Effect of the wobbling (50 Hz)
Proton beam onto the disk
ΔTMAX ≈ 2.5°C
σVM_MAX = 198 MPa
Request for an higher wobbling frequency
Δσ = 14 MPa
After 1 s, ΔTMAX ≈ 350°C
Warning on the sudden increase of the proton beam power!
Proton beam onto the disk
Stop of the proton beam
Reference: A. Monetti et al., “The RIB production target for the SPES project”, Eur. Phys. J. A 51, 128 (2015)
Proton beam thermal load: 40 MeV, 0.2 mA (≈ 8 kW) (power density input for the Finite Element model calculated by means of particle physics MonteCarlo codes)
Mattia Manzolaro slide 22/46

## Slide 23
SUMMARY
1- Introduction
2- The SPES target
3- Numerical models
4- On-line tests
5- Target material characterization @ HT
6- ISOL targets @ other facilities
7- Conclusions and future developments
Mattia Manzolaro slide 23/46

## Slide 24
4- On-line tests: scaled SiC target prototype tested @ ORNL
Scaled (d = 13 mm) SiC SPES Target Prototype
tested @ ORNL (2007)
SPES target architecture
tested successfully with a
42 MeV, 12 µA proton beam
Conventional Target Architecture
TMAX ≈ 2200 °C - 40 MeV, 6 µA proton beam
SPES Target Architecture
TMAX ≈ 2200 °C - 40 MeV, 18 µA proton beam
Total Deposited Power / Total Disks Surface = constant
Mattia Manzolaro slide 24/46

## Slide 25
Mechanical Design by Michele Lollo
4- On-line tests: scaled SiC target prototype tested @ ORNL
Mattia Manzolaro slide 25/46

## Slide 26
high power tests @ iThemba LABS (A. Monetti)
Full scale SPES target successfully tested
- 66 MeV, 60 µA proton beam (40 MeV, 200 µA @ SPES)
- SiC disks (UCx disks @ SPES) → acceptable activation levels
- 13 disks (7 disks @ SPES)
Reference: A. Monetti et al., “On-line test using multi-foil SiC target at iThemba LABS”, Eur. Phys. J. A 52, 168 (2016)
4- On-line tests: SiC target prototype tested @ iThemba LABS
Mattia Manzolaro slide 26/46

## Slide 27
On-line testing of the SPES target material and architecture @ ORNL
40 MeV, 50 nA proton beam on a UCx target
 | 2010 | 2011
Density (g/cm³) | 4.25 | 2.59
Diameter (mm) | 12.50 | 13.07
Thickness (g/cm²) | 0.41 | 0.41
Calculated porosity (%) | 58 | 75
2010 Test
Standard UCX
2011 Test
Low density UCX
4- On-line tests: scaled UCx target prototype tested @ ORNL
Mattia Manzolaro slide 27/46

## Slide 28
- 2 target prototypes tested at 3 different temperature levels (2000°C, 1800°C and 1600°C)
- approximately 80 isotopes (20 elements) collected
4- On-line tests: scaled UCx target prototype tested @ ORNL
On-line testing of the SPES target material and architecture @ ORNL
40 MeV, 50 nA proton beam on a UCx target
Mattia Manzolaro slide 28/46

## Slide 29
4- On-line tests: scaled UCx target prototype tested @ ORNL
Special Thanks to Dr. Daniel Stracener (ORNL)
Mattia Manzolaro slide 29/46

## Slide 30
4- On-line tests: commissioning plan @ SPES
First SPES RIB (26Al)
2020: 40 MeV, 20 µA
SiC target
the full-scale SPES target for high intensity RIBs
Nominal parameters
- Target material: UCx (SiC as an alternative)
- Proton beam energy: 40 MeV
- Proton beam intensity: 200 µA
- Proton beam sigma: 7 mm
- Wobbling radius : 11 mm
to high proton beam intensities
(increase by a factor of 10)
40 MeV, 200 µA, 1013 f/s
UCx target
40 MeV, 20 µA, 1012 f/s
first n-rich fission isotopes
UCx target
the next two steps of the commissioning phase
Mattia Manzolaro slide 30/46

## Slide 31
SUMMARY
1- Introduction
2- The SPES target
3- Numerical models
4- On-line tests
5- Target material characterization @ HT
6- ISOL targets @ other facilities
7- Conclusions and future developments
Mattia Manzolaro slide 31/46

## Slide 32
5- Target material characterization @ HT
homemade materials for the target disks (strong R&D activity required)
Mattia Manzolaro slide 32/46

## Slide 33
homemade materials for the target disks (strong R&D activity required)
main requirements for ISOL target materials @ high temperatures
- open porosity and reduced grain size (diffusion & effusion)
- low vapor pressure (low gas load in the ion source and long term stability at high temperature)
- high emissivity
- high thermal conductivity
- good mechanical properties
total isotope yield deeply affected by open porosity (diffusion/effusion processes)
5- Target material characterization @ HT
Courtesy of Stefano Corradetti
Mattia Manzolaro slide 33/46

## Slide 34
Emissivity e (th. radiation) and thermal conductivity l (th. conduction) control the target temperature field
Temperature gradients generate stress states and a good tensile/compressive strength σTS is required
5- Target material characterization @ HT
Mattia Manzolaro slide 34/46

## Slide 35
M. Manzolaro, S. Corradetti, A. Andrighetto, L. Ferrari, Rev. Sci. Instrum. 84, (2013) 054902
L. Biasetto, M. Manzolaro, A. Andrighetto, Eur. Phys. J. A 38 (2008) 167-171
Emissivity e meas. method
Thermal conductivity l meas. method
5- Target material characterization @ HT
Mattia Manzolaro slide 35/46

## Slide 36
Emissivity measurements for different Uranium Carbides
- Direct emissivity measurements on heated UCx discs using a dual frequency pyrometer
- UCx samples of different composition and synthesis routes produced in different laboratories participating to ActiLab
5- Target material characterization @ HT
Thermal Conductivity estimations for the SPES Uranium Carbide
- Creation of thermal gradients on UCx disks → thermal conductivity obtained by inverse analysis using Ansys®
- Activity performed in the context of ActiLab Work
Package in ENSAR (7th Framework Program)
Mattia Manzolaro slide 36/46

## Slide 37
5- Target material characterization @ HT
average stress level during operation with primary beam
A new method to estimate the Tensile Strength @ HT (Silicon Carbide)
SiC disk (Hexoloy SA) – Matteo Sturaro master’s thesis, University of Padova
Supervisors: G. Meneghetti, A. Andrighetto, M. Manzolaro, M. Ballan
Mattia Manzolaro slide 37/46

## Slide 38
SUMMARY
1- Introduction
2- The SPES target
3- Numerical models
4- On-line tests
5- Target material characterization @ HT
6- ISOL targets @ other facilities
7- Conclusions and future developments
Mattia Manzolaro slide 38/46

## Slide 39
6- ISOL targets @ other facilities
courtesy of Dr. W. Hwang (RISP)
Mattia Manzolaro slide 39/46

## Slide 40
6- ISOL targets @ other facilities
courtesy of Dr. João Pedro Ramos (ISOLDE-CERN)
ID35-A first integrated CERN-ISOLDE spallation source operated at 2000°C with GW instantaneous beam power for isotope production-Dr. RAMOS, J.p.
Mattia Manzolaro slide 40/46

## Slide 41
6- ISOL targets @ other facilities
courtesy of Dr. João Pedro Ramos (ISOLDE-CERN)
ID35-A first integrated CERN-ISOLDE spallation source operated at 2000°C with GW instantaneous beam power for isotope production-Dr. RAMOS, J.p.
Mattia Manzolaro slide 41/46

## Slide 42
6- ISOL targets @ other facilities
courtesy of Dr. Alexander Gottberg (TRIUMF)
ABSTRACT 71: A. Gottberg – TRIUMF High-Power Targets – Novel Concepts and Operational Experience
Mattia Manzolaro slide 42/46

## Slide 43
6- ISOL targets @ other facilities
courtesy of Ferran Boix Pamies (ISOLDE-CERN)
ID60-The LIEBE high-power target: Offline commissioning results-Mr. BOIX PAMIES, Ferran
Mattia Manzolaro slide 43/46

## Slide 44
SUMMARY
1- Introduction
2- The SPES target
3- Numerical models
4- On-line tests
5- Target material characterization @ HT
6- ISOL targets @ other facilities
7- Conclusions and future developments
Mattia Manzolaro slide 44/46

## Slide 45
7- Conclusions and future developments
Numerical models and simulation activities are fundamental for the design of High Temperature ISOL Targets
The goal is to design a target system that can be used for the highest RIB production (and so for the highest primary beam intensity) without exceeding the material limiting temperature
Validation of numerical models by means of dedicated experimental tests (both off-line and on-line) is extremely important
Numerical models and simulation activities can be extremely useful for Safety and Machine Protection Systems
The aforementioned multiphysics approach could be improved introducing CFD (water cooling, …) and diffusion/effusion analysis (GEANT4 custom routines)
ABSTRACT 71 (poster session): M. Ballan - Targets for the SPES project and its applications: material selection and release simulations
Mattia Manzolaro slide 45/46

## Slide 46
MANY THANKS FOR YOUR ATTENTION!
Acknowlegments: Prof. G. Meneghetti and Prof. P. Colombo (UNIPD-DII), Prof. L. Biasetto (UNIPD-DTG), Dr. D.W. Stracener (ORNL), the ENSAR-ActiLab collaboration (2010-2014, CERN, PSI, IPNO, GANIL)
Mattia Manzolaro slide 46/46