## Slide 1: CM02, CM03 HOM Q_ext Tuning Status
Ari Palczewski, Anna Solopova, Bob Legg

## Slide 2: Outline
  Introduction
    CM02
    CM03
  Results from Investigations
  Ideas
  Plans

## Slide 3: Introduction – Results of CM02 acceptance testing
Cavity | Serial # | QxtFPC | Qprobe | QHOMA | QHOMB | Emax CM / VTA | Emaxop | FE Onset CM / VTA | Limit CM
1 | L2_014 | 4.14E+07 | 3.46E+11 | 1.03E+11 | 1.76E+12 | 20.5 / 24.0 | 20.0 | N/A / N/A | Quench
2 | L2_009 | 3.94E+07 | 2.86E+11 | 4.81E+11 | 1.03E+11 | 15.4 / 17.1 | 15.0 | N/A / N/A | Quench
3 | L2_001 | 4.25E+07 | 3.50E+11 | 1.34E+11 | 2.96E+11 | 20.5 / 24.0 | 20.0 | N/A / N/A | Quench
4 | L2_010 | 4.17E+07 | 3.80E+11 | 4.67E+11 | 8.25E+10 | 8.0 / 24.0 | 4.5 | 3.7 / N/A | Quench
5 | L2_002 | 3.99e+07 | 3.70E+11 | 7.16E+10 | 2.35E+11 | 19.7 / 24.0 | 19.0 | N/A / N/A | Quench
6 | L2_005 | 4.07E+07 | 3.99E+11 | 6.23E+11 | 2.06E+11 | 16.9 / 16.4 | 16.4 | N/A / N/A | Quench
7 | L2_004 | 3.91E+07 | 3.36E+11 | 6.86E+11 | 2.34E+11 | 19.4 / 21.0 | 18.9 | N/A / N/A | Quench
8 | L2_012 | 3.96E+07 | 3.03E+11 | 2.19E+13 | 5.05E+11 | 17.9 / 23.0 | 17.1 | N/A / N/A | End Group Quench
  Performance Requirements (LCLSII-4.5-PP-0670-R1, rev’d 10-2016)
  QHOMA – 6 below spec; QHOMB – 6 below spec

## Slide 4: Introduction – Preliminary results of CM03 acceptance testing
* Admin - pulsed
** Measured at 10 MV/m
*** Needs further verification
**** Might increase with further vacuum processing

## Slide 5: Results from Investigations
  Collected data using FNAL software
  Cross-checked measurements with 2 different setups
  FNAL (Timergali) recalculated notch frequency from our data:
    Cavity 1 HOM A tuned same as cavity 8, but results are better
      Cavity 1 frequency was lower, 1299.95MHz vs 1300.000MHz
    Cavity 1 and 7 HOM B Qext are close, but notch is different by 0.4MHz.
    Cavity 3 HOM A severely mistuned – good Q, cavity 5 HOM B severely mistuned – bad Q.
Cavity | HOM A notch | HOM A Qext | HOM B notch | HOM B Qext | Limit | Spike
1 | 1296.6 | 4.12E+12 | 1296.5 | 3.21E+11 | Admin | N/A
2 | 1297.2 | 4.80E+10 | 1296.8 | 9.74E+10 | End group | None
3 | 1298.9 | 4.50E+11 | 1297.0 | 4.04E+11 | Quench | N/A
4 | 1297.2 | 9.10E+10 | 1296.9 | 8.54E+10 | Fwd power | N/A
5 | 1297.0 | 4.20E+10 | 1298.7 | 1.70E+10 | CARM | N/A
6 | 1296.5 | 4.00E+12 | 1297.8 | 1.56E+11 | End group | Cplr side
7 | 1296.9 | 7.70E+10 | 1296.9 | 3.50E+11 | End group | Cplr side
8 | 1296.6 | 3.70E+10 | 1296.9 | 1.80E+11 | End group | Cplr side
Notes: HOM A on 1 and 8 – same f, different Q
HOM B on 1 and 7 – close Q, different f
Cav 3 HOM A severely mistuned – good Q.
Cav 5 HOM B severely mistuned – bad Q.

## Slide 6: CM03 HOM A data

## Slide 7: HOM B data

## Slide 8: Ideas
  Tune A and B to different specs?
    Experiments to be done in VTA
  Tuning procedure is consistent in VTA and CMTF – results are not
    Cavities are in the same state – tuning should be the same
    VTA cooldown performed “vacuum to vacuum”, Qext didn’t change.
  VTA and CMTF notch position must be different – how?
  We now suspect clamps, cables or other interference changing Qext
Notes: FNAL atm\atm 1296.5
JLAB atm\vac 1297.0

## Slide 9: Schedule
  CM03 – in the cave, planning to take out later this week
    Evaluate HOMs and retune as needed
    Cooldown in the first week of October
  CM02 – stored for now.
    Data is collected, not analyzed
    Retune HOMs after all issues have been resolved and procedures verified.

## Slide 10: Plans
  Continuing with verification of procedures
    Formalize documented internal procedure
    Compare with FNAL procedures by Timergali
  Measure CM03 HOMs to see if the notch is shifted
  Re-tune CM03 HOM with Timergali’s help
  Compile lessons learned into report
  Cooldown CM03 first week of October for re-test
  Re-tune CM04 and CM02

## Slide 11: HOM Evaluation Plan (began in August)
CM02:
  1. Pull U tubes
  2. Remove WG
  3. Re-establish insulating vacuum
  4. Measure HOM's, Vac to Vac
  5. Break insulating vacuum.
  6. Measure HOM's, Vac to Atm
  7. Open module and check HOM heat Stationing.
  8. Re-verify HOM measurement Vac to Atm
  9. Analyze data and retune as needed
CM03:
  1. Open ports.
  2. Check HOM heat stationing
  3. Measure HOM's Vac to Atm
  4. Tune HOMA and/or B, if needed
  5. Close up VV. Complete BB installation.
  6. Move CM03 into cave.
  7. Pump down insulating vacuum space
  8. Measure HOM's Vac to Vac
  9. U-tube party
  10. Tune couplers Cold (Mircea)
  11. Check HOM spectrum cold
  12. Connect WGs and HOM cables
  13. Test
  14. Verify tuning procedure (Timergali at Jlab)
  15. Verify data analysis
  16. Retune HOMs