## Slide 1: MQXFAP2 Readiness Review Strand data
Lance Cooley – NHMFL / ASC
7 Dec 2017

## Slide 2: Content
Coil | Cable | Strand | Spec.
QXFA101 | P43OL1072 | 0.85 mm 108/127 | LARP 8004.D / HiLumi (2015)
QXFA102 | P43OL1073 | 0.85 mm 108/127 | LARP 8004.D / HiLumi (2015)
QXFA104 | P43OL1081 | 0.85 mm 108/127 | LARP 8004.D / HiLumi (2015)
QXFA105 | P43OL1082 | 0.85 mm 108/127 | LARP 8004.D / HiLumi (2015)
QXFA106 | P43OL1084 | 0.85 mm 108/127 | LARP 8004.D / HiLumi (2015)
PxxOLnnnn is the cable ID:
  “xx” is the project and strand type
    30 series = QXF gen 1 with annealed strands; 40 series = QXF gen 2 with annealed strands;
    Odd = cored cable; x3, x5, x7 determines strand type
  “nnnn” is the cable map number

## Slide 3: Consult Fermilab Vector System
Coil reports identify the cable used
  Example: S/N QXFA-CL-101-0
    464308-NONE--HL-LHC Magnet QXFA Preparation for Coil Winding and Curing Traveler

## Slide 4: Consult Fermilab Vector System
Cable reports identify the strand map
  S/N P43OL1072

## Slide 5: Consult Fermilab Vector System
Strand reports identify the spool and billet reports
  S/N PO08S00006A07U-0
    464269-NONE--HL-LHC: Quality Nb3Sn Strand Spool Report and Certification
      Contains mechanical property data
      Contains electrical property data
      Links to 464219-NONE—HL-LHC: Quality Nb3Sn Strand Billet Pedigree Report
        Contains all raw material certs and assembly IDs
    464341-NONE--HL-LHC: Nb3Sn Strand Shipment Traveler
      Contains Certificate of Compliance and approval records
Graded QC approach means that only certain spools are chosen to receive full characterization  travelers will have blanks
  Usually piece A01 contains representative billet info
  Usually the last spool in billet series has representative property info

## Slide 6: Cable acceptance Selection of witness samples
Acceptance criteria for cables includes RRR of extracted strands (XS) from each billet
  At least 5 regions: 3 straights and 2 bends
New fixture allows 6 witness samples to be reacted directly with the coil
  Mitigates risk of temperature difference between witness sample retort and coil
4 samples are representative extracted strands (determines SSL)
2 samples are virgin strands (qualifies HT)
3 samples are tested: two XS and one VS
  The other two XS and other one VS are backups

## Slide 7: Coil QXFA101, cable 1072 – Witness samples
ID | RRR (293K / 20K) | Ic(12T) | Ic(13T) | Ic(14T) | Ic(15T)
PO08S00008A01U |  | 724 | 596 | 494 | 402
P43OL1072AA03E † | 296 | 699 | 581 | 478 | 386
P43OL1072AA13E | 294 | 711 | 586 | 489 | 397
P43OL1072AA29E | 267 | 712 | 592 | 487 | 395
P43OL1072AA37E | 280 | 700 | 580 | 476 | 382
Dan Turrioni, Al Rusy, Pei Li performed measurements
† Cable degradation < 3.1%
Notice that the cable IDs have “AA” in them, which denotes a sample taken from the FRONT end of the cable. This is not typical. This was the cable that experienced a strand break and received special handling.

## Slide 8: Coil QXFA101, Cable 1072 – SSL report (Note: traveler in development)
1.9 K SSL intercept 14.9 T, 21.9 kA
16.5 kA Operating point at 75% SSL
SSL crosses 11.4 T, 16.5 kA @ TCS = 7.29 K
TCS – TOP = 5.4 K
Cable Ic at 11.4 T = 40.5 kA
16.5 kA IOP = 40.7% Cable Ic
Chart: 
| 12.270970522141441 | 15.141916523463317
Strand specs | 25240 | 13240
Witness virgin strand | 16063.88 | 19766.12 | 23859.88 | 28957.4
Witness extracted strand 1 | 15440.36 | 19116.64 | 23236.96 | 27963.44
Witness extracted strand 2 | 15879.52 | 19547.44 | 23446.72 | 28437.56
Load Line | 0 | 16470 | 17780 | 21945.3031
SPEC Fit 4.2K | 57270.0499 | 54686.6706 | 52218.7006 | 49858.9463 | 47600.8871 | 45438.5957 | 43366.6685 | 41380.1663 | 39474.5632 | 37645.7022 | 35889.7562 | 34203.1945 | 32582.7531 | 31025.4085 | 29971.2993 | 28088.9843 | 26704.8671 | 25295.5082 | 24093.4799 | 22862.1126 | 21677.7805 | 20538.7424 | 19443.3625 | 18390.102 | 17377.5115 | 16404.2242 | 15468.9496 | 13707.6264 | 13239.5924 | 12879.3309 | 12084.5458 | 11322.2878 | 10591.6231 | 9891.6636 | 9221.5646 | 8580.5214
XS Fit 4.2K | 60938.4716 | 58308.3286 | 55793.964 | 53388.1024 | 51084.151 | 48876.1179 | 46758.5419 | 44726.4326 | 42775.2181 | 40900.7 | 39099.0144 | 37366.5971 | 35700.1542 | 34096.6351 | 33102.0898 | 31067.2475 | 29636.2995 | 28204.0193 | 26930.4615 | 25651.4432 | 24419.1579 | 23231.8522 | 22087.8794 | 20985.6905 | 19923.8272 | 18900.9143 | 17915.6541 | 16302.3749 | 16053.2528 | 15173.8534 | 14327.5809 | 13513.4477 | 12730.5158 | 11977.8937 | 11254.7334 | 10560.2272
SPEC Fit 1.9K | 68646.4013 | 65802.8373 | 63082.8703 | 60478.6754 | 57983.1636 | 55589.8934 | 53292.9953 | 51087.1065 | 48967.3154 | 46929.1127 | 44968.349 | 43081.1977 | 41264.1232 | 39513.8518 | 38326.7749 | 36201.7876 | 34634.5468 | 33034.2197 | 31665.3888 | 30259.0468 | 28902.1474 | 27592.8124 | 26329.2782 | 25109.8863 | 23933.0755 | 22797.3741 | 21701.3935 | 19623.4184 | 19067.7872 | 18639.0088 | 17689.4801 | 16773.7767 | 15890.8964 | 15039.8867 | 14219.8419 | 13429.8996
SPEC cable 1.9K | 65214.0812 | 62512.6955 | 59928.7268 | 57454.7416 | 55084.0054 | 52810.3988 | 50628.3455 | 48532.7512 | 46518.9497 | 44582.6571 | 42719.9315 | 40927.1378 | 39200.917 | 37538.1592 | 36410.4362 | 34391.6982 | 32902.8194 | 31382.5087 | 30082.1194 | 28746.0945 | 27457.04 | 26213.1718 | 25012.8143 | 23854.392 | 22736.4217 | 21657.5054 | 20616.3238 | 18642.2474 | 18114.3979 | 17707.0583 | 16805.0061 | 15935.0879 | 15096.3516 | 14287.8924 | 13508.8498 | 12758.4046
Cable 1.9K (-3.16%) | 70355.9089 | 67557.1744 | 64878.6994 | 62312.815 | 59852.5752 | 57491.6695 | 55224.3491 | 53045.3628 | 50949.902 | 48933.553 | 46992.2551 | 45122.2648 | 43320.1234 | 41582.6295 | 40503.1804 | 38289.9197 | 36729.3787 | 35163.626 | 33767.9466 | 32362.7334 | 31005.2038 | 29693.5243 | 28425.9734 | 27200.933 | 26016.8799 | 24872.3786 | 23766.075 | 21945.3031 | 21663.015 | 20663.9047 | 19698.2751 | 18765.0979 | 17863.3971 | 16992.2455 | 16150.7612 | 15338.1052
OP (7.29K) | 20722.2622 | 19489.1566 | 18311.2884 | 17186.2404 | 16492.8864 | 15085.7815 | 14106.334 | 13135.1239 | 12279.9011
108% OP (6.29K) | 23845.9366 | 22559.2225 | 21763.872 | 20143.604 | 19010.3404 | 17881.6138 | 16883.0819 | 15885.5365 | 14929.8655

## Slide 9: Coil QXFA102, cable 1073 – Witness samples
ID | RRR (293K / 20K) | Ic(12T) | Ic(13T) | Ic(14T) | Ic(15T)
PO08S00042-Unknown |  | 750 | 624 | 512 | 414
P43OL1073AE21E † | 367 | 700 | 588 | 479 | 383
P43OL1073AE55E | 347 | 724 | 600 | 494 | 399
P43OL1073AE25E | 318 |  |  |  | 
P43OL1073AE27E | 329 |  |  |  | 
Dan Turrioni, Al Rusy, Pei Li performed measurements
The full virgin strand ID was not reported by them (lost?)
† Cable degradation < 6.5%

## Slide 10: Coil QXFA102, Cable 1073 – SSL report (Note: traveler in development)
1.9 K SSL intercept 14.8 T, 21.75 kA
16.5 kA Operating point at 76% SSL
SSL crosses 11.4 T, 16.5 kA @ TCS = 7.19 K
TCS – TOP = 5.3 K
Cable Ic at 11.4 T = 39.6 kA
16.5 kA IOP = 41.6% Cable Ic
Chart: 
| 12.270970522141441 | 15.141916523463317
Strand specs | 25240 | 13240
Witness virgin strand | 16550.96 | 20497.24 | 24969.52 | 29982.96
Witness extracted strand 1 | 15325.32 | 19162.28 | 23524.72 | 27985.96
Witness extracted strand 2 | 16550.96 | 20497.24 | 24969.52 | 29982.96
Load Line | 0 | 16470 | 17780 | 21753.6563
SPEC Fit 4.2K | 57270.0499 | 54686.6706 | 52218.7006 | 49858.9463 | 47600.8871 | 45438.5957 | 43366.6685 | 41380.1663 | 39474.5632 | 37645.7022 | 35889.7562 | 34203.1945 | 32582.7531 | 31025.4085 | 29971.2993 | 28088.9843 | 26704.8671 | 25295.5082 | 24093.4799 | 22862.1126 | 21677.7805 | 20538.7424 | 19443.3625 | 18390.102 | 17377.5115 | 16404.2242 | 15468.9496 | 13707.6264 | 13239.5924 | 12879.3309 | 12084.5458 | 11322.2878 | 10591.6231 | 9891.6636 | 9221.5646 | 8580.5214
XS Fit 4.2K | 61941.0758 | 59243.1855 | 56664.4066 | 54197.2666 | 51834.994 | 49571.4338 | 47400.9764 | 45318.4951 | 43319.293 | 41399.057 | 39553.817 | 37779.911 | 36073.9543 | 34432.8122 | 33415.1441 | 31333.5436 | 29870.1969 | 28405.9273 | 27104.3273 | 25797.5611 | 24538.969 | 23326.7487 | 22159.2072 | 21034.752 | 19951.8836 | 18909.1883 | 17905.3316 | 16717.1123 | 16009.1579 | 15114.5186 | 14254.0636 | 13426.7773 | 12631.6948 | 11867.8991 | 11134.5179 | 10430.7205
SPEC Fit 1.9K | 68646.4013 | 65802.8373 | 63082.8703 | 60478.6754 | 57983.1636 | 55589.8934 | 53292.9953 | 51087.1065 | 48967.3154 | 46929.1127 | 44968.349 | 43081.1977 | 41264.1232 | 39513.8518 | 38326.7749 | 36201.7876 | 34634.5468 | 33034.2197 | 31665.3888 | 30259.0468 | 28902.1474 | 27592.8124 | 26329.2782 | 25109.8863 | 23933.0755 | 22797.3741 | 21701.3935 | 19623.4184 | 19067.7872 | 18639.0088 | 17689.4801 | 16773.7767 | 15890.8964 | 15039.8867 | 14219.8419 | 13429.8996
SPEC cable 1.9K | 65214.0812 | 62512.6955 | 59928.7268 | 57454.7416 | 55084.0054 | 52810.3988 | 50628.3455 | 48532.7512 | 46518.9497 | 44582.6571 | 42719.9315 | 40927.1378 | 39200.917 | 37538.1592 | 36410.4362 | 34391.6982 | 32902.8194 | 31382.5087 | 30082.1194 | 28746.0945 | 27457.04 | 26213.1718 | 25012.8143 | 23854.392 | 22736.4217 | 21657.5054 | 20616.3238 | 18642.2474 | 18114.3979 | 17707.0583 | 16805.0061 | 15935.0879 | 15096.3516 | 14287.8924 | 13508.8498 | 12758.4046
Cable 1.9K (-6.46%) | 69151.0063 | 66377.101 | 63722.6614 | 61180.0808 | 58742.4687 | 56403.5651 | 54157.6669 | 51999.5643 | 49924.4865 | 47928.0543 | 46006.2386 | 44155.3246 | 42371.8803 | 40652.7289 | 39584.8432 | 37395.728 | 35852.5936 | 34304.6529 | 32925.1682 | 31536.587 | 30195.4613 | 28899.971 | 27648.407 | 26439.1628 | 25270.726 | 24141.6715 | 23050.6547 | 21753.6563 | 20977.7229 | 19993.4707 | 19042.5717 | 18124.0049 | 17236.8006 | 16380.0381 | 15552.8413 | 14754.3767
OP (7.188K) | 20707.3836 | 19473.1791 | 18294.3162 | 17168.3741 | 16474.4988 | 15066.4138 | 14086.3528 | 13114.5973 | 12258.9523
108% OP (6.188K) | 23731.8135 | 22446.829 | 21652.6054 | 20034.7831 | 18903.362 | 17776.5912 | 16779.9001 | 15784.3084 | 14830.6277

## Slide 11: Coil QXFA104, cable 1081 – Witness samples
ID | RRR (293K / 20K) | Ic(12T) | Ic(13T) | Ic(14T) | Ic(15T)
PO08S00074A01U | 134 | 756 | 634 | 525 | 430
P43OL1081AE25E † | 135 | 703 | 587 | 484 | 391
P43OL1081AE55E | 126 | 718 | 600 | 497 | 405
Dan Turrioni, Al Rusy, Pei Li performed measurements
† Cable degradation < 7.1%

## Slide 12: Coil QXFA104, Cable 1081 – SSL report (Note: traveler in development)
1.9 K SSL intercept 14.8 T, 21.74 kA
16.5 kA Operating point at 76% SSL
SSL crosses 11.4 T, 16.5 kA @ TCS = 7.19 K
TCS – TOP = 5.3 K
Cable Ic at 11.4 T = 38.9 kA
16.5 kA IOP = 42.4% Cable Ic
Chart: 
| 12.270970522141441 | 15.141916523463317
Strand specs | 25240 | 13240
Witness virgin strand | 17194.2 | 21017.08 | 25352.76 | 30242
Witness extracted strand 1 | 15653.28 | 19370.24 | 23461.28 | 28119.56
Witness extracted strand 2 | 16180.44 | 19890.24 | 24016 | 28725.84
Load Line | 0 | 16470 | 17780 | 21739.6579
SPEC Fit 4.2K | 57270.0499 | 54686.6706 | 52218.7006 | 49858.9463 | 47600.8871 | 45438.5957 | 43366.6685 | 41380.1663 | 39474.5632 | 37645.7022 | 35889.7562 | 34203.1945 | 32582.7531 | 31025.4085 | 29971.2993 | 28088.9843 | 26704.8671 | 25295.5082 | 24093.4799 | 22862.1126 | 21677.7805 | 20538.7424 | 19443.3625 | 18390.102 | 17377.5115 | 16404.2242 | 15468.9496 | 13707.6264 | 13239.5924 | 12879.3309 | 12084.5458 | 11322.2878 | 10591.6231 | 9891.6636 | 9221.5646 | 8580.5214
XS Fit 4.2K | 60857.2677 | 58250.871 | 55758.9251 | 53374.2278 | 51090.253 | 48901.0696 | 46801.2722 | 44785.9213 | 42850.4922 | 40990.8298 | 39203.1101 | 37483.8061 | 35829.6582 | 34237.6478 | 33250.0693 | 31229.0361 | 29807.409 | 28384.1032 | 27118.2006 | 25846.5352 | 24620.9888 | 23439.827 | 22301.421 | 21204.2388 | 20146.8378 | 19127.8581 | 18146.0163 | 17015.5657 | 16288.9608 | 15411.5141 | 14566.7298 | 13753.6315 | 12971.2917 | 12218.8291 | 11495.4052 | 10800.2218
SPEC Fit 1.9K | 68646.4013 | 65802.8373 | 63082.8703 | 60478.6754 | 57983.1636 | 55589.8934 | 53292.9953 | 51087.1065 | 48967.3154 | 46929.1127 | 44968.349 | 43081.1977 | 41264.1232 | 39513.8518 | 38326.7749 | 36201.7876 | 34634.5468 | 33034.2197 | 31665.3888 | 30259.0468 | 28902.1474 | 27592.8124 | 26329.2782 | 25109.8863 | 23933.0755 | 22797.3741 | 21701.3935 | 19623.4184 | 19067.7872 | 18639.0088 | 17689.4801 | 16773.7767 | 15890.8964 | 15039.8867 | 14219.8419 | 13429.8996
SPEC cable 1.9K | 65214.0812 | 62512.6955 | 59928.7268 | 57454.7416 | 55084.0054 | 52810.3988 | 50628.3455 | 48532.7512 | 46518.9497 | 44582.6571 | 42719.9315 | 40927.1378 | 39200.917 | 37538.1592 | 36410.4362 | 34391.6982 | 32902.8194 | 31382.5087 | 30082.1194 | 28746.0945 | 27457.04 | 26213.1718 | 25012.8143 | 23854.392 | 22736.4217 | 21657.5054 | 20616.3238 | 18642.2474 | 18114.3979 | 17707.0583 | 16805.0061 | 15935.0879 | 15096.3516 | 14287.8924 | 13508.8498 | 12758.4046
Cable 1.9K (-7.28%) | 67210.7991 | 64556.0953 | 62015.2444 | 59580.9769 | 57246.7089 | 55006.4589 | 52854.7782 | 50786.6898 | 48797.6365 | 46883.4352 | 45040.2378 | 43264.4969 | 41552.935 | 39902.5186 | 38877.0336 | 36774.0697 | 35290.992 | 33802.6833 | 32475.7818 | 31139.5547 | 29848.401 | 28600.5839 | 27394.4728 | 26228.5349 | 25101.3275 | 24011.4912 | 22957.7434 | 21739.6579 | 20953.7345 | 20001.2443 | 19080.3757 | 18190.1549 | 17329.6578 | 16498.0064 | 15694.3659 | 14917.9418
OP (7.188K) | 20574.3581 | 19382.7547 | 18243.6519 | 17154.7411 | 16483.1822 | 15119.0674 | 14168.45 | 13224.8234 | 12392.964
108% OP (6.188K) | 23526.5712 | 22287.2283 | 21520.7791 | 19958.3984 | 18864.7533 | 17774.6915 | 16809.6347 | 15844.7755 | 14919.6364

## Slide 13: Coil QXFA105, cable 1082 – Witness samples
ID | RRR (293K / 20K) | Ic(12T) | Ic(13T) | Ic(14T) | Ic(15T)
PO08S00080A03U |  | 729 | 608 | 500 | 407
P43OL1082AE18E |  | 720 | 600 | 495 | 404
P43OL1082AE60E † |  | 700 | 585 | 483 | 393
Dan Turrioni, Al Rusy, Pei Li performed measurements
† Cable degradation < 4.2%

## Slide 14: Coil QXFA105, Cable 1082 – SSL report (Note: traveler in development)
1.9 K SSL intercept 14.9 T, 21.9 kA
16.5 kA Operating point at 73% SSL
SSL crosses 11.4 T, 16.5 kA @ TCS = 7.38 K
TCS – TOP = 5.5 K
Cable Ic at 11.4 T = 39.9 kA
16.5 kA IOP = 40.2% Cable Ic
Chart: 
| 12.270970522141441 | 15.141916523463317
Strand specs | 25240 | 13240
Witness virgin strand | 16270.6 | 20011.44 | 24330.52 | 29154.92
Witness extracted strand 1 | 16172.84 | 19812.48 | 24015.96 | 28811.76
Witness extracted strand 2 | 15715.1483 | 19334.8114 | 23402.0886 | 28017.778
Load Line | 0 | 16470 | 17780 | 21934.1538
SPEC Fit 4.2K | 57270.0499 | 54686.6706 | 52218.7006 | 49858.9463 | 47600.8871 | 45438.5957 | 43366.6685 | 41380.1663 | 39474.5632 | 37645.7022 | 35889.7562 | 34203.1945 | 32582.7531 | 31025.4085 | 29971.2993 | 28088.9843 | 26704.8671 | 25295.5082 | 24093.4799 | 22862.1126 | 21677.7805 | 20538.7424 | 19443.3625 | 18390.102 | 17377.5115 | 16404.2242 | 15468.9496 | 13707.6264 | 13239.5924 | 12879.3309 | 12084.5458 | 11322.2878 | 10591.6231 | 9891.6636 | 9221.5646 | 8580.5214
XS Fit 4.2K | 60201.3666 | 57639.7783 | 55190.4435 | 52846.2899 | 50600.9094 | 48448.4782 | 46383.689 | 44401.6922 | 42498.0453 | 40668.6691 | 38909.8095 | 37218.004 | 35590.0529 | 34022.9932 | 33050.753 | 31060.7466 | 29660.6269 | 28258.565 | 27011.2925 | 25758.0695 | 24550.0157 | 23385.4293 | 22262.7117 | 21180.3597 | 20136.9578 | 19131.1716 | 18161.7419 | 16598.1684 | 16327.257 | 15460.0108 | 14624.7304 | 13820.4578 | 13046.2833 | 12301.3423 | 11584.8124 | 10895.9106
SPEC Fit 1.9K | 68646.4013 | 65802.8373 | 63082.8703 | 60478.6754 | 57983.1636 | 55589.8934 | 53292.9953 | 51087.1065 | 48967.3154 | 46929.1127 | 44968.349 | 43081.1977 | 41264.1232 | 39513.8518 | 38326.7749 | 36201.7876 | 34634.5468 | 33034.2197 | 31665.3888 | 30259.0468 | 28902.1474 | 27592.8124 | 26329.2782 | 25109.8863 | 23933.0755 | 22797.3741 | 21701.3935 | 19623.4184 | 19067.7872 | 18639.0088 | 17689.4801 | 16773.7767 | 15890.8964 | 15039.8867 | 14219.8419 | 13429.8996
SPEC cable 1.9K | 65214.0812 | 62512.6955 | 59928.7268 | 57454.7416 | 55084.0054 | 52810.3988 | 50628.3455 | 48532.7512 | 46518.9497 | 44582.6571 | 42719.9315 | 40927.1378 | 39200.917 | 37538.1592 | 36410.4362 | 34391.6982 | 32902.8194 | 31382.5087 | 30082.1194 | 28746.0945 | 27457.04 | 26213.1718 | 25012.8143 | 23854.392 | 22736.4217 | 21657.5054 | 20616.3238 | 18642.2474 | 18114.3979 | 17707.0583 | 16805.0061 | 15935.0879 | 15096.3516 | 14287.8924 | 13508.8498 | 12758.4046
Cable 1.9K (-4.16%) | 68671.149 | 65974.916 | 63394.1341 | 60921.4242 | 58550.1028 | 56274.0987 | 54087.8811 | 51986.3987 | 49965.0261 | 48019.5177 | 46145.9684 | 44340.7778 | 42600.6199 | 40922.4165 | 39879.553 | 37740.6573 | 36231.9821 | 34717.7516 | 33367.5258 | 32007.5903 | 30693.3015 | 29422.8972 | 28194.7232 | 27007.2246 | 25858.9379 | 24748.484 | 23674.562 | 21934.1538 | 21631.4664 | 20660.0319 | 19720.5985 | 18812.1787 | 17933.8353 | 17084.6778 | 16263.8597 | 15470.5754
OP (7.38K) | 20096.4294 | 18914.9445 | 17785.9918 | 16707.2677 | 16042.2497 | 14692.095 | 13751.7996 | 12818.9631 | 11997.1169
108% OP (6.41K) | 23027.7876 | 21797.3719 | 21036.6651 | 19486.5666 | 18402.0251 | 17321.4997 | 16365.31 | 15409.7551 | 14493.9914

## Slide 15: Coil QXFA106, cable 1084 – Witness samples
ID | RRR (293K / 20K) | Ic(12T) | Ic(13T) | Ic(14T) | Ic(15T)
PO08S00079A01U | 174 | 724 | 603 | -- | 406*
P43OL1084AE39E | 174 | 650* | 538* | 439* | 348*†
P43OL1084AE03E | 156 | 676* | 559* | 459* | 371*
P43OL1084AE41E | 139 | 683* | 571* | 477* | 381*
Dan Turrioni, Al Rusy, Pei Li performed measurements
* Ic was determined by extrapolating voltage rise; sample was not stable enough to achieve voltage at or above the voltage criterion
† Cable degradation 10.2%

## Slide 16: Coil QXFA106, Cable 1084 – SSL report (Note: traveler in development)
1.9 K SSL intercept 14.3 T, 21.0 kA
16.5 kA Operating point at 78.5% SSL
SSL crosses 11.4 T, 16.5 kA @ TCS = 6.75 K
TCS – TOP = 4.85 K
Cable Ic at 11.4 T = 35.3 kA
16.5 kA IOP = 46.7% Cable Ic
Chart: 
| 12.270970522141441 | 15.141916523463317
Strand specs | 25240 | 13240
Witness virgin strand | 16240 | 19840 | 24120 | 28960
Witness extracted strand 1 | 13938.9443 | 17559.4301 | 21510.8617 | 26007.4194
Witness extracted strand 2 | 14839.1614 | 18373.471 | 22370.7085 | 27045.3012
Load Line | 0 | 16470 | 17780 | 20994.125
SPEC Fit 4.2K | 57270.0499 | 54686.6706 | 52218.7006 | 49858.9463 | 47600.8871 | 45438.5957 | 43366.6685 | 41380.1663 | 39474.5632 | 37645.7022 | 35889.7562 | 34203.1945 | 32582.7531 | 31025.4085 | 29971.2993 | 28088.9843 | 26704.8671 | 25295.5082 | 24093.4799 | 22862.1126 | 21677.7805 | 20538.7424 | 19443.3625 | 18390.102 | 17377.5115 | 16404.2242 | 15468.9496 | 13707.6264 | 13239.5924 | 12879.3309 | 12084.5458 | 11322.2878 | 10591.6231 | 9891.6636 | 9221.5646 | 8580.5214
XS Fit 4.2K | 57963.5147 | 55400.6438 | 52951.4872 | 50608.9306 | 48366.5264 | 46218.4138 | 44159.2508 | 42184.1549 | 40288.6527 | 38468.6356 | 36720.3218 | 35040.2226 | 33425.1131 | 31872.0067 | 30909.2695 | 28940.9123 | 27557.9493 | 26174.8198 | 24945.9912 | 23712.9509 | 22526.0532 | 21383.5794 | 20283.9152 | 19225.5421 | 18207.03 | 17227.0304 | 16284.2704 | 16949.9192 | 14505.7225 | 13667.7189 | 12862.5146 | 12089.1402 | 11346.6752 | 10634.2442 | 9951.0145 | 9296.1933
SPEC Fit 1.9K | 68646.4013 | 65802.8373 | 63082.8703 | 60478.6754 | 57983.1636 | 55589.8934 | 53292.9953 | 51087.1065 | 48967.3154 | 46929.1127 | 44968.349 | 43081.1977 | 41264.1232 | 39513.8518 | 38326.7749 | 36201.7876 | 34634.5468 | 33034.2197 | 31665.3888 | 30259.0468 | 28902.1474 | 27592.8124 | 26329.2782 | 25109.8863 | 23933.0755 | 22797.3741 | 21701.3935 | 19623.4184 | 19067.7872 | 18639.0088 | 17689.4801 | 16773.7767 | 15890.8964 | 15039.8867 | 14219.8419 | 13429.8996
SPEC cable 1.9K | 65214.0812 | 62512.6955 | 59928.7268 | 57454.7416 | 55084.0054 | 52810.3988 | 50628.3455 | 48532.7512 | 46518.9497 | 44582.6571 | 42719.9315 | 40927.1378 | 39200.917 | 37538.1592 | 36410.4362 | 34391.6982 | 32902.8194 | 31382.5087 | 30082.1194 | 28746.0945 | 27457.04 | 26213.1718 | 25012.8143 | 23854.392 | 22736.4217 | 21657.5054 | 20616.3238 | 18642.2474 | 18114.3979 | 17707.0583 | 16805.0061 | 15935.0879 | 15096.3516 | 14287.8924 | 13508.8498 | 12758.4046
Cable 1.9K (-10.16%) | 62264.9189 | 59732.5709 | 57309.7079 | 54989.3758 | 52765.2749 | 50631.6813 | 48583.3801 | 46615.6072 | 44723.9995 | 42904.5516 | 41153.5783 | 39467.6815 | 37843.7216 | 36278.7921 | 35306.9633 | 33315.4324 | 31912.1663 | 30505.0649 | 29251.5814 | 27990.3361 | 26772.713 | 25597.0457 | 24461.7697 | 23365.4141 | 22306.5941 | 21284.0048 | 20296.4147 | 20994.125 | 18421.6431 | 17532.3206 | 16673.7068 | 15844.8662 | 15044.9105 | 14272.9959 | 13528.3198 | 12810.1184
OP (6.75K) | 20557.5093 | 19370.7292 | 18236.1347 | 17151.4297 | 16482.4093 | 15123.3061 | 14176.0539 | 13235.6509 | 12406.526
108% OP (5.66K) | 23531.5535 | 22297.4338 | 21534.1463 | 19978.0322 | 18888.617 | 17802.6281 | 16841.0459 | 15879.5247 | 14957.4457

## Slide 17: Summary of Data
Coil | SSL field (T) | SSL current (kA) | IOP/ISSL (%) | T margin (K) | Cable IC (kA) | IOP/IC (%)
MQXFA101 | 14.9 | 21.9 | 75 | 5.4 | 40.5 | 40.7
MQXFA102 | 14.8 | 21.8 | 76 | 5.3 | 39.6 | 41.6
MQXFA104 | 14.8 | 21.7 | 76 | 5.3 | 38.9 | 40.2
MQXFA105 | 14.9 | 21.9 | 73 | 5.5 | 39.9 | 40.2
MQXFA106 | 14.3 | 21.0 | 79 | 4.8 | 35.3 | 46.7
No RRR data yet for coil 105