## Slide 1: Coil Reaction & Impregnation at FNAL Coils QXFA101,104,106 for Magnet MQXFAP2
Fred Nobrega
Coil Fabrication at FNAL, L3
U.S. HL-LHC Accelerator Upgrade Project
MQXFAP2 Conductor & Coils Readiness Review
December 7, 2017

## Slide 2: Outline of Talk, Coils QXFA101, 104, & 106
Notes & Photos
Coil heat treatment plots
Coil CMM results
Final electrical measurements and discrepancy reports (DR’s) covered in Carlo’s talk

## Slide 3: Materials Used
  Reaction:
    3 layers Hexcel 4522 glass cloth on coil OD
    2 layers mica on coil OD & ID
  Impregnation:
    3 mil instrumentation trace on coil OD
    2 layers Hexcel 4522 glass cloth on coil OD + 10 mil Mold released 10 mil Mylar
    3 mil instrumentation trace on coil ID
    1 layer Hexcel 4522 glass cloth on coil ID
    10 mil G11 shims on midplane
    Instrumentation wires (A104 & A106):
    - QH Wires - 8X Axon 18 AWG (Yellow) - VT Wires -7X Axon 26 AWG (Red)
    - 2850 Stycast

## Slide 4: Coil QXFA101 Heat Treatment
Recipe: 25°C*210°C /48h +50°C*400° C/48h + 50°C*665°C/50h
(ramp, plateau T, dwell)
(ramp, plateau T, dwell)
(ramp, plateau T, dwell)
Chart: Average T/C Temperature

## Slide 5: Coil QXFA101 Heat Treatment
T/C #9
4.6° C
665° C Plateau
T/C # 1,15
T/C # 13
6.3° C
210° C Plateau
T/C # 1,15
T/C # 13
T/C #9
9.6° C
400° C Plateau
T/C # 13
T/C # 1, 15
QXFA101 Reaction Fixture

## Slide 6: Coil QXFA104 Heat Treatment
Recipe: 25°C*210°C /48h +50°C*400° C/48h + 50°C*665°C/50h
(ramp, plateau T, dwell)
(ramp, plateau T, dwell)
(ramp, plateau T, dwell)
1
2
3
4
5
6
7
Results:
1-2 Ramp 14 hrs
2-3 210 °C plateau 205° C hrs & 43 hrs
3-4 Ramp 8 hrs
4-5 400 °C plateau 396° C & 44 hrs
5-6 Ramp 6 hrs
6-7 665 °C plateau 660° C & 74 hrs

## Slide 7: Coil QXFA104 Heat Treatment
6.9° C
8.5° C
T/C #9
T/C #9
T/C #13
T/C #13
210° C Plateau
400° C Plateau
6.7° C
T/C #9
T/C #13
665° C Plateau
T/C # 1,15
T/C # 1, 4, 15
T/C # 1, 4, 15
QXFA104 Reaction Fixture

## Slide 8: Coil QXFA106 Heat Treatment
Recipe: 25°C*210°C /48h +50°C*400° C/48h + 50°C*665°C/50h
(ramp, plateau T, dwell)
(ramp, plateau T, dwell)
(ramp, plateau T, dwell)
1
2
3
4
5
6
7
Results:
1-2 Ramp 14 hrs
2-3 210 °C plateau 207° C hrs & 43 hrs
3-4 Ramp 7 hrs
4-5 400 °C plateau 398° C & 44 hrs
5-6 Ramp 6 hrs
6-7 665 °C plateau 661° C & 55 hrs

## Slide 9: Coil QXFA106 Heat Treatment
210° C Plateau
400° C Plateau
665° C Plateau
QXFA106 Reaction Fixture
6.9° C
T/C #1,4,15
T/C #13
T/C #4
T/C #13
10.7° C
9.5° C

## Slide 10: Coil Reaction Summary
Nominal Values | A101 | A104 | A106
210° C & 48 hr | 206° C & 42 hr | 205° C & 43 hr | 207° C & 43 hr
400° C & 48 hr | 398° C & 43 hr | 396° C & 44 hr | 396° C & 44 hr
665° C & 50 hr | 662° C & 47 hr | 660° C & 74 hr* | 661° C & 55 hr*
210 spread, 6 °C | 6.3° C | 6.9° C | 6.9° C
400 spread, 6 °C | 9.6° C | 8.5° C | 10.7° C
665 spread, 6 °C | 4.6° C | 6.7° C | 9.5° C
* Time at 665° C plateau extended after consultation with conductor group.

## Slide 11: Witness Sample Holder QXFA106 & Subsequent Coils

## Slide 12: Impregnation Process
Strip heaters on tooling

## Slide 13: Coil QXFA101 CMM Results
Measured cross sections in
mm from Lead End Key Datum hole.
Station 1 -70
Station 2 -270
Station 3 -327
Station 5 -1140
Station 6 -1540
Station 7 -1940
Station 8 -2340
Station 9 -2740
Station 10 -3140
Station 11 -3540
Station 12 -3940
Station 13 -4323
Station 14 -4426
View of Profile scans along length of coil
Mid-planes only
Lead End of Coil

## Slide 14: Coil QXFA101 CMM Results
Sample Number: QXFA 101 Cross Section Station 05 at -1140mm from LEAD END. X100
Alignment is: this Cross-Section only -Z- to O.D. & -X- to Sides
Sample Number: QXFA 101 Cross Section Station 09 at -2740mm from LEAD END. x100
Alignment is: this Cross-Section only -Z- to O.D. & -X- to Sides
Sample Number: QXFA 101 Cross Section Station 12 at -3940mm from LEAD END. x100
Alignment is: this Cross-Section only -Z- to O.D. & -X- to Sides
Sample Number: QXFA 101 Cross Section Station 07 at -1940mm from LEAD END. x100
Alignment is: this Cross-Section only -Z- to O.D. & -X- to Sides
4 mils/square
4 mils/square
4 mils/square
4 mils/square

## Slide 15: Coil QXFA104 CMM Results
Measured cross sections in
mm from Lead End Key Datum hole.
Station 1 -70
Station 2 -270
Station 3 -327
Station 5 -1140
Station 6 -1540
Station 7 -1940
Station 8 -2340
Station 9 -2740
Station 10 -3140
Station 11 -3540
Station 12 -3940
Station 13 -4323
Station 14 -4426
View of Profile scans along length of coil
Mid-planes only
Lead End of Coil

## Slide 16: Coil QXFA104 CMM Results
Sample Number: QXFA 101 Cross Section Station 05 at -1140mm from LEAD END. X100
Alignment is: this Cross-Section only -Z- to O.D. & -X- to Sides
Sample Number: QXFA 101 Cross Section Station 09 at -2740mm from LEAD END. x100
Alignment is: this Cross-Section only -Z- to O.D. & -X- to Sides
Sample Number: QXFA 101 Cross Section Station 12 at -3940mm from LEAD END. x100
Alignment is: this Cross-Section only -Z- to O.D. & -X- to Sides
Sample Number: QXFA 101 Cross Section Station 07 at -1940mm from LEAD END. x100
Alignment is: this Cross-Section only -Z- to O.D. & -X- to Sides
4 mils/square
4 mils/square
4 mils/square
4 mils/square

## Slide 17: Coil QXFA106 CMM Results
Measured cross sections in
mm from Lead End Key Datum hole.
Station 1 -70
Station 2 -270
Station 3 -327
Station 5 -1140
Station 6 -1540
Station 7 -1940
Station 8 -2340
Station 9 -2740
Station 10 -3140
Station 11 -3540
Station 12 -3940
Station 13 -4323
Station 14 -4426
View of Profile scans along length of coil
Mid-planes only
Lead End of Coil

## Slide 18: Coil QXFA106 CMM Results
Sample Number: QXFA 101 Cross Section Station 05 at -1140mm from LEAD END. X100
Alignment is: this Cross-Section only -Z- to O.D. & -X- to Sides
Sample Number: QXFA 101 Cross Section Station 09 at -2740mm from LEAD END. x100
Alignment is: this Cross-Section only -Z- to O.D. & -X- to Sides
Sample Number: QXFA 101 Cross Section Station 12 at -3940mm from LEAD END. x100
Alignment is: this Cross-Section only -Z- to O.D. & -X- to Sides
Sample Number: QXFA 101 Cross Section Station 07 at -1940mm from LEAD END. x100
Alignment is: this Cross-Section only -Z- to O.D. & -X- to Sides
4 mils/square
4 mils/square
4 mils/square
4 mils/square

## Slide 20
MS measurement deviation, mm
MX maximum, mm
MI minimum, mm
MN mean, mm
SD std dev, mm
NP number of points