## Slide 1: MQXFAP2 Coil Review Coils QXFA102 & QXFA105 React & Impreg at BNL
J. Schmalzle
December 7, 2017

## Slide 2: Outline
Notes / photos
Reaction plots
Electrical Data
CMM
DRs

## Slide 3: QXFA102
2nd generation coil
  Reaction:
    3 layers Hexcel 4522 glass cloth on coil OD
  Impregnation:
    2 layer Hexcel 4522 glass cloth on coil OD
    1 layer Hexcel 4522 glass cloth on coil ID
    10 mil G11 shims on midplane

## Slide 4: QXFA102
Reaction Cycle:
48 Hours at 210 C
48 hours at 400 C
50 hours at 665 C
Witness samples in separate canister.

## Slide 5: QXFA102

## Slide 6: QXFA102

## Slide 7: QXFA102

## Slide 8: QXFA102
Faro arm coil size measurements:
  Primary best fit to coil OD, secondary to keyway (midplane where no keyway).
Nominal Coil Dimensions:
Outer Radius = 113.376 mm
Midplane offset = .125 mm
Keyway Width = 14.00 mm

## Slide 9: QXFA102

## Slide 10: QXFA102
No DRs noted.

## Slide 11: QXFA105
2nd generation coil
  Reaction:
    3 layers Hexcel 4522 glass cloth on coil OD
  Impregnation:
    2 layer Hexcel 4522 glass cloth on coil OD
    1 layer Hexcel 4522 glass cloth on coil ID
    10 mil G11 shims on midplane
CERN approved wires.
  AXON HH2619 / HH1819
Shorter pole pins to accommodate tube support bumpers (pions).

## Slide 12: QXFA105
Witness samples inside reaction fixture.
Reaction Cycle:
48 Hours at 210 C
48 hours at 400 C
50 hours at 665 C

## Slide 13: QXFA105

## Slide 14: QXFA105

## Slide 15: QXFA105

## Slide 16: QXFA105
Faro arm coil size measurements:
  Primary best fit to coil OD, secondary to keyway (midplane where no keyway).
Nominal Coil Dimensions:
Outer Radius = 113.376 mm
Midplane offset = .125 mm
Keyway Width = 14.00 mm

## Slide 17: QXFA105

## Slide 18: QXFA105
DRs:
  Ceramic coating on edge of OL saddle tip was chipped and insulation on IL coil lead was chafed in a small area by OL saddle tip.
    Fluffy coil and loose saddle likely created a pressure point that rubbed during shipping.
    No damage to conductor.
    Loose chips of ceramic were removed.
    Double layer of 2 mil kapton added to cover insulation damage area.

## Slide 19
Extra slides…

## Slide 20: QXF Coils
Coil size comparison: