## Slide 1: Silicon Basics
Silicon is wonderful stuff
Low energy to create e-hole pair (3.6 eV)
Long mean free path
High mobility (fast charge collection)
Low Z (low multiple scattering)
Well-developed technology
  Fine lithography of structures
  “native” oxide

## Slide 2: Silicon Basics
Silicon detectors are typically high resistivity >1 KW-cm “float zone” silicon
The small energy gap between impurity “donor” or “acceptor” levels means most mobile electrons and holes are due to dopants (at RT)
This is why we are not overwhelmed with current when a bias is applied
Intrinsic
n-type
p-type
band
diagram
density of
states
Fermi-dirac
distribution
carrier
concentrations

## Slide 3: Charge Drift and Collection
Diode depletion
Silicon detectors have lightly doped bulk (usually n) and heavily doped contacts. Unusually large depleted area.
Diffusion of charge carriers will form a local depleted region with no applied voltage
As we apply external bias the depletion region (and the internal field) grows until it hits the bottom.
Very asymmetric doping in our devices
pn junction no external
fields

## Slide 4: Device Characteristics
Resistivity:
Depletion :
Electric Field:
electron, hole mobility
Effective carrier concentration
x = distance from junction D = silicon thickness

## Slide 5: Device Testing - CV
There are a few standard tests which measure the basic properties of silicon detectors
Detectors are normally operated fully depleted – all impurities ionized. This leaves a “space charge” region depleted of charge carriers that acts like a dielectric in the junction/ohmic capacitor
Assume this acts as a parallel plate capacitor (diode test structures):

## Slide 6: Device Testing - IV
A high quality detector will also have low leakage current – current driven by carrier generation in the depleted bulk.
Strongly temperature dependent
Avalanche breakdown at 3x105 V/cm
Measure Vbias vs I curves
Look for anomalous currents
Breakdown voltage
Current can be affected by surface defects, problems with the ohmic contact, cut edge currents, impurities (especially metals), and physical
damage
Test structures
Rapid rise until
depletion

## Slide 7: Charge Drift, diffusion
A ~300 micron thick piece of silicon with initial doping concentration of 1x1012 has Vd of 68 V – operate at ~100 V
In p(n) type silicon electrons (holes) are collected at the junction
As carriers drift they diffuse
As carriers drift they move due to Lorentz forces from the solenoid field
As carriers drift electrons can recombine with holes
As carriers drift they may be “eaten” by traps in the silicon
Carriers in field-free regions can still diffuse to collection electrodes
me = 1.5x10-1 m2/Vsec
mh = 4.5 x10-2 m2/Vsec
(affected by temperature, doping concentration and the magnitude of the applied field)
Drift time to an electrode:

## Slide 8: Carrier Drift and Diffusion
Chart: Charge Collection point

## Slide 9: Carrier Drift
Electron, hole drift:
Drift time to an electrode:

## Slide 10: Signal Development
Signal induced by moving charges depend on work done by circuit. The charge induced on an electrode depends on the coupling between the moving charge and the electrode
In a multi-electrode system the induced current on an electrode depends on the velocity of the charge and the value of the effective “weighting” field
(Radeka – from Ramo and Shockley)
Weighting field - determined by putting 1V on strip, grounding all other electrodes

## Slide 11: Strip Detector
(Radeka)

## Slide 12: Signal Shapes
Spieler
Weighting potential for a 300 μm thick strip detector 50μm pitch

## Slide 13: Simulation
A silicon detector is rather complex. There are commercial “TCAD” packages that can simulate silicon-based devices utilizing finite element analysis using the detailed semiconductor equations:
Internal fields
Coupling to electrodes
Charge diffusion and drift
Traps
Surface effects

## Slide 14
TCAD simulation of hole currents due to a track impact in a n-bulk 50 micron thick pixel detector

## Slide 15: Strip Detector
Bias resistor integrated on each strip usually implanted polysilicon resistor
Coupling capacitor formed by very thin (2500 A) dielectric. The dielectric is usually a “grown thermal” oxide supplemented with deposited layers formed by CVD (chemical vapor deposition)
In addition there are “guard rings” which keep the field from reaching the damaged silicon near cut edges.
“Microdischarge” breakdown can occur when fields near the implant increase due to charges in the oxide and potential of the coupling aluminization
Si
n-
p+
n+
oxide
junction
Ohmic
contact

## Slide 16: Detector Fabrication (Spieler)
To fabricate silicon detectors the basic process is similar to IC fabrication
Lithography utilizing masking and exposure of photoresists
Growth and deposition of silicon dioxide layers (glass)
Implantation or diffusion of dopants
Thermal annealing to incorporate dopants into the silicon lattice
We deal with micron-level features where ICs are at ~14 nm

## Slide 17: n, p and junctions
Silicon can be doped with donor or acceptor impurities. This corresponds to n (usually phosphorus) or p (boron) type silicon.
The contact between the heavily doped and lightly doped regions provide the junction (p-n) and ohmic (n-n+ or p-p+) contacts
Junction contacts are high field (possible breakdown) regions
Ohmic contacts need to be heavily doped for a proper metal- semiconductor contact

## Slide 18: Semiconductor Surface
The surface is a crucial part of the detector design
Junction side must be polished and defect-free
Field must be ~0 at damaged cut edge
Silicon dioxide used as insulator and passivation can accumulate charge (usually positive)
An electron accumulation layer builds up near the positively charged silicon/silicon dioxide interface – this acts as an insulator on a p+/n or a conductor on a n+/p junction – need an additional “p-stop” to electrically isolate n strips on p conductor
Detectors can also be sensitive to charge attracted to the surface – affected by humidity
Electron concentration
1e11 oxide charge
n-type

## Slide 19: Detector Layout
bias
resistor
DC test
pad
coupling
capacitor
aluminization
Guard
ring
bond
pad
strip
implant
Bias line
100mm

## Slide 20: Wirebonding
Aluminum ultrasonic welding or gold thermocompression
Aluminum wedge bonding achieves the finest pitch and does not need elevated temperature
This is a bit of an art – getting good bonds depends on machine, operator, and especially the surface properties of the materials

## Slide 21: Interconnect
How we connect the detectors to the electronics, cool them, and mount them is increasingly important
Interconnect is a common point of failure
Determines pitch
Can be expensive
Adds capacitance and inductance
Can determine geometry
Hybrid Pixel Interconnect using bump bonds
hybrid
Analog
cable
SVX4
hybrid
Analog
cable
SVX4