## Slide 1: Quality of Copper Plated Beamline Bellows and Spools
Katherine M. Wilson with Ken Premo and Liang Zhao
Photos courtesy of Brian Carpenter and John Ogle
LCLS-II QA/QC Review
22 January 2018

## Slide 2: Parts Received and Inspected
 | Initial Order | Production Order | Add’l Order
PrCM Bellows | 35 | 224 | 52
Short Bellows | 6 | 31 | 10
DS Long Spool | 6 | 31 | 21
US Short Spool | Replaced with US Bellows |  | 
US Bellows | 14 |  | 
Total Parts Ordered (JLab + FNAL)
Additional parts ordered:
    As spares for existing CMs
    For 5 additional/spare CMs

## Slide 3: Quality Control
Inspection steps at JLab include:
Visual inspection (borescope for internal surfaces)
Careful inspection of seal surfaces
Leak check
Cleaning (bake if needed)
Inspection steps at FNAL are similar, except for bake
 | BLBP | BLBS | BLBU | BLXD | BLXU
HOLD MODIFY | 68 | 5 | 0 | 4 | 14
HOLD REMEASURE | 2 | 0 | 0 | 0 | 0
NOT DISPOSITIONED | 4 | 0 | 0 | 3 | 0
PROCEED TO NEXT WCA | 0 | 0 | 1 | 0 | 0
REJECT | 9 | 2 | 0 | 0 | 0
RETURN | 51 | 4 | 0 | 16 | 1
USE AS IS | 210 | 29 | 14 | 61 | 25
JLab QC Results

## Slide 4: Seal Surfaces
Scratches/nicks
Surface finish

## Slide 5: Quality Problem – Spools Surface Finish
Drawing originally called out Ra = 3.2 um = 125 u-in. Revised to 32 u-in

## Slide 6: Quality Problem – Plating

## Slide 7: Cleaning of Plating
Before
After cleaning
After baking
800 C for 3h

## Slide 8: Cleaning of Plating
Before
After cleaning
After baking

## Slide 9: Quality Problem – Possible Flaking
What causes FE in CM?
Series of experiments to quantify particulate from bellows - possibly released during flexing (See Liang Zhao for details.)
  Flexing bellows with particle count
  HPR and VTA test
  Clean room-grade bottle brush
  Assembly mock-ups
Production changes made to improve cleanliness
  Bellows are cycled and blown clean prior to assembly
  Bottle brush used during cleaning to remove loose debris
  Cleaning procedure approved during clean room audit

## Slide 10: Particulate Sampling/Material Analysis
Bellows were wiped at different locations at various stages of assembly/flexing
  SEM was used to analyze particulate
  Copper was seen, but also other materials
A failed bellows was cut up to facilitate material studies. It will be used to improve our understanding of plating in a beamline
  Surface characterization
  Mechanical deformation
  Water test
  HPR test

## Slide 11: Conclusions / Lessons Learned
Plater should review design and specifications
  Surface finish
  Interface with tooling plating (weld bead issue)
Many plating problems can be overcome with cleaning. (Baking is essential.)
Flexing of bellows causes shedding of particles. Unclear so far if this causes FE or how to improve. Studies underway.
Conclusion: Issues with bellows/spools generally understood, and we have procedures for resolving issues. Studies of possible flaking of plating continue, but mitigations have been implemented.

## Slide 12: Backup

## Slide 13: Beamline Bellows and Spools
Short Spool
PrCM “Long” Bellows
Short
Bellows
Long Spool
1.3 GHz Cryomodule