## Slide 1
Sam Posen
Energy Frontier WG Meeting
April 3, 2018
SRF Cavities at the Energy Frontier

## Slide 2: SRF Accelerators Around the World
RAON
Soleil
Circular
Planning
Light src
<10 cavities
Linear
NP
HEP
Produc’n
Oper’n
10-100 cavities
100-1000 cavities
>1000 cavities
CEBAF
SNS
FRIB
EIC
CLS
ISAC
LHC
XFEL
ESS
TLS
BESSY
ATLAS
FLASH
CESR
C-ADS
LIPAc
BEPC-II
HIE-ISOLDE
cERL
SPIRAL2
ALPI
ALICE
ELBE
ANURIB
J-PARC
SC-LINAC
SARAF
ANU
USP
PIP-II/III
FCC
ILC
ISNS
ADS
MaRIE
LCLS-II
CepC-SppC
Sam Posen
Map from Wikipedia. Non-exhaustive facility list.
TARLA
Notes: survey
I hope this shows how many accelerators there are around the world that use SRF cavities, but also… MANY UPCOMING

## Slide 3: Future HEP SRF Accelerators Under Discussion
EIC
SC-LINAC
SARAF
RAON
HIE-ISOLDE
cERL
J-PARC
LIPAc
ANURIB
BEPC-II
TLS
ANU
USP
ALPI
BESSY
ELBE
FLASH
Soleil
ESS
C-ADS
ALICE
ISNS
ADS
MaRIE
LHC
ATLAS
FRIB
CEBAF
SNS
LCLS-II
CLS
CESR
ISAC
SPIRAL2
XFEL
Circular
Planning
Light src
<10 cavities
Linear
NP
HEP
Produc’n
Oper’n
10-100 cavities
100-1000 cavities
>1000 cavities
PIP-II/III
FCC
CepC-SppC
ILC
High DF
Low DF
Sam Posen
Map from Wikipedia. Non-exhaustive facility list.
Need High Gradient and High Q0
Need High Q0
Notes: The goal of this talk is to very briefly give you an idea of progress in SRF progress over the past 40 years, overview the current status, and give you an idea of what we’re working on for the future

## Slide 4: SRF Performance Improvements Driven by R&D
2013 - N-doping: high Q0 at medium field [6]
2017 - N-infusion: high gradient and high Q0 [7]
[1] IEEE Trans. Mag. 15 1
[2] IEEE Trans. Mag. 19 3
[3] K. Saito, Proc SRF
[4] Proc EPAC 1269-1271
[5] TESLA DESY 98-05
[6] Supercond. Sci. Tech. 26 102001
[7] Supercond. Sci. Tech. 30 094004
1998 – 120C bake: prevent high field Q-slope [5]
1989 – electropolishing: smooth surfaces to nm-scale [3]
1992 – High pressure rinsing: prevent field emission [4]
1983 – control of impurities at welds: prevent thermal breakdown [2]
1979 – elliptical shapes: prevent multipacting [1]

## Slide 5: SRF Performance Improvements Driven by R&D
2013 - N-doping: high Q0 at medium field [6]
2017 - N-infusion: high gradient and high Q0 [7]
[1] IEEE Trans. Mag. 15 1
[2] IEEE Trans. Mag. 19 3
[3] K. Saito, Proc SRF
[4] Proc EPAC 1269-1271
[5] TESLA DESY 98-05
[6] Supercond. Sci. Tech. 26 102001
[7] Supercond. Sci. Tech. 30 094004
1998 – 120C bake: prevent high field Q-slope [5]
1989 – electropolishing: smooth surfaces to nm-scale [3]
1992 – High pressure rinsing: prevent field emission [4]
1983 – control of impurities at welds: prevent thermal breakdown [2]
1979 – elliptical shapes: prevent multipacting [1]
There is a strong historical trend of SRF R&D leading to substantial advances in cavity performance

## Slide 6: SRF Performance Improvements Driven by R&D
2013 - N-doping: high Q0 at medium field [6]
2017 - N-infusion: high gradient and high Q0 [7]
[1] IEEE Trans. Mag. 15 1
[2] IEEE Trans. Mag. 19 3
[3] K. Saito, Proc SRF
[4] Proc EPAC 1269-1271
[5] TESLA DESY 98-05
[6] Supercond. Sci. Tech. 26 102001
[7] Supercond. Sci. Tech. 30 094004
1998 – 120C bake: prevent high field Q-slope [5]
1989 – electropolishing: smooth surfaces to nm-scale [3]
1992 – High pressure rinsing: prevent field emission [4]
1983 – control of impurities at welds: prevent thermal breakdown [2]
1979 – elliptical shapes: prevent multipacting [1]
There is a strong historical trend of SRF R&D leading to substantial advances in cavity performance
Stronger performance improves the feasibility of building new accelerators with unprecedented scientific reach
CEBAF, 1st year of operation 1992
SNS, 1st year of operation 2007
XFEL, 1st year of operation 2017
LCLS-II, 1st year of operation ~2019

## Slide 7: Pushing Gradient – Beyond Hsh of Niobium
Limitation observed currently is consistent with superheating field Hsh of niobium (maximum of metastable flux-free state)
At high field, if magnetic flux penetrates, it moves through superconductor at RF frequencies; strong dissipation occurs
Several pathways expected to push beyond Hsh of bulk Nb:
  Engineered thin layers (e.g. a dirty layer of Nb on top of clean Nb) to modify the maximum metastable limit – already showing early signs of success via N-infusion
  New SRF materials with higher Hsh than Nb (e.g. Nb3Sn)
  Prevent flux penetration by using materials with long flux nucleation time relative to RF period
Bapplied

## Slide 8: Pushing Gradient – Beyond Hsh of Niobium
Limitation observed currently is consistent with superheating field Hsh of niobium (maximum of metastable flux-free state)
At high field, if magnetic flux penetrates, it moves through superconductor at RF frequencies; strong dissipation occurs
Several pathways expected to push beyond Hsh of bulk Nb:
  Engineered thin layers (e.g. a dirty layer of Nb on top of clean Nb) to modify the maximum metastable limit – already showing early signs of success via N-infusion
  New SRF materials with higher Hsh than Nb (e.g. Nb3Sn)
  Prevent flux penetration by using materials with long flux nucleation time relative to RF period
Bapplied
Fermilab SRF R&D has active programs in all of the above

## Slide 9: In-Accelerator Operating Gradient
In an accelerator cryomodule, additional restrictions tend to reduce accelerating gradient in operation, including:
  Cryogenic power (dissipated power scales with Eacc2), especially for high duty factor accelerators (i.e. not short pulses)
  Field emission (from dirt during cavity string assembly), heating or arcing of RF antennas
Low duty factor SRF linacs with hundreds of cavities
*CEBAF is CW but limited at ~5 MV/m due to field emission
PIP-III

## Slide 10: In-Accelerator Operating Gradient
In an accelerator cryomodule, additional restrictions tend to reduce accelerating gradient in operation, including:
  Cryogenic power (dissipated power scales with Eacc2), especially for high duty factor accelerators (i.e. not short pulses)
  Field emission (from dirt during cavity string assembly), heating or arcing of RF antennas
Low duty factor SRF linacs with hundreds of cavities
*CEBAF is CW but limited at ~5 MV/m due to field emission
PIP-III
Substantial and steady progress over the last decades. Still room to progress within Hsh of bulk niobium

## Slide 11: High Q0 Cavities for High Duty Factor Applications
In high energy e+e- storage rings (e.g. FCC-ee, CepC) and some linac applications (e.g. PIP-II) – RF is always on – Q0 is crucial to keep cryogenic costs reasonable
Major progress in last 5 years: >2x higher Q0 at relevant gradients with N-doping
Collaboration with CERN to study 800 MHz cavities for FCC-ee under N-doping and Nb3Sn coating
European XFEL Production – 120 C bake
LCLS-II Production – Nitrogen Doping
Red: after improved recipe implemented for production

## Slide 12: Normal Conducting RF High Energy Linac
70 MV/m demonstrated with limited breakdown frequency
Very high peak power dissipation in walls (10s of MW/m for CLIC vs ~100 W/m for ILC) pushes into regime with small duty factor (~1e-5 [ILC ~1e-2]) and high peak current
  Complicated RF compression system involving secondary “drive beam” and combiner rings to generate high power RF
  Detectors must be able to handle very high peak event rate
  High frequency (small) cavities: decreased aperture
  Strong HOM damping and focusing required
Very challenging alignment (over 200 m, CLIC ~10 μm vs ILC ~300 μm)
As a result, many unproven aspects for NCRF HE linac, whereas for SRF e.g. EXFEL is prototype for ILC