## Slide 1
G.Velev
Strategic Planning Group for Energy Frontier
Apr 3rd, 2018
HFM status: or why we cannot build 16 T dipole today?

## Slide 2: Outline
2014 P5 Report identified the HFM R&D as vital for the future of the field.
The strongest field achieved in the accelerator type dipole is 13.7 T in 1997, D20
Current status of the SCs
  Nb3Sn
  HTS (Bi-2212, REBCO, IBS) - $$$
Magnet Program at Fermilab
  11-12 T magnets are reality for HL-LHC
  B[T] ~ N* I/d, d = 50 mm, everything is Ampere-turns
  Magnet stress management for coil protection
Summary

## Slide 3: FCC activities (D. Tommasini)
FCC Conceptual Design Report (to be delivered by end 2018)
Feed the CDR with one reference option, including cost model, plus a description of alternative options.
Conductor
Procurement of up to 1.5 t of conductor/year to feed models and demonstrators
Increase of Jc up to FCC target (1500 A/mm2 @ 4.2 K, 16 T) for Nb3Sn
Electro-mechanical characterization of the conductor.
R&D Magnets
Design, Manufacture & Test of ERMC and RMM Magnets.
Identify and implement required technological R&D (wound conductor, splices, impregnation …)
Model magnets
Design, Manufacture & Test of Model Magnets

## Slide 4: Exciting advances in HTS vs Nb3Sn properties, but cost remains a major hurdle

## Slide 5: Superconductor cost
Today if we take NbTi (the accelerator “workhorse”) as a base = 1 unit cost
  NB3Sn - 3 times more expensive
  Bi-2212 - 100 times, 70% Ag matrix
  REBCO ~ 80-90 more expensive, production technology limited
  IBS - material are cheap, production technology cost unknown
  Others?
According to the present cost model the target cost for a 16 T magnet for HE-LHC built according to the cos- design would be:
  Conductor cost: 670 kEUR/magnet
  Assembly cost: 600 kEUR/magnet
  Parts cost: 420 kEUR/magnet
  Total cost: 1690 kEUR/magnet
  HE-LHC: 1232 dipoles, FCC-hh: 4664 dipoles, ~16 T (15.71 T), aperture 50 mm, Inter-beam distance 204 mm
Notes: Iter 700 tons, 7000 tons

## Slide 6: From Conductor to Magnet Design
Nb3Sn passes two stages:
  Wind a coil
  React the coil at 650C
After reaction the conductor is very fragile practically brittle.
HTS wires and tapes are much better related to stress – no accelerator type magnet. Issues: cost production, reaction, QP …
L.Bottura

## Slide 7: FNAL 15 T Demonstrator
Two major goals
  first to pave the way of designing 16 T and higher mechanical structure which can be used as prototyping of HE-LHC and FCC dipoles
  “to beat the curse” of the 20 years old D20.

## Slide 8: Conductor stress (I. Novitski) – why is 15T?

## Slide 9: 15 T Status
All the magnet parts are in house
Inner and outer coils are wound and reacted
Impregnation is in progress
Assembly starts at end of May
Test in September

## Slide 10: Summary
15-20% improvement in the Nb3Sn conductor Jc is needed to reach the requirements for 16T dipole
HTSs are on horizon but still cost prohibited
Fermilab is assembling the first-in-the-World 15T demonstrator, paving the way to 16 T dipoles
The U.S. Magnet Development Program is base for the US R&D: FNAL, LBNL and NHMFL
  working on 16-17 T Nb3Sn magnets
  HTS R&D for “hybrid magnets”
  Conductor R&D
  Thank You !