## Slide 1: Serial Ganging of Two sensL 3mm x 3mm C series SiPMs
PRELIMINARY
Kurt Francis
3/28/2018

## Slide 2
Sensl 3mm x 3mm C series are ¼ size versions of
The 6mm x 6mm for protodune
Vbr = 24.2V to 24.7V (~24.5)
Estimate two stacked should be 49V warm
The 6mm x 6mm were around 21V at LN2 temp.
Estimate two stacked should be 42V at LN2 temp.

## Slide 3
LED SETTING:
Red: 1.5V
Black: 1.7V
Green: 2.0V
Can’t measure dark current
At LN2 temperature,
Not enough charge carriers,
So we turn on the LED
Vbr ~= 19.5V

## Slide 4
Bias = 24.75V
Vovr = 5.25V
Gain = 24ADC/PE
Bias = 24.75V

## Slide 5
LED SETTING:
Purple: 1.5V
Green: 1.6V
Red: 1.7V
Black: 1.9V
Blue: 2.1V
Can’t measure dark current
At LN2 temperature,
Not enough charge carriers,
So we turn on the LED
New FEB readings are
more unstable at
Low nAmps
TWO SensL 3mm x 3mm ganged at CryoTemperatures

## Slide 6
TWO SensL 3x3 COLD bias=54V
Vovr_combined = 12.75V
Vovr_individual = 6.35V

## Slide 7
Actually 53.77V
Gain = 19.5 ADC/PE
Vovr_combined = 12.75V
Vovr_individual = 6.35V

## Slide 8
Vovr_combined = 10.75V
Vovr_individual = 5.35V
Gain = 16.3 ADC/PE
For Comparison
The single device at Vovr=5.25
Gain = 24.0 ADC/PE