## Slide 1: Titanium M6 Fastener Torque Testing
Peter Owen
June 12, 2018

## Slide 2: Test Setup
Started with 32 new fasteners, four new gaskets, four production feed-throughs, and washers
All fasteners and gaskets labelled
BPM housing held in vice for torqueing
Began each feed-through at 105, 110, 115, & 120 in-lbs
Removed each bolt and gasket to measure deformation between torques
Increased torque in 5 in-lb increments
Tightened one flange up to 175 in-lbs, other three flanges up to 150 in-lbs
Tests carried out in February 2018 by myself and Danny Forehand

## Slide 3: Bolt Extension Results
Each color represents one of four flanges
Each data point is average of the eight bolts on each flange measured
BPM Fastener Investigation, 6/12/2018
Chart: Average Bolt Extension
| 105 | 110 | 115 | 120 | 125 | 130 | 135 | 140 | 145 | 150 | 155 | 160 | 165 | 170
Flange 1 | 0.00125 | 0.0020625 | 0.003375 | 0.006 | 0.00875 | 0.018563 | 0.026563 | 0.031563 | 0.034357
Flange 2 | 0.0020625 | 0.002625 | 0.0044375 | 0.005875 | 0.007875 | 0.0094375 | 0.010778 | 0.013813
Flange 3 | 0.0015625 | 0.003875 | 0.005875 | 0.00725 | 0.0088125 | 0.010688 | 0.013313
Flange 4 | 0.0008125 | 0.0011875 | 0.0023125 | 0.002875 | 0.005125 | 0.0074375 | 0.011938 | 0.014688 | 0.0165 | 0.018938 | 0.0215 | 0.024688 | 0.0285 | 0.037125
Chart: Gasket Crush
| 110 | 115 | 120 | 125 | 130 | 135 | 140 | 145 | 150
Flange 1 | -0.014 | -0.0155 | -0.018 | -0.02 | -0.02 | -0.0205 | -0.0205 | -0.0205 | -0.0205
Flange 2 | -0.016 | -0.019 | -0.02 | -0.02 | -0.02 | -0.0205
Flange 3 | -0.0175 | -0.0205 | -0.022 | -0.023 | -0.0235 | -0.024 | -0.024
Flange 4 | -0.0125 | -0.0155 | -0.0175 | -0.021 | -0.021 | -0.0225 | -0.023 | -0.023 | -0.0235 | -0.0235 | -0.024 | -0.024 | -0.024 | -0.024

## Slide 4: Gasket Crush Test
Same setup with three new gaskets and three new sets of fasteners
Lower amounts of crush may be due to fewer stress cycles
Torque (in-lb) | Bolt Strech | Gasket Crush
120 | < 0.002” | 0.008 – 0.010”
145 | 0.003 – 0.009” | 0.010 – 0.012”
Chart: Crush in Gasket
| 120 | 145
seal 2 thickness | -0.0075 | -0.01
seal 3 thickness | -0.009 | -0.0115
seal 1 thickness | -0.008 | -0.0105

## Slide 5: Torque Wrench Details
BPM Fastener Investigation, 6/12/2018
Wrench setting (in-lb) | Applied (Real) torque (in-lb) | Error
60 | 56 | 6.6%
120 | 116 | 3.3%
175 | 169 | 3.4%
Torque wrench tested with Snap On electronic torque tester immediately after testing finished

## Slide 6: Conclusion
One bolt broke at 150 in-lbs
Two bolts broke at 175 in-lbs
Some bolt stretching at all torque settings
“Significant” stretching above 130 in-lbs
The exact torque applied to bolts is critical such that bolts remain tight, but do not deform excessively
Chart: Average Bolt Extension
| 105 | 110 | 115 | 120 | 125 | 130 | 135 | 140 | 145 | 150 | 155 | 160 | 165 | 170
Flange 1 | 0.00125 | 0.0020625 | 0.003375 | 0.006 | 0.00875 | 0.018563 | 0.026563 | 0.031563 | 0.034357
Flange 2 | 0.0020625 | 0.002625 | 0.0044375 | 0.005875 | 0.007875 | 0.0094375 | 0.010778 | 0.013813
Flange 3 | 0.0015625 | 0.003875 | 0.005875 | 0.00725 | 0.0088125 | 0.010688 | 0.013313
Flange 4 | 0.0008125 | 0.0011875 | 0.0023125 | 0.002875 | 0.005125 | 0.0074375 | 0.011938 | 0.014688 | 0.0165 | 0.018938 | 0.0215 | 0.024688 | 0.0285 | 0.037125