## Slide 1
Martina Martinello
12 Jun 2018
FCC Workshop SRF summary

## Slide 2: SRF talk at the FCC week
2 plenary talks:
    “SRF R&D overview” by Anne-Marie Valente-Feliciano (Jlab)
    “Summary SRF” by Erk Jensen (CERN)
4 SRF sessions (1 full day):
                Directions for R&D (5 talks)
                Cavity Technology (5 talks)
                Studies (4 talks)
                Innovation (4 talks)

## Slide 3
M. Benedikt, FCC 2018

## Slide 4: FCC-ee RF staging scenario
M. Benedikt, FCC 2018

## Slide 5: SRF technology for FCC-ee
SRF cavities for FCC-ee:
      Technology comparison for FCC-ee:
        Bulk Nb (N-doping): high-Q at medium field
        Nb3Sn/Nb: higher Tc
        Nb/Cu: cheaper technology
        Nb3Sn/Cu: higher Tc and cheaper
FCC-ee W
FCC-ee Higgs & top
S. Aull, FCC 2017

## Slide 6: SRF technology for FCC-ee
        Bulk Nb (N-doping)
        Nb3Sn/Nb
        Nb/Cu
        Nb3Sn/Cu
        Alternative fabrication methods

## Slide 7: SRF technology for FCC-ee
        Bulk Nb (N-doping)
        Nb3Sn/Nb
        Nb/Cu
        Nb3Sn/Cu
        Alternative fabrication methods

## Slide 8: Frequency dependence of Nb SRF cavities
New frequency-dependence studies show that anti-Q-slope typical of N-doping cavities is absent at 650 MHz
Doping need some optimization for low frequencies
N-doping still very promising for 800 MHz cavities
N-doping
N-doping
120C baking
f0=1.3 GHz
M. Martinello et Al., FCC 2018

## Slide 9: Frequency dependence of Nb SRF cavities
P. Sha et Al., FCC 2018

## Slide 10: Frequency dependence of Nb SRF cavities
F. Marhauser et Al., FCC 2018

## Slide 11: Frequency dependence of Nb SRF cavities
F. Marhauser et Al., FCC 2018

## Slide 12: SRF technology for FCC-ee
        Bulk Nb (N-doping)
        Nb3Sn/Nb
        Nb/Cu
        Nb3Sn/Cu
        Alternative fabrication methods

## Slide 13: Nb3Sn Coatings for High Q0
With a critical temperature of 18 K, Nb3Sn at 4.4 K can have similar Q0 to Nb at 2.0 K
Cryogenic plant at 4.4 K vs 2.0 K: efficiency is 3-4 times better, capital costs are smaller, higher reliability…
In last ~5 years, substantial improvements to Nb3Sn cavity performance under Cornell program
New Fermilab program now achieving good performance on 1-cell 1.3 GHz cavities—larger cavities to be coated soon
Tc ~ 18 K
Cavity surface – matte gray
New results March 2018
Courtesy of S. Posen

## Slide 14: Summary on SRF technology for FCC
Technology comparison for FCC-ee (400/800 MHz SRF Nb cavities):
  N-doping: high-Q at medium field
      Best technology for 2 K operation
      Suitable for operation at 10 and 20 MV/m
      Mature technology already applied to cryomodules production and fully transferred to industry
  Nb3Sn: higher Tc
      Best technology for 4.5 K operation at 10 MV/m
      Need to improve quench field to be suitable for operation at 20 MV/m (potential for operation at very high gradient → 80 MV/m)
      Not yet implemented to cryomodules production
M. Martinello et Al., FCC 2018

## Slide 15: SRF technology for FCC-ee
        Bulk Nb (N-doping)
        Nb3Sn/Nb
        Nb/Cu
        Nb3Sn/Cu
        Alternative fabrication methods

## Slide 16: Nb/Cu thin film technology
Nb/Cu technology is cheaper therefore particularly attractive for low frequency cavities
Nb/Cu cavities affected by Q-slope problem

## Slide 17: Nb/Cu thin film cavities at CERN
25 Nb/Cu Quarter Wave Resonators for HIE-ISOLDE. Thin film deposition via diode sputtering
Recently measured 2 cavities with the best performance ever obtained for HIE-ISOLDE cavities
Improvement given by the seamless copper substrate
G. J. Rosaz et Al., FCC 2018

## Slide 18: Nb/Cu thin film cavities at CERN
25 Nb/Cu Quarter Wave Resonators for HIE-ISOLDE. Thin film deposition via diode sputtering
Recently measured 2 cavities with the best performance ever obtained for HIE-ISOLDE cavities
Improvement given by the seamless copper substrate
G. J. Rosaz et Al., FCC 2018

## Slide 19: Nb/Cu thin film cavities at CERN
Looking back at LHC cavities, spun cavities show the best performances
The substrate matter!! More investigation is on-going
G. J. Rosaz et Al., FCC 2018

## Slide 20: Nb/Cu thin film cavities at CERN
Looking back at LHC cavities, spun cavities show the best performances
The substrate matter!! More investigation is on-going
SPINNING
DEEP DRAWING

## Slide 21: Nb/Cu thin film cavities at Jlab
A.M. Valente-Feliciano et Al., FCC 2018
M. Arzeo et Al., FCC 2018

## Slide 22: Nb/Cu thin film cavities at INFN/LNL
Nb/Cu coating on 6 GHz spun Cu cavities
Nb deposited via magnetron sputtering
Many parameters investigated: thick vs thin films, multilayer/single shot deposition, pressure, etc.
Some defects remain even after mechanical grinding
C. Pira et Al., FCC 2018

## Slide 23: SRF technology for FCC-ee
        Bulk Nb (N-doping)
        Nb3Sn/Nb
        Nb/Cu
        Nb3Sn/Cu
        Alternative fabrication methods

## Slide 24: Nb3Sn/Cu thin film deposition at CERN
K. Ilyina-Brunner et Al., FCC 2018

## Slide 25: Nb3Sn/Cu thin film deposition at CERN
Tc suppressed with both annealing after coating and during coating
Cu inter-diffusion observed in both cases
Film cracking after annealing observed
Intermediate layer approach proposed to solve these issues
K. Ilyina-Brunner et Al., FCC 2018

## Slide 26: Nb3Sn/Cu thin film deposition at CERN
K. Ilyina-Brunner et Al., FCC 2018

## Slide 27: SRF technology for FCC-ee
        Bulk Nb (N-doping)
        Nb3Sn/Nb
        Nb/Cu
        Nb3Sn/Cu
        Alternative fabrication methods

## Slide 28: Electrohydraulic forming applied to SRF cavities
C. Abajo et Al., FCC 2018

## Slide 29: Selective Laser Melting for SRF application
R. Gerard et Al., FCC 2018

## Slide 30: Conclusions
E. Jensen, FCC 2018