## Slide 1
Mentor: Alexander Romanenko
Group: Technical Division-Quantum Computing
Presenter: Andrew Lambert
06 August 2018
Qubit Defect Analysis

## Slide 2: Introduction
Quantum Computing is meant to solve problems that are intractable to classical computers- e.g. molecular modeling etc
Utilizes quantum mechanical phenomena such as quantum superposition-classical computer scales 2n, Quantum Computer scales 2^n
One of the biggest challenges facing quantum computing is coherence.
My work aims to investigate sources of decoherence

## Slide 3: Our Qubit
Figure 2. a) (left) SEM image of qubit, b) (middle) superconducting resonator, c) (right) superconducting qubit.

## Slide 4: Experiment Overview
Qubit did not work
LSCM
SEM
AFM
Figure 1. Dispersive Shift

## Slide 5: Laser Scanning Confocal Microscope
Used for profilometry, surface roughness, and imaging
Image constructed pixel by pixel
Figure 3. LCM

## Slide 6: Scanning Electron Microscopy
Used for elemental analysis, imaging, and crystallographic structure
Energy Dispersive Spectroscopy utilizes secondary electrons and back scattered electrons
Electron Backscattered Diffraction is for analyzing chrystollography
Figure 4. SEM

## Slide 7: Atomic Force Microscopy
Used for imaging and surface topology
Uses force difference between sample and tip to generate surface topology.
Figure 5. AFM

## Slide 8: LSCM
Possible Defect
Figure 6. a) (left) 150x magnification, b) (middle) 50x magnification, c) (right) measurement comparison between 50x and 150x.

## Slide 9: SEM Analysis
Figure 7. EDS analysis done at 15 kV a) (left) Layered image, b) (middle) silicon, c) (right) oxygen.

## Slide 10: SEM Analysis Continued
Figure 8. SEM Analysis done at 27 kV

## Slide 11: EBSD Analysis
Figure. (left) arrangement of crystal planes clearly seen. (right) noisy image

## Slide 12: EBSD Analysis
Figure 9. Monte Carlo Simulation of electron penetration depth at 15 kV

## Slide 13: AFM
Figure 10. (top left and right) AFM image of niobium step height.

## Slide 14: AFM Continued
 | Niobium Step Height (nm) |  | 
Measurement | Area 1 | Area 2 | Area 3
1 | 100 | 100 | 130
2 | 110 | 110 | 150
3 | 110 | 120 | 160
4 | 110 | 110 | 150
Figure 11. AFM measurements

## Slide 15: AFM Continued
300 K
200 K
50 K
10 K
Figure 12. AFM images.

## Slide 16: Conclusion
Nb film deposition process is uneven
Possible foreign material that may affect superconductivity
Next Steps
Better sample prep
Cross sectional analysis
Qubit device modeling
Analise multiple working and non-work qubits for comparison