## Slide 1
Martina Martinello
International Workshop on Cryomodule Design and Standardization
7th September 2018
High-Q Performance

## Slide 2: Overview of state-of-the-art surface treatments for SRF cavities

## Slide 3: State-of-the-art treatments
High-Q0
(e.g. LCLS-II)
High-Q0
High-Eacc
(e.g. ILC)
High-Eacc
(e.g. ILC)

## Slide 4: High-Q0 treatments
High-Q0
(e.g. LCLS-II)

## Slide 5: N-doping treatment
800 C (3 hours)
25 mTorr (2 minutes)
Example of a N-doping process (2/6 recipe):
Nb bulk EP cavity annealed for 3 hours in vacuum (UHV furnace) at 800C
Nitrogen injected (25 mTorr) at 800C for 2 minutes
Cavity stays for another 6 minutes at 800C in vacuum
Cooling in vacuum
5 um electro-polishing (EP)
Cavity after welding
EP 140 μm
3 h at 800C UHV baking
48 h at 120C baking
N2 injection 800C
EP 5 μm

## Slide 6: N-doping treatment (2/6 recipe)
N
Nb
N Interstitial
Only Nb from TEM/NED spectra:
N must be interstitial
Final RF Surface
Y. Trenikhina et Al, Proc. of SRF 2015

## Slide 7: Origin of the anti-Q-slope
Anti-Q-slope emerges from the BCS surface resistance decreasing with field
Anti-Q-slope
A. Grassellino et al, Supercond. Sci. Technol. 26 102001 (2013) - Rapid Communications
A. Romanenko and A. Grassellino, Appl. Phys. Lett. 102, 252603 (2013)

## Slide 8: High-Q0/High-G treatments
High-Q0
High-Eacc

## Slide 9: Example of N-infusion processing sequence
Bulk electro-polishing
High T furnace (with caps to avoid furnace contamination):
  800C 3 hours HV
  120C 48 hours with N2 (25 mTorr)
NO chemistry post furnace
HPR, VT assembly
Protective caps and foils are BCP’d prior to every furnace cycle and assembled in clean room, prior to transporting cavity to furnace area
A. Grassellino et al., arXiv:1305.2182
A. Grassellino et al 2017 Supercond. Sci. Technol. 30 094004
160 C
48 h
96 h
25 mTorr
10-5 mTorr

## Slide 10: Comparison N-doped vs N-infusion
N-doped N profiles are up to deep
N-infused N profiles are deep
N-doped
N-infusion

## Slide 11: What gives the Q improvement at high field with 120C infused?
Improvement stems from both lower residual and lower BCS surface resistance
Standard 120C baking
120C N-infusion
Standard
120C baking
120C N-infusion
A. Grassellino et al 2017 Supercond. Sci. Technol. 30 094004

## Slide 12: N-infusion easily affected by furnace contamination
Example of N-infused cavity contaminated by furnace environment
Quite high level of hydrocarbons may be absorbed by the cavity
Notes: We’re doing cost savings studies to try to make the ILC more affordable and increasing the gradient has the largest impact, but Q0 also has a strong impact

## Slide 13: Modified 120C baking: 4h at 75C + 48h at 120C
A thermocouple went faulty and oven went to standby. Cavity lingered around 75C for about 2 hours, then resumed the 120C 48 hours -> increase in both Q and gradient observed
Several cavities made after that, adding the 75C step for 4 h, confirming the results -> work in progress to better understand treatment repeatability and physics

## Slide 14: 120 C modified baking: new discovery
times higher gradient
UP TO
A. Grassellino et al., to be published (2018)

## Slide 15: Next surprise: the BCS resistance is ~ as 120C N infused
A. Grassellino et al, https://arxiv.org/abs/1806.09824
BCS surface resistance is lowered compare to standard 120C baking
Residual resistance comparable with standard 120C baking

## Slide 16: High-Q preservation: from vertical test to cryomodule

## Slide 17: Surface resistance contributions

## Slide 18: Surface resistance contributions
⇒ BCS (temperature-dependent part) surface resistance
⇒ intrinsic residual resistance
These contributions don’t change from vertical test to cryomodule, they only depends on material properties, surface treatment and temperature

## Slide 19: Surface resistance contributions
⇒ trapped magnetic flux surface resistance
—flux trapping efficiency
—trapped flux sensitivity
—external magnetic field
H. F. Hess et al., Phys. Rev. Lett. 62, 214 (1989)
Cooldown
Flux trapping efficiency and the amount of external magnetic field can significant change from vertical test to cryomodule, affecting the surface resistance depending on the trapped flux sensitivity

## Slide 20: Trapped flux surface resistance
These losses can be reduced by minimizing these contributions:
𝐵
Magnetic shielding/hygiene improvement
𝜂_𝑡
Fast Cooling
Material Optimization
S
Optimizing surface treatment (mean free path)
Magnetic shielding/hygiene improvement
Fast Cooling
Material Optimization
S
Optimizing surface treatment (mean free path)

## Slide 21: Trapped flux surface resistance
These losses can be reduced by minimizing these contributions:
𝐵
Magnetic shielding/hygiene improvement
𝜂_𝑡
Fast Cooling
Material Optimization
S
Optimizing surface treatment (mean free path)
Magnetic shielding/hygiene improvement
Fast Cooling
Material Optimization
S
Optimizing surface treatment (mean free path)
External magnetic field

## Slide 22: Minimization of remnant field in LCLS-II pCM
Demagnetization
Empty vacuum vessel
Assembled Cryomodule
Coils for magnetic field demagnetization
Demagnetization

## Slide 23: Trapped flux surface resistance
These losses can be reduced by minimizing these contributions:
𝐵
Magnetic shielding/hygiene improvement
𝜂_𝑡
Fast Cooling
Material Optimization
S
Optimizing surface treatment (mean free path)
Magnetic shielding/hygiene improvement
Fast Cooling
Material Optimization
S
Optimizing surface treatment (mean free path)
Flux Trapping Efficiency

## Slide 24: Fast cooldown helps flux expulsion
Fast cool-down lead to large thermal gradients efficient flux expulsion
Slow cool-down lead to small thermal gradients poor flux expulsion
A. Romanenko et al., Appl. Phys. Lett. 105, 234103 (2014)
A. Romanenko et al., J. Appl. Phys. 115, 184903 (2014)
D. Gonnella et al, J. Appl. Phys. 117, 023908 (2015)
M. Martinello et al., J. Appl. Phys. 118, 044505 (2015)
S. Posen et al., J. Appl. Phys. 119, 213903 (2016)
S. Huang, Phys. Rev. Accel. Beams 19, 082001 (2016)
T1
T2
All flux trapped
Efficient flux expulsion
Bsc/Bnc=1.74 after complete Meissner effect
Bsc/Bnc=1 after full flux trapping
Bsc/Bnc
Q0

## Slide 25: High T baking for flux expulsion improvement
Not all materials show good flux expulsion even with large thermal gradient
High T treatments are capable to improve materials flux expulsion properties
S. Posen et al., J. Appl. Phys. 119, 213903 (2016)
Full trapping
Full expulsion
Full expulsion
Full trapping

## Slide 26: High T baking for flux expulsion improvement
S. Posen et al., J. Appl. Phys. 119, 213903 (2016)
After 900C
Full trapping
Full expulsion
After 1000C
Full expulsion
Full trapping
Not all materials show good flux expulsion even with large thermal gradient
High T treatments are (usually) capable to improve materials flux expulsion properties

## Slide 27: Trapped flux surface resistance
These losses can be reduced by minimizing these contributions:
𝐵
Magnetic shielding/hygiene improvement
𝜂_𝑡
Fast Cooling
Material Optimization
S
Optimizing surface treatment (mean free path)
Magnetic shielding/hygiene improvement
Fast Cooling
Material Optimization
S
Optimizing surface treatment (mean free path)
Trapped Flux Sensitivity

## Slide 28: Light doping to minimize trapped flux sensitivity
Trapped flux sensitivity:
Bell-shaped trend of as a function of mean free path
N-doping cavities present higher sensitivity than standard treated cavities
Light doping is needed to minimize trapped flux sensitivity
M. Martinello et al., App. Phys. Lett. 109, 062601 (2016)

## Slide 29: Status of SRF Technology for PIP-II

## Slide 30: 162.5 MHz Half-Wave Resonators
*HWR technology developed at ANL via ANL/FNAL PIP-II Collaboration.
Z. Conway, A. Barcikowski, S. Gerbik, C. Hopper, M.P. Kelly, M. Kedzie, S. Kim, P. Ostroumov, T. Reid.
Bulk and light EP of jacketed HWR @ ANL
Bare HWR before jacketing
Surface treatments:
Light BCP
Deep EP
Baking at for 10 hours in UHV furnace
Light EP

## Slide 31: HWR 2 K Test Results
PIP-II specs
Curtesy of A. Lunin and Z. Conway

## Slide 32: SSR1: 325 MHz Single Spoke Resonators
Surface treatments:
Bulk BCP
Baking at for 10 hours in UHV furnace
Light BCP
Low T baking at for 48 hours
particularly favorable to process MP
L. Ristori, M.H. Awida ,P. Berrutti, T.N. Khabiboulline, M. Merio, D. Passarelli, A. Rowe, D.A. Sergatskov, A.I. Sukhanov, Proc. of IPAC 2013, Shangai, China

## Slide 33: SSR1 VTS Test Result
PIP-II
specs
Curtesy of A. Sukanov

## Slide 34: Fully-Integrated Tests in STC
9 cavities pre-qualified after test at STC with low power coupler
Some degradation observed between VTS test and STC test that may be due to flux trapping -> some studies are being carried out to better understand trapped flux sensitivity in SSR cavities
5 cavities tested with high power coupler → cavities meet spec and are now waiting for string assembly
PIP-II
specs
Courtesy of A. Sukhanov
STC tests with low power coupler
STC tests with high power coupler

## Slide 35: HB650 Single-cell Test Results
PIP-II
specs
120C baked cavities not always meet specs
N-doping capable to double the Q-factor at medium field, sometimes affected by early quench
World record Q-factor of 7e10 at 2K,17 MV/m and 650 MHz with N-doping

## Slide 36: Frequency dependence of RBCS(Eacc)
N-doped cavities at 650 MHz do not show the RT reversal (anti-Q-slope) typically observed at 1.3 GHz
N-doping
120C baking
M. Martinello et al. SRF 2017 (TUYAA02), IPAC 2018 (WEPML013)
Also for 120C baked cavities, the field dependence of RT is unfavorable at low frequencies
The physical mechanism underneath the reversal of RBCS (here called RT) has a stronger effect at high frequencies
650 MHz cavities

## Slide 37: HB650 Single-cell R&D program
Because of the recent significant improvement in the SRF technology, now we started an intensive R&D program for 650 MHz cavities
  GOAL: reach the highest possible Q at medium/high field for 650 MHz cavities
  Flux expulsion and trapped flux sensitivity will be also taken into account for Q preservation in cryomodule
Surface treatments under studies: EP, BCP for baseline and modified 120C (75-120C baking), N-doping, N-infusion for Q improvement
Trapped flux sensitivity will be acquired for each treatment to understand magnetic flux shielding requisition in cryomodule

## Slide 38: Summary RF results of 650 MHz cavities new R&D program
T=2 K
T=1.4 K

## Slide 39: HB650 5-cells Tests Results (all N-doped + “heavy” EP)
PIP-II
specs
B9A-AES-010
B9A-AES-009
B9A-AES-008
Light N-doping applied to 650 MHz cavities
3 N-doped 5-cells 650 MHz cavities meet PIP-II specification
B9A-AES-010 is now being dressed with He vessel

## Slide 40: Conclusion and Future plan
Thanks to recent advance in the SRF technology, several treatments are suitable for high-Q at medium/high gradient
Since the field dependence of Rbcs strictly varies with frequencies, N-doping in 650 MHz cavities is not as effective as in 1.3 GHz cavities
The optimal surface treatment for 650 MHz cavities is therefore under investigation, taking into account the needed for low trapped flux sensitivity at medium field
Trapped flux sensitivity and flux expulsion to be studied to set specification of magnetic field shielding
HWR and SSR cavities meet PIP-II spec with standard BCP/baking treatment -> R&D is planned to further improve Q in SSR2 cavities

## Slide 41: Thank you for your attention!