## Slide 1
Thomas Smart
University of St Andrews
Mentor: Dr Mattia Checchin
Study of the field-dependency of surface resistance for SRF cavities

## Slide 2: Project Overview
Weeks 1 - 2 | Initial reading
Weeks 2 - 5 | AES022 first test – 120°C bake
Weeks 6 - 8 | Romanenko Hydride model
Weeks 9 - 10 | AES022 second test – modified 120°C bake Final Report and Presentation

## Slide 3: The problem to be addressed…
Future accelerators (i.e ILC and FCC) rely on an efficient acceleration of particles to minimize size and cost.
Key factor in this is a high Q0 and high Eacc
Wish to test different surface treatments on the same cavity to see if improvements are possible -> RF characterization & T-map

## Slide 4: Surface Resistance
G = 270Ω
‘Geometry factor’

## Slide 5: AES022 – First Test (standard 120°C bake)
120°C bake:
150μm EP
800C HV for 3h
HPR and VTS assembly
120C for 48h in situ HV
AES022 – 1.3GHz, single cell
2K
1.5K
Heavily understood within SRF

## Slide 6: Temperature mapping in AES022
2K
1.5K
Strong heating along column 8 (equator), some effect of weld?
Characterise via hydride heating model?

## Slide 7
Model for heating for HFQS proposed by A. Romanenko et al (2013)
Now try and model the local heating of AES022 using Romanenko EP model.
Use 4D parameter search (B0, ⍺Rn, R0, σ) using custom Python script.
Model should not work globally for AES022 but this model has not been readily tested locally.
Model assumes heating due to the formation of nano-hydrides within the Nb bulk.
SC
SC
NH
Proximity Effect
Modelling the heating on T-Map
A.Romanenko and F.Barkov, “Proximity breakdown of hydrides in superconducting niobium cavities,” Superconductor Science and Technology 26 (2013) .

## Slide 8
Both data sets are is agreement with model.
Compare with EP to check validity
120°C bake

## Slide 9
Global presence of hydrides indicated from fits
Local modelling of R0 valid
EP

## Slide 10
AES022 – Second Test (modified 120C bake)
Modified 120°C Bake:
40μm EP
HPR and VTS assembly
75°C 4h bake HV
120°C 48h in situ HV
Only discovered a few months ago
Previous data taken by A. Grassellino et al (2018)
A.Grassellino et al.,“Accelerating fields upto 49MV/m in TESLA-shape superconducting RF niobium cavities via 75C vacuum bake,” arXiv:1806.09824
2K
1.5K

## Slide 11
AES022 – Second Test (modified 120C bake) continued…
The quench field for collected data is ~42MV/m compared to fields ~50MV/m achieved in earlier data. Rs change also odd.
Material problem?
Hydride formation of different phases (⍺, ε, δ etc.) ?
Cooldown speed? Higher sensitivity to temperature ?

## Slide 12
Temperature Mapping in AES022 – second test
2K
1.5K
Global heating observed
Hydrides still along weld?

## Slide 13
Conclusion
Modified 120°C bake has the potential for v high accelerating fields (~50MV/m) -> Many more factors at work?
Presence of hydrides can be predicted locally using model proposed by A. Romanenko et al.
More investigations need to be performed on the modified 120°C bake before it can be adequately used in future colliders
Further investigations into hydride formation during electro-weld process need to be performed

## Slide 14
Quench ~ 41MV/m