## Slide 1
Patrick Hurh, Robert Zwaska et al
Target Systems Dept, AD
Fermilab
The Fermilab High Power Targetry R&D Program

## Slide 2: Neutrinos continue to make news

## Slide 3: The Nobel of Neutrinos
Invented as a particle “impossible” to detect (Pauli, 1930)
  Save conservation of energy and angular momentum
Detected by Cowan & Reines in 1956 (Nobel 1995)
Lederman, Schwartz, & Steinberger developed the Neutrino Beam in 1962 (Nobel 1988)

## Slide 4: The Nobel of Neutrinos
Cosmic Neutrinos (solar, atmospheric, and supernovae) discovered over several decades, for Koshiba & Davis (Nobel 2002)
Neutrino Oscillations (solar & in-beam) for Kajita & McDonald (Nobel 2015)
What is left in store?

## Slide 5: Fermilab Accelerator Complex

## Slide 6: The NuMI Facility “Neutrinos (ν – Nu) at the Main Injector”
Intense muon-neutrino beam directed towards Minnesota
Main Injector supplies 25 – 50 trillion 120GeV protons every 1.33 seconds
  Operating regularly at 700 kW
Each pulse produces about 1014 ν 
  ~ 20,000,000 Pulses per year
Direct beam 3o down
On-site and off-site experiments
Different types of neutrino beams
Beam is 10s of kilometers wide at exit
Near Detector: 980 tons
Far Detector: 5400 tons
5

## Slide 7: Multiple Experiments in the NuMI Beam
Long-baseline oscillation experiments
Neutrino scattering experiments

## Slide 8
Neutrino mixing drives the push to beams
Accelerator/Atmospheric/Reactor
Solar sector
Majorana phases
increasing neutrino mass
→ Why is 23 near maximal?
→ What is 13 and why is it small?
→ Why so different than quark mixing?
→ Is CP violation is present?
→ Are neutrinos Majorana?
→ What is the hierarchy of neutrino masses?

## Slide 9: Why a Beam? – Controlled Laboratory Experiment
Natural sources exist – but they are very weak and not necessarily well understood
  Solar and atmospheric neutrinos only understood once oscillations were established and well understood
    Moving from observation to experiment
  Supernovae are hard to come by
Artificial beams are controlled and intense
  Decide when, where, and how the beam is generated
  Detectors are placed strategically
  Beams can be controlled with precision – vital as measurements approach 1%
Applications:
  Today neutrino oscillation is the first focus
  Probe of nuclear structure
  Observation of the neutral current
  Demonstration of neutrino flavor (muon, tau)
  Measurement of weak mixing angle

## Slide 10: The NuMI Beam “Neutrinos at the Main Injector”
400 kW design average power
700 kW upgrade for NOvA
s ~ 1 mm
2 interaction length, C target
Produces p+, K+ mesons
Pulsed focusing horns
Toroidal magnetic field
Parabolic inner conductor profile
Focuses meson momentum band
2 m diameter
Roughly decay length for 10 GeV p+
He-filled
Absorbs ~ 40 % of beam power
Allows high-energy muons to penetrate
Measure hadron & muon fluxes
Arrays measure distributions
Notes: Go light on horn description, other details

## Slide 11: Pion Decay
Neutrinos produced at random direction in pion rest frame
  Boosted in the direction of the beam
  Ultimate energy determined by the decay angle with respect to the boost, in the lab:
  Muon carries the balance of the energy
Flux is also affected such that the beam is strongly directed in the direction of the pion velocity:
All two-body decays have this functional form. Three body-decays are boosted in the same way, but are complicated by the decay kinematics

## Slide 12: Off-Axis Beam
Technique used by T2K in Japan & NOvA at Fermilab
  First proposed by BNL
  Fewer total number of neutrino events
  More at one narrow region of energy, tuned to oscillation probability
  For nm to ne oscillation searches, backgrounds spread over broad energies

## Slide 13: Defining Characteristics of Long Baseline Beams
Proton Beams: synchrotron based, nearing 1 MW
  High Stored Energy: ~ 1 MJ
  Small Beam Spot: 1 – few mm
  High Proton Energy: 30-120 MJ
  Single-turn extraction, long cycle time: 1 – few seconds
Pion Focusing: Pulsed horns
  Horns more efficient than quads
  High currents: few hundred kA
Large Decay volume
  Meters in cross-section
  100s of meters in length
Beam radiation dispersed over extended area
  Tritium, activation, corrosion, cooling

## Slide 14: The MINOS Target
Water cooled
graphite core
Encased in
vacuum / helium can
with beryllium windows
~ 4 kW beam power
deposited in target

## Slide 15: NOvA Target
Graphite fins: 50 x 24 mm; 7.4mm wide
Helium atmosphere
Beryllium windows
Water cooled aluminum pressing plates
fins not brazed to cooling (cf. NT-series)
Water cooled outer vessel
IHEP Protvino (Russia) did initial design
STFC-RAL / FNAL did final design and construction

## Slide 17: Horn Fabrication

## Slide 18: Challenging Environments
Replaced NuMI Horn summer 2015 due to failed stripline
  First 700 kW capable horn, in service since Sept. 2013, accumulated ~ 27 million pulses
Failure was due to fatigue, likely enhance by vibrations

## Slide 19: DUNE: Deep Underground Neutrino Experiment LBNF: Long-Baseline Neutrino Facility

## Slide 20: DUNE Considering optimized focusing systems
Automated optimizations yielding 2m target and 3 large horns
NuMI-like
80 GeV protons
Optimized target & horns push the envelope of technology, particularly with a 1.2 MW beam (upgradeable to 2.4 MW)

## Slide 21: High Power Targetry Challenges
Recently major accelerator facilities have been limited in beam power not by their accelerators, but by their target facilities (SNS, NuMI/MINOS)
Plans for future high power, high intensity target facilities will present even greater challenges
To maximize the benefit of high power accelerators (physics/$), these challenges must be addressed in time to provide critical input to multi-MW target facility design

## Slide 22: Recognition of HPT Challenges
“Sustained, focused research into target technology in the context of a broad international collaboration of interested laboratories will be essential.”
-Snowmass 2013 Report, Section 6.4.3 High Power Targets
“High power targets, as noted at Snowmass, will address critical needs and should be included in GARD.”
-2014 Report of the Particle Physics Project Prioritization Panel
“Fund generic high-power component R&D at a level necessary to carry out needed thermal shock studies and ionizing radiation damage studies on candidate materials that are not covered by project-directed research."
-Recommendation 1 from Accelerator R&D Sub-panel 2015 Report

## Slide 23: Fermilab HPT R&D Program
      Objectives
          To enable the design, construction, and operation of multi-MW target facilities through development of the required simulation/modeling methods and through measurement of required irradiated material behavior data;
          To develop advanced targetry technologies using these methods and data;
          And to point the way to new radiation and thermal shock compatible materials and technologies.
      Outcomes Reduce the cost and enhance the effectiveness of existing and future facilities by:
          Lowering operation costs;
          Increasing operating time;
          And optimizing useful secondary particle production.
        Beneficiaries
          Specifically planned to benefit HEP projects such as LBNF and other multi-MW or high intensity beamlines
          But also generally benefits all HPT facilities such as spallation neutron sources and rare isotope beam facilities

## Slide 24: High Power Targetry Scope
Target
  Solid, Liquid, Rotating, Rastered
Other production devices:
  Collection optics (horns, solenoids)
  Monitors & Instrumentation
  Beam windows
  Absorbers
Collimators (e.g. 100 TeV pp collimators)
Facility Requirements:
  Remote Handling
  Shielding & Radiation Transport
  Air Handling
  Cooling System
R&D Needed to Support:
Notes: Add tie in with 100 TeV pp collider collimator

## Slide 25: High Power/Intensity Targetry Challenges
Material Behavior
  Thermal “shock” response
  Radiation damage
  Highly non-linear thermo-mechanical simulation
Targetry Technologies (System Behavior)
  Remote handling
  Target system simulation (optimize for physics & longevity)
  Rapid heat removal
  Radiation protection
  Radiation accelerated corrosion
  Manufacturing technologies
Subjects of the RaDIATE Collaboration
Proton Accelerators for Science and Innovation Workshop 2012 identified radiation damage as the most cross-cutting challenge facing HPT facilities
P5 2014 Recommendation for GARD
Prioritized first by 2017 HPT R&D Roadmap Workshop

## Slide 26: Thermal Shock (stress waves)
Fast expansion of material surrounded by cooler material creates a sudden local area of compressive stress
Stress waves (not shock waves) move through the target
Plastic deformation, cracking, and fatigue can occur
Ta-rod after irradiation with 6E18 protons in 2.4 s pulses of 3E13 at ISOLDE (photo courtesy of J. Lettry)
Simulation of stress wave propagation in Li lens (pbar source, Fermilab)
Notes: Ta-rod after irradiation with 6E18 protons in 2.4 s pulses of 3E13 at ISOLDE

## Slide 27: Stress wave example: T2K window
Material response dependent upon:
  Specific heat (temperature jump)
  Coefficient of thermal expansion (induced strain)
  Modulus of elasticity (associated stress)
  Flow stress behavior (plastic deformation)
  Strength limits (yield, fatigue, fracture toughness)
Heavy dependence upon material properties, but:
Material properties dependent upon Radiation Damage…
S. Bidhar, FNAL
Preliminary
Notes: Note that magnitude of stresses is not the issue, but the number of stress cycles from just one pulse. High Cycle Fatigue!

## Slide 28: Radiation Damage Effects
Displacements in crystal lattice (expressed as Displacements Per Atom, DPA)
  Embrittlement
  Creep
  Swelling
  Fracture toughness reduction
  Thermal/electrical conductivity reduction
  Coefficient of thermal expansion
  Modulus of Elasticity
  Fatigue response
  Accelerated corrosion
  Transmutation products
    H, He gas production can cause void formation and embrittlement (expressed as atomic parts per million per DPA, appm/DPA)
Very dependent upon material condition and irradiation conditions (e.g. temp, dose rate)
S. A. Malloy, et al., Journal of Nuclear Material, 2005. (LANSCE irradiations)
0 DPA
3.2 DPA
23.3 DPA
14.9 DPA
Notes: One notes that all the properties that are important for thermo-mechanical health of the target are affected by radiation damage. The dependence on irradiation temperature is due to annealing (or healing) the crystal structure is faster at higher temperatures.

## Slide 29: Radiation damage effects can be significant
N. Maruyama and M. Harayama, “Neutron irradiation effect on … graphite materials,” Journal of Nuclear Materials, 195, 44-50 (1992)
Factor of 10 reduction in conductivity at 0.02 DPA
D.L. Porter and F. A. Garner, J. Nuclear Materials, 159, p. 114 (1988)
Void swelling in 316 Stainless steel tube (on right) exposed to reactor dose of 1.5E23 n/cm2

## Slide 30
In 2017, MoU revision has counted J-PARC (KEK+JAEA) & CERN as official participants
R a D I A T E Collaboration
http://radiate.fnal.gov
To generate new and useful materials data for application within the accelerator and fission/fusion communities;
To recruit and develop new scientific and engineering experts who can cross the boundaries between these communities;
To initiate and coordinate a continuing synergy between research in these communities, benefitting both proton accelerator applications in science and industry and carbon-free energy technologies
Radiation Damage In Accelerator Target Environments
@J-PARC, Sep.20, 2017
STFC
CERN
FRIB
PNNL
ESS
FNAL
J-PARC
@FNAL, Dec.11, 2017

## Slide 31: Summary of Major HPT Accomplishments & Impacts
RaDIATE collaboration grew from 5 institutions (2013) to 14 institutions (2017) on the MOU and 70 participants
Completed comprehensive literature study on Reactor Radiation Damage in Tungsten, Graphite and Beryllium within context of HPT irradiation environment
Proton Irradiation Studies on Graphite
  Degradation of mechanical/thermal properties and swelling can be partially negated by irradiating at high temperature
  Identified most radiation damage resistant graphite grade
  NSLS-II studies confirmed lattice swelling in HE proton irradiated graphite is similar to reactor irradiated graphite
Proton and Ion Beam Studies on Beryllium
  Significant hardening at low dose can be partially overcome by higher irradiation temperature
  Both Li and He production and subsequent diffusion effects may limit high temperature operation
Note: Targets not included as GARD thrust in 2013 review
Very relevant to HEP (NOvA, LBNF, Mu2e) and also NP and BES (FRIB, SNS-TS2)
Informed design of LBNF target cooling system and choice of graphite grade
Allows confidence to use reactor data for lattice swelling in High Energy (HE) proton regime
Will inform design of Be beam windows for LBNF (desired operating temperature)

## Slide 32: Summary of Major HPT Accomplishments & Impacts (con’t)
In-beam Thermal Shock Test on Beryllium at CERN’s HiRadMat (see next talk, K. Ammigan)
  Validated empirically developed Johnson-Cook strength model used to predict deformation at high temperature and strain rates
RaDIATE organized proton irradiation at BNL’s Isotope Production (BLIP) facility completed
  100’s of specimens supported by 8 RaDIATE institutions subjected to 4.5x1021 181 MeV protons
  Post-Irradiation Examinations (PIE) underway now
  Includes fatigue testing of irradiated Ti alloys utilizing FNAL custom designed and built testing machine
Preparations for In-beam Thermal Shock Test on previously irradiated material at CERN’s HiRadMat
  Will bring together radiation damage and thermal shock for the first time in a controlled experimental setting
  Beam time scheduled for Oct 1, 2018
  See next talk (K. Ammigan)
Allows prediction of stress and deformation of Be beam windows or targets (alternate target material for LBNF)
Benefits many facilities including LBNF, T2K, BDF at CERN, FRIB, and even LHC-HiLumi (collimators)
Radiation damage effects on high cycle fatigue are relatively unknown. Immediately benefits LBNF, T2K, FRIB
Benefits facilities that use Be or Ti beam windows or graphite targets (LBNF, T2K, FRIB, and more)

## Slide 33: Meetings, Conferences, Workshops and Publications
4 in-person annual RaDIATE collaboration meetings
  FNAL, Oxford, PNNL, J-PARC
50 RaDIATE video conference meetings
FNAL hosted HPT R&D Roadmap Workshop
Many invited/contributed oral presentations & session chair roles at conferences & workshops such as:
  High Power Targetry Workshops
  ANS Nuclear Applications of Accelerators
  International Workshop on Spallation Materials and Technology
  IPAC & NAPAC
  Particle Accelerators for Science and Innovation Workshops
  International Congress on Fracture
  International Workshop on Beryllium Technology
List of Publications (7)
  In Back-up Slides
  Phys Rev Acc-Beams
  Journal of Nuclear Materials
  Nuclear Materials and Energy

## Slide 34: Graphite Results –Tensile Properties Partially Recover When Annealed
Chart: Strain (%)
| 2.2055580061755599E-2 | 2.2055580061755599E-2 | 4.4111160123511198E-2 | 6.6166740185266804E-2 | 6.6166740185266804E-2 | 0.132333480370534 | 0.132333480370534 | 0.154389060432289 | 0.154389060432289 | 0.17644464049404501 | 0.17644464049404501 | 0.17644464049404501 | 0.19850022055580099 | 0.220555800617556 | 0.220555800617556 | 0.24261138067931201 | 0.24261138067931201 | 0.26466696074106699 | 0.26466696074106699 | 0.286722540802823 | 0.286722540802823 | 0.30877812086457901 | 0.33083370092633402 | 0.33083370092633402 | 0.33083370092633402 | 0.35288928098809003 | 0.35288928098809003 | 0.37494486104984598 | 0.37494486104984598 | 0.39700044111160099 | 0.419056021173357 | 0.44111160123511201 | 0.46316718129686801 | 0.46316718129686801 | 0.48522276135862402 | 0.50727834142037898 | 0.50727834142037898 | 0.50727834142037898 | 0.52933392148213498 | 0.52933392148213498 | 0.52933392148213498 | 0.55138950154389099 | 0.55138950154389099 | 0.573445081605646 | 0.573445081605646 | 0.59550066166740201 | 0.61755624172915702 | 0.63961182179091303 | 0.66166740185266903 | 0.66166740185266903
0.056DPA | 7.5 | 8.75 | 10 | 11.25 | 12.5 | 12.5 | 14.375 | 16.25 | 17.5 | 18.75 | 20 | 21.87 | 23.12 | 24.37 | 25.62 | 26.87 | 28.12 | 29.37 | 31.25 | 32.5 | 33.75 | 35 | 36.25 | 37.5 | 38.75 | 40 | 41.87 | 43.75 | 45 | 46.87 | 48.12 | 50 | 51.87 | 53.12 | 54.37 | 56.25 | 57.5 | 59.37 | 61.25 | 62.5 | 63.75 | 65.62 | 66.87 | 68.75 | 70 | 71.87 | 73.75 | 75 | 76.25 | 78.12
0DPA 300 C Anneal | 10.5 | 11 | 11.5 | 12 | 12.5 | 13 | 13 | 13.5 | 14 | 14.5 | 15.25 | 15.75 | 16.5 | 17 | 17.75 | 18.5 | 19 | 19.75 | 20.25 | 21 | 21.75 | 22.25 | 23 | 23.5 | 24.25 | 24.75 | 25.5 | 26 | 26.75 | 27.5 | 28 | 28.75 | 29 | 29.5 | 30 | 30.5 | 31.25 | 31.75 | 32.25 | 33 | 33.5 | 34 | 34.75 | 35.25 | 35.75 | 36.5 | 37 | 37.5 | 38 | 38.75 | 39.25 | 39.75 | 40.25 | 11.25
Irradiation Temperature ~150 ˚C
Simos et al

## Slide 35: Graphite Results – Tensile Properties Summary Plot
Simos et al
Chart: Tensile Property Changes Vs DPA
| 0.10299999999999999 | 0.13100000000000001 | 5.6000000000000001E-2
POCO ZXF-5Q Tensile | 0.31244 | 0.31244 | 0.45509
POCO ZXF-5Q Elastic Mod | 0.23167 | -0.084572 | 0.27542
SGL R7650 Tensile | 0.61079 | 0.60007 | 0.54593 | 0.5352
SGL R7650 Elastic Mod | 0.74869 | 0.64797 | 0.47848 | 0.54163
IG-430 Tensile | 1.1134 | 1.0966 | 1.0289 | 1.2995
IG-430 Elastic Modulus | 1.5589 | 1.172 | 1.2233 | 1.3463
IG-430 Tensile 300 C Anneal | 0.44055
IG-430 Modulus 300 C Anneal | 0.83054
POCO ZXF-5Q exhibited smallest change
IG-430 exhibited largest change
Increase in E lowers IG-430 thermal shock resistance

## Slide 36: Graphite Results – X-ray diffraction
W. Bollmann. “Electron-microscopic observations on radiation damage in graphite” Phil. Mag., 5(54):621-624, June 1960.
Simos et al
XRD on BLIP irradiated POCO graphite indicates agreement with c-axis lattice growth results from neutron irradiation

## Slide 37: Neutron irradiated graphite dimensional changes
B.J. Marsden, “Irradiation Damage in Graphite due to fast neutrons in fission and fusion systems,” IAEA-TECDOC-1154, 2000
Big change in c-axis growth ~250 ˚C

## Slide 38: Graphite Results – X-ray diffraction of NuMI graphite fin shows lattice growth and amorphitization at beam center
Simos et al

## Slide 39: Be Results - Beryllium beam window from NuMI (1.6E21 POT)
NuMI Be window (Kuksenko, Oxford)
  Nanohardness shows significant hardening
  Atomic Probe Tomography shows Li production matches MARS [6] predictions and remains homogeneously distributed at ~50 ˚C
Chart: NuMI

## Slide 40: Ion implantation of Beryllium indicates reduced hardening at higher irradiation temperature
He implantation study at Surrey/Oxford
  Maximum beam energy: 2 MeV => 7.5µm implantation depth (SRIM)
  Dose: up to 0.1 dpa currently
  Temperature: 50ºC and 200ºC
  Nano-indentation indicates significant hardening dominated by 2000 appm He production (DPA is lower order effect)
  Less hardening at higher temperature
  Micro-cantilever work shows increase of fracture strength and decrease of work to fracture with severe drop for 50C implantation

## Slide 41: High Energy Proton Irradiation Completed
    181 MeV p irradiation @ BNL’s BLIP facility
  Includes graphite at various temp (up to ~1,000 ˚C)
  Also Beryllium, Ti alloys, Si, TZM, Al, & Ir
  Over 200 specimens from 6 RaDIATE collaborators
  Participants: BNL, PNNL, FRIB, ESS, CERN, J-PARC, STFC, Oxford, FNAL
Completed irradiation on March 9, 2018
  4.5E21 accumulated protons on target
  1.52 peak DPA on Ti alloy achieved
  2nd shipment of activated samples to PNNL completed
  Be, Graphite, and Ti alloy samples will be included in thermal shock in-beam experiment at CERN
Tensile specimens
Microstructural analysis specimens
Fatigue specimens
70mm

## Slide 42: Post-Irradiation-Examinations (PIE) beginning
Preliminary results indicate hardening of Ti alloys at relatively low dose
Fatigue samples will be shipped to FNAL to conduct testing with unique machine compatible with testing highly active samples (25 Hz)
Will be the first time radiation effects on high cycle fatigue are tested on Titanium alloys
In collaboration with Oxford and STFC, meso-scale ultrasonic fatigue testing will also be employed (20 kHz)
3.4mm

## Slide 43: BeGrid1 (HRMT24) – experimental set-up
Experiment successfully completed in September 2015
Consisted of four specimen arrays of thin Beryllium discs and slugs
  Various commercial grades (S200F, S200FH, PF60, S65F) and thicknesses
  Real time measurements of temperature, strain and displacement
  PIE of thin disc specimen at the University of Oxford (2016-2017)

## Slide 44: BeGrid1 (HRMT24) – online results
Real-time thermomechanical measurements
Instrumented Be slugs in downstream containment boxes
LDV for radial displacement measurements
Strain and temperature gages
Array 3 – 24 bunches, 3.2e12 POT
Array 4 – 216 bunches, 2.8e13 POT
Distinctive strain response for the three different Be grades
Residual plastic strain observed upon cool-down

## Slide 45: BeGrid1 (HRMT24) – Post Irradiation Examination Results
Thin disc specimen PIE performed at University of Oxford
Optical microscopy and profilometry to measure out-of-plane plastic deformations
S-65F grade specimens
All Be grades showed less plastic deformation than predicted by available literature strength models
S200FH showed least plastic deformation, in agreement with empirical strength model
Observed plastic strain ratcheting in Array 3
Glassy carbon windows survived without signs of degradation
V. Kuksenko (University of Oxford)

## Slide 46: BeGrid1 (HRMT24) – data analysis
S-200FH 0.75 mm thick specimen
Beryllium S-200FH Johnson-Cook strength model
Strength model parameters empirically determined at Southwest Research Institute (SwRI)
High strain rate and elevated temperature testing with Split-Hopkinson pressure bar
HRMT24 completed successfully and safely with valuable PIE results and validation of advanced strength model
Good agreement
S. Bidhar (FNAL)
Yield stress (σy) dependent on strain rate and temperature
Model parameters A, B, C, m, n empirically determined
Be JC damage model postponed due to limited funding

## Slide 47: Preparations for HiRadMat Experiment
Finished final design
Rapidly fabricating and assembling parts
Working with CERN to create work-dose-plan and procedures
PNNL preparing activated specimens for shipment to CERN

## Slide 48: BeGrid2 (HRMT43) – Pictures

## Slide 49: BeGrid2 (HRMT43) – Pictures

## Slide 50: BeGrid2 (HRMT43) – Pictures

## Slide 51: BeGrid2 (HRMT43) – Pictures

## Slide 52: BeGrid2 (HRMT43) – Pictures

## Slide 53: BeGrid2 (HRMT43) – Pictures

## Slide 54: BeGrid2 (HRMT43) – Pictures

## Slide 55: BeGrid2 (HRMT43) – Pictures

## Slide 56
HPT R&D Summary
R&D for High Power Targetry is benefiting future accelerator target facilities such as LBNF-DUNE and T2K (US-Japan)
  Material choice
  Optimal operating temperature for annealing radiation damage
  Developing/validating material models and simulation techniques
Current HPT R&D Projects include bringing together, for the first time, radiation damage and thermal shock in the RaDIATE HiRadMat Experiment, BeGrid2
Many challenges remain to achieve stable and reliable multi-MW accelerator target facilities in the future
The HPT R&D core team is capable, but small. Additional investment is needed in order to:
  Increase research scope
  Further develop University partnerships
  Develop more efficient irradiation and examination methods
  Add needed capabilities
    Advanced Robotics Lab for Remote Handling
    Post-Irradiation Examination Lab for Active Materials

## Slide 57: RaDIATE
10 keV protons into Beryllium (simulated with SRIM 2008 and artistically rendered with Graphic Converter by P. Hurh)
Radiation Damage In Accelerator Target Environments
Questions?

## Slide 58: Back-Up Slides Follow

## Slide 59
From D. Filges, F. Goldenbaum, in:, Handb. Spallation Res., Wiley-VCH Verlag GmbH & Co. KGaA, 2010, pp. 1–61.
Microstructural response:
creation of transmutation products;
atomic displacements (cascades)
  average number of stable interstitial/vacancy pairs created = DPA (Displacements Per Atom)
Radiation Damage Disorders Microstructure
Slide prepared by V. Kuksenko (Oxford)

## Slide 60: HPT R&D Roadmap Workshop held at Fermilab to develop best R&D routes for next generation targetry facilities
HPT R&D Roadmap workshop held in late May 2017 to come to consensus among the HPT community on best path forward
Next generation target facility requirements were collected
Most promising R&D cycles were identified
Enabling R&D activities identified
Workshop report available on web-site
Final Roadmap report to be completed soon
http://indico.fnal.gov/e/HPT_Roadmap_Workshop_2017
Workshop Charge: Identify the required and most beneficial High Power Targetry (HPT) R&D routes and associated key milestones, considering the needs, objectives, and timeline of the HEP experimental program as recommended in the 2014 P5 report.

## Slide 61: Exploration of Radiation Damage Effects to High Doses Likely Requires High and Low Energy Irradiation Studies
High energy, high fluence, large volume proton irradiations are expensive and time consuming
  Long irradiation beam times (months)
  Difficulties of Post-Irradiation Examination (PIE) of highly activated samples
Low energy, small volume ion irradiations are inexpensive and can achieve several DPA in an hour
  Low to zero activation (PIE in “normal” lab areas)
  Greatly accelerated damage rates (several DPA in hours)
However Low energy ion irradiations have drawbacks:
  Very shallow penetration (0.5-100 microns)
  Little gas production (transmutation) in samples
Promising Solutions:
  Micro-mechanics (coupled with advanced microscopy techniques) may enable evaluation of critical properties
  Simultaneous implantation of He and H ions (triple-beam irradiation)
But still need HE proton irradiations to correlate and validate techniques

## Slide 62
Useful where only small samples are available (implanted layer)
Need for a sample design that can be machined in surface of bulk samples
Geometry that can be manufactured quickly and reproducibly
0.3mm
Beam Thickness 2um
Stress (Pa)
Strain
Fe 6%Cr
Chris Hardie, University of Oxford
, D.Armstrong. University of Oxford
Micro-mechanics can provide mechanical properties at the micro-scale

## Slide 63: New directions and techniques
  High frequency meso-scale fatigue testing (20 kHz, 100 um foil) (Wilkenson/Gong, Oxford)
Other planned work
  Graphite
    2017-18 Low E ion irradiation studies (Notre Dame/Michigan/BNL?)
    2017 – Micro-mechanics (Liu @ Oxford)
    2018? - NOvA TA-01 target autopsy/PIE (PNNL)
  Beryllium
    2016-17 – Irradiation of Be fins in NOvA TA-02 target with PIE in 2018-19?
  Titanium 6Al-4V
    2018 - Macro-fatigue testing of BLIP specimens 2018 - Meso-fatigue testing of BLIP specimens (20 kHz) (Oxford, Culham)
  Micro-mechanics on graphite (Liu, Oxford)

## Slide 64: Reactor materials studies are limited in relevance to Targetry
Irradiation Source | DPA rate (DPA/s) | He gas production (appm/DPA) | Irradiation Temp (˚C)
Mixed spectrum fission reactor | 3 x 10-7 | 1 x 10-1 | 200-600
Fusion reactor | 1 x 10-6 | 1 x 101 | 400-1000
High energy proton beam | 6 x 10-3 | 1 x 103 | 100-800
Effects from low energy neutron irradiations do not equal effects from high energy proton irradiations. Table compares typical irradiation parameters.
n
1-14 MeV
p
100+ MeV
Cannot directly utilize data from nuclear materials studies!
Notes: Add note that use of data from nuclear materials research is limited and should not be depended upon.

## Slide 65: Material Behavior Activities Overview
LE Ion Irradiations
HE Proton Irradiations
Strength & Damage Model Testing
Micro-mechanics Validation
Thermal Shock Tests
High Activity PIE
Low Activity PIE
LE to HE Correlation
Simulation Techniques Development
LE Ion Irradiations
Enabling Data & Tools Available
$$
$$
¢¢
¢¢
Notes: Points to make:
LE to HE Correlation and Micro-mechanics validation are necessary to enable affordable LE Ion Irradiations and PIE.
Thermal Shock tests and Simulation development is needed to make use of radiation damage results

## Slide 66
NT-02 Target Examination
Operation between 2006 to 2009, and again in 2011
Subjected to 120 GeV protons
  Integrated POT ~ 6.1 x 1020
  Gaussian beam spot size (1σ): 1.1 mm
  Peak fluence: 2.5 x 1022 p/cm2
  Estimated DPA ~ 0.63
Peak temperature ~ 330°C
  Heat to 330 C in 10 µs, cool to 60 C before next pulse (1.85 s cycle time)
Neutrino yield declined 10-15% during life, possibly due to radiation damage
  - Yield reduction not observed in other NT targets
  - NT-02 lifetime significantly longer than any other NT targets (2x or more)
Slides courtesy of K. Ammigan, Fermilab

## Slide 67
NT-02 Target
Graphite fin core
47 fins – 6.4 mm x 15 mm x 20 mm segments
Graphite fins soldered to water cooling tubes attached on top/bottom of fins
Proton beam
Upstream end
Downstream end
Target autopsy
Performed in hot cell at FNAL
Cracks observed along centerline
Some fins broken in halves
Cracks along centerline
Slides courtesy of K. Ammigan, Fermilab
Autopsy work by V. Sidorov, Fermilab

## Slide 68: Why use micro-mechanical testing?
Useful where only small samples are available
  Cost
  Processing
Need for a sample design that can be machined in surface of bulk samples
Suitable for measuring individual microstructural features
Samples that can be manufactured quickly and reproducibly
1um
3mm
10mm
4mm
3mm
3mm
Slides courtesy of DEJ Armstrong, Oxford

## Slide 69: Microcantilever Manufacture
10m
2m
Slides courtesy of DJ Armstrong, Oxford

## Slide 70: Current State of the Art
Slides courtesy of DJ Armstrong, Oxford

## Slide 71: Fracture at 600oC
1µm
Slides courtesy of DJ Armstrong, Oxford