## Slide 1
Lucas Brouwer
US Magnet Development Program
Lawrence Berkeley National Laboratory
Mechanical Design in the CCT Program
January 16th 2018
3rd MDP Collaboration Meeting: FNAL

## Slide 2: Outline
At last MDP meeting
CCT4
Concern about:
layer-layer interface
epoxy cracking
cable-channel
CCT5
This Year
addressing with bend+shim and mix61 epoxy
FEA on clusters
multi-physics/quench
de-bonding elements
CCT Subscale
Modeling Capabilities
Next Year
probing cable-channel interaction as a source of training

## Slide 3: Layer-layer interface and cable-groove interface are potential trouble areas identified at last MDP meeting
At last MDP meeting
CCT4
Concern about:
layer-layer interface
epoxy cracking
cond-groove interface
large conductor-channel shear at +- 45 deg
large shear between layers at pole of bonded model

## Slide 4: Individual layer impregnation was used on CCT5 to address layer-layer interface
Old Method: CCT3, CCT4
Layer 2
Layer 1
G10 slip plane
Step 1. Assemble Layers
Step 2. Layers 1+2 into shell
Step 3. all impregnated together
with the shell used as tooling
New for CCT5
Individually impregnated layers using vacuum bag technology

## Slide 5: CCT3 layer-layer interface showed significant epoxy delamination
New for CCT5
Individually impregnated layers using vacuum bag technology
Old Method: CCT3, CCT4
CCT3 layer-layer interface after test
fix for this

## Slide 6: Individually impregnated layers of CCT5 were assembled using inflatable epoxy shims
6
Designed to address many of the assembly challenges for CCT magnets
avoids large friction interfaces between layers during assembly
accounts for deviations along length from reaction (warpage)
well defined contact between layers with no epoxy bonding which can delaminate
applies pre-bending against the Lorentz forces (balances deviation from round)
has the potential to be reversible (replacement of individual layers)

## Slide 7: Shell pre-bending used for the assembly of CCT5
7
Layer 1 and 2 assembled with no bending
Shell bent, layers inserted while press holds shell bend, shims inflated, cured, and press released

## Slide 8: Shell strain gauge readings are aligned with ANSYS predictions during assembly
8
But, creep observed under load at room temperature!
several days
bend
inflate/cure
release bend

## Slide 9: Cold powering strain gauge data points to CCT5 bend+shim behaving as modeled
9
no creep observed cold
very little offset observed between ramps
results consistent before and after the thermal cycle
Azimuthal strain (on shell)
comparison with ANSYS
100
Axial strain (on shell)
comparison with ANSYS
700

## Slide 10: Future Work
At last MDP meeting
CCT4
Concern about:
layer-layer interface
epoxy cracking
cable-channel
CCT5
This Year
addressing with bend+shim and mix61 epoxy
FEA on clusters
multi-physics/quench
de-bonding elements
CCT Subscale
Modeling Capabilities
Next Year
probing cable-channel interaction as a source of training

## Slide 11: Bend and shim only addresses layer-layer interfaces, it does not dramatically impact cable–groove interface
11
With layer-layer interfaces and epoxy changed, channel behavior is one remaining explanation for CCT4/CCT5 training
CCT4: Lay1 radial-binormal
CCT5: Lay1 radial-binormal
+32 MPa
-32 MPa
+25 MPa
-25 MPa

## Slide 12: The subscale program can study the tradeoff between conductor normal and shear stress
12
Sxy (radial-azimuthal)
Thick spars
High shear
Low normal
Thin spars
Low shear
High normal
CCT5 Sxy training from 12-16 kA

## Slide 13: 3D FEA on clusters enables efficient mechanical solutions of full geometry
13
Example: CCT4 full mechanical model
Solid186, 7M DOFs
3 load steps: assembly, cooldown, Lorentz forces
PCG (iterative) solver
Speed up for CCT4 3D Mechanical Model
Chart: Number of Cores
| 2 | 4 | 6 | 8 | 12 | 16
shared memory | 11.14 | 8.19 | 6.07 | 6.39 | 6.18 | 6.11
distributed memory | 2.48 | 2.14 | 1.28 | 0.84 | 0.922 | 0.78
Use of Lawrencium cluster: overnight -> less than a hour

## Slide 14: Desired modeling capabilities for design of a hybrid, multi-layer CCT
14
3D FEA on clusters allows for full geometry with reasonable run times (optimization)
2D multi-physics simulation with ANSYS user elements can simulate CLIQ and other highly coupled quench scenarios
Current Capabilities
In Development
debonding contact elements for cable-groove interface (cohesive zone) – already used in HiLumi for pole unloading in cos(t)
extension of some multi-physics tools (user elements) to 3D to better represent the CCT and short magnets
Ex: CLIQ with user elements

## Slide 15: Mechanical Behavior of Interfaces is Important for the CCT
15
layer of epoxy around conductor (brown)
element coordinate system alignment allows for anisotropic conductor and epoxy (warp,fill,normal) properties
Epoxy interfaces are a possible source of quenches
between cable and channel
between layers
and b/w layers

## Slide 16: Summary
At last MDP meeting
CCT4
Concern about:
layer-layer interface
epoxy cracking
cable-channel
CCT5
This Year
addressing with bend+shim and mix61 epoxy
FEA on clusters
multi-physics/quench
de-bonding elements
CCT Subscale
Modeling Capabilities
Next Year
probing cable-channel interaction as a source of training

## Slide 17
Extra Slides

## Slide 18: Inflatable shims are created from sealed kapton sheet
18

## Slide 19: Towards the design of a four layer CCT for insert testing
19
steps toward first design (in progress – tradeoffs being studied)
choice of strand/cable
choice of spar thickness and external structure
best protection scheme: CLIQ, dump, etc.
2 m
125 mm clear bore
200 mm straight section