## Slide 1: Prediction of the JC(B) Behavior of Bi-2212 Wires at High Field
Authors:
Michael D. Brown, J. Jiang, C. Tarantini, D. Abraimov, G. Bradford, J. Jarozynski, E.E. Hellstrom, D.C. Larbalestier

## Slide 2: Bi-2212 is important for high field magnet applications
Bi-2212 is the only HTS taking the form of common LTS conductors:
  Round wire
  Multifilament
  Macroscopically isotropic
  Twisted
  Can be Rutherford cabled
…but unlike it’s LTS counterparts
  Hirr >> 24 T
  Low magnetization
High field magnet applications:
  General purpose high field research magnets
  Nuclear Magnetic Resonance (NMR)
  Next generation of particle accelerators
Relevant US-MDP Goals:
Investigation of the fundamental limits of superconducting materials for use in future high field HTS accelerators

## Slide 3: What is causing such large JC variations over the last decade?
Why?
We’ve had 9 years of development by DOE-HEP
  a variety of wires with a wide range of JC(B)
  We believe JC (B) differences are due to connectivity
Bi-2212 is now ready for applications in the 20 T – 30 T range.
  We need up-to-date info on JC(B) for Bi-2212
How?
Taking JC(B) measurements up to 31 T
  fitting to functional forms
VSM measurements ranging from 4.2 to 20 K.
  To probe vortex pinning differences between wire types
Notes: …

## Slide 4: The intrinsic properties of Bi-2212 remains unchanged.
What?
  All samples obey between 3 T and 19 T.
  There is evidence that Bi-2212 may obey up to 31 T.
   for all samples are quite similar
So What?
We ascribe the differences in JC(B) to connectivity
  alters the effective cross section of each sample
We propose that a low field data fit could predict the JC(B) behavior up to 31 T and possibly beyond.
Notes: First, a bit of motivation for this work.

## Slide 5: 5x variation of JC(15 T) in wires produced over the last decade.
Sample Set
17 samples from OST/B-OST
10 wire types with 2 architectures
5 powder types from 3 manufacturers
Precursor
521 composition (Bi2.17Sr1.94Ca0.90Cu1.98OX)
powder & granulate
Nexans, MetaMateria, and nGimat included
Large variation in JC (15 T) (over a factor of 5)!!!
Representative architectures for 37 x 18 and 55 x 18

## Slide 6: JC(B) behavior same for all up to ~19 T
y = 2.11x-0.277
W8-2 fit 3 T to 15 T
Normalized (@15 T) Critical Current vs. Field
JC(B) behavior for all Bi-2212 samples up to 31 T
  Normalized to 15 T
Power law fit from 3 T to 15 T shown for W-8
  Follows sample behavior up to JC(31 T)
Downward scatter seen above 19 T
  Heating artifact due to the slight diamagnetism of He
    [1] E. J. McNiff et. al. (1988)
    [2] H. W. Weijers et. al. (2010)
  Occurs when: BZ ∙ dB/dz < -21 T2/cm
bubble
no bubble
heating reduces IC
Notes: Add heating

## Slide 7: He bubble can cause sample heating and reduces critical current
31 T resistive magnet
50 mm bore
240 mm height
Helium is expelled from the region where
causing gaseous He to grow into the sample space.
[3] H. Bai, et. al. (2015)
H. Bai et. al. show that the bubble can encroach down to z = ~ -30

## Slide 8: fits well for all from 3 to 19 T
Log-log plot showing JC(B) behavior of all samples up to 31 T
  Normalized to 15 T
Power law behavior within the range of 3 T to 19 T defined by the relation:
Power law fit from 3 T to 15 T shown for W-8
  Follows sample behavior up to JC(31 T)
3 T to 19 T
Normalized (@15 T) Critical Current vs. Field

## Slide 9: For ,  values are quite similar
 values were found for ranges 3 T to 15 T, 17 T,… 31 T
  approaching the helium bubble region and beyond
The average value for  in the 3 T to 15 T range is 0.282
   varies by 0.044
Field Fit Range Upper Limit [T]
α
bubble
no bubble
For comparison, YBCO sees large variation in its pinning behavior due to dopant, heat treatment, manufacturer, conductor anisotropy…
   in YBCO: ~0.5 to ~0.9 (range of ~0.4) [4][5]
The ranges for 2212 and YBCO differ by an order of magnitude.

## Slide 10: Magnetization: pinning does not vary with powder or temperature
Magnetization from -2 T to 14 T
Comparison of two of the newer powder wires was made at 10, 15, and 20 K
  W8-2 (MetaMateria, M2-P4)
  W10-3 (nGimat, M3-P5)
Pinning force curves were produced on the wire containing MetaMateria powder at 4.2, 10, 12, 14, 16, 18 and 20 K.
We do not see a significant variation in vortex pinning…
  between two newest powders
  between temps from 4.2 to 20 K
Transport up to 15 T from 4.2 to 40 K to come at LTSW (A. Francis)

## Slide 11: Discussion and Conclusions
Similar values of  for all Bi-2212 wires in sample set…
  …shows that the pinning mechanism between powder type and architecture is unchanged.
  …indicates the large variation in JC is likely due to the connectivity of the Bi-2212 grains altering the effective filling factor of each wire.
Helium bubble causes low JC above ~ 19 T.
  can cause sample heating and damage
  complicates conclusions about the relation above 19 T for most wires
  However, some show power law obedience to higher fields, one in particular abides to 31 T.
Similar magnetization curves over the range of 10 K to 20 K for two newest powders show that the vortex pinning mechanism is independent of temperature in this range.
  further indicates that higher JC for the newest nGimat wires is an effect of connectivity between grains.
  Grain connectivity is hampered by obstructions in the filament channel which can cause grain misalignment.
Magnetization on MetaMateria wires show that similar behavior is seen down to 4.2 K (at least to 14 T).
Furthermore, 31 T is far below the estimated value for Hirr for Bi-2212 which means that measurements from 5 T to 15 T could be used to accurately approximate JC (~30T).

## Slide 12: Extrapolation for newest nGimat wires
JC (30 T) for 3T to 15T
  = 5406 A∙mm-2
JC (30 T) for 3T to 17T
  = 5353 A∙mm-2
JC (30 T) for 3T to 19T
  = 5288 A∙mm-2
JC (30 T) > 5200 A∙mm-2

## Slide 13: References
[1] E. J. McNiff, B. L. Brandt, S. Foner, L. G. Rubin, and R. J. Weggel, “Temperature anomalies observed in liquid 4He columns in magnetic fields with field–field‐gradient products >21 T2/cm,” Review of Scientific Instruments, vol. 59, no. 11, pp. 2474–2476, Nov. 1988.
[2] H. W. Weijers et al., “High Field Magnets With HTS Conductors,” IEEE Transactions on Applied Superconductivity, vol. 20, no. 3, pp. 576–582, Jun. 2010.
[3] H. Bai et al., “Impact of Trapped Helium Gas Bubble in Liquid Helium on the Cooling in High Magnetic Field,” IEEE Transactions on Applied Superconductivity, vol. 25, no. 3, pp. 1–4, Jun. 2015.
[4] V. Braccini et al., “Properties of recent IBAD–MOCVD coated conductors relevant to their high field, low temperature magnet use,” Supercond. Sci. Technol., vol. 24, no. 3, p. 035001, 2011.
[5] D. Abraimov et. al., ASC 2014 slides

## Slide 14: Acknowledgements
This work was supported by a grant from the US Department of Energy, Office of High Energy Physics (DE-SC0010421), from the NHMFL, which is supported by the NSF under NSF/DMR-1644779, and by the State of Florida.
Technical support from Y. Oz & V. Griffin

## Slide 15: Extra slides

## Slide 16: He bubble effect
31 T resistive magnet
Region of LHe expulsion
Sample position
Bore