## Slide 1
Tiziana Spina
52nd Annual Users Meeting
12 June 2019
Applied Physics and Superconducting Technology Division at FNAL
The Industrial Center Building (ICB), 1986.

## Slide 2
1980
Technical Support Section - TSS
1996
Technical Division - TD
2018
Applied Physics and Superconducting Technology Division – APS-TD
1981 – Installation of 1st Tevatron Magnet
1998 - U.S. and CERN sign LHC Agreement
2001 – SRF field was added to the Division
Historical background:
Notes: Which has substantially evolved from the days since the division was created.

## Slide 3: APS-TD MISSION
Educate and train the next generation of physicists and engineers
https://td.fnal.gov/
Pursue highly innovative R&D program in s.c. MAGNETS and SRF for accelerators to advance the lab’s scientific mission and to help in defining the lab’s future direction
Operate accelerator test facilities to maximize the lab’s scientific productivity and impact
Develop and build next generation accelerators and detectors using cutting-edge technologies
The Quantum Computing Lab and Materials Science Lab are part of the new TD.
Ph.: A. Grassellino
The division has its 2018 picnic. Ph.: T. Nicol

## Slide 4
Sergey Belomestnykh
Division Head
Anna Grassellino
Deputy Division Head
Alexander Romanenko
Associate Division Head/SRF sector
George Velev
Associate Division Head /Magnets sector
Jay C. Theilacker
Associate Division Head / Cryogenics sector
Romesh Sood
Associate Division Head
APS-TD Leadership

## Slide 5: Outline
Basic R&D:
  For SRF cavity
  For Superconductive magnets
Projects:
  LCLS-II
  PIPII
  HL-LHC AUP
  Mu2e
Summary

## Slide 6: Outline
Basic R&D:
  For SRF cavity
  For Superconductive magnets
Projects:
  LCLS-II
  PIPII
  HL-LHC AUP
  Mu2e
Summary
DOE HEP GARD (General Accelerator R&D) program

## Slide 7: R&D: SRF sector
Nb (Tc=9.2K) bulk or thin film;
Nb3Sn (Tc=18K) thin film;
LHe T of operation:
Different shapes and frequencies depending on application:
Standard ILC cavity
Q-factor ():
High → lower power consumption
Accelerating field ():
Determine the energy transferred to charged particles
High → lower accelerator length
High Q at large gradient may reduce both capital and operational costs of accelerators
Figures of Merit
SRF Cavities: main features
improvement of the cavity performance (Q0 and achievable Eacc);
full understanding of the underlying physics and materials science (doping/infusion; hydrides formation; flux trapping);
Keys focus of the research:

## Slide 8: Pushing the state of the art in High Q and high G driven by Fermilab SRF R&D program – A. Grassellino et al.
Q>3e10 at 35 MV/m with N doping
Q >1e10 at 50 MV/m with 75/120C bake
EP
120C bake
75/120C
N infusion
N doping
New optimized doping recipe is also capable of yielding record breaking Q0!
New World Record in Q0!
9x1010 !
Grassellino and Bafia, to be published 2019
Grassellino et al., to be published 2019
World Record in Eacc!

## Slide 9: Hydrides R&D studies:
Surface features on cavity cut-out samples: nanohydrides studies – A. Romanenko and Z. Sung
9 MeV RT Electron Irradiation up to fluence of 1022e/m2 T. Spina
AFM measurements at Materials Science Lab in ICB
Irradiation experiment and microscopy

## Slide 10: Magnetic Flux Expulsion R&D
Ambient magnetic field during cooldown
R&D in Vertical Test
Fermilab SRF R&D in the last 5 years has led to significant improvement in understanding of how to prevent magnetic fields from being trapped during cooldown
Lessons learned were applied design of LCLS-II cryomodules (ability to do fast cooldown) and cavity processing treatment (higher temperature heat treatment)
M. Checchin et al.

## Slide 11: Plasma processing R&D
Martinello, Berrutti, Giaccone, Penhollow
https://indico.fnal.gov/event/20381/timetable/#20190610.detailed

## Slide 12: New Progress in Maximum Accelerating Gradient of Nb3Sn Cavities – S. Posen
World record CW gradient for Nb3Sn accelerator cavities – 22.5MV/m: (~25% increase)
Cornell data from D. Hall and R. Porter
All 1.3 GHz single cell cavities
Nb3Sn accelerator cavities have been limited consistently to 17-18 MV/m for ~20 years, though theoretical predictions indicate ultimate limit is far higher
Research supported by S. Posen Early Career Award
New result proves that Nb3Sn had not reached an intrinsic limit
Notes: Nb3Sn accelerator cavities have been limited consistently to CW accelerating gradients of 17-18 MV/m for ~20 years, though theoretical predictions indicate ultimate limit is far higher

## Slide 13: Quantum technology R&D: Material treatment to suppress TLS dissipation
Nb
Nb2O5
5 nm
Nb
A. Romanenko, R. Pilipenko, S. Zorzetti, D. Frolov, M. Awida, S. Posen, A. Grassellino, arXiv:1810.03703
Record: high photon lifetimes up to 2s
Notes: 2 s

## Slide 14: Outline
Basic R&D:
  For SRF cavity
  For Superconductive magnets
Projects:
  LCLS-II
  PIPII
  AUP
Summary
DOE HEP GARD (General Accelerator R&D) program

## Slide 15: R&D: Magnets sector
Twin-aperture NbTi dipole during fabrication (HFM)
Keys focus of the research:
Mostly NbTi and Nb3Sn strands at LHe Top:
Insulator materials R&D
High field accelerator magnets R&D (Nb3Sn dipoles/quads; hybrid with HTS insertion)
Magnet diagnostics R&D (to reduce the quench training)
Superconducting materials R&D (wires, cables)

## Slide 16: Nb3Sn - Conductor R&D: X. Xu et al.
Artificial Pinning Center (APC):
Fermilab LDRD support, Hypertech and OSU
A Nb3Sn wires, record Jc, meet or exceed the FCC specifications
Nb3Sn with high heat capacity additives:
First wires produced by Hypertech - promising results
Optimize the recipe of high-C rods by Bruker-EAS
Gd2O3

## Slide 17: Nb3Sn Composite R&D S. Krave et al.
Work on the Nb3Sn-Insulation Composite is ongoing:
Initial Acoustic data for event characterization
Reduce magnet training
  Examining experimental materials under SBIR and other programs
Improve and homogenize material properties
  SBIR and other programs
Improve analysis techniques to better understand material behavior by
  Application of acoustic sensors to different loading configurations to characterize types of cracking events

## Slide 18: Magnet R&D: 15 T dipole - A. Zlobin et al.
Demonstrator
Assembly
First-in-the-world 15T demonstrator, paving the way to 16 T dipoles: Magnet Dipole Prototype Cos-Theta type 1 (MDPCT1);
1 m long, 60 mm bore diameter Nb3Sn dipole magnet
Main Features

## Slide 19: Magnet R&D: 15 T dipole First Test A. Zoblin, S. Stoynev et al.
15 T magnet test started in May at VMTF/APS-TD
The goal (13 T) was reached after 9 quenches:
Bmax=13.3T
Record Bmax for accelerator magnets at FNAL!
Highest field ever reached for an accelerator magnet with 60mm aperture
The magnet pre-stress level was set for the magnet to safely reach 13 T with possibility to continue to 14 T
Courtesy of S. Stoynev

## Slide 20: Cryogenics at APS-TD
To design and operate the cryogenic test facilities to qualify superconducting accelerator components LHC’s HILUMI, SLAC’s LCLS-II, and Fermilab’s PIP-II and Mu2e.
To deliver large scale superfluid He cryogenic system for the future SRF Linac, PIP-II
To support various mK cryogenic systems, utilizing cutting edge dilution refrigerators for Dark Matter Quantum Sensor experiments and Quantum Computing R&D.
APS TD Cryogenics sector is responsible:
New IB1 He Liquefier
IB1 Test Stand 4 Upgrades for HL-LHC Magnet Testing
Sub-Kelvin Cryogenics
Courtesy of J. Theilacker
Notes: Every project at FNAL requires cryogenic refrigeration of some kind……

## Slide 21: Outline
Basic R&D:
  For SRF cavity
  For Superconductive magnets
  For Cryogenics
Projects:
  LCLS-II
  PIPII
  AUP
  Mu2e
Summary

## Slide 22: APS-TD and LCLS-II
Upgrade of the Linear Coherent Light Source at SLAC
Nitrogen doping breakthrough from R&D to production-ready technology
FNAL single cell cavities
APS-TD plays a key role in designing and building:
Cryomodule (CM) assembly
Cryogenic Distribution System (CDS)
A. Grassellino et. al
New 4 GeV linac based on superconducting radio frequency (SRF) technology.
Courtesy of Rich Stanek
.

## Slide 23: Outline
Basic R&D:
  For SRF cavity
  For Superconductive magnets
Projects:
  LCLS-II
  PIPII
  AUP
  Mu2e
Summary

## Slide 24: APS-TD and PIP-II
To provide powerful beam for generating neutrinos for LBNF/DUNE
HWR SSR1 SSR2 LB650 HB650
Proton Improvement Plan-II (PIP-II) is Fermilab's plan for providing powerful, high-intensity proton beams
What is it?
APS-TD plays a key role in designing and building:
Modern SRF linac
New Cryogenic Distribution System (CDS)
Notes: HWR:Half Wave Resonators

## Slide 25: SRF cavities and cryomodules for PIP-II: status
Single spoke resonators (325MHz) | LB/HB (650MHz) | Results and PIP II spec
SSR1 string assembly Cold mass preparation and assembly is in progress.
SSR2 jacketed cavity preliminary design review completed
SSR1 cryomodule assembly preparation
SSR1 cryomodule assembly completes in October 2019.
LB650 bare cavity from INFN
prototype cavities are being fabricated at vendor site.
HB650:
First cavity jacketed
650MHz
Spoke cavity (SSR1)
650 MHz Cavity Jacketing at MP9
Notes: HB650 cryomodule design is in progress with international design team.
Spoke cavity SSR1 - Processed and qualified in VTS and qualified post-dressing in horizontal test stand
650MHz - N-dope recipe well exceeds specification (4.8e10@ 20MV/m).
Field emission is challenging without a proper HPR tool.

## Slide 26: Outline
Basic R&D:
  For SRF cavity
  For Superconductive magnets
  For Cryogenics
Projects:
  LCLS-II
  PIPII
  HL-LHC AUP
  Mu2e
Summary

## Slide 27: APS-TD and U.S. HL-LHC AUP
APS-TD plays a key role in the fabrication and test of:
MQXF Nb3Sn low β quadrupoles
RFD Crab Cavity
U.S. HL-LHC Accelerator Upgrade Project (AUP): to increase the luminosity of a factor of 10. High-Luminosity LHC (HL-LHC) at CERN will produce five to seven times more proton-proton collisions than the currently operating LHC, powering new discoveries about our universe.
What is it?

## Slide 28: Nb3Sn low β quadrupoles (MQXFA): status
Rutherford cable
HL-LHC AUP Coil Fabrication at FNAL
Efficient coil production ramping up
10 (out 49) Coils completed or in production
Target: 132.6 T/m
- 150mm aperture, 11.4T Bpeak
Q1/Q3 (by AUP)
2 magnets MQXFA with 4.2m
  Series:20 magnets
Q2a/Q2b (by CERN)
1 magnet MQXFB with 7.15m
  Series:10 magnets

## Slide 29: RFD crab cavities: status
RFD-LARP-001 has been successfully tested at FNAL, after undergoing full processing at APS-TD and ANL facilities
Rotational BCP tool for RFD cavity
RFD HPR and Cleanroom Assembly
RFD cavity 600 C and 120 C heat treatments
RFD-LARP-001 Q vs Vt, exceeding requirement for HL-LHC
(Nominal: 3.4 MV, Acceptance: 4.1 MV)
Processing and Facilities validation is complete
  New rotational Bulk & Light BCP
  600 C degassing and 120 C bake
  HPR and clean assembly
  VTS test

## Slide 30: Outline
Basic R&D:
  For SRF cavity
  For Superconductive magnets
  For Cryogenics
Projects:
  LCLS-II
  PIPII
  AUP
  Mu2e
Summary

## Slide 31: APS-TD and Mu2e
The Mu2e Experiment at Fermilab is designed to detect CLFV in the specific mode of a conversion of a muon to an electron. If detected, it would be the first clear evidence for Physics Beyond the Standard Model.
What is it?
APS-TD plays a key role in designing and procuring:
Superconducting Solenoid Magnets (PS/DS/TS)
Feedboxes, HTS Current Leads, Cryogenics
The three solenoid magnets of the Mu2e Experiment.
Four members of APS-TD standing beside the prototype Transport Solenoid (TS) module

## Slide 32: TS/DS/PS status
Vendor has given permission to start winding production coils
Notes: Vendor has given permission to start winding production coils
Completed demonstration coil
Autopsy performed

## Slide 33: Outline
Basic R&D:
  For SRF cavity
  For Superconductive magnets
Projects:
  LCLS-II
  PIPII
  AUP
  Mu2e
Summary

## Slide 34: Summary
APS-TD: The new name to reflect the division’s work which has substantially evolved from the days since the division was created
R&D for SRF and Magnets:
  Improvement of the cavity performance: record on Q0 and Eacc
  Good understanding of how to prevent flux expulsion
  Hydrides study and Plasma processing
  Quantum technology
  Record in Jc values of Nb3Sn wires
  Record in Bmax for 15T Nb3Sn dipole
Design, installation and operation of cryogenic refrigeration for every project at FNAL
Involvement of APS-TD in many projects as: LCLS-II; PIP-II; HL-LHC AUP; Mu2e.

## Slide 35
Thank you for your attention!

## Slide 36: Feedboxes, HTS Current Leads and Cryogenics

## Slide 37: PIP-II Cryogenic Distribution System (CDS)
Scope: Distribute 2 kW of 2 K refrigeration between Cryogenic Plant (CP) and Cryomodule (CM) Linac
  Distribution Valve Box
  > 200 m of Multi-circuit Transfer-Line between DVB and Linac
  Bayonets + U-tubes at each CM interface
CM interface
Distribution Box
Cryogenic Sector