## Slide 1: Quick Survey of Microwave Dielectric Structures and Current Projects
Chunguang Jing on behalf of collaboration (Euclid and AWA)
Euclid TechLabs, 365 Remington Blvd., Bolingbrook, IL 60440, USA
8/21/2019

## Slide 2
www.euclidtechlabs.com
History: the starting era (1947-1960)
Experimental Work(1948-1958)
Research Group | Scientists | References | Research Scope
Atomic Energy Research Establishment (AERE), UK | R.B. R.-Shersby-Harvie, etc. | 1. R.B. R.-Shersby-Harvie, Nature, 162 (1948) 890. 2. R.B. R.-Shersby-Harvie,etc., Proc. I.E.E. B., 104 (1957) 273. | Constructed and Tested a 4MeV Traveling wave Dielectric Disk Loaded Accelerator. Beam Acceleration. Discovered Multipactor in DLA.
Queen Mary College, Uni. of London, UK | G.B. Walker, etc. | 1. G.B.Walker and N.D.West, Proc. I.E.E. C., 104 (1957) 381. 2. G.B.Walker and E.L.Lewis, Nature, 181 (1958) 38. | Constructed and Tested Dielectric Disk Loaded Wavguide Cavities. Tested Dielectric Breakdown.
IIT, USA | G.I. Cohn and G.T. Flesher | 1. G.T.Flesher and G.I.Cohn, A.I.E.E. C., 70 (1951) 887. 2. G.I.Cohn and G.T.Flesher, IIT Report, 2 (1952). | Constructed and Tested a Quartz Tube Based Dielectric Loaded Accelerator.
Theoretical papers (1947---)

## Slide 3
www.euclidtechlabs.com
History: waiting years(1960-1985)

## Slide 4
www.euclidtechlabs.com
History: the reviving era (1988-present)

## Slide 5
www.euclidtechlabs.com
Variety of Dielectric Accelerator Structures
Variety of dielectric structures | Pros | Cons
Dielectric-loaded accelerator [7] | Most developed structure High group velocity, low surface fields | Moderate r/Q Weak points: tapered section
Dielectric-assisted accelerator [6] | Very high shunt impedance Low group velocity Prototype fabricated | No high group velocity optimization yet Current prototype is clamped together, and may not hold high gradient Weak points: high surface fields at joint of copper and dielectric
Disk-Ring hybrid accelerator [8] | High group velocity Various parameters for optimization | Moderate r/Q No prototype yet Weak points: high surface fields at joint of copper and dielectric
Hybrid dielectric accelerator [9] | Low surface fields, high r/Q Prototype reported | Low group velocity May be difficult to fabricate dielectric piece with desired shape Weak points: joint of copper and dielectric
Multilayer dielectric accelerator [10] | Higher r/Q than DLA High group velocity Low surface fields | Hard to eliminate the gap between dielectric layers Weak points: joint of layers

## Slide 6
www.euclidtechlabs.com
Euclid/AWA/NRL DLA work over years
Time | Structures | facility | Achievement
2001 ~2015 | 11.4GHz external powered Dielectric accelerators | NRL Magnicon, 20MW, 200ns | Multipactor suppression: different coating techniques, surface geometrical perturbations, external solenoid field, etc.
2005 ~2007 | X-band dielectric wakefield structures | AWA 15MeV beamline | Single bunch high charge wakefield excitation. 100MV/m, ~5ns; high transformer ratio collinear; tunable DWA, etc.
2015 ~2017 | 26GHz short pulse dielectric accelerator | AWA 70MeV beamline | Short pulse TBA, 50MeV/m
2017 | 11.7GHz short pulse dielectric accelerator (no test yet) | AWA 70MeV beamline | Short pulse TBA
Dielectric Accelerator

## Slide 7
www.euclidtechlabs.com
Euclid/AWA DPETS work over years
Time | Structures | facility | Achievement
2006~2008 | 7.8GHz DPETS | AWA 15MeV beamline | 50MW, 10ns
2009 | 26GHz DPETS | AWA 15MeV beamline | 20MW, 10ns
2013 | 11.4GHz DPETS | SLAC ASTA klystron | 40MW, 50ns, 100ns
2014 | 12GHz DPETS | AWA 15MeV beamline | Transverse wake damping
2016~2017 | 26GHz DPETS | AWA 70MeV beamline | 50MW, 10ns
2017 | 11.7GHz DPETS | AWA 70MeV beamline | >200MW, 10ns
Dielectric PETS

## Slide 8
Euclid/AWA current work---Dielectric Disk Accelerator
2019 HEP SBIR Phase1

## Slide 9
Dielectric disk accelerator
DLA
DDA
Comparison with DLA
- More optimization parameters: working mode, disk thickness
- High shunt impedance
Comparison with metallic disk-loaded structure
- More optimization parameters: dielectric constant
- High group velocity due to coupling through the disk
C. Jing, Rev. Accel. Sci. Tech.., vol. 9, 127-149, 2016

## Slide 10
Dielectric disk accelerator
Optimization of rf to main beam efficiency in AFLC
- Main beam: 0.5 nC/bunch, 13 GHz separation, 186 bunches
Fix mode at 2π/3
Additional advantages
- Standard deform tuning by side-wall tuners
- Can be applied in constant gradient and long structures
Fix disk thickness at 0.5 mm
AFLC
DDA candidates

## Slide 11
Dielectric disk accelerator
A detailed comparison with DLA for AFLC (26GHz)
 | Dielectric-loaded | Dielectric-disk
Aperture diameter | 3 mm | 3 mm
Outer diameter | 4.99 mm | 9.23 mm
Dielectric thickness | 1 mm | 0.5 mm
Dielectric constant | 10 | 50
Loss tangent | 1x10-4 | 5x10-4
vg | 0.11c | 0.16c
r/Q | 21.8 kΩ/m | 32.5 kΩ/m
Q | 2295 | 6431
r | 50.0 MΩ/m | 208.8 MΩ/m
Input power | 1.22 GW | 0.96 GW
ηrf-main | 27 % | 39 %
Beam loading | 15.1 % | 16.8 %
Emax | 363 MV/m | 660 MV/m

## Slide 12
Dielectric disk accelerator
Prototype I
- X-band 6 dielectric disk cells + 2 matching cells
- 8 tuning pins per cell
- Goal: demonstrate fabrication and tuning

## Slide 13
Single Cell DDA Prototype
1 Dielectric disk + 2 matching cell structure simulated
Each set of 4 tuners allows ± 3 MHz range
173.4 MV/m peak field on dielectric surface at 200 MW input power

## Slide 14
Dielectric disk accelerator
Fabrication
Dielectric disk
Metalized
dielectric disk
Copper tube
Tuner
Groove
for disk
Single cell

## Slide 15
Dielectric Material & Brazing
D-50 dielectric (Ba-Ti) to be used
Samples from manufacturer tested
  𝛜r = 50.14 ± 0.35, tan 𝛅 = 8.00E-5 ± 0.32E-5
Metallization and subsequent brazing to copper structure are difficult
Manufacturer does thick film silver
Positive feedback from potential brazing vendors for metallization-brazing processes
Sample coupons from manufacturer to be sent to brazing vendors for process testing

## Slide 16
Development of RF dielectric accelerator has been making steady progress over years. With more researchers participate, we expect to have a breakthrough sooner or later.
AWA is an ideal and critical platform for the dielectric accelerator development and test. We enjoy our collaboration over the years.
Remarks

## Slide 17
Acknowledgments
Numbers of DoE SBIR Projects.
Fully support from AWA
www.euclidtechlabs.com