## Slide 1
drhgfdjhngngfmhgmghmghjmghfmf
Eric Wisniewski
AWA Staff
AWA overview – Electron RF Gun Source R&D
Mission Statement:
Developing the science and technology of electron beam generation, manipulation and acceleration for beam-driven wakefield acceleration and other applications.
August 21-23, 2019
AWANOW Workshop
Argonne, IL

## Slide 2: Outline
AWA Electron sources research capabilities
  3 Normal Conducting RF (NCRF) photoinjectors
  Argonne cathode test-stand (ACT)
  Second cathode deposition chamber dedicated to R&D
Electron sources research highlights
  High quality photocathode beam generation
  NCRF gun characterization of photocathodes
  NCRF gun characterization of Field Emission cathodes

## Slide 3
AWA Electron sources research capabilities

## Slide 4: AWA Electron Sources Capabilities current and near-term
High Gradient Cathode Testing in NCRF gun
NCRF gun characterization of photocathodes and field emission cathodes
    High gradient testing
    Charge, QE measurement and mapping
    thermal emittance measurement and mapping
High quality photocathode beam generation (3 RF photoinjectors)
Load-lock system for cathode transfer from prep chamber to NCRF gun for characterization and testing.
Cathode Development
In situ QE measurements
Kelvin probe work function (CPD) measurements
High Gradient Cathode Testing in NCRF gun
Cathode Development

## Slide 5: AWA Electron Sources Capabilities current and near-term
High Gradient Cathode Testing in NCRF gun
NCRF gun characterization of photocathodes and field emission cathodes
    High gradient testing
    Charge, QE measurement and mapping
    thermal emittance measurement and mapping
    time response
High quality photocathode beam generation (3 RF photoinjectors)
Load-lock system for cathode transfer from prep chamber to NCRF gun for characterization and testing.
Cathode Development
Second photocathode growth and preparation chamber for cathode studies (Cesium Telluride, cesiation, flexibility for other options) - available soon
In situ QE measurements
Kelvin probe work function (CPD) measurements
Future SRF gun cathode testing (ANL/ASD) Talk at 9:30 AM (John Byrd)
High Gradient Cathode Testing in NCRF gun
Cathode Development

## Slide 6: Argonne cathode test-stand (act)
L-band single-cell rf gun
- High gradient (100-700 MV/m) with modest rf power (2.5 MW)
beam pipe
cathode insertion
tuner
pin
nose
gun iris
Detachable cathode
Pin-shape cathode
~Φ1 mm, metallic
Regular flat cathode
~Φ20 mm, metallic
3-part cathode
metallic/advanced

## Slide 7: Argonne cathode test-stand (act)
Beamline
Waveguide switches
Available for future extension
gun
guide
261 nm, ps laser

## Slide 8: Argonne cathode test-stand (act)
Beamline
- A test-stand for fundamental FE/BD study, advanced cathode research, and
low energy beam application
Capability
- FE/BD study: BD location, FE imaging
- Cathode study: fully benchmarking (thermal emittance under study)
Application: low energy beam (field emission/photoemission) delivered to the
ample space at the end of the beamline
Laser
input
Collimator
& slits & YAG
Faraday cup
& YAG
BPM
Faraday cup
& YAG
rf gun
ICT

## Slide 9: Secondary cathode deposition chamber
Dedicated to photocathode R&D program
- Designed to make Cs2Te photocathodes using evaporative deposition, similar
to the primary AWA deposition chamber
- Features include QE measurement at 6 wavelengths, a load-lock system compatible with the ACT gun, flexible cathode & plug size
- available for researchers wishing to cesiate a cathode surface.
- possibility of producing other types of photocathodes in the chamber
Power supplies
Deposition chamber
Cryo-pump

## Slide 10
AWA electron sources research highlights

## Slide 11: High quality photocathode beam generation
Emittance overestimation due to coupled transverse dynamics aberration (L. Zheng, AWA/THU)
A recently revealed emittance growth mechanism
Resulted from quadrupole components in RF gun followed by rotation in solenoid, or from quadrupole components in solenoid
Simulation results
Experiment:
emittance overestimation
Experiment:
beam distortion
L. Zheng, et al., PRAB 21, 122803 (2018)

## Slide 12: High quality photocathode beam generation
Correction of coupled transverse dynamics aberration (L. Zheng, AWA/THU)
Corrector consists of a pair of normal and skew quadrupoles
Systematic study of aberration correction
Corrector
Experiment: angle & strength dependence
Experiment: correction
Experiment:
shape correction
L. Zheng, et al., PRAB 22, 072805 (2019)

## Slide 13: NCRF gun characterization of photocathodes
QE / thermal emittance measurement of (N)UNCD cathode (G. Chen, L. Spentzouris, IIT) Talk at 10:30 AM
Proposed work of (N)UNCD photocathode characterization on ACT
To be compared with the results obtained in DC guns
G. Chen, et al., APL 114, 093103 (2019)
ACT
DC setup
Flexible cathode design

## Slide 14: NCRF gun characterization of photocathodes
QE / thermal emittance mapping of Cs2Te cathode (L. Zheng, AWA/THU)
Pattern beam generation with microlens array
Observed dependence of thermal emittance on QE
L. Zheng, et al., arXiv 1906.08074 (2019)
Experiment: thermal emittance measurement by solenoid scan

## Slide 15: NCRF gun characterization of Field emission cathode
Systematical benchmarking of (N)UNCD field emission cathode
(M. Schneider/S. Baryshev, MSU; G. Chen, IIT) Talk at 11:30 AM
Cathode characterization during rf conditioning from 8 to 42 MV/m on ACT
Emission model established to interpret the properties evolution
J. Shao, et al., arXiv 1907.08582 (2019)

## Slide 16: NCRF gun characterization of Field emission cathode
Pattern beam generation from field emission array cathode
(K. Nichols/H. Andrews/E. Simakov, LANL) Talk at 10:50 AM
Aims for bunch train generation together with emittance exchange
Observed pattern beam at 15 MV/m on ACT
K. Nichols, to be submitted

## Slide 17: Summary
Electron Sources R&D topics
  High quality photocathode beam generation
  NCRF gun characterization of photocathodes
  NCRF gun characterization of field emission cathodes
  Future SRF gun characterization of cathodes with ASD
The AWA group operates and maintains 3 NCRF photoinjectors.
One is installed on the Argonne Cathode Test-stand (ACT) beamline, dedicated to high-quality electron source R&D in a rich, collaborative environment.
The secondary photocathode prep chamber and load-lock system (under construction) will soon provide additional resources for electron source studies.
Thank you for your attention.