## Slide 1: Germanium Charge-Coupled Devices
Christopher Leitz
5 June 2019
christopher.leitz@ll.mit.edu
DISTRIBUTION STATEMENT A. Approved for public release. Distribution is unlimited.
This material is based upon work supported by the Under Secretary of Defense for Research and Engineering under Air Force Contract No. FA8702-15-D-0001. Any opinions, findings, conclusions or recommendations expressed in this material are those of the author(s) and do not necessarily reflect the views of the Under Secretary of Defense for Research and Engineering.
© 2019 Massachusetts Institute of Technology.
Delivered to the U.S. Government with Unlimited Rights, as defined in DFARS Part 252.227-7013 or 7014 (Feb 2014). Notwithstanding any copyright notice, U.S. Government rights in this work are defined by DFARS 252.227-7013 or DFARS 252.227-7014 as detailed above. Use of this work other than as specifically authorized by the U.S. Government may violate any copyrights that exist in this work.

## Slide 2: MIT-LL Microelectronics Laboratory An Enabling Resource for Advanced CCD Fabrication
Production-class 90-nm toolset on 200-mm wafers
Lithography capabilities from i-line to e-beam
Process capabilities include CCDs, APDs, low power FDSOI CMOS, 3D integration
R&D through flight deliverables

## Slide 3: Advantages of Germanium CCDs
…in a large format
200 mm
Large-diameter wafers, compatible with Si CCD tool set
High-quality gate dielectrics enable CCDs
The benefits of silicon CCDs but covering a broader range
Broadband sensitivity & low noise
Excellent material properties  low noise
Sensitivity to hard X-rays, infrared light, DM candidates (?)

## Slide 4: Germanium CCD Development at MIT Lincoln Laboratory
150-mm Wafers
Diodes, Capacitors
200-mm Wafers
Diodes, Capacitors, MOSFETs
200-mm Wafers
Imagers
100-mm Wafers
MOS Capacitors
0 mask levels
CD = 100 µm
5 mask levels
CD = 2 µm
7 mask levels
CD = 1 µm
11 mask levels
CD = 0.2 µm
2013
2017
2015
2019
512 x 512, 24 µm pixels
Additional arrays w/ up to 20 ports

## Slide 5: First-Generation Germanium CCD Reticle Set
  128 × 128, 8.0-µm pixel OTCCD
  32 × 32, 8.1-µm pixel full-frame CCD
  1 × 1024, 8.1-µm pixel linear CCD
  1 × 32, 8.1-µm pixel linear CCD
Reticle Layout
Device Cross-Section
  1024 × 1024, 8.1-µm pixel frame-transfer CCD
All devices utilize same single-stage MOSFET output
Abrupt jump from small arrays to Mpixel device
Metal gate process conceptually similar to “single-poly” Si CCDs being developed for Lynx
Germanium Substrate
(n-type)
Interlayer Dielectric
Gate Dielectric
Metal Gate
400 nm

## Slide 6: Recent Progress in Germanium CCDs
Highlights from Pixel Arrays
Demonstrated pixel arrays up to 128 × 128 format, improved charge-transfer efficiency, response to 109Cd X-rays
Steady progress in device understanding, building towards large-format CCDs in 2019
C.W. Leitz, et al., SPIE Proc. 10709 (2018).
C.W. Leitz, et al., presented at CPAD (2018).
June 2017
June 2018
1800
1200
1500
1600
1700
1400
1300
Intensity (arb .units)
Improvements in CCD Performance
Established that bulk metallic contaminants are limiting performance of first-generation germanium CCDs

## Slide 7: Path to Large-Format Arrays
Focusing on reducing metallic contamination, gate-to-gate short frequency to yield larger arrays
Reducing Occurrence of Gate-to-Gate Shorts
Utilizing inline metrology to identify yield limiters (e.g. particles bridging metal lines)
Improving Charge-Transfer Efficiency
Dependence of CTE on spacing between input pulses consistent with bulk metallic contamination
-95°C
-125°C

## Slide 8: Future Directions for Germanium CCDs
Increase the array size and charge-transfer efficiency
Perform backside illumination to show high sensitivity
A. Rogalski, Proc. SPIE 10433 (2017).
Pixel Counts over Time
Ge