## Slide 1
Sam Posen
LCLS II HE Cryomodule Performance Workshop
25 April 2019
VT/CM Performance for Flux Expulsion

## Slide 2: Acknowledgements
LCLS-II cryomodule production in partnership with teams at FNAL, JLab, and SLAC
All cryomodule measurements shown here are by FNAL LCLS-II team
Major thanks to Genfa Wu, Anna Grassellino, Elvin Harms, Nikolay Solyak

## Slide 3: What is Flux Expulsion?
For practical magnetic shielding, we expect some residual ambient field at the cavity
During cooldown, thermal gradients over the surface generate a force that expels magnetic flux out of the superconductor; expulsion force competes with pinning forces
Desirable to expel all flux during cooldown to minimize Q0 degradation
Meissner State
Mixed State
Pinning point
Flux Expulsion
Magnetic field lines

## Slide 4: Measuring Flux Expulsion in Vertical Dewar Test
Magnetic
field coils
(tens of mG applied field)
Fluxgate magnetometers
(3 around cell
of cavity)
Temperature
Sensors
(Top, middle, bottom of cell)

## Slide 5
Flux Expulsion Comsol simulation
Flux Trapping Comsol simulation
Flux Expulsion Measurement
Flux Trapping Measurement
Fluxgate magnetometer
Fluxgate magnetometer
BSC/BNC ~ 1.7
BSC/BNC ~ 1
Field lines bend around wall
Field lines go through wall

## Slide 6
Fast/High massflow cool-down leads to large thermal gradients which promote strong flux expulsion
Slow/low massflow cool-down → poor flux expulsion

## Slide 7: Thermal Gradient in CM Test
Measured thermal gradient in CM with prototype cryomodules
Data from FNAL pCM: low massflow results in very small top-bottom thermal gradient

## Slide 8
Significant variation in flux expulsion behavior for high RRR niobium given 800 C furnace treatment
Developed “cure” for poorly expelling material – heat treatment at 900-1000 C

## Slide 9: Original LCLS-II Production Material
Conclusion about original LCLS-II Nb:
  Very poor expulsion with only 800 C 3 h
  TD needs 900 C 3h (both cavities)
  NX needs 950 C – 975 C (NX2 more stubborn than NX1)
Fermilab pCM data shows importance of high massflow – of 4 cooldowns, only those with massflow >25 g/s extend into acceptable expulsion range; more g/s expected to achieve better expulsion

## Slide 10: Effect of Heat Treatment in Vertical Test
TD 800 C 3 h: Q0 degraded significantly even for relatively small applied field
TD 900 C 3 h: Q0 robust to applied field

## Slide 11: Effect of Heat Treatment in Vertical Test
TD 900 C 3 h
TD 800 C 3 h

## Slide 12: Fermilab CMTF and VTS Data F1.3-01 through 016
Fermilab vertical test
Fermilab module test
Dashed line includes correction at VTS for stainless flanges

## Slide 13: Effect of Massflow on Q0
Expected trend is observed – higher massflow -> improved expulsion -> higher Q0
(Appears to be effect of insufficient ‘soaking’ time to thermalize before Q0 measurement)

## Slide 14
Fast cooldown at CMTF, Eacc ~ 16 MV/m, 2.0 K

## Slide 15
Fast cooldown at CMTF, Eacc ~ 16 MV/m, 2.0 K
Blue - Higher temperature heat treatment
Red - Lower temperature heat treatment
TD cavities with insufficient heat treatment
NX cavities with insufficient heat treatment
Sufficient heat treatment applied

## Slide 16
Fast cooldown at CMTF, Eacc ~ 16 MV/m, 2.0 K
Blue - Higher temperature heat treatment
Red - Lower temperature heat treatment
TD cavities with insufficient heat treatment
NX cavities with insufficient heat treatment
Sufficient heat treatment applied
For HE, we want to avoid insufficient heat treatment as much as possible

## Slide 17: New Material from Tokyo Denkai
All baseline LCLS-II niobium from TD expelled well after 900 C 3 hours
New material purchased from Tokyo has more variability
A. Palczewski, JLab
Trip planned to visit TD to discuss differences in niobium production that could have caused this variability
Need to improve specifications to avoid this issue in the future and to better evaluate this new TD material

## Slide 18: Simple Measurements to Predict Flux Expulsion
Also performing R&D to explore simple method (e.g. can be done at vendor) to predict expulsion
Study correlation between grain GROWTH during heat treatment and flux expulsion
E.g. original TD material showed minimal change in expulsion after 800 C 3 hr, but strong after 900 C 3 hr. Similar for NX after 950 C 3 hr
Search for change in grain growth at 900 C/950 C in corners from single cell cavities with well characterized expulsion

## Slide 19: Search for Correlation
Strong flux trapping
Full expulsion
Initial grain size
Grain Growth
Heat treatment Temperature
Flux Expulsion/Grain Size

## Slide 20: Search for Correlation
Strong flux trapping
Full expulsion
Initial grain size
Grain Growth
Heat treatment Temperature
Flux Expulsion/Grain Size
Expulsion vs temperature characterized for several LCLS-II single cells
Temperature chosen for acceptable flux expulsion

## Slide 21: Search for Correlation
Strong flux trapping
Full expulsion
Initial grain size
Grain Growth
Heat treatment Temperature
Flux Expulsion/Grain Size
Expulsion vs temperature characterized for several LCLS-II single cells
Need to measure grain growth vs temperature for the same material
Temperature chosen for acceptable flux expulsion

## Slide 22: Summary
Poor flux expulsion created a risk of low Q0 for LCLS-II production material with baseline recipe. This was mitigated via a 900-1000 C heat treatment developed in timely R&D
Q0 ~ 3x1010 is regularly being achieved in LCLS-II cryomodules with modified heat treatment
Temperature required was found to depend on niobium production run, but material from both vendors was made to satisfy the stringent requirements of LCLS-II
Looking towards HE, we want to avoid cavities with poor flux expulsion as we had early in LCLS-II production
We are actively working on R&D to guide modifications to material specifications for HE