## Slide 1
Sam Posen
LCLS II HE Cryomodule Performance Workshop
25 April 2019
Source of Gradient Limitations in Fermilab Cryomodules

## Slide 2: Usable Gradient Limitation Mechanism at FNAL
We regularly see usable gradients in the 17.5-18.5 MV/m range when the maximum gradient is closer to 20-21 MV/m
Usable gradient requires 1 hour without quench, but regularly see cavities stable for many minutes then suddenly quench
What could be causing these “sporadic” quenches?

## Slide 3: Possible Cause of Quench: Multipacting
Electron hits surface. >1 electron is ejected. Repeat.
Range of fields in which quenches are observed is right where multipacting band is for this cavity shape
Pasi Yla-Oijala, “Electron multipacting in TeSLA cavities and input couplers,” Particle Accelerators, Vol. 63, pp. 105-137 (1999)
Multipacting band: Eacc range where resonant condition is met for electron impacts at equator (depends on SEY)
Processing is expected to reduce SEY and therefore reduce multipacting

## Slide 4: Possible Cause of Quench: Overheating
Endgroups heat up from RF dissipation, and if the heat power is greater than the conductive cooling power, thermal runaway can occur
Depends on thermal strapping of endgroups
Heat dissipated in cells is cooled directly by liquid helium in tank
Dissipation in endgroups is far smaller, but cooling is indirect via conduction

## Slide 5: Usable Gradient Determination – March 27, 2019

## Slide 6
HOM antenna temperature sensor

## Slide 7: HOM antenna Temperatures (2 per cavity)
Cernox sensors calibrated at Fermilab
>1 K temperature variation – inconsistent thermal strapping? Or variation in HOM cable length?
Cavity 8 upstream HOM
Cavity 8 downstream

## Slide 8: Processing Helps When it is Applied

## Slide 9: Processing Example

## Slide 10
Strong correlation between quench and x-ray burst on chipmunks

## Slide 11
Strong correlation between quench and x-ray burst on chipmunks

## Slide 12
Decarads not as sensitive to this

## Slide 13: Case Studies
CM16 is not ideal for case studies – for previous CMs, they would start at the maximum gradient, then work backwards as they tried to find usable gradient. For CM16, they started at ~17 MV/m at each cavity, then proceeded upwards till they reached a gradient at which they quenched prior to reaching 1 hour of operation, or else ran out of time for the shift
CM15 problem with file I/O from Matlab. Couldn’t access data in the Backup logger
CM14 has some useful examples

## Slide 14: F1.3-14 performance
*No VTS administrative limit
**21 MV/m is CMTF administrative limit
***50mR/h wall radiation detector and/or 0.5 MV/m below quench limit
Q0 measurements started xx hours after thermal bump
 | VTS |  |  | CMTF Test |  |  |  | 
Cavity | Eacc* [MV/m] | FE onset | Q0@16MV/m | Max** Gradient [MV/m] | Usable Gradient*** [MV/m] | FE onset [MV/m] | Q0 @16MV/m 2K @ 30 g/s | Material
CAV0139 | 26 | none | 2.9E+10 | 19.9 | 17.5 | none | 2.9E+10 | TD, 200/900
CAV0225 | 24.5 | 24 | 3.5E+10 | 20.5 | 18.3 | none | 3.1E+10 | TD, 200/900
CAV0096 | 21 | none | 3.5E+10 | 20.5 | 18.7 | none | 4.2E+10 | NX-B, 200/950
CAV0154 | 28 | none | 3.7E+10 | 21 | 18.5 | none | 2.9E+10 | TD, 200/900
CAV0230 | 18.7 | none | 3.6+10 | 17.5 | 17 | none | 2.9E+10 | NX-B, 200/900
CAV0205 | 18.5 | none | 4E+10 | 17 | 16.5 | none | 3.5E+10 | NX, 200/950
CAV0324 | 24 | none | 3.1E+10 | 21 | 20.5 | 14 | 2.6E+10 | TD, 200/900
CAV0150 | 22.5 | none | 3.1E+10 | 18.5 | 17.5 | none | 2.8E+10 | TD, 200/900
Average | 22.9 |  | 3.4E+10 | 19.4 | 18.0 |  | 3.1E+10 | 
Total Voltage | 190.1 |  |  | 161.8 | 150 |  |  | 

## Slide 15: Case Study – CM14, Cavity #2

## Slide 16: Case Study – CM14, Cavity #2
Duration at gradient not correlated with gradient – stable at 19.5 MV/m for 25 minutes then quench very quickly at 18.5 and 19.0
15:00
17:00

## Slide 17: Case Study – CM14, Cavity #2
15:00
17:00

## Slide 18
HOM antenna temperatures not correlated with quench – much higher T seen during stable times than during quench
Stable
Quench
Quench
Stable

## Slide 19
Coupler temperatures not correlated with quench – higher T seen during stable times than during quench

## Slide 20: Case Study – CM14, Cavities #3 & 4
8:30
13:45
5 K circuit temperature excursion!

## Slide 21
HOM antenna and 5 K circuit temperatures not correlated with quench – much higher T seen during stable times than during quench – But cavity turn-on may influence quench?

## Slide 22
Coupler temperatures not correlated with quench – higher T seen during stable times than during quench

## Slide 23: Summary
Observations that suggest quench is related to multipacting
  Processing helps increase quench field
  Quench strongly correlated with x-ray bursts
Observations that suggest quench not caused by overheating
  Anticorrelations observed with time to quench
  Anticorrelations observed with HOM antenna temperature and coupler temperature
  In one case, usable gradient achieved during a time when 5 K circuit temperature was increasing substantially
Some preliminary correlations between quench of one cavity and bringing up Eacc of another

## Slide 24: Next Steps
Experiments at CMTF (LCLS-II CM if possible, HE pCM)
  Attempt to process multipacting to improve maximum gradient and reduce quench frequency
  Measure Q0-degradation from flux trapping after 1 quench; multiple quenches
  Perform thermal bump to recover Q0-degradation – does it reset multipacting? If so, could be major problem
  Perform unit test at 18 MV/m to evaluate higher gradient operation for LCLS-II CM; higher gradient?
  Development of rapid quench detection to shut off RF power and prevent excessive boiling of helium in tank
Experiments in VTS
  Do we see this in VTS if we hold for ~1 hour plus in MP band?