## Slide 1: MQXFAP1b Quench Antenna and Coil Images
Dan Cheng, et al.
6/14/2019
LBNL

## Slide 2: Outline
Possible Quench Antenna locations and wedge gaps
Pre-MQXFAP1b assembly Coil Images
Virgin Coil Images of Coil P03

## Slide 3: P03 Wedge Gaps and Possible QA Location based on MQXFAP2 placement
Wedge-Spacer Gap
Non Transition Side
Wedge Gap
Transition Side
Wedge Gap
NTS Wedge Gap
TS Wedge Gap
NTS Wedge Gap
TS Wedge Gap
Wedge-Spacer Gap
QA 1-4
QA 5
QA 6
QA 7
QA 8
QA 9
QA 10
QA 11
QA 12
QA 13-16
QXFP Coil Length
QXFA Coil Length (ref)
Quench Antenna positions based on presumed location from MQXFAP2 test campaign

## Slide 4: P03 Wedge Gaps and Possible QA Location based on MQXFAP1 placement
Wedge-Spacer Gap
NTS Wedge Gap
TS Wedge Gap
NTS Wedge Gap
TS Wedge Gap
NTS Wedge Gap
TS Wedge Gap
Wedge-Spacer Gap
QA 1-4
QA 5
QA 6
QA 7
QA 8
QA 9
QA 10
QA 11
QA 12
QA 13-16
QXFP Coil Length
QXFA Coil Length (ref)
Quench Antenna positions based on presumed location 100 mm from MQXFAP2 test campaign

## Slide 5: Pre-MQXFAP1b Coil Images

## Slide 6: Pre-MQXFAP1b Coil Images (P03 LE)
Significant cracks/delamination
visible
Visible “Interface” crack
VTA03 (was lost during MQXFAP1 testing)
VTA02
VTA04
VTA05

## Slide 7: Pre-MQXFAP1b Coil Images (P03 ~2150 mm)
NTS Wedge Gap
~2143 mm from coil end
TS Wedge Gap
~2290 mm from coil end

## Slide 8: Pre-MQXFAP1b Coil Images (P03 RE)
Significant delamination
visible
Significant “Interface” cracking evident
VTA07
VTA06

## Slide 9: Pre-MQXFAP1b Coil Images (P02 LE)
Some cracks/delamination
visible

## Slide 10: Pre-MQXFAP1b Coil Images (P02 RE)
Some cracks/delamination
visible

## Slide 11: Pre-MQXFAP1b Coil Images (P04 LE)
Some cracks/delamination
visible

## Slide 12: Pre-MQXFAP1b Coil Images (P04 RE)

## Slide 13: Pre-MQXFAP1b Coil Images (P06 LE)

## Slide 14: Pre-MQXFAP1b Coil Images (P06 RE)

## Slide 15: Virgin Coil P03 Images

## Slide 16: Virgin Coil Images of Coil P03
Non-Transition Side (NTS) Wedge Gap
~285 mm from coil end
Transition Side (TS) Wedge Gap
~285 mm from coil end
VTA03
VTA04
VTA05
VTA08
VTA02

## Slide 17: Virgin Coil Images of Coil P03
NTS Wedge Gap
~1138 mm from coil end
TS Wedge Gap
~1295 mm from coil end

## Slide 18: Virgin Coil Images of Coil P03
NTS Wedge Gap
~2143 mm from coil end
TS Wedge Gap
~2290 mm from coil end

## Slide 19: Virgin Coil Images of Coil P03
NTS Wedge Gap
~3140 mm from coil end
TS Wedge Gap
~ 3290 mm from coil end

## Slide 20: Virgin Coil Images of Coil P03
NTS Wedge Gap
~4148 mm from coil end
TS Wedge Gap
~4148mm from coil end
VTA07
VTA06

## Slide 21: Summary
Quench Antenna array shown based on preliminary understanding of its location during both MQXFAP2 and MQXFAP1 tests
  These were combined with wedge and spacer gap locations in Coil P03
Significant cracking and delamination of epoxy was observed in Coil P03 after the MQXFAP1 test
  RE region had evidence of more “interface” cracking than seen in the LE
  Virgin P03 appears to have significant bubbles in the RE region
  Coils P02 and P04 showed minimal epoxy cracking and/or delamination of traces after MQXFAP1 test

## Slide 22: Additional Info

## Slide 23: MQXFAP1 Training
Notes:
P03 quenches appeared in pole turns and/or transition (VTA08 was lost)

## Slide 24: Coil P03 VTA08 Virgin

## Slide 25: Coil P03 VTA08, Pre-MQXFAP1b
Notes:
P03 quenches appeared in pole turns and/or transition (VTA08 was lost)