## Slide 1: MQXFA03 Coil Review Coil QXFA204
Henry M. Hocker, Jr.
June 27, 2019

## Slide 2: Outline
Notes / photos
Reaction plots
Electrical Data
CMM
DRs

## Slide 3: QXFA204
Prior to change for B6 adjustment
  4 layers glass on pole
  10 mil G11 shims on midplane
Pole gaps
  1.8 mm after reaction
Lead / Wire length
  2.6 m coil leads
  1 m coil tap wires
  4.5 m splice tap wires
  1 m quench heater wires
Coil length
  4525.1 mm overall length
Tap Wires A01 & B01 are attached to the leads (not connected in the wiring pocket, as they will be from now on

## Slide 4: QXFA204
Reaction Cycle:
48 Hours at 210 C
48 hours at 400 C
50 hours at 665 C

## Slide 5: QXFA204

## Slide 6: QXFA204

## Slide 7: QXFA204

## Slide 8: QXFA204
Faro arm coil size measurements:
  Primary best fit to coil OD, secondary to keyway (midplane where no keyway).
Nominal Coil Dimensions:
Outer Radius = 113.376 mm
Midplane offset = .125 mm
Keyway Width = 14.00 mm

## Slide 9: QXFA204
8 (207)
13 (320)
29 (740)
61 (1540)
92 (2340)
124 (3140)
155 (3940)
170 (4323)
174 (4426)

## Slide 10: QXFA Coils
Coil size comparison:

## Slide 11: QXFA204
DRs
  Small number of issues with supplied parts – Addressed via replacement.
  Conductor abrasions noted in a number of places during cable inspection
  Overall coil length out of range (low side)
R value slightly outside range listed in doc 521 v12.