## Slide 1: R&D Towards a 1.3MW T2K Target
Eric Harvey-Fishenden, Chris Densham, Mike Fitton, Geoff Burton, (High Power Targets STFC RAL)
In conjunction with the KEK Neutrino Beam Group
NBI 2019 Fermilab

## Slide 2
30 GeV Main Ring (MR)
3 GeV Rapid Cycling Synchrotron (RCS)
400 MeV LINAC
T2K neutrino facility
J-PARC, Tokai, Japan
T2K Target Station
295 km to Super-Kamiokande
Near detector (ND280)
J-SNS
Beam dump
Beam Power:
Current: 480kW
Design: 750kW
Upgrade (HK): 1.3MW

## Slide 3: Secondary Beam-line & Target Station
Baffle
1st horn
Target
2nd horn
3rd horn
BEAM
Iron shield (2.2m)
Concrete Blocks
Helium Vessel
Target station
To ND280 (280m) SuperK (295km)

## Slide 4: T2K Target
Remote connector + bellows + isolator (Al2O3)
Al2O3 Isolators
Bolted Titanium-Graphite joint (metal seals)
Graphite (purified)
(Toyo Tanso IG-430)
Ti-6Al-4V tube and windows (0.5 mm thick)
Titanium pipe + flange
Titanium target body
Graphite
(Toyo Tanso IG-43)
47.0
46.4
39.6
35.6
26.0
Stainless tubes + flange
Latest version produced at RAL and shipped to JPARC late 2018, suitable for beam operation up to 750kW

## Slide 5: Upgrade to 1.3MW (overview)
Current operational experience up to 480kW (0.48MW)
Beam power 0.751.3MW will increase the integrated heat load on the target
Can’t just increase flowrate
  Pressure drop
  Helium velocity
Increase operating pressure:
  Allows higher mass flow rate without big increase in dP or velocities
  Compressor will be smaller, and cheaper to purchase and operate (less power consumed)
60g/s @ 5.9bar (5barG outlet) – 1.3MW beam power (Scaled MARS heat input from c. 2006)
With outlet pressure @5 barG the pressure drop of the system become comparable to the 750kW design (32g/s @1.6bar/0.9barG outlet)
Target components must be: re-designed/optimised for operation at 5 bar, and pressure tested at 7.5 bar
M. Fitton

## Slide 6: Target Upgrades for Higher Pressure
Uprated edge-welded bellows suitable for 5 bar operation
Re-optimise upstream target window to reduce pressure stress & maintain good cooling
Re-optimise downstream target window to reduce pressure stress & maintain good cooling
Full penetration EB weld at downstream target window

## Slide 7: Target Windows Optimisation
Upstream Window:
Plate thickness increased
Window profile maintained the same up to R18mm – off centre beams
Blend radii increased
Stress reduced from 74MPa →38MPa
CFD shows modifications have little effect on flow/cooling
ANSYS plots: Mike Fitton
Prototype currently in manufacture

## Slide 8: Target Windows Optimisation
750kW design
1.3MW design
ANSYS plots: Mike Fitton
Prototype currently in manufacture
Downstream Window:
Curvature of window increased (both at edges and on beam centre)
Pressure stress reduced by a factor of 3
Small (0.01bar) increase in pressure drop but small increase in cooling (6% temperature reduction)

## Slide 9: Downstream Window EB Weld Development
Current design has just 0.25mm penetration – for higher pressure we would like a full penetration weld
Joint prep is consumed in the weld – if the fit is not very good, the weld will contain voids or lack fill – QA is very important
0.5mm
0.25mm penetration weld
Full penetration EB weld (joint prep is consumed)
Current
design
New
design
Top bead
Under bead
Section
Re-slice through weld
Visual inspection, cut section, dye pen & CT scan all look good – no visible pores or defects

## Slide 10: High Pressure Target Pipes
5 Bar capable edge-welded bellows have been sourced and a prototype target He pipe produced
Bellows protect fragile ceramic (more on this later)
Low pressure testing revealed that a re-design is required
  Expansion of free bellows “1” under pressure is excessive
0.6mm @2 Bar
1.3mm @ 2Bar
1
2
Pressure testing set up of prototype 5 bar pipes
Large moment transferred to target
Ceramic
isolator
Integration of a pressure balanced bellows system is necessary
  Allow compliance for thermal expansion
  Prevent length growth under internal pressure
Space is limited and mass/complexity must be kept low
  Currently in discussion with bellows companies

## Slide 11: High Pressure Target Pipes
Potential pressure balanced pipe design:
Just one reason that target helium pipes are challenging to design and manufacture
Time→
Active bellows
Balancing bellows
Adjustment bellows
Target Pipe Evolution

## Slide 12: Target Ceramics
Ceramic breaks are a necessity for electrical isolation in all Neutrino facilities (used in target, horn, striplines etc.)
  Typically Alumina (Al2O3) in purities between 90-99.5%
  They are brittle, fragile and easily broken if loaded in any manner except axial compression
They feature in several areas for the T2K target:
  Target mounting
  Helium cooling pipes
Ceramic breaks are a potential limiting factor for all Neutrino facilities
  Commonly see water leaks, gas leaks etc. at joints containing ceramic isolation
RAL HPT group has investigated several types of isolator for T2K with varying degrees of success
  Diffusion bonded
  Bolted
  Brazed
Target helium pipes with brazed alumina isolator for 750kW operation
Target helium pipes with diffusion bonded alumina isolator for 750kW operation
Notes: Ceramic breaks are a real weak point for Neutrino facilities everywhere.

## Slide 13: Target Helium Leak
June 2015: Helium leak detected in target cooling system
September 2015: Leak investigations in remote maintenance area (RMA) identify leak at ceramic isolator in target helium outlet pipe
Leaking pipe was replaced remotely with help of TRIUMF in December 2015
Possible causes:
  Stress relieving of cold bent stainless pipes?
  Thermal shock/fatigue due to rapid thermal cycling?
Leak location

## Slide 14: Stress Relieving of Bent Pipes
Pipes tested at RAL opened up by >3mm after furnace run @500°C/2hrs and 200°C/64hrs
Outcome:
Welded, mitred pipes (relieved for dimensional stability during manufacture)
(M. Fitton)
3mm lateral movement greater than tolerable by bellows
Shear/bending put on the ceramic isolator potentially caused failure → gas leak

## Slide 15: Beam Trips – Thermal Shock/Fatigue?
Beam trips are an inevitability during operation
Data from operations at JPARC suggest approximately hourly beam trips whilst running
Heat load is removed from target when the beam trips, but helium flow continues
Rapid cooling of target helium causes outlet pipes to see rapid thermal cycling during beam trips:
Chart: Time [MM:SS]
Target helium outlet temperature data from a beam trip at 480kW beam power operation (provided by KEK Neutrino group)
Outlet He temperature:
  Drops at a cooling rate of 80°C/minute
  Rises at a similar rate when the beam goes back on → thermal shock and thermal cycling on the brittle ceramic isolators
Hourly trips, 24hr operation, 180 days/year = 5000 thermal cycles per year
Offline testing?

## Slide 16: Testing – Thermal Cycling
HEATING - PID controlled ramp to set point temperature: 200°C @ 36°C/min
SOAK – Soak at 200°C for 3 minutes to eliminate thermal gradients in test section
COOL - Rapid cool w/ blower @ 70°C/min initial rate
Acoustic enclosure (air inlet)
Centrifugal blower ()
Ceramic test section
Acoustic enclosure (air exhaust)
Test section is heated by a 600W heater tape:
A test-bed was created at RAL to address the issue of thermal shock/fatigue on target ceramics

## Slide 17: Testing – Thermal Cycling
HEATING - PID controlled ramp to set point temperature: 200°C @ 36°C/min
SOAK – Soak at 200°C for 3 minutes to eliminate thermal gradients in test section
COOL - Rapid cool w/ blower @ 70°C/min initial rate
Acoustic enclosure (air inlet)
Centrifugal blower ()
Ceramic test section
Acoustic enclosure (air exhaust)
Test section is heated by a 600W heater tape:
A test-bed was created at RAL to address the issue of thermal shock/fatigue on target ceramics
Are test conditions as harsh as operating conditions?
Use operational data (485kW) and extrapolated simulations for higher power
 | Temperature Range (°C) | Max cooling rate (°C/min) | Max heating rate (°C/min) | Number of cycles completed | Failure detected
Testing Phase 1 | 40-140 | 50 | 36 | 5120 | No
Testing Phase 2 | 40-160 | 55 | 36 | 5200 | No
Testing Phase 3 | 40-180 | 60 | 36 | 5160 | No
Testing Phase 4 | 40-200 | 70 | 36 | 16118 | No

## Slide 18: Beam Trips - Thermal Analysis
480kW helium beam data used as an input to ANSYS transient thermal analysis
Temperature at outer surface extracted
  We can compare this with PT100 location on lab tested ceramics
Ceramic temperature lags behind helium temperature significantly
PT100 position
What about cooling rates at higher beam power/helium pressure?
Cooling rates:
Helium = 80°C/min
Ceramic = 25°C/min
Conjugate heat transfer simulations

## Slide 19: Beam Trip Simulation
Run steady state conjugate heat transfer model (CFX) of target
  MARS/Fluka heat inputs
Import steady state temperatures as input to transient simulation with heat load removed
Extract helium outlet temperature as a function of time and compare with operational data
This can be used as:
  An input to ceramic thermal analyses
  Verification of heat deposition calculations using Monte Carlo codes
Target model includes all material such as outer cover, ears and pipes - thermal mass is important for transient simulation.

## Slide 20: Beam Trips - Operational Data vs Simulations
To match the operational data:
Old (2006) MARS heat load needs to be scaled back to approximately 300kW
Fluka heat load needs to be scaled back to approximately 400kW
Operational data from 29/04/2018
Beam power = 480kW
Helium flow rate = 22.9g/s
Target helium outlet temperature (°C)
Time after beam trip (seconds)

## Slide 21: Heat Load Discrepancy
These simulations have highlighted some significant differences between operational data and the engineering analysis using heat loads from Monte Carlo codes
480kW operational data, temp. rise of He = 73.4°C @ 22.9g/s  8716W
MARS (2006)
FLUKA (2019)
M. Fitton
M. Fitton
This is good news for us as flow rate & pressure for 1.3MW could be reduced
  4 BarG outlet pressure looks feasible, reduced flow rate study is underway
We are aware that older versions of MARS can predict significantly more heat load
than newer versions of MARS and Fluka
480kW MARS (2006), temp. rise of He = 145.2°C @ 22.9g/s  14,121W (x1.6)
480kW FLUKA (2019), temp. rise of He = 89.0°C @ 22.9g/s  10,636W (x1.2)

## Slide 22: Other Heat Losses
Conduction from target head to target support plates:
  Target head mounting face is at 37°C
  TS ambient helium @40°C (negligible heat transfer)
  Target support plates water cooled, water temperature expected to vary with ambient conditions
  ANSYS thermal analysis, assuming perfect contact at interfaces:
  200W heat removed with 20°C cooling water
  35W heat flow into the target if cooling water is at 40°C
Max unaccounted for loss ~300W (<4% target heat load)
Heat loss from between target outlet and thermocouple position:
  Ø50.8mm pipe
  HTC ~ 10W/m2.K
  Ambient helium temperature = 40°C
  Helium pipe @ target outlet temp = 100°C
  Pipe surface area/meter = 0.159m2
  Power loss = 10 x 0.159m2 x (100-40) = 63.6W/meter
  Not significant over the approx. 1.5m between target outlet and thermocouple location (100W)

## Slide 23: Comparison – Ceramic Thermal Testing
Latest testing phase exceeds estimated operating conditions at 1.3MW for 3+ years operation
 | Temperature Range (°C) | Max cooling rate (°C/min) | Max heating rate (°C/min) | Number of cycles completed | Failure detected
480kW @23g/s (Op data - ANSYS) | 33-100 | 25 | 23 | - | -
1.3MW @32g/s (CFX-ANSYS) | 30-167 | 61 | - | - | -
1.3MW @60g/s (CFX-ANSYS) | 30-101 | 53 | - | - | -
Testing Phase 4 | 40-200 | 70 | 36 | 16118 | No
Linear extrapolation of beam data
Beam data
We have good reason to believe that the brazed isolator is suitable for 1.3MW operation

## Slide 24
Summary
Most R&D in order to achieve an operational 1.3MW T2K Target has been completed
A brazed Alumina isolator has been thermally tested at the equivalent of approximately 3 years running @1.3MW beam power
Heat loads from MARS and FLUKA codes have been compared to operational data highlighting approximately 40% and 10% respective overestimations of energy deposition in the T2K target
Key target components have been redesigned for a higher target helium operating pressure of approximately 5 bar
Prototyping of key components is currently underway

## Slide 26: Backup - Simulation Conditions
Inlet Temperature = 300K
Fluid = Helium (Ideal Gas)
Turbulence model = Shear Stress Turbulence (SST)
Reference pressure = 1atm (Gauge P)
Target container and window material = Ti-6Al-4V (Gr. 5 Titanium)
    Specific heat capacity = 526.3 J/kg.K
    Thermal conductivity = 6.7 W/m.K
Target material = Toyo Tanso IG-43 (non-linear properties as below)
Conjugate heat transfer model (coupled CFD-Thermal model)

## Slide 27: Backup - MARS (2006) heat deposition for target
750kW, 3.3e14ppp , 2.11sec
Target core
Peak energy density = 200J/g
Integrated energy = 39,262J/spill

## Slide 28
Backup - FLUKA (2019) heat deposition for target
Fluka Flair version: 2.3-0
Beam energy: 30GeV
Particle: Proton
Beam shape: 0.999cm FWHM Gaussian
 4.24mm Sigma
Number of primaries: 4,000,000
Geometry updated to be more representative of target

## Slide 29
Backup - FLUKA (2019) heat summary
T2K achieved operation
480kW @ 30GeV
2.48x1014ppp @ 2.48s
HK proposed upgrade
1.3MW @ 30GeV
3.2x1014ppp @ 1.16s
750kW proposed
750kW @ 30GeV
2.0x1014ppp @ 1.32s

## Slide 30: Backup – Mars/Fluka vs Ops Data
Yellow line – MARS 480kW @ 32g/s excludes the possibility that the flow rate was higher than measured – TOut is a closer match to operational data but cooling rate is much faster
Operational data from 29/04/2018
Beam power = 480kW
Helium flow rate = 22.9g/s