## Slide 1: Soldering and Quality Assurance
Pam Marr
UW Physical Sciences Lab
DUNE Electronics Review
2019 November 18

## Slide 2
Soldering Objectives for DUNE
Continue soldering wires to head boards as before using Sn62Pb36Ag02 formula with no-clean Type 44 rosin (Kester)
Continue using Metcal soldering stations for precise temperature control
Maintain a local IPC-qualified trainer to supervise soldering methods and inspect work
Improve access to work

## Slide 3
Soldering Objectives for DUNE
Adopt Vapor-Phase reflow soldering methods for CR Boards and G-bias boards to achieve more consistent results with less stress to components.
Use Wave or Selective Soldering on Samtec (through-hole) connectors installed on CR boards and Adapter boards to eliminate high stresses placed on solder joints

## Slide 4
Soldering Objectives for DUNE
Maintain a safe, clean, and comfortable work environment with adequate lighting
Avoid worker fatigue
Continue rules that prohibit anyone from handling boards at any time without gloves

## Slide 5
Soldering Quality Assurance
Inspect all work; no self-assessment is allowed
Record all instances of marginal or inadequate results and take corrective actions
Maintain equipment properly
Change soldering tips regularly
Do not allow the wrong soldering materials to enter the work area
Do not allow storage of any material in unmarked containers

## Slide 6
Soldering Quality Assurance
Do not allow the any soldering materials to enter the work area without being labeled
Any stray pieces of solder shall be discarded
Do not allow storage of any materials in unmarked containers
Do not use any materials that are older than their expiration date