## Slide 1: Ab-initio alloy design for C-band accelerators
Gaoxue Wang, Danny Perez
T-1, Theoretical Division
04/21/2021
International Workshop on Breakdown Science and High Gradient Technology (HG2021) (HG2021)
LA-UR-21-23694

## Slide 2: Acknowledgements
Danny Perez (T-1)
Timothy Germann (T-1)
Andrew Garmon (T-1)
Soumendu Bagchi (T-1)
Nirmal Rai (T-1)
C-band experimental team
LDRD-DR: 20200057DR, 20190079DR

## Slide 3: Outline
RF breakdown
Figure of merit (FOM) for Cu alloys
Cu-Ag as an example
High-throughput screening
Summary and plan

## Slide 4: RF breakdown
Breakdown probability is dependent on the material of the cavity.
Cu-Ag alloys can optimize breakdown resistance
Can we scan the whole periodic table in search of the optimal solute and concentration?
Simakov, Dolgashev, Tantawi, 2018

## Slide 5: Outline
RF breakdown
Figure of merit (FOM) for Cu alloys
Cu-Ag as an example
High-throughput screening
Summary and plan

## Slide 6: FOM overview
Tradeoffs:
  Good: Adding solute atoms can improve strength: limit plastic deformation under thermal loading
  Bad: Adding solute atoms can increase RF dissipation and thermal stresses: increase driving force for plastic deformation
Figure of merit (FOM):
  Critical stress to move dislocations / Thermal stress created by RF dissipation
Level of theory: Density Functional Theory (DFT)
Chemical space: Dilute binary Cu alloys

## Slide 7: FOM #1: Critical stress to move dislocations
Labusch–Nabarro (LN) model: Critical resolved shear stress required for dislocation motion:
With:
Two key parameters:
Size misfit
Modulus misfit
Johan Zander et al., Computational Materials Science 41 (2007) 86–95
M. Z. Butt, Journal of Materials Science 28 (1993) 2557-2576

## Slide 8: FOM #2: Thermal stress created by RF dissipation
Heating due to RF losses can be estimated from the solution of the heat equation:
Material properties
Accelerator parameters
Perry B. Wilson. In ITP Conference on Future High Energy Colliders.
University of California, Santa Barbara, October 1996.
Assuming that the surface is free to relax in z only, the corresponding in-plane thermal stress is

## Slide 9: FOM = FOM #1 / FOM #2
Estimating the FOM requires:
Lattice constant: direct relaxation
Thermal conductivity: Boltzmann transport
Electrical conductivity: Boltzmann transport
Mechanical properties: finite distortion
Thermal expansion coefficient: quasi-harmonic approximation
These quantities need to be computed vs solute concentration.
This requires tens of DFT calculations per solute per concentration (!)

## Slide 10: High-throughput workflow
Solution: workflow management tool called pyiron
Standardizes calculations, manages job execution, stores results in database

## Slide 11: Outline
RF breakdown
Figure of merit (FOM) for Cu alloys
Cu-Ag as an example
High-throughput screening
Summary and plan

## Slide 12: FOM #1: Critical stress to move dislocations
Cu experiments

## Slide 13: FOM #1: Critical stress to move dislocations
Estimated from
DFT results

## Slide 14: FOM #2: Thermal stress created by RF dissipation
keep as a constant 1
Estimated from DFT
Using experimental data
wavelength

## Slide 15: FOM = FOM #1 / FOM #2
  Critical stress to move dislocations / Thermal stress created by RF dissipation
optimal concentration

## Slide 16: Outline
Introduction
Figure of merit (FOM) for Cu alloys
Cu-Ag as an example
High-throughput screening
Summary and plan

## Slide 17: Execution plan and current status:
Solutes: atomic numbers up to 86
Concentrations: 3.1%, 6.2%, 9.4%
High-throughput workflows:
  Structure optimization
  Thermal/electrical conductivities
  Mechanical properties
  Critical resolved shear stress
  Thermal expansion coefficients
Current status:
All workflows written with pyiron. Currently sequentially executing them.
Cu
solute

## Slide 18: Conductivities
3.1% solute
(Normalized by conductivity of pure Cu)

## Slide 19: Conductivities
6.2% solute
(Normalized by conductivity of pure Cu)

## Slide 20: Shear modulus (GPa)
3.1% solute
(In units of GPa)

## Slide 21: Summary and plan
Summary:
FOM: tradeoff between solute strengthening and RF losses
Development of a high-throughput workflow
Execution across the periodic table ongoing
Identification of solutes that are promising to maintain high conductivity of Cu and increase mechanical properties
Future plans:
Compute FOM of all binary alloys on the periodic table
Consider surface structure (e.g., solute segregation) and properties (electronic work function)
Engage with experimental efforts to assess potential candidate alloys

## Slide 22: Electrical and thermal conductivity
Semiclassical Boltzmann transport equation
(1)
(2)
(3)
(4)
Electronic structure calculations
BoltzTrap2
(Relaxation time approximation)
Madsen, Georg KH, and David J. Singh., Computer Physics Communications 175, no. 1 (2006): 67-71.

## Slide 23: Electrical and thermal conductivity
σ/τ = 1.6*1E21 (Ωms)-1
Relaxation time τ = 2.7*1E-14 s (experiments)
σ = 4.32*1E7 (Ωm)-1
Resistivity ρ = 1/σ = 2.3*1E-8 Ωm
(Experiments ~1.72*1E-8 Ωm)
κ/τ = 125*1E14 W(mKs)-1
Relaxation time τ = 2.7*1E-14 s (experiments)
κ = 337.5 W(mK)-1
(Experiments ~386 W(mK)-1)
Pure Cu

## Slide 24: Mechanical properties
Bulk modulus
Shear modulus
Hooke’s law
Young’s modulus
Poisson’s ratio
Elastic constants Cij

## Slide 25: Thermal expansion coefficient
Calculated using the Quasi-harmonic approximation (QHA)