## Slide 1: Local power coupling as a predictor of high-gradient breakdown performance
Jan Paszkiewicz, Alexej Grudiev, Walter Wuensch
High Gradient Workshop 2021
21 April 2021

## Slide 2: High-Gradient Limits: Electric Field
Dependence of peak E field with group velocity (C. Adolphsen)
Kilpatrick’s criterion: ‘classic’ quantity defining maximum surface E field.
Different structure designs can reach different peak accelerating gradients and surface fields.
It appears that breakdown is not just a function of E field. Dependence on H field, group velocity, power flow, and total voltage have all been observed.

## Slide 3: High-Gradient Limits: Power Flow
Experimental data from CERN, SLAC and KEK suggests ultimate limit depends on power flow, not E field.
  Global power flow: input RF power divided by aperture circumference
  Local power flow: modified Poynting vector, Sc – used to optimise geometries
Example of structure tapering profile:
Example of surface Sc calculation in 1/8th of a damped cell:
Irises get smaller, E field gets bigger
Structure design and simulations: A. Grudiev

## Slide 4: Limitations of Sc
Breakdown locations:
  Many structures tend to have most breakdowns close to the input despite tapering.
  Post-mortem results of CLIC Crab Cavity, BTW Structure do not match Sc prediction.
Compatibility with DC experiments:
  No (real or imaginary) power flow at f = 0.
Sc uses unperturbed RF fields – what if we consider how local fields change during a breakdown?
Breakdown locations vs. Sc
Breakdown locations vs. E field
Structure post-mortem: E. R. Castro

## Slide 5: Evolution of a Breakdown
H. Timko et. al., Contrib. Plasma. Phys. 4, 229 (2015).
Animation by K. Sjobaek
PIC simulations and experiments show that:
Breakdown is a runaway process involving heating of an emission site and plasma formation.
Takes a short but finite time to develop.
A large number of charge particles is produced in the process – accelerating these particles requires a large influx of power.
If power flow is insufficient, the field will decrease.
Note that breakdowns are typically very small: ~10s of nm initially and ~50 um craters

## Slide 6: Evolution of a Breakdown
H. Timko et. al., Contrib. Plasma. Phys. 4, 229 (2015).
Animation by K. Sjobaek
Experiments and PIC simulations show that:
Breakdown is a runaway process involving heating of an emission site and plasma formation.
Takes a short but finite time to develop.
A large number of charge particles is produced in the process – accelerating these particles requires a large influx of power.
If power flow is insufficient, the field will decrease.
Note that breakdowns are typically very small: ~10s of nm initially and ~50 um craters

## Slide 7: Stages of breakdown
time
voltage
current
power
Field emission,
no plasma, tiny currents
Onset of breakdown and plasma formation
Fully formed plasma
Voltage collapse
Peak power demand during breakdown onset!

## Slide 8: Hypothesis
Ultimate BD limit is a function of available power, like with Sc.
  But: consider power during BD onset, not before!
Nascent breakdown extracts power from RF by acceleration of charged particles (electrons). Interaction through E field only.
Emitted current is a function of surface E field.
Local surface E field decreases under BD loading. (In this case, we approximate the effect of complex plasma dynamics by a simple antenna on the surface.)
Higher sustained E field under loading = higher BDR.

## Slide 9: Outline of Procedure
Assume that any breakdown site will emit current as this function of surface field:
(material property, to be fitted)
For every point in the structure, calculate a dependence of local field on antenna current:
E
I
surface field, E
breakdown current I
Unperturbed field at I = 0, as determined by usual RF simulations.
Slope Rbd depends on available power.
During BD onset.
We care about this one!
Field emission
Burning plasma

## Slide 10: Outline of Procedure
Combine the two plots to find a quasi-equilibrium solution:
Original, unperturbed field
Field when loaded by a breakdown.
This is our new quantity.

## Slide 11: Dependence on properties
Same unloaded field
Lower Rbd = more power coupling (eg. Larger aperture, better impedance match, etc.)
Compare with a different case:
Higher loaded field than before: higher breakdown rate

## Slide 12: Dependence on properties
Lower unloaded field
Same Rbd
Compare with a different case:
Lower unloaded field
= lower loaded field
= lower breakdown rate
Implications: No BD without E field, but power flow plays an important role.
The calculation is repeated for every point in the structure.

## Slide 13: Circuit Model of an Accelerating Structure
Infinite 1D array of coupled resonant cells.
Use an eigenmode solver to get values for circuit parameters: Q & dispersion curve give enough information to solve for L, C, R and M.
Solve to get characteristic impedance Z0, which relates power flow to cell voltage.
Dispersion curve derived from model:

## Slide 14: Circuit Model of an Accelerating Structure
Insert a port to represent the breakdown.
Modelled as a small antenna connected to a load.
Coupling (transformer ratio) varies with location and related to surface field at that point.
Strong dependence on group velocity and bandwidth.
Breakdown resistance vs frequency and aperture size:
Local E-field at breakdown site

## Slide 15: Numerical Calculation of Rbd
Method 1: Run a separate simulation where the antenna is the power source. Note the perturbation in E field for a given antenna current I:
Power from waveguide port (i.e. normal operation for acceleration):
Power from antenna (not physical, used for calculating Rbd):
Input port
Output port
Input port
Output port
Antenna
Method 2: Calculate Z-parameter matrix including the antenna as a port:
Better in principle but more sensitive to mesh quality.

## Slide 16: Study with Simple TM010 Structures
Simulated a series of accelerating
cells with the following properties:
120° phase advance
2 mm iris thickness
2 mm corner rounding
8.33 mm periodicity (for β = 1)
Iris radius scanned from 2.5 mm to 6 mm
Tuned to 12 GHz by varying cell diameter
Structures of 3 regular cells + 2 matching cells fed with TM01 via circular waveguide.
  Important to know details of power coupling & matching for this calculation!
E
H
Sc
Eigenmode field distributions

## Slide 17: TM010 Structures – Breakdown Locations
0 position is apex
Antennas placed along surface of centre cell:
Structure post-mortem: A. P. Fontenla
Sc distribution:
Unloaded E-field distribution:
BD-loaded E-field distribution:
Antennas representing possible breakdown sites.

## Slide 18: TM010 Structures – Maximum Gradient
Calculated maximum gradient for each aperture size using different limiting quantities.
Agreement for high vg, differences with regards to how low - vg and standing-wave structures are treated.
P/C implies infinite gradient for vg = 0.
Loaded field model (E*) implies high but finite gradient (since some power flow still exists)
P/C and Sc give satisfactory results for typical CLIC structures.
Good agreement for high vg

## Slide 19: TM010 Structures – Transient Correction
Single-frequency model implies steady state, after all stored energy discharged.
S-parameters over frequency contain information about stored energy.
Bandwidth related to transient phenomena, i.e., contribution stored energy.
Replace with , and rescale the emission function.
This formula assumes a short pulse of emitted current and the resulting resistive heating of the emission site.

## Slide 20: Stored Energy vs. Power Flow
Less power flow
More power flow
More stored energy
Less stored energy
Large aperture, high group velocity
Small aperture, low group velocity
Data points represent different locations in each structure.

## Slide 21: Application: X-Band Deflecting Structure
0° position
Antennas placed in rings around each iris.
180° position
90° position
Antennas angled to capture peak E-field region:

## Slide 22: Application: X-Band Deflecting Structure
Peak value of 118 MV/m
0° 180 °
0° 180 °
Structure post-mortem: E. R. Castro
Cell 1
Cell 2
Breakdown locations vs. Sc:

## Slide 23: Application: T24 Accelerating Structures
RF Input
RF Output
Iris #2
Iris #26
T24 PSI structure, E-field complex magnitude
Antennas placed near peak E-field region of each iris.
Loading plot for peak E-field region of each cell:

## Slide 24: Application: T24 Accelerating Structures
Peak value of 125 MV/m
T24 PSI 1
full history
Input
T24 PSI 2
112 MV/m, 200 ns flat run
T24N4
until 1/6/2019
Breakdown locations in T24 structures:
Output
T24N5
until 1/6/2019

## Slide 25: Application: BTW Proton Linac Structure
E-field in output cell
Sc in output cell @ 1W
63 kW/m^2
54 kW/m^2
66 kW/m^2
42 kW/m^2
A
B
C
D
Endoscopy photos from K. Szypula’s talk
Backward-travelling-wave structure with coupling holes between cells.
Large Sc on both iris and coupling holes
Region A has very few breakdown craters even though it has a larger Sc than region B.
Breakdown locations more closely correlated to E-field distribution, consistent with E* prediction.

## Slide 26: Application: DC Experiments
Electrodes tested at the DC LES at CERN regularly show breakdowns concentrated at the edge despite efforts to minimize field enhancement. (e.g. large cathode + small anode)
Rbd simulation shows clear distinction in power coupling between locations near the edge and at the electrode centre.
Electrode photo: I. Profatilova
centre
edge
intermediate

## Slide 27: Application: DC Experiments
Some experiments show that maximum achievable E field depends on total voltage, i.e. smaller gaps can reach higher fields.
Corroborated by simulations which show L decreasing with gap size.
Intuitively: easier to couple power into a larger gap.
Conditioning curves for various gap sizes.
CERN DC system results: I. Profatilova

## Slide 28: Summary
BD-loaded E field appears to be a good predictor of BD performance.
Makes distinction between unperturbed fields and fields under breakdown.
Better agreement with experimental breakdown locations.
Bottom line for high-gradient design:
  Consideration of power coupling is crucial.
  When optimizing a single cell, limiting peak E field is sufficient.
  Structures should be optimized for a specific gradient.

## Slide 29: Thank you!