## Slide 1: RFQ development at CERN field limit considerations and material study
Alexej Grudiev
20/04/2021

## Slide 2: Outline
Introduction
Breakdowns and beam loss in RFQs: is there any connection?
Material Study for better high gradient performance in the presence of beam loss

## Slide 3: Very briefly: what is an RFQ?
accelerator of choice for low-energy hadrons up to few MeV/u
strong electric quadrupole focusing field
modulation on quadrupole electrodes produces Ez field
accepts continuous input beam from LEBT, performs adiabatic bunching
Hermann Pommerenke

## Slide 4: Recent RFQs developed at CERN
older RFQs…
Linac4-RFQ 352 MHz 3 m
HF-RFQ 750 MHz 2 m
PIXE-RFQ 750 MHz 1 m
Carbon-RFQ 750MHz 4.8 m
commissioned 2018
V = 68 kV
Es,max = 51 MV/m
= 2 Kilpatrick
operational, 2014
V = 78 kV
Es,max = 34 MV/m
= 1.8 Kilpatrick
RF tuning complete 2020
Beam dynamics & RF design completed early 2020, now mechanical design by CIEMAT
C. Rossi et al., „Commissioning and operational experience gained with the Linac4-RFQ at CERN”, Proc. Linac14, 2014
Hermann Pommerenke

## Slide 5: Breakdown rate (BDR) in RFQ
Rolf Wegner
Surface field: ~35 MV/m
BDR: ~10-4
RF pulse 1 ms
Rep rate 1 Hz

## Slide 6: BDR in CLIC accelerating structures, a comparison
W. Wuensch, S. Stapnes
RF pulse 230 ns
Rep rate 50 Hz

## Slide 7: Damage from breakdowns
A replacement RFQ is being manufactured
Need to understand origin of enhanced breakdown rate, and find a mitigation
Could breakdowns be correlated with beam losses ?

## Slide 8: Working Hypothesis
Possible chain of events for current L4-RFQ (maybe too pessimistic):
L4-RFQ is designed for smaller beams from the source and Emax limit for no beam loss
RFQ is conditioned very fast to nominal voltage
Beam loss -> blistering
Blistering, degrade high gradient performance --> more breakdowns
More breakdowns, more blisters, -> more surface erosion
L4-RFQ is dead => ‘long live’ L4-RFQ2
Few years consumable
To break this chain two directions are proposed to be followed up within this WP:
Design an RFQ with 0% losses in high E-field area for given beam parameters using standard material and assembly: brazed OFE-Cu
Find alternative material which resists to blistering and is OK for RFQ fabrication. => Design RFQ with acceptable beam loss based on this material
RFQ operated with larger beams and suffered significant 25% beam loss

## Slide 9: Link 1
L4-RFQ is designed for smaller beams from the source and Emax limit for no beam loss
https://indico.cern.ch/event/754020/
The design transmission is 95%

## Slide 10: Link 2
RFQ is conditioned very fast to nominal voltage
Carlo Rossi
https://indico.cern.ch/event/754020/
410 kW => 78.3 kV => 34 MV/m
RFQ went up to 480 kW in 2 weeks!

## Slide 11: Link 3
RFQ operated with larger beams and suffered significant beam loss of 25%
Alessandra Lombardi Jean-Baptiste Lallement and Magdalena Kaja
10 march 2020
https://indico.cern.ch/event/895036/

## Slide 12: Link 4
1e19 H-
/ 2.5cm^2
= 4e18 H-/cm^2

## Slide 13: Links 5, 6
Blistering, degrade high gradient performance --> more breakdowns
This needs to be verified
More breakdowns, more blisters, -> more surface erosion
In order to characterize and understand the impact of the beam induced damage on the high gradient performance of the L4-RFQ it has been proposed to used high voltage DC breakdown test setup at CERN in combination with irradiation in the H- source test stand

## Slide 14: Connection between L4-RFQ and DC setup
Electric field distribution for V=1V
DC pulses, 500 ns to 100 µs, voltages up to 10 kV with gap range of 20 to 100 µm and repetition rate of up to 3 kHz.
78.3 kV => 34 MV/m

## Slide 15
Gap dependency
I. Profatilova

## Slide 16
In, https://indico.cern.ch/event/774570/
Walter suggested that this scaling might be relevant not only for DC gap systems abut also for RFQs
Voltage vs surface E-field scaling law in DC gaps

## Slide 17
Making one step further gives the connection: L4-RFQ <-> DC setup
V = 78.3 kV;
Es = 34 MV/m
d = V/Es
=>
Enorm = 1.05

## Slide 18: „Gap scaling“ for RFQs
d = V/Emax
where
V = max. measured inter-vane voltage Emax = max. measured surface field
VDC = 7747 V, dDC = 100 µm from DC experiment
Hermann Pommerenke
Kilpatrick limit: A CRITERION FOR VACUUM SPARKING DESIGNED TO INCLUDE BOTH R.F. AND D.C (escholarship.org)

## Slide 19: What about Sc and RF pulsed heating? (HF-RFQ)
Emax on vane tip (2.0 Kilpatrick)
small hotspot on inter-module gap
(2.2 Kilpatrick)
Es,max = 50 MV/m
Hmax on vane undercut edge resulting pulsed heating:
ΔT = 1.8 K (critical: 40K)
Sc maximum is not on vane, i.e. not in location of breakdowns
E & H are well-separated in RFQ
Sc maximum is located on undercut edge next to dipole rod
not critical either, scaled threshold at 20 us: 860 mW/um²
Hermann Pommerenke

## Slide 20: L4-RFQ: E-field and Sc (2D)
Sc [W/m^2] for V=1V
V | 1 V | 78.27 kV
E-field | 394 V/m | 30.8 MV/m
Sc | 0.66 W/m2 | 0.004 MW/mm2
Sc limit scaled to 200us: 4(200ns/200us)^1/3 = 0.4 MW/mm2
E-field [MV/m] for V=1V

## Slide 21: Summary on the high-power RF constraints for CLIC X-band RF structure design (2013)
RF breakdown and pulsed surface heating constraints used for CLIC_G design (2007):
Esmax < 250 MV/m
Pin/Cin·(tpP)1/3 = 18 MW·ns1/3/mm
dTmax(Hsmax, tp) < 56 K
Optimistic RF breakdown and pulsed surface heating constraints for BDR=10-6 bpp/m:
Esmax ·(tpP)1/6 < 250 MV/m · (200ns)1/6
Pin/Cin·(tpP)1/3 < 2.8 MW/mm · (200ns)1/3 = 17 [Wu]
Scmax ·(tpP)1/3 < 5 MW/mm2 · (200ns)1/3
and
dTmax(Hsmax, tp) < 50 K
Update on the analysis of the high-power test results (cern.ch)
20% margin
200 MV/m
4 MW/mm2
40 K
The high gradient X-band limits do not apply to RFQs

## Slide 22: Material study

## Slide 23: How to limit hydrogen bubble formation
Criteria for material choice I:
  Material strength larger than copper
  Reduced dislocation movement
  Presence of trapping centers for hydrogen to prevent coalescence
Criteria for material choice II:
  Hydrogen solution must be energetically favorable
  Hydrogen must have high diffusivity at room temperature
  Hydrogen solubility limit must be high
Selected material candidates:
  Cu-OFE (reference), CuCr1Zr, CuBe, Nb, -Ti-6Al-4V, Ta
  (electrical conductivity is not a primary concern for RFQ vanes)

## Slide 24: Irradiation
Anite Perez Fontenla

## Slide 25: Cu-OFE: H- source
Anite Perez Fontenla

## Slide 26: Nb: H- source
Anite Perez Fontenla

## Slide 27: CuCrZr: H- source
Anite Perez Fontenla

## Slide 28: Irradiation summary table
 | Materials | Dose [1E18p/cm^2] | Energy [keV/H] | Particle type | Angle of incidence [deg] | Blisters
Collimator test | OFE-Cu | 4 | 45 | H- | 90 | YES
L4-RFQ operation | Annealed OFE-Cu | 200 | 45 - 500 | H- | 10 - 90 | 
Electrode irradiation | Annealed OFE-Cu | 12 - 24 | 45 | H- | 90 | YES
Helsinki samples Batch #1 | OFE-Cu; CuCrZr; Nb; Ti6Al4V | 1, 4 | 45 | H2+ | 90 | YES: OFE-Cu; CuCrZr; NO: Nb; Ti6Al4V
Electrode irradiation | Nb | ~20 = 4.9p / 0.24cm^2 | 45 | H- | 90 | NO (no SEM yet)
Electrode irradiation | CuCrZr1 | ~20 = 9.8p / 0.44cm^2 ~40 = 9.8p / 0.22cm^2 (only central dark spot) | 45 | H- | 90 | YES

## Slide 29
Ruth Peacock

## Slide 30
Ruth Peacock
Cu-OFE

## Slide 31
Ruth Peacock
Cu-OFE

## Slide 32
Ruth Peacock

## Slide 33
Ruth Peacock

## Slide 34: Acknowledgements to people whose materials have been used
Sergio Calatroni
Anite Perez Fontenla
Alessandra Lombardi
Ruth Peacock
Hermann Pommerenke
Carlo Rossi
Walter Wuensch
Thank you !

## Slide 35: Spare slides

## Slide 36: Different exponents for gap term

## Slide 37: RFQs worldwide – Kilpatrick criterion
Kilpatrick criterion is used for most RFQ developments (common design choices CW-RFQ: <=1.8 Kp, pulsed RFQ: <=2.0 Kp)
but: during commissioning: more can often be achieved:
experiment
design
Hermann Pommerenke

## Slide 38: Cu-OFE: Helsinki

## Slide 39: Nb and Ti6Al4V: Helsinki

## Slide 40: CuCrZr: Helsinki