## Slide 1: MQXFA04 Coil Acceptance Review Introduction & Charge
Giorgio Ambrosio
Magnets L2
U.S. HL-LHC Accelerator Upgrade Project
MQXFA04 Coil Acceptance Review
October 30, 2019

## Slide 2: Review Goals
The HL-LHC AUP project is planning to start assembly of MQXFA04 magnet in November 2019. MQXFA04 is the second pre-series low-beta quadrupole (MQXFA) to be used in Q1 and Q3 for the High Luminosity LHC. If MQXFA04 meets MQXFA requirements [1] it will be used in the first Q1/Q3 cryo-assembly to be installed in the HL-LHC.
For MQXFA04 assembly AUP is planning to use QXFA coils 203, 112, 113 and 115. Coil 206 will be the spare coil. The reviewers are requested to assess that the 5 proposed coils and their conductor meet specifications [2], and to evaluate the impact of non-conformities in strands, cables and coils.
Acceptance Criteria Part A: MQXFA Magnet, US-HiLumi-doc-1103.
MQXFA Final Design Report, US-HiLumi-doc-948 sections 3 and 5.1.1;
and QXFA Coil Fabrication Electrical QA, US-HiLumi-doc-521 step 16.

## Slide 3: CHARGE Questions - I
The committee is requested to answer the following questions:
Do the proposed coils meet MQXFA coil specifications [2]?
Are conductor/coil fabrication and QC data of the proposed coils adequate for a thorough evaluation and for allowing MQXFA04 to meet MQXFA requirements [1]?
Are there major non-conformities? If answer is yes, have they been adequately documented and processed?
Do you have any other comment or recommendation regarding conductor or coils for allowing MQXFA04 to meet MQXFA requirements [1]?
Acceptance Criteria Part A: MQXFA Magnet, US-HiLumi-doc-1103.
MQXFA Final Design Report, US-HiLumi-doc-948 sections 3 and 5.1.1;
and QXFA Coil Fabrication Electrical QA, US-HiLumi-doc-521 step 16.

## Slide 4: Specifications at:
Strand: FDR pp. 9-10
Cable: FDR pp. 10-13
Coils dimensional: FDR pp. 68-69
Coils electrical: QXFA Coil Fabrication Electrical QA
All docs on review Indico page

## Slide 5: Coil Ordering
The use of coils with different conductor properties (RRR and Cu/NCu) may increase Coil-Ground voltages
Since CLIQ is introducing an asymmetric behavior, coil ordering may be used to compensate for different conductor properties
Therefore, starting from MQXFA03, AUP is checking peak Coil-Ground voltages for any possible coil ordering
  All options with peak voltage above spec will be forbidden
  Voltages of other options will be taken into account together with other data, when deciding coil ordering
 talk “Coil Ordering based on Conductor Properties”

## Slide 6: Quench Protection Simulations: Peak voltage to ground for MQXFB
For realistic* parameters, with up to two failures, and coil ordering
→ Worst-case: Ug<670 V at Inom, Ug<850 V at Iult
Ordering coils within a magnet is needed to keep peak voltages to ground within electrical design criteria
Nominal current (Inom=16.5 kA) |  |  | 
STEAM-LEDET sims MQXFB, 7.15 m | Reference parameters | Realistic* parameters uniformly distributed | Realistic* parameters not uniformly distributed
No failures | ≤615 | ≤636 | ≤927
2 QH failures | ≤641 | ≤657 | ≤920
1 CLIQ and 1 QH failures | ≤578 | ≤604 | ≤820
Ultimate current (Iult=17.8 kA) |  |  | 
STEAM-LEDET sims MQXFB, 7.15 m | Reference parameters | Realistic* parameters uniformly distributed | Realistic* parameters not uniformly distributed
2 QH failures | ≤816 | ≤846 | ≤1167
*Realistic conductor parameters by B. Bordini: Cu/noCu = 1.10-1.25; RRR = 150-250 indico.cern.ch/event/828604/contributions/3471761/ Re-assessment in progress |  |  | 
Initial hot-spot resistance neglected. All simulations run with STEAM-LEDET . Simulations cross-checked by V. Marinozzi (FNAL). |  |  | 
Original by E. Ravaioli
Note: MQXFA values are ~1.7 lower (ordering may not be needed)

## Slide 7: Field Quality
After FQ measurements of some short models and prototypes HL-LHC Working Package Leader (E. Todesco) requested a small design change to adjust b6
MQXFA03 is going to have 3 coils w/o correction (112, 113 and 203) and one coil w correction (206 or 115)
We expect a small impact and FQ within requirements
In any case we may do a re-assembly based on FQ measurements after coil-pads assembly
 talk “Expected Harmonics”

## Slide 8: Back up Slides

## Slide 9: US Contribution to HL-LHC Inner Triplets
10 Q1/Q3 Cryo-assemblies
  20 Magnets (MQXFA) with 4.2 m magnetic length
  Two magnets in each cold mass
Q2 cold masses by CERN
  Magnetic length: 7.15 m (MQXFB)
US cold mass
Magnet
(MQXFA)

## Slide 10: MQXFA/B Main Parameters
Parameter | Unit | MQXFA/B
Coil aperture | mm | 150
Magnetic length | m | 4.2/7.15
N. of layers |  | 2
N. of turns Inner-Outer layer |  | 22-28
Operation temperature | K | 1.9
Nominal gradient | T/m | 132.6
Nominal current | kA | 16.5
Peak field at nom. current | T | 11.4
Stored energy at nom. curr. | MJ/m | 1.2
Diff. inductance | mH/m | 8.2
Strand diameter | mm | 0.85
Strand number |  | 40
Cable width | mm | 18.15
Cable mid thickness | mm | 1.525
Keystone angle |  | 0.4
G. Ambrosio et al., “MQXFS1 Quadrupole Design Report” LARP DocDB 1074
P. Ferracin et al., “Development of MQXF, the Nb3Sn Low-β Quadrupole for the HiLumi LHC ” IEEE Trans App. Supercond. Vol. 26, no. 4, 4000207

## Slide 11: Acceptance Criteria for MQXFA Magnets
Acceptance Plan for Cryo-assembly has 3 parts with Acceptance Criteria:
Acceptance Criteria Part A for MQXFA magnets is approved by CERN
  EDMS# 2031083
  It contains the requirements
US-HiLumi-doc-1103

## Slide 12: Acceptance Criteria (with examples)
Based on Acceptance Plan for MQXB magnets (present IT quads at LHC)
Content: Requirements, Verification Method, Procedure summary and References,

## Slide 13: MQXFA Final Design Report
Final Design Report was reviewed by external team
FDR is on Review website
It contains Specifications for Strands, Cables and Coils
US-HiLumi-doc-948
Electronic signature on DocDB