## Slide 1: Magnets 302.2.02 and 03 – Strand Procurement and Testing Cable Fabrication
Lance Cooley – NHMFL/ASC (302.2.02 L3)
Vito Lombardo – FNAL (302.2.02 CAM)
Ian Pong – LBNL (302.2.03 L3 and CAM)

## Slide 2: Outline
Cable Summary
Wire Summary
Cable and Wire Details for Coil
  Date and Lengths
  Strand and SS Core ID
  Respooling Wire Diameter
  Cable Mechanical QC
  Braiding Details
  Wire Parameters
    Extracted Strand RRR and Witness IC and RRR
  SSL
Summary

## Slide 3: Cable Summary
Coils used:
  203, 206, 112, 113, 115 (spare)
Corresponding cables:
  P43OL1096, P43OL1103, P43OL1100, P43OL1094, P43OL1102 (spare)
All cables are 2nd generation QXF cables with 108/127 RRP® strands procured under LARP
4 AUP cables, 1 LARP cable

## Slide 4: Wire Summary
All “HiLumi” spec, procured by LARP under:
  FNAL 632982 B – Spec 0
  FNAL 632982 C – Spec 0
  FNAL 632982 D – Spec 0
0.85 mm, Ti-doped, reduced Sn
Procurement specification was US-HiLumi-Doc-40, modification to HT was applied to PO 632982, changing the final stage from 665°C for 75 h to 665°C for 50 h.
Total volume under FNAL PO 632982 is 400 km

## Slide 5: Billets in the LARP production run
Supplier is conservative by 2.1% after accounting for heat treatment
2.1% is comparable to the inter-lab test uncertainty (1.6 % in 2015) and past BNL-OST comparison (3% primarily due to strain).
331 A
314 A

## Slide 6
3-sigma (99.7%) SPC upper
3-sigma (0.3%) SPC lower
SPEC
X = verification test
Ic@12T
203
113
113
206
206
115
112

## Slide 7
3-sigma (99.7%) SPC upper
3-sigma (0.3%) SPC lower
SPEC
X = verification test
Ic@15T
203
112
113
113
206
206
115

## Slide 8
3-sigma (99.7%) SPC upper
3-sigma (0.3%) SPC lower
SPEC
X = verification test
RRR Round wire
203
112
113
113
206
206
115

## Slide 9
N-value at 15 T
3-sigma (99.7%) SPC upper
3-sigma (0.3%) SPC lower
SPEC
X = verification test
203
112
113
113
206
206
115

## Slide 10: Strand Procured by LARP and Supplier’s QC
A change of the heat treatment was approved in 2017  shift in data
Final step from 665C 75hr to 665C 50hr
  4.9% reduction in Ic(15 T) for 14.7% gain in RRR (15% rolled)
Verification testing did not receive HT change notice in time
Round
Rolled
331 A
314 A

## Slide 11: Billets in the LARP production run
PO624035
PO632982
A
B
C
D
AUP
Supplier is conservative by 2.1% after accounting for heat treatment
2.1% is comparable to the inter-lab test uncertainty (1.6 % in 2015) and past BNL-OST comparison (3% primarily due to strain).
Due to HT
Due to Test
Spec (round)
331 A
314 A
Spec (15% rolled)

## Slide 12: QXFA-203 / P43OL1096

## Slide 13: P43OL1096 – Cable Date, Lengths
Cable Manufacture Date
  2018 02 06 (Production run)
Cable Length:
  465 m (LBNL, fabricated, including LBNL samples)
  ### m (Measured by FNAL)

## Slide 14: P43OL1096 – Strand and SS Core ID
Spool:
  PO08S00182A03U x 8 ULs
  PO08S00183A04U x 10 ULs
  PO08S00183A03U x 7 ULs
  PO08S00182A01U x 4 ULs
  PO08S00217A06U x 3 ULs
  PO08S00217A07U x 3 ULs
  PO08S00182A04U x 2 ULs
  PO08S00179A03U x 1 ULs
  PO08S00217A02U x 1 ULs
  PO08S00217A04U x 1 ULs
Core:
  120L49A7322313
    Core width: 12.0 mm; material: 316L;
    Heat: 844979; Lot: 16-597;
    Chemical Properties CoT/CoC 172660-1: 0.14 wt% Co
From 4 billets

## Slide 15: P43OL1096 Respooling Wire Diameter
Below LSL: 0.01%
Above USL: 0.00%

## Slide 16: P43OL1096 – Cable QC Data Summary
CME:
Residual Twist:
  115°
10-stack:
  Qualification: 1.530 mm
  Production tail end: 1.525 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 17.1 | 0.455 | 18.158 | 1.530
Average | 17.0 | 0.434 | 18.144 | 1.524
Minimum | 17.0 | 0.412 | 18.139 | 1.519
Sigma | 0.01 | 0.007 | 0.003 | 0.002

## Slide 17
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 18
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 19
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 20: P43OL1096 – Braiding
Fiberglass Lot #91309 & 100104
P/I: 18.0
Spool tension: 10 lbs. (payoff); 12 lbs. (takeup)
Bobbin payoff tension: 0.125 lbs. (min), 0.250 lbs. (max)
NEWT 10-stack QC:
  Cycle #1) 0.149 mm; #2) 0.146 mm; #3) 0.144 mm;
  Mean 0.147 mm
LBNL 10-stack verification QC:
  Cycle #1) 0.153 mm; #2) 0.148 mm; #3) 0.147 mm;
  Mean 0.149 mm
Vector #464342

## Slide 21: P43OL1096 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.850 ± 0.001 mm (LBNL)1
Cu ratio a | 53.8% (OST)
Strand twist pitch a | 18.3 mm (OST)
RRR (RW) a | 315 (OST)
RRR (15% rolled) a | 236 (OST)
IC (4.2 K, 15 T) a | 370 A (OST)
IC (4.2 K, 14 T) a | 463 A (OST)
IC (4.2 K, 13 T) a | 570 A (OST)
IC (4.2 K, 12 T) a | 690 A (OST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received, all LBNL respooling data; mean ± 1 sigma

## Slide 22: P43OL1096 – Extracted Strand RRR
Vector #464342

## Slide 23: QXFA-CL-203 Cable P43OL1096
Tests of backup samples were required to fulfill witness sample testing requirements
  Unstable tests are shaded above
Witness extracted strand (XS)
Witness virgin strand (VS)

## Slide 24: Coil QXFA203, cable 1096 – Witness samples
ID | RRR (293K / 20K) XS > 100 RW > 150 | Ic(12T) XS > 600 RW > 632 | Ic(13T) | Ic(14T) | Ic(15T) XS > 314 RW > 331
PO08S00183A04U | 329 | 695Q | 577Q | 471Q | 380Q
PO08S00182A03U | 327 | 711Q | 608 | 501 | 405
P43OL1096AE42E | 317 | Q | Q | 398Q | 320Q
P43OL1096AE39E | 290 | 607Q | 542Q | 462 | 369
P43OL1096AE13E | 320 | 571Q | 502Q | 452Q | 366Q
P43OL1096AE33E | 325 | 694 | 578 | 478 | 384
nnnQ denotes a critical current measurement that showed a transition but quenched before the criterion was reached
Q denotes a critical current measurement that did not show a transition before quenching

## Slide 25: Coil 203 SSL
Margins | Margin | Operating Point (X)
Load line margin (purple arrow) | 27.3% | 72.8%
Current margin (green arrow) | 63.5% | 36.5%
Temperature margin [K] | 5.5 | 7.4

## Slide 26: QXFA-206 / P43OL1103

## Slide 27: P43OL1103 – Cable Date, Lengths
Cable Manufacture Date
  2018 05 29 (Production run)
Cable Length:
  470 m (LBNL, fabricated, including LBNL samples)
  ### m (Measured by FNAL)

## Slide 28: P43OL1103 – Strand and SS Core ID
Spool:
  PO08S00218A01U x 5 ULs
  PO08S00224A03U x 4 ULs
  PO08S00224A05U x 1 ULs
  PO08S00225A06U x 1 ULs
  PO08S00227A01U x 4 ULs
  PO08S00227A02U x 3 ULs
  PO08S00229A02U x 5 ULs
  PO08S00238A01U x 17 ULs
Core:
  120L42A7322313
    Core width: 12.0 mm; material: 316L;
    Heat: 844979; Lot: 16-597;
    Chemical Properties CoT/CoC 172660-1: 0.14 wt% Co
From 6 billets

## Slide 29: P43OL1103 Respooling Wire Diameter
Below LSL: 0.00%
Above USL: 0.00%

## Slide 30: P43OL1103 – Cable QC Data Summary
CME:
Residual Twist:
  120°
10-stack:
  Qualification: 1.527 mm
  Production tail end: 1.528 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 17.0 | 0.442 | 18.163 | 1.530
Average | 17.0 | 0.414 | 18.151 | 1.524
Minimum | 17.0 | 0.382 | 18.143 | 1.519
Sigma | 0.01 | 0.009 | 0.003 | 0.002

## Slide 31
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 32
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 33
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 34: P43OL1103 – Braiding
Fiberglass Lot #100415
P/I: 18.0
Spool tension: 10 lbs. (payoff); 20 lbs. (takeup)
Bobbin payoff tension: 0.125 lbs. (min), 0.250 lbs. (max)
NEWT 10-stack QC:
  Cycle #1) 0.149 mm; #2) 0.147 mm; #3) 0.145 mm;
  Mean 0.147 mm
LBNL 10-stack verification QC:
  Cycle #1) 0.145 mm; #2) 0.142 mm; #3) 0.140 mm;
  Mean 0.143 mm
Vector #464342

## Slide 35: P43OL1103 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.850 ± 0.001 mm (LBNL)1
Cu ratio a | 54.7% (OST)
Strand twist pitch a | 18.8 mm (OST)
RRR (RW) a | 242 (OST)
RRR (15% rolled) a | 147 (OST)
IC (4.2 K, 15 T) a | 375 A (OST)
IC (4.2 K, 14 T) a | 472 A (OST)
IC (4.2 K, 13 T) a | 581 A (OST)
IC (4.2 K, 12 T) a | 705 A (OST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received, all LBNL respooling data; mean ± 1 sigma

## Slide 36: P43OL1103 – Extracted Strand RRR
Vector #464342

## Slide 37: QXFA-CL-206 Cable P43OL1103
NO tests of backup samples were required to fulfill witness sample testing requirements
  Unstable tests are shaded above
Witness extracted strand (XS)
Witness virgin strand (VS)

## Slide 38: Coil QXFA206, cable 1103 – Witness samples
ID | RRR (293K / 20K) XS > 100 RW > 150 | Ic(12T) XS > 600 RW > 632 | Ic(13T) | Ic(14T) | Ic(15T) XS > 314 RW > 331
PO08S00238A01U | 286 | 646 | 518 | 415 | 326
PO08S00229A02U | 304 |  |  |  | 
P43OL1103AE29E | 236 |  |  |  | 
P43OL1103AE31E | 241 |  |  |  | 
P43OL1103AE47E | 204 | 693 | 573 | 477 | 387
P43OL1103AE53E | 217 | 687 | 569 | 464 | 369
nnnQ denotes a critical current measurement that showed a transition but quenched before the criterion was reached
Q denotes a critical current measurement that did not show a transition before quenching

## Slide 39: Coil 206 SSL
Margins | Margin | Operating Point (X)
Load line margin (purple arrow) | 26.2% | 73.9%
Current margin (green arrow) | 62.4% | 37.6%
Temperature margin [K] | 5.3 | 7.2

## Slide 40: QXFA-112 / P43OL1100

## Slide 41: P43OL1100 – Cable Date, Lengths
Cable Manufacture Date
  2018 03 30 (Production run)
Cable Length:
  464 m (LBNL, fabricated, including LBNL samples)
  449 m (Measured by FNAL)

## Slide 42: P43OL1100 – Strand and SS Core ID
Spool:
  PO08S00205A02U x 8 ULs
  PO08S00213A02U x 8 ULs
  PO08S00208A04U x 13 ULs
  PO08S00213A05U x 5 ULs
  PO08S00217A05U x 5 ULs
  PO08S00214A01U x 1 ULs
Core:
  120L45A7322313
    Core width: 12.0 mm; material: 316L;
    Heat: 844979; Lot: 16-597;
    Chemical Properties CoT/CoC 172660-1: 0.14 wt% Co
From 5 billets

## Slide 43: P43OL1100 Respooling Wire Diameter
Below LSL: 0.00%
Above USL: 0.05%

## Slide 44: P43OL1100 – Cable QC Data Summary
CME:
Residual Twist:
  109°
10-stack:
  Qualification: 1.536 mm
  Production tail end: 1.533 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 17.1 | 0.423 | 18.181 | 1.532
Average | 17.0 | 0.405 | 18.164 | 1.527
Minimum | 17.0 | 0.382 | 18.151 | 1.522
Sigma | 0.01 | 0.006 | 0.006 | 0.002

## Slide 45
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 46
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 47
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 48: P43OL1100 – Braiding
Fiberglass Lot #100415
P/I: 18.9
Spool tension: 10 lbs. (payoff); 12 lbs. (takeup)
Bobbin payoff tension: 0.125 lbs. (min), 0.250 lbs. (max)
NEWT 10-stack QC:
  Cycle #1) 0.150 mm; #2) 0.148 mm; #3) 0.146 mm;
  Mean 0.148 mm
LBNL 10-stack verification QC:
  Cycle #1) 0.148 mm; #2) 0.147 mm; #3) 0.143 mm;
  Mean 0.146 mm
Vector #464342

## Slide 49: P43OL1100 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.851 ± 0.001 mm (LBNL)1
Cu ratio a | 54.1% (OST)
Strand twist pitch a | 18.6 mm (OST)
RRR (RW) a | 318 (OST)
RRR (15% rolled) a | 214 (OST)
IC (4.2 K, 15 T) a | 371 A (OST)
IC (4.2 K, 14 T) a | 464 A (OST)
IC (4.2 K, 13 T) a | 569 A (OST)
IC (4.2 K, 12 T) a | 688 A (OST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received, all LBNL respooling data; mean ± 1 sigma

## Slide 50: P43OL1100 – Extracted Strand RRR
Vector #464342

## Slide 51: QXFA-CL-112 Cable P43OL1100
Tests of 1 backup sample was required to fulfill witness sample testing requirements
  Unstable tests are shaded above
Witness extracted strand (XS)
Witness virgin strand (VS)

## Slide 52: Coil QXFA112, cable 1100 – Witness samples
ID | RRR (293K / 20K) XS > 100 RW > 150 | Ic(12T) XS > 600 RW > 632 | Ic(13T) | Ic(14T) | Ic(15T) XS > 314 RW > 331
PO08S00213A02U | 230 |  |  |  | 
PO08S00208A04U | 228 | 711Q | 608 | 501 | 405
P43OL1100AE15E | 190 | 677 | 559 | 456 | 368
P43OL1100AE29E | 179 | 704 | 583 | 476 | 386
P43OL1100AE18E | 171 | 679 | 565 | 465 | 375
P43OL1100AE53E | 148 |  |  |  | 
nnnQ denotes a critical current measurement that showed a transition but quenched before the criterion was reached
Q denotes a critical current measurement that did not show a transition before quenching

## Slide 53: Coil 112 SSL
Margins | Margin | Operating Point (X)
Load line margin (purple arrow) | 25.4% | 74.6%
Current margin (green arrow) | 60.5% | 39.5%
Temperature margin [K] | 5.2 | 7.1

## Slide 54: QXFA-113 / P43OL1094

## Slide 55: P43OL1094 – Cable Date, Lengths
Cable Manufacture Date
  2018 01 18 (Production run)
Cable Length:
  466 m (LBNL, fabricated, including LBNL samples)
  444 m (Measured by FNAL)

## Slide 56: P43OL1094 – Strand and SS Core ID
Spool:
  PO08S00198A02U x 18 ULs
  PO08S00219A01U x 17 ULs
  PO08S00181A06U x 3 ULs
  PO08S00181A05U x 1 ULs
  PO08S00182A05U x 1 ULs
Core:
  120L51A7322313
    Core width: 12.0 mm; material: 316L;
    Heat: 844979; Lot: 16-597;
    Chemical Properties CoT/CoC 172660-1: 0.14 wt% Co
From 4 billets

## Slide 57: P43OL1094 Respooling Wire Diameter
Below LSL: 0.11%
Above USL: 4.27%

## Slide 58: P43OL1094 – Cable QC Data Summary
CME:
Residual Twist:
  95°
10-stack:
  Qualification: 1.532 mm
  Production tail end: 1.531 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 17.1 | 0.437 | 18.162 | 1.528
Average | 17.1 | 0.418 | 18.149 | 1.524
Minimum | 17.0 | 0.391 | 18.143 | 1.520
Sigma | 0.01 | 0.008 | 0.003 | 0.002

## Slide 59
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 60
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 61
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 62: P43OL1094 – Braiding
Fiberglass Lot #91309
P/I: 18.0
Spool tension: 10 lbs. (payoff); 12 lbs. (takeup)
Bobbin payoff tension: 0.125 lbs. (min), 0.250 lbs. (max)
NEWT 10-stack QC:
  Cycle #1) 0.151 mm; #2) 0.148 mm; #3) 0.147 mm;
  Mean 0.149 mm
LBNL 10-stack verification QC:
  Cycle #1) 0.148 mm; #2) 0.145 mm; #3) 0.143 mm;
  Mean 0.145 mm
Vector #464342

## Slide 63: P43OL1094 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.851 ± 0.003 mm (LBNL)1
Cu ratio a | 53.8% (OST)
Strand twist pitch a | 18.6 mm (OST)
RRR (RW) a | 322 (OST)
RRR (15% rolled) a | 225 (OST)
IC (4.2 K, 15 T) a | 369 A (OST)
IC (4.2 K, 14 T) a | 464 A (OST)
IC (4.2 K, 13 T) a | 571 A (OST)
IC (4.2 K, 12 T) a | 694 A (OST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received, all LBNL respooling data; mean ± 1 sigma

## Slide 64: P43OL1094 – Extracted Strand RRR
Vector #464342

## Slide 65: QXFA-CL-113 Cable P43OL1094
NO backup samples were required to fulfill witness sample testing requirements
  Unstable tests are shaded above
Witness extracted strand (XS)
Witness virgin strand (VS)

## Slide 66: Coil QXFA113, cable 1094 – Witness samples
ID | RRR (293K / 20K) XS > 100 RW > 150 | Ic(12T) XS > 600 RW > 632 | Ic(13T) | Ic(14T) | Ic(15T) XS > 314 RW > 331
PO08S00198A02U | 225 | 723 | 600 | 491 | 397
PO08S00219A01U | 228 |  |  |  | 
P43OL1094AE01E | 166 | 695 | 575 | 470 | 377
P43OL1094AE03E | 184 |  |  |  | 
P43OL1094AE29E | 162 | 721 | 598 | 489 | 394
P43OL1094AE30E | 185 |  |  |  | 
nnnQ denotes a critical current measurement that showed a transition but quenched before the criterion was reached
Q denotes a critical current measurement that did not show a transition before quenching

## Slide 67: Coil 113 SSL
Margins | Margin | Operating Point (X)
Load line margin (purple arrow) | 25.8% | 74.3%
Current margin (green arrow) | 61.1% | 38.9%
Temperature margin [K] | 5.3 | 7.2

## Slide 68: QXFA-115 / P43OL1102

## Slide 69: P43OL1102 – Cable Date, Lengths
Cable Manufacture Date
  2018 05 18 (Production run)
Cable Length:
  470 m (LBNL, fabricated, including LBNL samples)
  449 m (Measured by FNAL)

## Slide 70: P43OL1102 – Strand and SS Core ID
Spool:
  PO08S00239A05U x 2 ULs
  PO08S00220A04U x 3 ULs
  PO08S00230A04U x 3 ULs
  PO08S00239A03U x 3 ULs
  PO08S00235A01U x 12 ULs
  PO08S00237A01U x 17 ULs
Core:
  120L43A7322313
    Core width: 12.0 mm; material: 316L;
    Heat: 844979; Lot: 16-597;
    Chemical Properties CoT/CoC 172660-1: 0.14 wt% Co
From 5 billets

## Slide 71: P43OL1102 Respooling Wire Diameter
Below LSL: 0.00%
Above USL: 0.00%

## Slide 72: P43OL1102 – Cable QC Data Summary
CME:
Residual Twist:
  135°
10-stack:
  Qualification: 1.525 mm
  Production tail end: 1.528 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 17.1 | 0.451 | 18.169 | 1.530
Average | 17.0 | 0.425 | 18.153 | 1.526
Minimum | 16.9 | 0.395 | 18.145 | 1.522
Sigma | 0.01 | 0.009 | 0.004 | 0.001

## Slide 73
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 74
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 75
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 76: P43OL1102 – Braiding
Fiberglass Lot #100415
P/I: 18.9
Spool tension: 10 lbs. (payoff); 20 lbs. (takeup)
Bobbin payoff tension: 0.125 lbs. (min), 0.250 lbs. (max)
NEWT 10-stack QC:
  Cycle #1) 0.150 mm; #2) 0.147 mm; #3) 0.146 mm;
  Mean 0.148 mm
LBNL 10-stack verification QC:
  Cycle #1) 0.143 mm; #2) 0.140 mm; #3) 0.137 mm;
  Mean 0.140 mm
Vector #464342

## Slide 77: P43OL1102 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.850 ± 0.001 mm (LBNL)1
Cu ratio a | 55.1% (OST)
Strand twist pitch a | 18.6 mm (OST)
RRR (RW) a | 263 (OST)
RRR (15% rolled) a | 154 (OST)
IC (4.2 K, 15 T) a | 365 A (OST)
IC (4.2 K, 14 T) a | 459 A (OST)
IC (4.2 K, 13 T) a | 567 A (OST)
IC (4.2 K, 12 T) a | 690 A (OST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received, all LBNL respooling data; mean ± 1 sigma

## Slide 78: P43OL1102 – Extracted Strand RRR
Vector #464342

## Slide 79: QXFA-CL-115 Cable P43OL1102
NO tests of backup samples were required to fulfill witness sample testing requirements
  Unstable tests are shaded above
Witness extracted strand (XS)
Witness virgin strand (VS)

## Slide 80: Coil QXFA115, cable 1102 – Witness samples
ID | RRR (293K / 20K) XS > 100 RW > 150 | Ic(12T) XS > 600 RW > 632 | Ic(13T) | Ic(14T) | Ic(15T) XS > 314 RW > 331
PO08S00235A02U | 192 | 700 | 581 | 473 | 380
P43OL1102AE18E | 127 | 688 | 569 | 463 | 370
P43OL1102AE35E | 125 | 688 | 572 | 468 | 380
P43OL1102AE41E | 125 |  |  |  | 
P43OL1102AE59E | 104 |  |  |  | 
nnnQ denotes a critical current measurement that showed a transition but quenched before the criterion was reached
Q denotes a critical current measurement that did not show a transition before quenching

## Slide 81: Coil 115 SSL
Margins | Margin | Operating Point (X)
Load line margin (purple arrow) | 26.2% | 73.9%
Current margin (green arrow) | 62.4% | 37.6%
Temperature margin [K] | 5.3 | 7.2

## Slide 82: Summary of Data
Coil | SSL field (T) | SSL current (kA) | IOP/ISSL (%) | T margin (K) | Cable IC (kA) | IOP/IC (%)
MQXFA112 | 15.0 | 22.1 | 74.6 | 5.2 | 41.7 | 39.5
MQXFA113 | 15.1 | 22.2 | 74.3 | 5.3 | 42.3 | 38.9
MQXFA203 | 15.4 | 22.6 | 72.8 | 5.5 | 45.1 | 36.5
MQXFA206 | 15.2 | 22.3 | 73.9 | 5.3 | 43.8 | 37.6
MQXFA115 | 15.2 | 22.3 | 73.9 | 5.3 | 43.8 | 37.6