## Slide 1: QXFA112, QXFA113, and QXFA115 Review for Magnet MQXFA04
Fred Nobrega, CAM/L3
Miao Yu, Deputy L3
Marcellus Parker, Electrical
Coil Fabrication at FNAL
U.S. HL-LHC Accelerator Upgrade Project
MQXFA04 Coil Selection Review
October 30, 2019

## Slide 2: Outline
Coil Mechanical Measurements
  Coil Pole Gaps
  Cable & Coil Lengths
  Coil Reaction/Impregnation Plots
  Coil Size, CMM
Coil Electrical Results
  Hipot Results
  Impulse Test Results
  Electrical Measurements
Discrepancy Reports

## Slide 3: Pole Gaps
Chart: Coil #
| 112 | 113 | 115
Original Gap | 12.7 | 12.7 | 12.7
After Curing L1 | 12.08 | 11.58 | 10.96
After release tension | 8.42 | 7.11 | 6.96
Before Reaction | 7.56 | 5.45 | 5.63
After reaction | 1.83 | 1.92 | 1.207

## Slide 4: Cable & Coil Length
FDR Coil length = 4532 ± 3.5

## Slide 5: QXFA112 Reaction Plots
Driver issue

## Slide 6: QXFA113 Reaction Plots
Heater Zone Balance and
T/C calibration issue.

## Slide 7: QXFA115

## Slide 8: QXFA112 Coil Size, CMM
1540
270
327
740
2340
3140
3940
4323
4426
mm, from Coil LE

## Slide 9: QXFA113 Coil Size, CMM
1540
270
740
327
2340
3140
3940
4316
4426
mm, from Coil LE

## Slide 10: QXFA115 Coil Size, CMM (b6 shift)
1540
270
740
327
2340
3140
3940
4316
4426
mm, from Coil LE

## Slide 11: Final Hi-pot Tests

## Slide 12: QXFA112 Impulse Test
Chart: Impulse Test QXFA 112 - Outer to Inner
Chart: Impulse Test QXFA 112 - Inner to Outer

## Slide 13: QXFA113 Impulse Test
Chart: Impulse Test QXFA 113 - Inner to Outer
Chart: Impulse Test QXFA 113 - Outer to Inner

## Slide 14: QXFA115 Impulse Test
Chart: Impulse Test QXFA 115 - Outer to Inner
Chart: Impulse Test QXFA 115 - Inner to Outer

## Slide 15: Final Electrical Checks
Measurement | QXFA112 | QXFA113 | QXFA 115* |  | Avg | StDev | StDev/Avg | Min | Max
Coil R @1 A (mV) | 609.3 | 606.12 | 613.07 |  | 608.655 | 11.18489334 | 0.01837641 | 589 | 639.7
Ls @ 20 Hz (mH) | 4.56 | 4.914 | 6.29 |  | 4.89430769 | 1.372540507 | 0.28043609 | 4.56 | 6.29
Q | 0.73 | 0.801 | 1.28 |  | 0.99753846 | 0.686510971 | 0.68820501 | 0.73 | 3.146
Ls @ 100 Hz (mH) | 3.17 | 3.423 | 6.24 |  | 3.39614286 | 0.905308545 | 0.26656963 | 1.86 | 6.24
Q | 1.61 | 1.637 | 5.44 |  | 1.88942857 | 1.02169101 | 0.54074074 | 1.52 | 5.44
Ls @ 1 kHz (mH) | 1.91 | 1.92 | 5.75 |  | 2.15607143 | 1.031657402 | 0.47848944 | 1.812 | 5.75
Q | 2.15 | 2.007 | 8.41 |  | 2.48228571 | 1.70309985 | 0.68610146 | 1.86 | 8.41
VTA1 (mV) | 0.0233 | 0.04 | 0.1 |  | 0.09985833 | 0.094520768 | 0.94654863 | 0.008 | 0.3
VTA2 | 0.072 | 0.09 | 0.1 |  | 0.14691667 | 0.099653117 | 0.67829689 | 0.055 | 0.35
VTA3 | 195.622 | 196.12 | 205.62 |  | 196.280167 | 3.662416174 | 0.01865913 | 190.21 | 205.62
VTA4 | 254.833 | 255.91 | 266.43 |  | 255.52025 | 4.455349269 | 0.01743638 | 247.79 | 266.43
VTA5 | 255.098 | 255.7 | 266.64 |  | 255.720667 | 4.439629498 | 0.01736125 | 248.02 | 266.64
VTA6 | 260.827 | 261.44 | 272.5 |  | 261.350583 | 4.546806317 | 0.01739735 | 253.58 | 272.5
VTA7 | 260.97 | 261.45 | 272.7 |  | 261.536667 | 4.53983671 | 0.01735832 | 253.74 | 272.7
VTA8 | 266.271 | 266.89 | 278.1 |  | 266.85675 | 4.602241558 | 0.01724611 | 258.86 | 278.1
VTB8 | 266.81 | 267.3 | 278.5 |  | 267.348333 | 4.595306085 | 0.01718846 | 259.29 | 278.5
VTB7 | 266.919 | 267.64 | 278.7 |  | 267.576583 | 4.595637088 | 0.01717503 | 259.52 | 278.7
VTB6 | 272.248 | 273.13 | 284.3 |  | 272.9315 | 4.735065814 | 0.01734892 | 264.94 | 284.3
VTB5 | 272.81 | 273.46 | 284.7 |  | 273.2775 | 4.765522874 | 0.0174384 | 265.27 | 284.7
VTB4 | 278.378 | 279.72 | 290.3 |  | 279.113167 | 4.696444092 | 0.01682631 | 270.67 | 290.3
VTB3 | 421.24 | 422.17 | 436.8 |  | 421.775 | 6.647560666 | 0.01576092 | 409.36 | 436.8
VTB2 | 606.05 | 593.7 | 629.8 |  | 605.8425 | 10.41682039 | 0.01719394 | 589.08 | 629.8
VTB1 | 606.1 | 607.82 | 629.8 |  | 606.700909 | 9.776191352 | 0.01611369 | 589.13 | 629.8
QHB1 | 1.96 | 1.855 | 2.07 |  | 1.89664286 | 0.141004973 | 0.0743445 | 1.61 | 2.08
QHB2 | 1.94 | 1.869 | 2.1 |  | 1.91785714 | 0.132417977 | 0.06904476 | 1.65 | 2.1
QHB3 | 1.96 | 1.878 | 2.07 |  | 1.92414286 | 0.128815909 | 0.06694716 | 1.62 | 2.08
QHB4 | 1.94 | 1.865 | 2.03 |  | 1.89935714 | 0.126214198 | 0.06645101 | 1.61 | 2.05
* b6 shift

## Slide 16: QXFA112 Discrepancy Reports
DR Number | Document | DR Status
11605 | QXFA Coil Winding and Curing Traveler, cable insulation damage from vendor repaired. | Closed
11662 | QXFA Splice / Epoxy Impregnation Traveler, wedge insulation flaked off after reaction and repaired. | Closed
11680 | QXFA Splice / Epoxy Impregnation Traveler, peristaltic pump error, reset with power cycle. | Closed
11689 | QXFA Splice / Epoxy Impregnation Traveler, epoxy flash removal at midplane repaired. | Closed

## Slide 17: QXFA113 Discrepancy Reports
DR Number | Document | DR Status
11649 | Preparation for Coil Winding and Curing Traveler, black marks and popped strands, repaired. | Closed
11660 | QXFA Coil Winding and Curing Traveler, cable insulation damage from vendor, repaired. | Closed
11681 | QXFA Reaction Traveler, Kapton found between turns before reaction and removed. | Closed
11682 | QXFA Reaction Traveler, technician concern regarding fit of the shell. Assembly inspected and no issues found. | Closed
11695 | QXFA Splice / Epoxy Impregnation Traveler, wedge insulation separation after reaction, repaired. | Closed
11696 | QXFA Splice / Epoxy Impregnation Traveler, chipped plasma coating after reaction, repaired. | Closed
11711 | QXFA Splice / Epoxy Impregnation Traveler, epoxy hose damaged from clamp overtightening, repaired. | Closed
11718 | QXFA Splice / Epoxy Impregnation Traveler, a portion of a modified L1 QH trace included a sliver of copper. No action taken. | Closed

## Slide 18: QXFA113, DR11718

## Slide 19: QXFA115 Discrepancy Reports
DR Number | Document | DR Status
11730 | QXFA Coil Winding and Curing Traveler, one layer of the multilayer pole tape frayed during installation due to tech error, repaired. | Closed
11753 | QXFA Reaction Traveler, after L2 coil curing, L1 pole insulation moved out of position, repaired. | Closed
11770 | QXFA Splice / Epoxy Impregnation Traveler, wedge bare spot after reaction, repaired. | Closed
11791 | QXFA Splice / Epoxy Impregnation Traveler, 1 mil SS strip used as a lead for QH trace electrical measurements tore. Torn piece removed at later step. | Closed
11793 | Electrical Testing Traveler, electrical measurements skipped due to late trace. Measurements taken at a later step. | Closed
11858 | Splice / Epoxy Impregnation Traveler, small nonmetallic foreign object potted above S2 glass. | Closed
11869 | QXFA Splice / Epoxy Impregnation Traveler, CMM bumps on coil, S2 glass delamination. | Closed

## Slide 20: QXFA115, DR11770
Near return end of coil, 3.87 m from LE.

## Slide 21: QXFA115, DR11770
Cause of Nonconformance:
  Clear cause is unknown. Possible cause is a high-pressure seam between 2 form blocks #78 & #79. The contact between these 2 form blocks coincides with the tear in glass and the missing insulation on the L2 wedges on both sides.
Disposition:
  Repair the wedge insulation using GE varnish diluted with acetone.
  Swap reaction form blocks #78 & #79 with form blocks #1 & #2 for the next reaction cycle.
  Etch affected form blocks with revised position numbers.
  Add a reminder in the next traveler (QXFA116) to inspect position at for blocks #78/79 (152.5" from LE)to see if swapping blocks made an improvement.
QXFA116

## Slide 22: QXFA115, DR11858
Cause of Nonconformance:
  Unidentified foreign object, nonmetallic in appearance, surrounded by epoxy above the S2 glass. Not known how it got there, but timing wise it occurred after the installation of the S2 glass and before or during the installation of the mold released Mylar.

## Slide 23: Addition Information

## Slide 24: MQXFA Coil CMM Profile Measurement Locations

## Slide 25
Zone and Thermocouple explanation
= K Thermocouple (Controlling)
= Over-temperature Thermocouple
Purple numbers= Thermocouple label
Green text= Zone label
TC= Abbreviation for thermocouple
Each thermocouple controls the zone that they are labeled. For example, TC 1 controls zone 1, TC 2 controls zone 2, etc.
The one over-temperature thermocouple is not assigned a number nor a zone because it monitors the entire furnace for overheating.
TC 7 controls zone 7, which is located at the top back and top door of the furnace
TC 8 controls zone 8, which is located at the bottom back and bottom door of the furnace.
Since the top back and top door sections of the furnace are very similar, such that they do very little to heat up the furnace, zone 7 covers two areas of the furnace while only being controlled by TC 7. The same applies for the bottom back and bottom door, being controlled by TC 8.
7
8
1
2
3
5
6
4
Zone 1
Zone 3
Zone 4
Zone 5
Zone 6
Zone 2
Zone 7
Zone 7
Zone 8
Zone 8
Zones 1 & 2 use 18,913.3 Watts
Zones 3 & 4 use 28,640 Watts
Zones 5 & 6 use 9,546.7 Watts
Zones 7 & 8 use 5,220 Watts