## Slide 1: Magnet Fabrication Travelers, Non-Conformities and Resolution
Katherine Ray – LBNL (QA)
Mike Solis – LBNL (Procurement Technical Contact)
December 12, 2019 – MQXFA04 Structure and Loading Review

## Slide 2: Overview
State of the Magnet Fabrication Travelers
Part Inspection Plan
Non-Conformances on MQXFA04

## Slide 3: Magnet Fabrication Travelers Overview
# | Title | Revision | ID
1 | Coil Acceptance WI | A | SU-1011-5294
2 | Yoke Pre-Stack WI | B | SU-1008-8072
3 | Yoke Half Stack WI | C | SU-1009-7829
4 | Shell Instrumentation WI | C | SU-1009-3745
5 | Shell-Yoke Assy WI | B | SU-1008-2169
6 | Loadpad Pre-Stack WI | B | SU-1008-8075
7 | Dressed Coil WI | D | SU-1008-8073
8 | Pad-Collar Assy WI | A | SU-1010-1610
9 | Coil Pack Subassy WI | B | SU-1008-8074
10 | Magnet Electrical QA at LBNL | C | SU-1010-1903
11 | Magnetic Measurements | Not released | SU-1010-2018
12 | Integration and Loading WI (based on 2 other WI, both @ Rev B) | Not released | SU-1011-5294
13 | Axial Rods Instrumented WI | B | SU-1008-8069
14 | Splice Box WI | A | SU-1008-8067
15 | Magnet Shipping WI | A | SU-1011-3284

## Slide 4: Magnet Fabrication Travelers Overview
# | Title | Revision | ID
1 | Coil Acceptance WI | A | SU-1011-5294
2 | Yoke Pre-Stack WI | B | SU-1008-8072
3 | Yoke Half Stack WI | C | SU-1009-7829
4 | Shell Instrumentation WI | C | SU-1009-3745
5 | Shell-Yoke Assy WI | B | SU-1008-2169
6 | Loadpad Pre-Stack WI | B | SU-1008-8075
7 | Dressed Coil WI | D | SU-1008-8073
8 | Pad-Collar Assy WI | A | SU-1010-1610
9 | Coil Pack Subassy WI | B | SU-1008-8074
10 | Magnet Electrical QA at LBNL | C | SU-1010-1903
11 | Magnetic Measurements | Not released | SU-1010-2018
12 | Integration and Loading WI (based on 2 other WI, both @ Rev B) | Not released | SU-1011-5294
13 | Axial Rods Instrumented WI | B | SU-1008-8069
14 | Splice Box WI | A | SU-1008-8067
15 | Magnet Shipping WI | A | SU-1011-3284
Lessons Learned from A03 have been integrated into the first 10 travelers.
We are working on the next 5 travelers now.

## Slide 5: Part Inspection Plans
Our overall inspection plan is set out in the Advanced Acquisition Plan (docDB #962)
Includes first article inspection, 10% inspection of yokes/loadpads/collars, inspection at LBNL

## Slide 6: Shell Inspection Plans
100% of shells are inspected both at the vendor and at LBNL
Fluourescent (Dye) Penetrant Inspection (FPI) required
Ultrasonic inspection to class AA required

## Slide 7: Change Records
We are tracking Non-Conformances, Deviations and Engineering Changes in one spreadsheet
These are currently communicated to Fermilab L2 on a monthly basis

## Slide 8: MQXFA04 Change Records
The NCRs on A04 thus far include:
  (#28) Ultrasonic testing to grade A instead of AA for 3 long shells
  (#29) Wrong serial number on 2 collars
  (#31) Coil 113 had a short (retested and passed)
  (#49, 59) Coil 206 shifted during shipment, then saw a bubble under the GPI (passed electrical tests)
  (#50) 203 and 113 were hipoted to 4600V instead of 3680V
  (#53) Short shell -003 had a 0.006” deep, ¼” long gouge in it
  (#58) Shell strain gauges wires were swapped (wrong length)

## Slide 9: MQXFA04 Change Records
The NCRs on A04 thus far include:
  (#28) Ultrasonic testing to grade A instead of AA for 3 long shells
  (#29) Wrong serial number on 2 collars
  (#31) Coil 113 had a short (retested and passed)
  (#49, 59) Coil 206 shifted during shipment, then saw a bubble under the GPI (passed electrical tests)
  (#50) 203 and 113 were hipoted to 4600V instead of 3680V
  (#53) Short shell -003 had a 0.006” deep, ¼” long gouge in it
  (#58) Shell strain gauges wires were swapped (wrong length)
Discussed during Coil Selection
Rewired
Indico Pages:
https://indico.fnal.gov/event/22009/
https://indico.fnal.gov/event/22526/
https://indico.fnal.gov/event/22659/

## Slide 10: NCR-0028, Ultrasonic testing to Grade A
Ultrasonic testing was only performed to Grade A, not AA (3mm flaw, not 2mm)
Performed analysis available in Tech Note SU-1011-4084
Analysis showed the shells still meet the design criteria
Approved by L2
Have communicated with vendor so that future shells will be tested to Grade AA

## Slide 11: NCR-0053, Gouge in Shell
The 0.006” x 0.125” x 0.25” gouge was modeled.
Analysis available in Tech Note SU-1011-5149
The stress on the shell is not significantly impacted by the gouge, and the shell was accepted at the L2 level

## Slide 12: Summary
The travelers continue to be updated with Lessons Learned from the A03 magnet
We are following a part inspection plan that includes full inspection of the shells and 10% inspection of the laminations
There were 2 possible issues with the A04 shells which were analyzed and determined to be acceptable