## Slide 1: Magnets 302.2.02 and 03 – Strand Procurement and Testing Cable Fabrication
Lance Cooley – NHMFL/ASC (302.2.02 L3)
Vito Lombardo – FNAL (302.2.02 CAM)
Ian Pong – LBNL (302.2.03 L3 and CAM)
Jonathan Lee – LBNL Intern Student

## Slide 2: Outline
Cable Summary
Wire Summary
Cable and Wire Details for Coil -- x4 times
  Summary
  Date and Lengths
  Strand and SS Core ID
  Respooling Wire Diameter
  Cable Mechanical QC
  Braiding Details
  Wire Parameters
    S & V QC data, XS RRR and Witness IC and RRR
  SSL
Summary

## Slide 3: Cable Summary
Coil | Cable | Strand | Spec.
QXFA116 | P43OL1105 | 0.85 mm 108/127 | HiLumi (2017)
QXFA117 | P43OL1107 | 0.85 mm 108/127 | HiLumi (2017)
QXFA207 | P43OL1106 | 0.85 mm 108/127 | HiLumi (2017)
QXFA209 | P43OL1114 | 0.85 mm 108/127 | HiLumi (2017)
QXFA115 | P43OL1102 | 0.85 mm 108/127 | HiLumi (2017)
PxxOLnnnn is the cable ID:
  “xx” is the project and strand type
    30 series = QXF gen 1 with annealed strands; 40 series = QXF gen 2 with annealed strands;
    Odd = cored cable; x3, x5, x7 determines strand type
  “nnnn” is the cable map number
QXFA 209 made with strand exchanged from CERN
QXFA 116 backup sample needed to pass supplier QC (spool PO08S00216A02U)

## Slide 4: Cable Summary
Coils used:
  116, 117, 207, 209 (spare: 115, presented previously and approved for MQXFA04)
Corresponding cables:
  P43OL1105, P43OL1107, P43OL1106, P43OL1114
All cables are 2nd generation QXF cables with 108/127 RRP® strands procured under LARP
All AUP cables

## Slide 5: Wire Summary
All “HiLumi” spec, these are spools manufactured after 2017 CERN-LARP spec review
  Procured by LARP under:
    FNAL 632982 C – Spec 0 (coils 116, 117)
    FNAL 632982 D – Spec 0 (coils 116, 117, 207)
  Procured by CERN under:
    CERN Contract F663 Ship F and Ship G (coil 209)
0.85 mm, Ti-doped, reduced Sn
LARP procurement spec was US-HiLumi-Doc-40, modification to HT was applied to PO 632982, changing the final stage from 665°C for 75 h to 665°C for 50 h.
  Purpose: protect 15% rolled RRR in exchange for minimal trade-back of critical current (this will be evident for coil 209)
  Coil HT has always been 665 °C / 50 h per Doc 109
CERN procurement spec HT for Ship F and Ship G was 665°C for 75 h – so, IC higher but RRR lower

## Slide 6: Billets in the LARP production run
Supplier is conservative by 2.1% after accounting for heat treatment
2.1% is comparable to the inter-lab test uncertainty (1.6 % in 2015) and past BNL-OST comparison (3% primarily due to strain).
331 A
314 A

## Slide 7: Strand Procured by LARP and Supplier’s QC
A change of the heat treatment was approved in 2017  shift in data
Final step from 665C 75hr to 665C 50hr
  4.9% reduction in Ic(15 T) for 14.7% gain in RRR (15% rolled)
Verification testing did not receive HT change notice in time
Round
Rolled
331 A
314 A

## Slide 8: Billets in the LARP production run
PO624035
PO632982
A
B
C
D
AUP
Supplier is conservative by 2.1% after accounting for heat treatment
2.1% is comparable to the inter-lab test uncertainty (1.6 % in 2015) and past BNL-OST comparison (3% primarily due to strain).
Due to HT
Due to Test
Spec (round)
331 A
314 A
Spec (15% rolled)

## Slide 9
3-sigma (99.7%) SPC upper
3-sigma (0.3%) SPC lower
SPEC
X = verification test
Ic@12T
207
117
116
115
AUP
LARP
116
117
209

## Slide 10
3-sigma (99.7%) SPC upper
3-sigma (0.3%) SPC lower
SPEC
X = verification test
Ic@15T
207
117
116
115
AUP
LARP
116
117
209

## Slide 11
3-sigma (99.7%) SPC upper
3-sigma (0.3%) SPC lower
SPEC
X = verification test
RRR Round wire
207
117
116
115
AUP
LARP
116
117
209

## Slide 12
N-value at 15 T
3-sigma (99.7%) SPC upper
3-sigma (0.3%) SPC lower
SPEC
X = verification test
207
117
116
115
AUP
LARP
116
117
209

## Slide 13: QXFA-116 / P43OL1105

## Slide 14: Cable Summary
Magnet: MQXFA-05
Coil: QXFA-116
Corresponding Cable: P43OL1105 (AUP 010)
Cable is 2nd generation QXF cables with 108/127 RRP® strands procured under LARP

## Slide 15: Wire Summary
All “HiLumi” spec, procured by LARP under:
  FNAL 632982 C – Spec 0 (33 ULs)
  FNAL 632982 D – Spec 0 (7 ULs)
0.85 mm, Ti-doped, reduced Sn

## Slide 16: P43OL1105 – Cable Date, Lengths
Cable Manufacture Date
  2019 01 29 (Production run)
Cable Length:
  484 m (LBNL, fabricated, including LBNL samples)
  468 m (shipped to NEWT, including S & V samples)
  462.9 m (Measured by FNAL)

## Slide 17: P43OL1105 – Strand and SS Core ID
Spool:
  PO08S00209A03U x 9 ULs
  PO08S00204A02U x 7 ULs
  PO08S00204A01U x 8 ULs
  PO08S00216A02U x 9 ULs
  PO08S00231A03U x 7 ULs
Core:
  120L41A7322313
    Core width: 12.0 mm; material: 316L;
    Heat: 844979; Lot: 16-597;
    Chemical Properties CoT/CoC 172660-1: 0.14 wt% Co
From 5 billets

## Slide 18: P43OL1105 Respooling Wire Diameter
Below LSL: 0.00%
Above USL: 0.02%

## Slide 19: P43OL1105 – Cable QC Data Summary
CME:
Residual Twist:
  115°
10-stack:
  Qualification: 1.534 mm
  Production tail end: 1.531 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 17.1 | 0.445 | 18.165 | 1.533
Average | 17.0 | 0.425 | 18.151 | 1.529
Minimum | 16.9 | 0.399 | 18.145 | 1.525
Sigma | 0.02 | 0.008 | 0.002 | 0.001

## Slide 20
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 21
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 22
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 23: P43OL1105 – Braiding
Fiberglass Lot #100415
P/I: 18.0
Spool tension: 10 lbs. (payoff); 20 lbs. (takeup)
Bobbin payoff tension: 0.125 lbs. (min), 0.250 lbs. (max)
NEWT 10-stack QC:
  Cycle #1) 0.149 mm; #2) 0.145 mm; #3) 0.142 mm;
  Mean 0.145 mm
LBNL 10-stack verification QC:
  Cycle #1) 0.147 mm; #2) 0.143 mm; #3) 0.141 mm;
  Mean 0.143 mm
Vector #464342

## Slide 24: P43OL1105 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.850 ± 0.0008 mm (LBNL)1
Cu ratio a | 54.3% (OST)
Strand twist pitch a | 18.1 mm (OST)
RRR (RW) a | 324 (OST)
RRR (15% rolled) a | 217 (OST)
IC (4.2 K, 15 T) a | 367 A (OST)
IC (4.2 K, 14 T) a | 459 A (OST)
IC (4.2 K, 13 T) a | 564 A (OST)
IC (4.2 K, 12 T) a | 683 A (OST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received, all LBNL respooling data; mean ± 1 sigma

## Slide 25: P43OL1105 – Wire Parameters Supplier (S) and Verification (V) IC Data
Number of spools from that billet used in the cable

## Slide 26: P43OL1105 – Wire Parameters Supplier (S) and Verification (V) RRR Data
Number of spools from that billet used in the cable

## Slide 27: P43OL1105 – Extracted Strand RRR
 | Cable ID | No. of Units from Billet (spool) | HT/sample ID | Major edge RRR | Minor edge RRR | Straight section 1 RRR | Straight section 2 RRR
ID #1 | P43OL1105AE01E PO08S00209A03U | 9 (9) | LRLK180613ALC1 | 416 | 401 | 423 | 440
ID #2 | P43OL1105AE06E PO08S00209A03U | 9 (9) | LRLK180613ALC1 | 362 | 307 | 455 | 457
ID #3 | P43OL1105AE27E PO08S00204A01U | 8 (15) | LRLK180613ALC1 | 356 | 331 | 443 | 420
ID #4 | P43OL1105AE33E PO08S00204A01U | 8 (15) | LRLK180613ALC1 | 426 | 318 | 434 | 454
ID #5 | P43OL1105AE43E PO08S00216A02U | 9 (9) | LRLK180613ALC1 | 357 | 324 | 458 | 457
Vector #464342

## Slide 28: P43OL1105 – Witness Samples
RRR extracted strand
Witness extracted strand (XS)
Witness virgin strand (VS)
All tests succeeded

## Slide 29: P43OL1105 – Witness Samples
ID | RRR (293K / 20K) XS > 100 RW > 150 | Ic(12T) XS > 600 RW > 632 | Ic(13T) | Ic(14T) | Ic(15T) XS > 314 RW > 331
PO08S00216A02U | 234 |  |  |  | 
PO08S00209A03U | 312 | 719 | 600 | 493 | 397
P43OL1105AE01E | 189 | 671 | 555 | 449 | 357
P43OL1105AE11E | 285 | 682 | 568 | 466 | 377
P43OL1105AE37E | 265 |  |  |  | 
P43OL1105AE48E | 196 |  |  |  | 
nnnQ denotes a critical current measurement that showed a transition but quenched before the criterion was reached
Q denotes a critical current measurement that did not show a transition before quenching

## Slide 30
Margins | Margin | Operating Point (X)
Load line margin (purple arrow) | 25.1% | 74.9%
Current margin (green arrow) | 60.7% | 39.3%
Temperature margin [K] | 5.2 | 7.1

## Slide 31: QXFA-117 / P43OL1107

## Slide 32: Cable Summary
Magnet: MQXFA-05
Coil: QXFA-117
Corresponding Cable: P43OL1107 (AUP 012)
Cable is 2nd generation QXF cables with 108/127 RRP® strands procured under LARP

## Slide 33: Wire Summary
All “HiLumi” spec, procured by LARP under:
  FNAL 632982 C – Spec 0 (26 ULs)
  FNAL 632982 D – Spec 0 (14 ULs)
0.85 mm, Ti-doped, reduced Sn

## Slide 34: P43OL1107 – Cable Date, Lengths
Cable Manufacture Date
  2018 07 05 (Production run)
Cable Length:
  467 m (LBNL, fabricated, including LBNL samples)
  455 m (shipped to NEWT, including S & V samples)
  451.6 m (Measured by FNAL)

## Slide 35: P43OL1107 – Strand and SS Core ID
Spool:
  PO08S00206A02U x 4 ULs
  PO08S00189A02U x 4 ULs
  PO08S00209A04U x 6 ULs
  PO08S00211A02U x 6 ULs
  PO08S00227A04U x 6 ULs
  PO08S00211A01U x 6 ULs
  PO08S00223A01U x 8 ULs
Core:
  120L39A7322313
    Core width: 12.0 mm; material: 316L;
    Heat: 844979; Lot: 16-597;
    Chemical Properties CoT/CoC 172660-1: 0.14 wt% Co
From 6 billets

## Slide 36: P43OL1107 Respooling Wire Diameter
Below LSL: 0.00%
Above USL: 0.22%

## Slide 37: P43OL1107 – Cable QC Data Summary
CME:
Residual Twist:
  145°
10-stack:
  Qualification: 1.534 mm
  Production tail end: 1.530 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 17.0 | 0.467 | 18.164 | 1.535
Average | 17.0 | 0.441 | 18.152 | 1.529
Minimum | 17.0 | 0.413 | 18.142 | 1.524
Sigma | 0.01 | 0.010 | 0.003 | 0.002

## Slide 38
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 39
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 40
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 41: P43OL1107 – Braiding
Fiberglass Lot #100415
P/I: 18.0
Spool tension: 10 lbs. (payoff); 20 lbs. (takeup)
Bobbin payoff tension: 0.125 lbs. (min), 0.250 lbs. (max)
NEWT 10-stack QC:
  Cycle #1) 0.149 mm; #2) 0.146 mm; #3) 0.145 mm;
  Mean 0.147 mm
LBNL 10-stack verification QC:
  Cycle #1) 0.142 mm; #2) 0.141 mm; #3) 0.139 mm;
  Mean 0.140 mm
Vector #464342
LBNL boat subsequently found to have possibly misaligned
CAPA: hardware record to include realignment

## Slide 42: P43OL1107 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.850 ± 0.0009 mm (LBNL)1
Cu ratio a | 54.3% (OST)
Strand twist pitch a | 18.4 mm (OST)
RRR (RW) a | 286 (OST)
RRR (15% rolled) a | 188 (OST)
IC (4.2 K, 15 T) a | 372 A (OST)
IC (4.2 K, 14 T) a | 466 A (OST)
IC (4.2 K, 13 T) a | 572 A (OST)
IC (4.2 K, 12 T) a | 693 A (OST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received, all LBNL respooling data; mean ± 1 sigma

## Slide 43: P43OL1107 – Wire Parameters Supplier (S) and Verification (V) IC Data
Number of spools from that billet used in the cable

## Slide 44: P43OL1107 – Wire Parameters Supplier (S) and Verification (V) RRR Data
Number of spools from that billet used in the cable

## Slide 45: P43OL1107 – Extracted Strand RRR
 | Cable ID | No. of Units from Billet (spool) | HT/sample ID | Major edge RRR | Minor edge RRR | Straight section 1 RRR | Straight section 2 RRR
ID #1 | P43OL1107AE33E PO08S00227A04U | 6 (6) | LRLK180717ALC1 | 282 | 216 | 343 | 303
ID #2 | P43OL1107AE37E PO08S00227A04U | 6 (6) | LRLK180717ALC1 | 293 | 231 | 338 | 331
ID #3 | P43OL1107AE15E PO08S00209A04U | 6 (6) | LRLK180717ALC1 | 390 | 324 | 398 | 402
ID #4 | P43OL1107AE49E PO08S00223A01U | 8 (8) | LRLK180717ALC2 | 287 | 214 | 372 | 335
ID #5 | P43OL1107AE54E PO08S00223A01U | 8 (8) | LRLK180717ALC2 | 286 | 164 | 315 | 278
Vector #464342

## Slide 46: P43OL1107 – Witness Samples
Witness extracted strand (XS)
Witness virgin strand (VS)

## Slide 47: P43OL1107 – Witness Samples
ID | RRR (293K / 20K) XS > 100 RW > 150 | Ic(12T) XS > 600 RW > 632 | Ic(13T) | Ic(14T) | Ic(15T) XS > 314 RW > 331
PO08S00223A01U | 201 | 694 | 575 | 470 | 378
PO08S00211A01U | 231 |  |  |  | 
P43OL1107AE49E | 149 | 676 | 562 | 459 | 369
P43OL1107AE54E | 125 | 641 | 532 | 433 | 348
P43OL1107AE43E | 189 | 590 | 574 | 475 | 385
P43OL1107AE47E | 174 | 676 | 560 | 456 | 367
nnnQ denotes a critical current measurement that showed a transition but quenched before the criterion was reached
Q denotes a critical current measurement that did not show a transition before quenching

## Slide 48
Margins | Margin | Operating Point (X)
Load line margin (purple arrow) | 24.3% | 75.7%
Current margin (green arrow) | 58.4% | 41.6%
Temperature margin [K] | 5.0 | 6.9

## Slide 49: QXFA-207 / P43OL1106

## Slide 50: Cable Summary
Magnet: MQXFA-05
Coil: QXFA-207
Corresponding Cable: P43OL1106 (AUP 011)
Cable is 2nd generation QXF cables with 108/127 RRP® strands procured under LARP

## Slide 51: Wire Summary
All “HiLumi” spec, procured by LARP under:
  FNAL 632982 D – Spec 0
0.85 mm, Ti-doped, reduced Sn

## Slide 52: P43OL1106 – Cable Date, Lengths
Cable Manufacture Date
  2018 06 18 (Production run)
Cable Length:
  465 m (LBNL, fabricated, including LBNL samples)
  455 m (shipped to NEWT, including S & V samples)
  ??? m (Measured by BNL)

## Slide 53: P43OL1106 – Strand and SS Core ID
Spool:
  PO08S00220A01U x 1 ULs
  PO08S00220A02U x 3 ULs
  PO08S00220A03U x 1 ULs
  PO08S00220A05U x 2 ULs
  PO08S00225A03U x 2 ULs
  PO08S00224A02U x 3 ULs
  PO08S00225A02U x 2 ULs
  PO08S00239A07U x 1 ULs
  PO08S00224A01U x 1 ULs
  PO08S00239A04U x 1 ULs
  PO08S00225A05U x 2 ULs
  PO08S00239A02U x 2 ULs
  PO08S00239A01U x 2 ULs
  PO08S00224A04U x 1 ULs
  PO08S00225A01U x 3 ULs
  PO08S00239A06U x 2 ULs
  PO08S00223A02U x 11 ULs
Core:
  120L40A7322313
    Core width: 12.0 mm; material: 316L;
    Heat: 844979; Lot: 16-597;
    Chemical Properties CoT/CoC 172660-1: 0.14 wt% Co
From 5 billets

## Slide 54: P43OL1106 Respooling Wire Diameter
Below LSL: 0.00%
Above USL: 0.04%

## Slide 55: P43OL1106 – Cable QC Data Summary
CME:
Residual Twist:
  130°
10-stack:
  Qualification: 1.533 mm
  Production tail end: 1.531 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 17.0 | 0.459 | 18.159 | 1.531
Average | 17.0 | 0.426 | 18.149 | 1.526
Minimum | 17.0 | 0.398 | 18.143 | 1.523
Sigma | 0.01 | 0.009 | 0.002 | 0.001

## Slide 56
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 57
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 58
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 59: P43OL1106 – Braiding
Fiberglass Lot #100415
P/I: 18.0
Spool tension: 10 lbs. (payoff); 20 lbs. (takeup)
Bobbin payoff tension: 0.125 lbs. (min), 0.250 lbs. (max)
NEWT 10-stack QC:
  Cycle #1) 0.149 mm; #2) 0.147 mm; #3) 0.145 mm;
  Mean 0.147 mm
LBNL 10-stack verification QC:
  Cycle #1) 0.146 mm; #2) 0.143 mm; #3) 0.141 mm;
  Mean 0.143 mm
Vector #464342

## Slide 60: P43OL1106 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.850 ± 0.0006 mm (LBNL)1
Cu ratio a | 54.7% (OST)
Strand twist pitch a | 18.7 mm (OST)
RRR (RW) a | 258 (OST)
RRR (15% rolled) a | 168 (OST)
IC (4.2 K, 15 T) a | 368 A (OST)
IC (4.2 K, 14 T) a | 463 A (OST)
IC (4.2 K, 13 T) a | 571 A (OST)
IC (4.2 K, 12 T) a | 694 A (OST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received, all LBNL respooling data; mean ± 1 sigma

## Slide 61: P43OL1106 – Wire Parameters Supplier (S) and Verification (V) IC Data
Number of spools from that billet used in the cable

## Slide 62: P43OL1106 – Wire Parameters Supplier (S) and Verification (V) RRR Data
Number of spools from that billet used in the cable

## Slide 63: P43OL1106 – Extracted Strand RRR
 | Cable ID | No. of Units from Billet (spool) | HT/sample ID | Major edge RRR | Minor edge RRR | Straight section 1 RRR | Straight section 2 RRR
ID #1 | P43OL1106AE05E PO08S00220A02U | 7 (3) | LRLK180717ALC1 | 284 | 270 | 399 | 410
ID #2 | P43OL1106AE17E PO08S00224A02U | 5 (3) | LRLK180717ALC1 | 271 | 200 | 307 | 301
ID #3 | P43OL1106AE37E PO08S00225A01U | 9 (3) | LRLK180717ALC1 | 312 | 238 | 326 | 334
ID #4 | P43OL1106AE45E PO08S00223A02U | 11 (11) | LRLK180717ALC1 | 189 | 175 | 252 | 259
ID #5 | P43OL1106AE49E PO08S00223A02U | 11 (11) | LRLK180717ALC1 | 263 | 222 | 304 | 305
Vector #464342

## Slide 64: P43OL1106 – Witness Samples
All tests were successful
Witness extracted strand (XS)
Witness virgin strand (VS)

## Slide 65: P43OL1106 – Witness Samples
ID | RRR (293K / 20K) XS > 100 RW > 150 | Ic(12T) XS > 600 RW > 632 | Ic(13T) | Ic(14T) | Ic(15T) XS > 314 RW > 331
PO08S00223A02U | 292 | 671 | 549 | 441 | 351
PO08S00220A02U | 388 | 678 | 555 | 447 | 352
P43OL1106AE45E | 253 | 654 | 541 | 439 | 349
P43OL1106AE55E | 228 | 617 | 494 | 400 | 310
P43OL1106AE05E | 310 |  |  |  | 
P43OL1106AE17E | 236 |  |  |  | 
nnnQ denotes a critical current measurement that showed a transition but quenched before the criterion was reached
Q denotes a critical current measurement that did not show a transition before quenching

## Slide 66
Margins | Margin | Operating Point (X)
Load line margin (purple arrow) | 25.0% | 75.0%
Current margin (green arrow) | 61.0% | 39.0%
Temperature margin [K] | 5.1 | 7.0

## Slide 67: QXFA-209 / P43OL1114

## Slide 68: Cable Summary
Magnet: MQXFA-06
Coil: QXFA-209
Corresponding Cable: P43OL1114 (AUP 016)
Cable is 2nd generation QXF cables with 108/127 RRP® strands procured under LARP

## Slide 69: Wire Summary
All “HiLumi” spec, procured by CERN under:
  CERN Contract F663
0.85 mm, Ti-doped, reduced Sn
Strand data from CERN:
ID | Ic12 A | Ic15 A | RRR | n15 | Ic15 roll A | RRR roll
AO08S00125A01U.Y | 707 | 393 | 218 | 31 | 399 | 101
AO08S00125A01U.X | 711 | 395 | 201 | 34 |  | 
AO08S00136A01U | 675 | 373 | 254 | 43 | 375 | 146
(Spec) | 632 | 331 | 150 | 30 | 314 | 100

## Slide 70: P43OL1114 – Cable Date, Lengths
Cable Manufacture Date
  2018 12 19 (Production run)
Cable Length:
  481 m (LBNL, fabricated, including LBNL samples)
  455 m (shipped to NEWT, including S & V samples)
  ??? m (Measured by BNL)

## Slide 71: P43OL1114 – Strand and SS Core ID
Spool:
  AO08S00123A02U x 3 ULs
  AO08S00136A03U x 3 ULs
  AO08S00123A04U x 5 ULs
  AO08S00136A01U x 12 ULs
  AO08S00125A01U x 17 ULs
Core:
  120L35A7322313
    Core width: 12.0 mm; material: 316L;
    Heat: 844979; Lot: 16-597;
    Chemical Properties CoT/CoC 172660-1: 0.14 wt% Co
From 3 billets

## Slide 72: P43OL1114 Respooling Wire Diameter
Below LSL: 0.42%
Above USL: 4.68%
(Does not exceed Diameter DR Criteria 1 or 2, therefore no DR needed)

## Slide 73: P43OL1114 – Cable QC Data Summary
CME:
Residual Twist:
  120°
10-stack:
  Qualification: 1.529 mm
  Production tail end: 1.533 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 17.1 | 0.426 | 18.173 | 1.531
Average | 17.0 | 0.406 | 18.152 | 1.527
Minimum | 17.0 | 0.385 | 18.147 | 1.523
Sigma | 0.01 | 0.006 | 0.003 | 0.001

## Slide 74
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 75
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 76
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 77: P43OL1114 – Braiding
Fiberglass Lot #100858
P/I: 18.0
Spool tension: 10 lbs. (payoff); 20 lbs. (takeup)
Bobbin payoff tension: 0.125 lbs. (min), 0.250 lbs. (max)
NEWT 10-stack QC:
  Cycle #1) 0.146 mm; #2) 0.144 mm; #3) 0.143 mm;
  Mean 0.144 mm
LBNL 10-stack verification QC:
  Cycle #1) 0.139 mm; #2) 0.138 mm; #3) 0.136 mm;
  Mean 0.138 mm (see DR #11758)
Vector #464342
LBNL boat subsequently found to have possibly misaligned
CAPA: hardware record to include realignment

## Slide 78: DR #11758

## Slide 79: P43OL1114 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.850 ± 0.0015 mm (LBNL)1
Cu ratio a | 54.6% (OST)
Strand twist pitch a | 19.3 mm (OST)
RRR (RW) a | 226 (OST)
RRR (15% rolled) a | 119 (OST)
IC (4.2 K, 15 T) a | 390 A (OST)
IC (4.2 K, 14 T) a | 481 A (OST)
IC (4.2 K, 13 T) a | 584 A (OST)
IC (4.2 K, 12 T) a | 701 A (OST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received, all LBNL respooling data; mean ± 1 sigma
Supplier QC: 665°C for 75 h

## Slide 80: P43OL1114 – Wire Parameters Supplier (S) and Verification (V) IC Data
Number of spools from that billet used in the cable

## Slide 81: P43OL1114 – Wire Parameters Supplier (S) and Verification (V) RRR Data
Number of spools from that billet used in the cable

## Slide 82: P43OL1114 – Extracted Strand RRR
 | Cable ID | No. of Units from Billet (spool) | HT/sample ID | Major edge RRR | Minor edge RRR | Straight section 1 RRR | Straight section 2 RRR
ID #1 | P43OL1114AE19E AO08S00136A01U | 15 (12) | LRLK190205ALC1 | 269 | 276 | 335 | 353
ID #2 | P43OL1114AE18E AO08S00136A01U | 15 (12) | LRLK190205ALC1 | 250 | 317 | 325 | 333
ID #3 | P43OL1114AE37E AO08S00125A01U | 17 (17) | LRLK190205ALC1 | 228 | 227 | 341 | 336
ID #4 | P43OL1114AE36E AO08S00125A01U | 17 (17) | LRLK190205ALC1 | 179 | 272 | 321 | 328
ID #5 | P43OL1114AE11E AO08S00123A04U | 8 (5) | LRLK190205ALC1 | 225 | 278 | 297 | 280
Vector #464342

## Slide 83: P43OL1114 – Witness Samples
All tests were successful
  Virgin strand tests were not stable on inner taps
Witness extracted strand (XS)
Witness virgin strand (VS)

## Slide 84: P43OL1114 – Witness Samples
ID | RRR (293K / 20K) XS > 100 RW > 150 | Ic(12T) XS > 600 RW > 632 | Ic(13T) | Ic(14T) | Ic(15T) XS > 314 RW > 331
PO08S00125A01U | 304 | 729 | 605 | 495 | 400
PO08S00136A01U | 296 | 709 | 592 | 486 | 395
P43OL1114AE36E | 221 | 731 | 613 | 505 | 412
P43OL1114AE39E | 233 | 727 | 608 | 502 | 409
P43OL1114AE18E | 250 |  |  |  | 
P43OL1114AE21E | 252 |  |  |  | 
nnnQ denotes a critical current measurement that showed a transition but quenched before the criterion was reached
Q denotes a critical current measurement that did not show a transition before quenching
Extracted strands and witness samples using 665°C for 50 h
clearly outperform the supplier data to CERN using 665°C for 75 h

## Slide 85: SSL
Margins | Margin | Operating Point (X)
Load line margin (purple arrow) | 26.7% | 73.3%
Current margin (green arrow) | 62.1% | 37.9%
Temperature margin [K] | 5.4 | 7.3

## Slide 86: Summary
Coil | SSL field (T) | SSL current (kA) | IOP/ISSL (%) | T margin (K) | Cable IC (kA) | IOP/IC (%)
MQXFA116 | 15.0 | 22.0 | 74.9 | 5.2 | 41.9 | 39.3
MQXFA117 | 14.8 | 21.8 | 75.7 | 5.0 | 39.6 | 41.6
MQXFA207 | 14.9 | 21.9 | 75.0 | 5.1 | 42.2 | 39.0
MQXFA209 | 15.3 | 22.5 | 73.3 | 5.4 | 43.4 | 37.9
MQXFA115 | 15.2 | 22.3 | 73.9 | 5.3 | 43.8 | 37.6
Although the strand for coil 209 did not test well according to CERN data, the coil performs well based on XS data.

## Slide 87: Extra – Spare Coil QXFA-115 / P43OL1102
As presented on 2019 10 30 at MQXFA04 Coils Acceptance

## Slide 88: QXFA-115 / P43OL1102

## Slide 89: P43OL1102 – Cable Date, Lengths
Cable Manufacture Date
  2018 05 18 (Production run)
Cable Length:
  470 m (LBNL, fabricated, including LBNL samples)
  449 m (Measured by FNAL)

## Slide 90: P43OL1102 – Strand and SS Core ID
Spool:
  PO08S00239A05U x 2 ULs
  PO08S00220A04U x 3 ULs
  PO08S00230A04U x 3 ULs
  PO08S00239A03U x 3 ULs
  PO08S00235A01U x 12 ULs
  PO08S00237A01U x 17 ULs
Core:
  120L43A7322313
    Core width: 12.0 mm; material: 316L;
    Heat: 844979; Lot: 16-597;
    Chemical Properties CoT/CoC 172660-1: 0.14 wt% Co
From 5 billets

## Slide 91: P43OL1102 Respooling Wire Diameter
Below LSL: 0.00%
Above USL: 0.00%

## Slide 92: P43OL1102 – Cable QC Data Summary
CME:
Residual Twist:
  135°
10-stack:
  Qualification: 1.525 mm
  Production tail end: 1.528 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 17.1 | 0.451 | 18.169 | 1.530
Average | 17.0 | 0.425 | 18.153 | 1.526
Minimum | 16.9 | 0.395 | 18.145 | 1.522
Sigma | 0.01 | 0.009 | 0.004 | 0.001

## Slide 93
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 94
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 95
Rollers: P-91 (2017-12-08) and P-92 (2017-12-08)

## Slide 96: P43OL1102 – Braiding
Fiberglass Lot #100415
P/I: 18.9
Spool tension: 10 lbs. (payoff); 20 lbs. (takeup)
Bobbin payoff tension: 0.125 lbs. (min), 0.250 lbs. (max)
NEWT 10-stack QC:
  Cycle #1) 0.150 mm; #2) 0.147 mm; #3) 0.146 mm;
  Mean 0.148 mm
LBNL 10-stack verification QC:
  Cycle #1) 0.143 mm; #2) 0.140 mm; #3) 0.137 mm;
  Mean 0.140 mm
Vector #464342

## Slide 97: P43OL1102 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.850 ± 0.001 mm (LBNL)1
Cu ratio a | 55.1% (OST)
Strand twist pitch a | 18.6 mm (OST)
RRR (RW) a | 263 (OST)
RRR (15% rolled) a | 154 (OST)
IC (4.2 K, 15 T) a | 365 A (OST)
IC (4.2 K, 14 T) a | 459 A (OST)
IC (4.2 K, 13 T) a | 567 A (OST)
IC (4.2 K, 12 T) a | 690 A (OST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received, all LBNL respooling data; mean ± 1 sigma

## Slide 98: P43OL1102 – Extracted Strand RRR
Vector #464342

## Slide 99: QXFA-CL-115 Cable P43OL1102
NO tests of backup samples were required to fulfill witness sample testing requirements
  Unstable tests are shaded above
Witness extracted strand (XS)
Witness virgin strand (VS)

## Slide 100: Coil QXFA115, cable 1102 – Witness samples
ID | RRR (293K / 20K) XS > 100 RW > 150 | Ic(12T) XS > 600 RW > 632 | Ic(13T) | Ic(14T) | Ic(15T) XS > 314 RW > 331
PO08S00235A02U | 192 | 700 | 581 | 473 | 380
P43OL1102AE18E | 127 | 688 | 569 | 463 | 370
P43OL1102AE35E | 125 | 688 | 572 | 468 | 380
P43OL1102AE41E | 125 |  |  |  | 
P43OL1102AE59E | 104 |  |  |  | 
nnnQ denotes a critical current measurement that showed a transition but quenched before the criterion was reached
Q denotes a critical current measurement that did not show a transition before quenching

## Slide 101: Coil 115 SSL
Margins | Margin | Operating Point (X)
Load line margin (purple arrow) | 26.2% | 73.9%
Current margin (green arrow) | 62.4% | 37.6%
Temperature margin [K] | 5.3 | 7.2

## Slide 102: Summary of Data
Coil | SSL field (T) | SSL current (kA) | IOP/ISSL (%) | T margin (K) | Cable IC (kA) | IOP/IC (%)
MQXFA112 | 15.0 | 22.1 | 74.6 | 5.2 | 41.7 | 39.5
MQXFA113 | 15.1 | 22.2 | 74.3 | 5.3 | 42.3 | 38.9
MQXFA203 | 15.4 | 22.6 | 72.8 | 5.5 | 45.1 | 36.5
MQXFA206 | 15.2 | 22.3 | 73.9 | 5.3 | 43.8 | 37.6
MQXFA115 | 15.2 | 22.3 | 73.9 | 5.3 | 43.8 | 37.6