## Slide 1
Vacuum firing effect on stainless steel & titanium
Junichiro Kamiya
on behalf of the RCS vacuum group
Japan Atomic Energy Agency (JAEA) / J-PARC center
This presentation is the summary of the articles on the e-Journal of Surface Science and Nanotechnology (eJSSNT).
J. Kamiya, et. al, “Evaluation of Titanium Vacuum Chamber as Getter Pump”, eJSSNT 2023.
J. Kamiya, et. al, “Evaluation of Vacuum Firing Effect on Stainless Steel from Vacuum and Surface Point of View”, eJSSNT 2023.

## Slide 2
Vacuum firing
High-temperature heating of vacuum chambers or vacuum materials in a HV furnace “vacuum firing” has been known as the process of reducing the amount of dissolved hydrogen in the bulk.
EX1) Stainless steel, 950 ℃ for a few hours: CERN recipe
EX2) Titanium, 650 ℃ -850 ℃ for 10 hours: J-PARC recipe
Vacuum in Particle Accelerators, Oleg B. Malyshev © 2019 Wiley‐VCH Verlag GmbH & Co. KGaA.
Residual gas in the vacuum chamber in an ultra-high vacuum region is known to be dominated by desorbed gas molecules adsorbed on the surface and diffused atoms (such as hydrogen) from inside the bulk that recombine and desorb.

## Slide 3
Vacuum firing effect: hydrogen content
Vacuum firing temperature vs. H content for pure Ti grade 2
H content before and after vacuum firing
Vacuum firing reduces the hydrogen concentration in the bulk.
Ogiwara et al., Reduction of hydrogen content in pure Ti, J. of Phys.: Conf. Ser. 100 (2008) IVC-17/ICSS-13 and ICN+T2007
Kamiya et al., Vacuum chamber made of soft magnetic material with high permeability, Vacuum 98 (2013)

## Slide 4
Vacuum firing effect: outgassing
Vacuum firing 950℃24H
×10 [Pa m3/(s m2)]
SS chamber with and w/o vacuum firing (aft. 150 ℃ 3days baking)
×1.3e3 Pa m3/(s m2)
SS chamber with and w/o vacuum firing (aft. 200 ℃ 48h baking)
Vacuum firing 950℃2H
Fedchak et al., Outgassing rate comparison of seven
geometrically similar vacuum chambers of
different materials and heat treatments, JVSTB (2021)
Hseuh and Cul, Outgassing and desorption of the stainless-steel beam tubes after different degassing treatments, JVSTA (1989)

## Slide 5
Study purpose
Systematic research for the outgassing characteristics of the vacuum-fired vacuum material.
Understanding the mechanism of the vacuum firing effect from surface microscopic point of view.
Only a few research compares the outgassing rate of vacuum-fired material with non-vacuum-fired one in the same experimental condition.
There is almost no research about detailed mechanism for the low outgassing rate by vacuum firing.

## Slide 6
Experimental
V: 0.00255 m3, A: 0.10 m2
Test chamber
Max temp. 1000 ℃
Work space: 1 m×1 m × ~2 m
TMP 3200 l/s×3, Cryopump 10000 l/s×1
Mo heater, Mo+SS refrector
Pressure at 850℃: ≤1×10-3 Pa
Pressure at RT: ~1×10-6 Pa
J-PARC HV furnace
 | Material | Surface polish | V.F.
Stainless steel chamber | SS304L | #400 buff+EP | Non/ 850℃ 10H
Titanium chamber | Pipe: pure Ti grade-2 Flange: Ti-6Al-4V | #400 buff+CP | Non/ 850℃ 10H
100CF

## Slide 7
Surface morphology: titanium
Ra: 0.05 um
Rz: 0.4 um
Ra: 0.2 um
Rz: 1.1 um
Vacuum-fired Ti
Non-vacuum-fired Ti
Larger grain size, larger roughness for vacuum-fired Ti

## Slide 8
Too small grain size to detect
Surface morphology: stainless steel
Ra: 0.009 um
Rz: 0.06 um
Ra: 0.02 um
Rz: 0.17 um
Vacuum-fired SS
Non-vacuum-fired SS
Larger grain size, larger roughness for vacuum-fired SS

## Slide 9
Buildup test
Evacuation
Buildup
~1day
200℃ 8H bake
300℃ 3.5 H bake
cooling
400℃ 3.5 bake
Buildup
350℃ 3.5 bake
Buildup
Buildup
cooling
cooling
cooling
Buildup
MV close
MV open
MV open
MV close
MV close
MV open
MV close
MV open
MV close
@Room Temperature
@RT
@RT
@RT
@RT
Buildup test procedure
Thermal desorption spectroscopy (TDS):
To see the effect on the absorbed & desorbed gas on the surface
X-ray photoelectron spectroscopy (XPS):
To see the surface modification
Other surface analyses with sample peace

## Slide 10
Vacuum firing on titanium: build-up results
Vacuum-fired Ti chamber
Non-vacuum-fired Ti chamber
Vacuum firing clearly reduced outgassing of a titanium chamber.
Baking of the vacuum fired titanium chamber is very effective to achieve low outgassing rate.

## Slide 11
Vacuum firing on titanium: mechanism
Non heating
200℃
300℃
350℃
400℃
XPS result
Titanium sample w/o vacuum firing O1s depth profile
Increasing baking temperature allows oxides to diffuse into the interior.
Above 300 ℃, surface of the titanium is partially metallized and becomes getter.

## Slide 12
Vacuum firing on titanium: mechanism
Vacuum-fired titanium has thinner surface oxide layer.
Surface O is easy to diffuse into the bulk by baking, resulting metalization of surface Ti.
Findings on Vacuum firing of titanium
Surface getter function of Ti-metal contributes to the low outgassing.

## Slide 13
Non-vacuum-fired SUS chamber
Vacuum-fired SUS chamber
(2 hors)
(2 hors)
Vacuum firing on stainless steel: build-up results
Vacuum firing clearly reduced outgassing of a SS chamber.
Baking of the vacuum fired SS chamber is very effective to achieve low outgassing rate.

## Slide 14
Long-term buildup result of SS chamber
For a vacuum-fired chamber, especially hydrogen outgassing, which is the main component after baking, is much reduced.
(8 days)
(8 days)

## Slide 15
TDS result of SS samples: surface molecules
Vacuum-fired SUS (in-situ) is almost background level.
Outgassing is suppressed by the vacuum firing even after air exposure.
Comparison:
Background
Sample A: Non-vacuum-fired SUS
Sample B: Vacuum-fired SUS (air-exposed):
850℃ 10 H in TDS apparatus → Exposed to atmosphere more than a week → TDS measurement
Sample C: Vacuum-fired SUS (in-situ):
850℃ 10 H in TDS apparatus → TDS measurement
Sample: size 10 mm×10 mm ×t1 mm

## Slide 16
TDS result of SS samples: surface molecules
Other gases reabsorb by air exposure, but degassing effect by the vacuum firing partially remains.
Hydrogen of a vacuum-fired SUS is near background level even after air exposure.
Resistant surface to gas adsorption would have been formed.
H diffused to vacuum from bulk by vacuum firing and reabsorption in atmosphere is little.
Background
Sample A: Non-vacuum-fired SUS
Sample B: Vacuum-fired SUS (air-exposed)
Sample C: Vacuum-fired SUS (in-situ)

## Slide 17
XPS result of SS samples: surface modification
While non-vacuum-fired SS surface was mainly Cr-oxide, vacuum-fired SS surface was covered by Fe-oxide.
XPS measurement was performed for SS samples without and with vacuum firing.
Cr-oxide
Fe-oxide

## Slide 18
Surface Fe-oxide layer formation
Auger electron spectroscopy (Achard et al. 1979, VACUUM):
Fe peak increases in higher temperature up to 900℃.
Fe-oxide surface was formed by the air exposure after vacuum firing.
200℃
300℃
400℃
500℃
600℃
700℃
800℃
900℃
Fe
Cr
During vacuum firing, Fe-metal becomes main surface composition.
Previous research by Sugimoto et. al revealed that the adsorbed water on Cr-oxide surface largely contributes the outgassing of the stainless steel.
T. Sugimoto, K. Takeyasu, K. Fukutani, “Gas behavior in the vacuum chamber with a single adsorption site on the chamber wall: Origin of the exponential pressure decay with the time constant of sub-kilo seconds. “ J. Vac. Soc. Jpn. 2013.
Fe-oxide surface layer has an important role for outgassing reduction.

## Slide 19
Summary
Titanium:
  Formation of very thin Ti-oxide layer is formed by the Ti metalization during the vacuum firing and Ti oxidation by following air exposure
    as a getter by the high temperature baking
Stainless steel:
  Formation of the surface Fe-oxide layer, which is formed by the Fe metalization during vacuum firing and Fe oxidation by following air exposure
    as a diffusion barrier from the gas phase to the bulk
    as a gas readsorption resistant surface.
Mechanism of outgassing reduction by vacuum firing

## Slide 20
Backup

## Slide 21
Build-up results: residual gas components
Vacuum firing reduced all the residual gas components.

## Slide 22
Surface modification process by heating
Non-vacuum-fired SS:
Cr-oxide increase at 300 & 400℃.
Vacuum-fired SS:
Fe-oxide decreases and Cr-oxide increase at 300 & 400℃.
Clear dependence of Cr-oxide and F-oxide values on the heating temperature.