## Slide 1: LBNF Kicker Ceramic Beam Tube Coatings
Jason Morin
OLAV
18 April 2024

## Slide 2: LBNF Project

## Slide 3: LBNF Kicker Beam Tubes
Long Baseline Neutrino Project (LBNF/DUNE) requires 6 new extraction kickers
Project requirements call for the use of ceramic beam tubes
  High permeability to magnetic fields
  Will build up static electric charge
  Unwanted Secondary Electron Yield (SEY)
Surface coatings can improve both the electrical and SEY performance

## Slide 4: LBNF Kicker Beam Tubes

## Slide 5: Kicker End Cross Section
Details of beam tube to magnet case interface
Conflat flange vacuum seal
Metal bellows
Ceramic beam tube
Magnet case end plate

## Slide 6: Beam Tube Coating Technical Requirements
Coating must be even and defect free
Low outgassing rate: <1x10-10 Torr Liters/second/cm2
Ultimate vacuum pressures: <10-8 Torr
Electrical resistivity of coating: 1-10 kOhm/square
End to end electrical resistance: 10-40 kOhms
Low SEY: <1.37
Subject to > 1MRad of Gamma radiation during lifetime
Operating temperature 10-100° C
Free of hazardous materials like lead
Compatible with Kovar
Can survive at brazing temp: 900-1200°C
OR safe to coat a previously brazed joint (coating application temperature <400° C)

## Slide 7: Previously Used Coating- Aerodag
From past project experience, coating with Aerodag (amorphous graphite “paint”) is effective but problematic:
  Technical challenge to achieve suitable coating in a consistent and repeatable manner
  Requires significant labor resources
  Risk of damage to assembled tubes, especially if repeated attempts at coating are required
  Technician expertise not retained due to the infrequency of need (>10 years since last produced in house)
  Loss of processing equipment

## Slide 8: Previously Researched Coatings
Cermet
  Metal/ceramic composite
  Resistance was too high
  Contained lead
Indium Tin Oxide
  Met electrical and vacuum requirements
  SEY too high

## Slide 9: SEY Testing of Indium Tin Oxide (ITO) Coating in FNAL Main Injector
Studies conclude 1.37 SEY is required threshold to avoid issues
  ITO did not condition below this value
~1.25 peak
~1.65 peak
316L Control Sample
ITO Sample

## Slide 10: Most Recent Coating Investigation
Polyteknik, Denmark
  Only vendor found with both suitable coating and ability to apply it to inside surface of tubes
  Has worked with many European labs
Coatings applied with magnetron sputtering
Chromium Oxide
  Cr2O3 (may be green or gray)
  Used at several European labs
Titanium Nitride
  TiN (may be gold or gray)
  Used at J-PARC

## Slide 11: Chromium Oxide Literature Search
Outgassing rate: Better than stainless
Kim, K. R. et al. “UTILIZATION OF Cr2O3 PASSIVATION PROCESS ON STAINLESS-STEEL CHAMBER FOR XHV ENVIRONMENT*.” (2004).
Barnes, Michael & Adraktas, A & Bregliozzi, G & Goddard, Bethany & Ducimetiere, L. & Salvant, B & Sestak, Josef & Vega, Lorena & Weterings, W & Yin Vallgren, Christina. (2017). Operational experience of the upgraded LHC injection kicker magnets during Run 2 and future plans. Journal of Physics: Conference Series. 874. 012101. 10.1088/1742-6596/874/1/012101.
S.E.Y. vs Energy

## Slide 12: Chromium Oxide- More S.E.Y.
Conditioning after heating to 850C
As received values are similar to those on previous slide

## Slide 13: Titanium Nitride Literature Search
Outgassing rate: 10-9 Pa m3/s /m2 (after baking at 420 K in 23h) ~10-12 Torr L/S /cm2
(Vacuum components in J-PARC RCS & Application of vacuum engineering to beam profile measurement. Annual US-Japan collaboration meeting for “Accelerator and Beamline Research and Technology Development for High-Power Neutrino Beams” 1, Feb. 2023)
S.E.Y. vs Energy
Ji, Yichen. Electron Cloud Studies at Fermilab. United States. https://doi.org/10.2172/1594127
Note: Colors are NOT consistent between figures

## Slide 14: Titanium Nitride- S.E.Y. Testing at FNAL
Ji, Yichen. Electron Cloud Studies at Fermilab. United States. https://doi.org/10.2172/1594127
SS316L and TiN

## Slide 15: Additional In-House Testing
Electrical Resistivity:
  TiN:
    10 k ohm/square
    Point to point resistance consistent
  Cr2O3:
    1 M ohm/square (way too high)
    Point to point resistance varied wildly

## Slide 16: TiN Outgassing Verification Testing at FNAL
Outgassing rate measured by throughput method
q=(P1 –P2 )C/A
Initial results are promising but inconclusive:
  3.62 x 10-10 Torr Liters/second/cm2 after 24 hours
  Anomalous reading at 48 hours
  Retesting underway soon
Redhead, P.A., “Recommended practices for measuring and reporting outgassing data”, Journal of Vacuum Science & Technology A20, 1667-1675 (2002)

## Slide 17: Questions?