## Slide 1
R&D on LEM improvements
for phase II of ProtoDUNE-DP
E. Mazzucato, A. Delbart, G. Eurin, P. Granger, M. Karolak
(CEA/Irfu, Université Paris-Saclay)
R. De Oliveira (CERN/EP-DT-EF (MPT lab.))
Alain Delbart, R&D on LEM for phase II of ProtoDUNE-DP, LEM, Workshop on the LEM/Thick GEM cryogenic utilization in pure Argon over large detection surfaces, 6-7th april, 2020

## Slide 2
outline
2
Where we are with LEM performances in ProtoDUNE-DP
R&D on improvements of the LEM manufacturing & design
  Improved CERN RIM etching process
  Covering copper-FR4 LEM borders with an insulating layer
  Full size single-sided DLC resistive LEM
  Covering RIM edges with an insulating ring ?
Discussion on other ways of improvements for ProtoDUNE Phase II
Alain Delbart, R&D on LEM for phase II of ProtoDUNE-DP, LEM, Workshop on the LEM/Thick GEM cryogenic utilization in pure Argon over large detection surfaces, 6-7th april, 2020

## Slide 3
Reminder : where we are
50 cm
50 cm
2 mm FR4 + 2 mm coper
LEM CFR-34
(96% active area)
3 m
LEM CFR-35
(85% active area)
3 m
3 m
CFR-35 – NP02
CFR-34 – 3x1x1 m3
Alain Delbart, R&D on LEM for phase II of ProtoDUNE-DP, LEM, Workshop on the LEM/Thick GEM cryogenic utilization in pure Argon over large detection surfaces, 6-7th april, 2020
3

## Slide 4
4
VLEM = 3.5 kV in Ar @ 3.3 bar
- 34 kV/cm max amplification field in NP02
35 kV/cm for single LEM in 3,3 bar Ar
- max gain ~ 100 in DLAr before charging up
- spark rate: 3/h @ 35 kV/cm(3,3 bar Ar)
- sparks are no more stimulated on borders
- 86% active area
CFR-35 – NP02
CFR-34 – 3x1x1 m3
- 31 kV/cm max amplification field in 3x1x1
32 kV/cm for single LEM in 3,3 bar Ar
- Max gain ~20 before charging up
- spark rate: 20/h @ 34-35 kV/cm (3,3 bar Ar)
> 45% sparks on edges or corners
- 95% active area
multiple
sparks
VLEM = 3.3-3.5 kV in Ar @ 3.3 bar
LEM performances
Alain Delbart, R&D on LEM for phase II of ProtoDUNE-DP, LEM, Workshop on the LEM/Thick GEM cryogenic utilization in pure Argon over large detection surfaces, 6-7th april, 2020

## Slide 5
5
LEM for ProtoDUNE-DP challenge
Max 32kV/cm
3x1x1 m3 (CFR-34)
Geff = eextraction x GLEM x ecoll
Max 34kV/cm
NP02 (CFR-35)
Geff=20 with <5% dead zone out of the 9 m2 CRP area (~3,1 kV before charging-up)
With a long term stability <1 spark / h / CRP (=1/36 per LEM)
Alain Delbart, R&D on LEM for phase II of ProtoDUNE-DP, LEM, Workshop on the LEM/Thick GEM cryogenic utilization in pure Argon over large detection surfaces, 6-7th april, 2020
~3,3 bar Ar
(same gas density
as DLAr)
DV

## Slide 6
Ways of improvements of the LEM
6
LEM paremeters : increase thickness, decrease number of holes ? Other parameters to optimize ? Different RIM size on the 2 sides ? (see P. Correia’s talk)
Global quality of holes’ drilling & RIM etching locally affecting electric field
  With a 40 mm RIM, can an even more smooth RIM edge help ?
  Improve RIM etching (etching defects for holes on borders and corners)
  Other improvement in the manufacturing procedure ?
  Covering of the RIM copper edges with an insulating layer
  How to set-up the burn-in procedure to remove residual copper asperities ?
Electric field increase on LEM borders & in the holes close to the borders/corners
  Larger holes on the first few rows of holes from the border ?
  LEM active area segmentation ?
  Optimize the FR4 & copper guard rings dimensions on borders/corners
  Covering of the copper edges with an insulator layer
Other ideas ? Resistive LEM, multi-LEMs, …
 The R&D requires testing long term operation stability & ageing, both with individual LEMs in laboratory (3,3 bar argon) and with large area (> 4 LEMs) in DLAr conditions (« cold box »)
Alain Delbart, R&D on LEM for phase II of ProtoDUNE-DP, LEM, Workshop on the LEM/Thick GEM cryogenic utilization in pure Argon over large detection surfaces, 6-7th april, 2020

## Slide 7
LEM manufacturing & QA/QC
7
By LEM manufacturer
By WA105
+ final 160 °C polymerization
« standard »
global RIM micro-etching (CERN-ELTOS)
65 mm
65 mm
1 mm
F500 mm hole
with pumice powder
4 steps (+/- 90°, top/bottom)
Change drills every 1000 holes
Drilling of stack of PCBs is forbidden
3 mn Ultrasonic bath in 65°C NGL 17.40 ALU
Karcher Normal + DM water
3h Baking @ 80°C
HV test synth. Air & 3,3 bar Ar
Alain Delbart, R&D on LEM for phase II of ProtoDUNE-DP, LEM, Workshop on the LEM/Thick GEM cryogenic utilization in pure Argon over large detection surfaces, 6-7th april, 2020

## Slide 8: Global etching defects on borders
8
LEM corner
Decentered RIM
with
copper residues
 New RIM etching process developped by CERN
Alain Delbart, R&D on LEM for phase II of ProtoDUNE-DP, LEM, Workshop on the LEM/Thick GEM cryogenic utilization in pure Argon over large detection surfaces, 6-7th april, 2020

## Slide 9
New RIM etching process
CERN/EP-DT-EF (MPT lab.)
9
LEM copper surfaces protected with thin adhesive copper foils before drilling.
Micro-etching only around holes, visible through transparent glue to control RIM
Copper thickness is not etched
4 x CFR-35 prototypes produced : CERN LEM #1 to #5 made with 0,92-0,93 mm thick FR4
35 mm
35 mm
1 mm
35 mm
35 mm
1 mm
35 mm
35 mm
1 mm
35 mm
35 mm
1 mm
Measured
0,92-0,93 mm
Alain Delbart, R&D on LEM for phase II of ProtoDUNE-DP, LEM, Workshop on the LEM/Thick GEM cryogenic utilization in pure Argon over large detection surfaces, 6-7th april, 2020
~15 mm

## Slide 10: New RIM etching process Improved RIM quality
10
Alain Delbart, R&D on LEM for phase II of ProtoDUNE-DP, LEM, Workshop on the LEM/Thick GEM cryogenic utilization in pure Argon over large detection surfaces, 6-7th april, 2020
LEM corner
CERN LEM #5
New RIM etching process to be used for future productions
Can and have to be transfered to industrials

## Slide 11
CFR-35 CERN LEM #5
New sparks located in vicinity of screw holes
11
Possible explanation : the RIM global etching process naturally smoothed copper edges
whereas the new CERN RIM etching process left sharp the edges of copper guard ring.
Alain Delbart, R&D on LEM for phase II of ProtoDUNE-DP, LEM, Workshop on the LEM/Thick GEM cryogenic utilization in pure Argon over large detection surfaces, 6-7th april, 2020

## Slide 12
CFR-35 CERN LEM #5
New sparks located in vicinity of screw holes
12
Original CFR-35 & CERN LEM with new rim etching
Modified CFR-35 copper edges
Sparks
Modified CFR-35 copper edges + 64 mm pyralux PC1025 to cover LEM boders
Alain Delbart, R&D on LEM for phase II of ProtoDUNE-DP, LEM, Workshop on the LEM/Thick GEM cryogenic utilization in pure Argon over large detection surfaces, 6-7th april, 2020

## Slide 13
CERN CFR-35 + pyralux
13
This should improve HV stability by insulating areas where E-field is high (edges, corners, boundary regions).
Use CERN improved RIM micro-etching process  35 mm copper thick
2 prototypes produced @ CERN : CERN CFR-35 + pyralux #1 & 2
Alain Delbart, R&D on LEM for phase II of ProtoDUNE-DP, LEM, Workshop on the LEM/Thick GEM cryogenic utilization in pure Argon over large detection surfaces, 6-7th april, 2020

## Slide 14
First new CFR-35 + pyralux #1
Localization of sparks
14
Several weeks of operation & spark recording : no more sparks on insulated areas & border holes
Ar 3,3 bar
LEM HV
2,8-3,2 kV
Alain Delbart, R&D on LEM for phase II of ProtoDUNE-DP, LEM, Workshop on the LEM/Thick GEM cryogenic utilization in pure Argon over large detection surfaces, 6-7th april, 2020

## Slide 15
New CERN LEMs Gain measurements
15
Ar 3,3 bar
LEM HV
2,8-3,2 kV
#1
In 3,3 bar Argon, with Ed=500 V/cm for CERN New RIMs prototypes
With same measurement protocol in HP chamber as for CFR-35 gain measurements
Alain Delbart, R&D on LEM for phase II of ProtoDUNE-DP, LEM, Workshop on the LEM/Thick GEM cryogenic utilization in pure Argon over large detection surfaces, 6-7th april, 2020
DV
20

## Slide 16
First LEM CFR-35 + pyralux borders
Spark rate over 14 weeks of operation in 3,3 bar
16
Spark monitoring with cathode mesh + LEM + grounded anode in NP02 Electric Field configuration
1 sp/h/CRP goal at 3,1 kV
Burn-in/ageing ?
Alain Delbart, R&D on LEM for phase II of ProtoDUNE-DP, LEM, Workshop on the LEM/Thick GEM cryogenic utilization in pure Argon over large detection surfaces, 6-7th april, 2020
LEM DV

## Slide 17: First try of single-sided DLC-resistive LEM
17
1 mm (measured : 0,92-0,93 mm)
50 mm APICAL + “standard” DLC
PCB
35 mm copper
Glue the 2 parts with prepreg
Drilling like a THGEM
NO RIM etching
~250 MW/sq.
150 mm glue
Raw materials
DLC-resistive LEM
no RIM on copper side, no Ni/Au plating
Alain Delbart, R&D on LEM for phase II of ProtoDUNE-DP, LEM, Workshop on the LEM/Thick GEM cryogenic utilization in pure Argon over large detection surfaces, 6-7th april, 2020

## Slide 18: Single-sided DLC Resistive LEM CFR-35 full size prototype
18
Tests with 241Am source in Ar @ 3.3 bar
DLC face
Copper face
Signal from 5.5 MeV alpha
HP chamber
CU side
DLC side
Alain Delbart, R&D on LEM for phase II of ProtoDUNE-DP, LEM, Workshop on the LEM/Thick GEM cryogenic utilization in pure Argon over large detection surfaces, 6-7th april, 2020

## Slide 19: Single-sided DLC-Resistive LEM first week of operation in 3,3 bar Ar
19
DLC PS supply
current limit
Alain Delbart, R&D on LEM for phase II of ProtoDUNE-DP, LEM, Workshop on the LEM/Thick GEM cryogenic utilization in pure Argon over large detection surfaces, 6-7th april, 2020
<100 nA current
Sparks ? with no OVC
LEM DV

## Slide 20
Single sided-DLC Resistive LEM
Camera recording
20
Ar 3,3 bar
LEM HV
2,8-3,2 kV
Setup : LEM mounted alone on a support frame, copper side at GND
DLC side facing camera.
DLC HV
DLC PS
current
Corresponding Camera recording (2’20s)
3,3 bar Ar
Alain Delbart, R&D on LEM for phase II of ProtoDUNE-DP, LEM, Workshop on the LEM/Thick GEM cryogenic utilization in pure Argon over large detection surfaces, 6-7th april, 2020
- Sparks are heard but not seen on camera
- Still under investigations (some sparks
are seen in other recordings)
- LEM was then mounted on anode & a gain curve was done
50 s
8/10/2019
DLC PS supply
current limit

## Slide 21
Single-sided DLC-Resistive LEM
Gain measurement in 3,3 bar Ar
21
Ar 3,3 bar
LEM HV
2,8-3,2 kV
#1
Alain Delbart, R&D on LEM for phase II of ProtoDUNE-DP, LEM, Workshop on the LEM/Thick GEM cryogenic utilization in pure Argon over large detection surfaces, 6-7th april, 2020
In 3,3 bar Argon, with Ed=500 V/cm for CERN New RIMs & DLC prototypes
With same measurement protocol in HP chamber as for CFR-35 gain measurements
20
Cu side facing anode.

## Slide 22: Single-sided DLC-Resistive LEM appearance of unstable operation after one month
22
DLC PS supply
current limit
Alain Delbart, R&D on LEM for phase II of ProtoDUNE-DP, LEM, Workshop on the LEM/Thick GEM cryogenic utilization in pure Argon over large detection surfaces, 6-7th april, 2020
LEM DV
No eye-visible damages on the LEM : still need further inspection

## Slide 23
Adding insulating rings over RIM edges
CERN/EP-DT-EF (MPT lab.)
23
Alain Delbart, R&D on LEM for phase II of ProtoDUNE-DP, LEM, Workshop on the LEM/Thick GEM cryogenic utilization in pure Argon over large detection surfaces, 6-7th april, 2020
The process is applied on a LEM once finished. Requires precise mask alignment
Process to be tested : mask alignment on LEM holes, insulator uniformity, efficient covering ?
How will this affect LEM charging-up and performances ?
35 mm
35 mm
1 mm
~30 mm
Soldermask
spray
a)
b)
c)
d)
35 mm
35 mm
1 mm
~30 mm
UV exposure
40 mm RIM
LEM
mask
After soldermask development
80mm
80mm
140 mm

## Slide 24
10x10 cm2 LEM prototypes
with insulating rings
24
Next steps :
  Test these prototypes : compare gain, spark rate & spark localization, for RIM 40 mm, RIM 80 mm & RIM 40 mm + 80 mm soldermask rings
  include all modifications in a full size LEM for protoDUNE-DP : increased active area from 86% in CFR-35 up to ~95% (back to CFR-34 border design), insulated LEM borders, improved RIM etching & (if successfull prototype tests) add soldermask rings
Alain Delbart, R&D on LEM for phase II of ProtoDUNE-DP, LEM, Workshop on the LEM/Thick GEM cryogenic utilization in pure Argon over large detection surfaces, 6-7th april, 2020
2 x standard LEMs with 40 mm & 2 x standard LEMs with 80 mm RIM. Just produced @ CERN
2 x LEMs with with 40 mm & 80 mm large soldermask rings  under production @ CERN
Production of 10x10 cm2 prototypes, with improved CERN RIM etching :

## Slide 25
Towards ProtoDUNE-DP phase II
LEM design
25
Alain Delbart, R&D on LEM for phase II of ProtoDUNE-DP, LEM, Workshop on the LEM/Thick GEM cryogenic utilization in pure Argon over large detection surfaces, 6-7th april, 2020
CFR-35 – NP02
NP02 phase II ?
FR4 border decrease : 10 ↘ ~2 mm
Copper border : 5 ↘ ~2 mm
Pyralux covering of copper borders
F0,5 ↑ F0,6 mm LEM holes on borders ?
Segmentation ?
+ LEM-Grid HV distribution modification
+ adding a guard ring on anode PCB
from modified CFR-35 + pyralux design
« secured design » (dvpt time / production)
Resistive LEM (DLC or else)
Soldermask rings on RIMs
New ideas for charge readout in DLAr
Longer time scale developments (>2022)

## Slide 26
Anode guard ring
26
Alain Delbart, R&D on LEM for phase II of ProtoDUNE-DP, LEM, Workshop on the LEM/Thick GEM cryogenic utilization in pure Argon over large detection surfaces, 6-7th april, 2020
New design with a guard ring on both faces of the PCB (3 mm < LEM dead zone)
to mitigate risks associated with sparks causing damages to the FE electronics
2 prototypes will be ordered to PCB industrial partners ELTOS (it.) and ELVIA (Fr.).