## Slide 1: Ultrasensitive Detectors and Broadband Quantum-limited Amplifiers Based on Nitride Superconductors
NIST Quantum Devices Group
Boulder, CO
Jiansong Gao
Argonne, Sep 19, 2014

## Slide 2: An overview: TiN/NbTiN projects at Quantum Devices Group
On-chip 2D transmon qubit
TiN circuit + Al junction, T1~40 ms
NearIR
photon
counting
MKID
for QO
Quantum Sensor group
(Novel Devices Team)
Feedhorn-coupled dual-pol LEKID for Submm
Quantum material group
(Dave Pappas, Mike Vissers)
Kinetic Inductance Traveling-Wave Parametric Amplifier
detector & qubit readout
Si substrate
TiN Tc~4.5 K
TiN Tc~4.5K
Ti Tc~0.4 K
TiN growth: Tc~ 0 – 5K
Stoichiometric
TiN/Ti/TiN trilayer
Novel nonlinear
Kinetic
Inductance
Devices
(e.g. Tunable Resonator)

## Slide 3: Kinetic Inductance of Superconductor
Kinetic inductance: Lki
Electrons are bound into Cooper pairs at T<Tc

## Slide 4
Microwave Kinetic Inductance Detectors
(MKIDs)
Use superconducting resonators to sense quasiparticles
CPW: coplanar waveguide
readout tone
  Invented by J. Zmuidzinas and H. Leduc at Caltech/JPL in 2000.
Vin
Vout
Al, Nb, …

## Slide 5: Frequency domain multiplexing
In
Out
HEMT
A high electron mobility transistor amplifier (HEMT) provides ~ 4 GHz of bandwidth with Tn <5 K, allowing >1000 MKIDs to be readout with one pair of coaxial cables!
Broadband low-noise amplifier
Digital readout – 500MHz AD/DA

## Slide 6: TiN - ideal material for MKID
high Lki and responsivity
high Q
high rn ~100 mW•cm
efficient photon absorption
Leduc, etal, APL 97, 102509 (2010)
Vissers, etal , APL 97, 232509 (2010)
tunable Tc (400mK -> 0 -> 5 K)
Stoichiometric
TiN
Sub-stoichiometric
TixN , x>1
2010 started in Pappas’ group
10M
=1/Qi
Similar for NbTiN, Tc ~ 15 K
Applied to MKID in 2009
1M
Qi~30M!

## Slide 7: TiN MKID for NIR photon counting
f0 ~ 5 – 8 GHz, Q ~10 -100 k
20nm sub-stoichiometric TiN film on Si, target Tc~800 mK
100mm
1550nm
photon
frequency
dissipation
P

## Slide 8: Counting 1550 nm Photons
- Single photon resolving, DE (FWHM) = 0.27, 0.40, 0.44 for the 0-, 1-, 2-photon peak
- Fits to Possion distribution of l = 1.16
Histogram of optimally-filtered pulse height
1 ms
100ns
10000 laser pulses
J. Gao et al., APL 101 (14), 142602 (2012)

## Slide 9: TiN/Ti/TiN trilayer
Steep slope in Tc vs N2 around 1K
Difficult to reach target Tc
Si substrate
TiN Tc~4.5 K
TiN Tc~4.5K
Ti Tc~0.4 K
t
Solution (Mike Vissers): trilayer + proximity effect
M. R. Vissers et al., APL 102 (23), 232603 (2012)
Film is very uniform
Tc tunable between 0.8 – 3K
Adequate high Q (500k)

## Slide 10: Feedhorn-coupled MKIDs
BLAST: Balloon-borne Large Aperture Submillimeter Telescope
1.8 m mirror
feedhorn coupled
250, 350, and 500µm
study star formation
PI: Mark Devlin (Upenn)
BLAST | BLAST-Pol | Super BLAST-TNG
270 NTD detectors 2006 | BLAST + Single Pol. 2010 | 2000 MKID Dual –pol detector 2016

## Slide 11: POLEKID - detector concept
feedhorn -> waveguide interface-> detector wafer
Via bridges at crossing
3 detectors wafers with total 2000 MKIDs
Dual-pol on single pixel hard for TES

## Slide 12: Optical test of prototype detector
20nm trilayer TiN, Tc ~ 1.5 K
19um Si membrane (SOI) with Nb backshort
Big IDC to suppress TLS noise
Small inductor strip to boost responsivity

## Slide 13: Photon noise limited sensitivity

## Slide 14: Kinetic Inductance Traveling-wave parametric amplifier (KIT)
Solution
- Saturation power: nonlinear junction inductance -> nonlinear kinetic inductance
- Bandwidth: resonator -> traveling wave (transmission line)
Multiplexed readout of MKID detector and qubits both require broadband, high saturation power and quantum limited amplifier.
New problem to solve in KIT
Harmonic generation and shock wave formation R. Landauer, JAP 31 (1960)
Phase matching for broad bandwidth and high gain
            G.P. Agrawal, Nonlinear Fiber Optics (2001)
Josephson Parametric Amplifier (JPA) has achieved quantum-limited noise, but the saturation power is low and bandwidth is narrow.

## Slide 15: Dispersion engineering
fp
3fp
Dk=k-w/vp
…
Periodic impedance loadings create 3 stops bands.
Suppress the 3rd harmonic (prevent shock)
Make pump travel slower (phase match!)
Easy to make (a layer of metal, no junctions)
Proposed by J. Zmuidzinas (Caltech/JPL) in 2011
Demonstrated by Eom etal., Nature 8 (2012)
s
g
sl
g

## Slide 16: NIST KIT amplifier
2 cm
Z0~200W
- 20 nm NbTiN film (Tc ~ 14 K) on intrinsic Si
- 2.2-m long double spiral CPW on 2cm chip
- Klopfenstein taper for impedance transformation
C. Bockstiegel, @ LTD15
s = 2mm, sl = 6mm, g = gl =2mm
Numerical simulation: S. Chaudhuri
Design & Measurement: C. Bockstiegel
Fabrication: M. Vissers

## Slide 17: Device characterization – S21
- Low power transmission showing band structure created by periodic loadings
4K
30 mK
- Measurement config in dilution refrigerator

## Slide 18: Broadband gain – single device
Gain profile of the KIT amplifier, fp ~ 7.5 GHz, Pp~-7dBm (200mW)

## Slide 19: Broadband gain – two devices in series
Greater than 20 dB gain over 4GHz achieved!

## Slide 20
Nonlinear KI devices – tunable devices
Tunable coupler, resonator, phase shifter, filter, antenna ….
Applications in QC, detector, …
Tunable coupler
Tunable resonator
Idc
N

## Slide 21: TiN Qubit (Pappas’ group)
x
TiN circuit + Al junction
NIST: ~35 ms
IBM: ~50 ms
3D qubit: ~100 ms
(Yale, IBM)
Sandberg, APL 102, 072601 (2013)
Chang, APL 103, 012602 (2013)
x

## Slide 22: Why TiN Qubit
Qi>10M!
=1/Qi
Chang etal, APL 103, 012602 (2013)
Goal:
T1 ~ 50 ms => Qi ~ 1 M
T1 ~ 500 ms => Qi ~ 10 M
IBM TiN qubits
Only TiN Qi>10 M at high power (no 3D)
other losses, such as quasipartile, trapped flux and radiation, are already low. TLS is the only problem to address.
Open question:
Loss of bulk Si? Q > 10 M ?

## Slide 23: Summary – research theme
Kinetic Inductance Detectors
Supercond. Qubits
Quantum -limited Amplifiers
Two-level systems
TiN, NbTiN, trilayer
Micro-resonators
Our Goal:
- photon noise limited
- as sensitive as TES
Current: achieved@1.2 THz
Prob.: TLS noise
Approach:
- reduce TLS
- QL amplifier
Our Goal: quantum-limit
Current: a factor of ~3 away
Prob.: heat-sinking, yield, gain ripple
Our Goal: T1~ 500 ms
Current: a factor of ~10 away
Prob.: TLS decoherence
Approach: reduce TLS
Novel Nonlinear KI Devices

## Slide 24: Collaborators
NIST:
Detector: Joel Ullom, Jiansong Gao, Johannes Hubmayr, Dan Becker, Dan Schimidt, Jeff Van Lanen, Yiwen Wang, Gene Hilton, Leila Vale
Qubit: David Pappas, Mike Vissers, Jose Aumentado, Leonardo Ranzani
Optical: Sae Woo Nam, Ariana Lita
Imaging: Aric Sanders
……
CU: Konrad Lehnert, Christ Abeles
Caltech/JPL: Jonas Zmuidzinas, Peter Day, Rick Leduc
Stanford: Kent Irwin, Saptarshi Chaudhuri, Dale Li, Sherry Cho
UCSB: Ben Mazin, John Martinis, Clint Bockstiegel
SLU: David Wisbey
BLAST: Mark Devlin (UPenn) + Cardiff + ASU + …
IBM: Matthias Steffen, Martin Sandberg, Josie Chang …

## Slide 25
Thank you !