## Slide 1
Saptarshi Das, PhD
2. Adjunct Birck Research Scholar
Birck Nanotechnology Center
Purdue University
West Lafayette, Indiana 47907
Post-doctoral Research Scholar
Division of High Energy Physics
Argonne National Laboratory
Lemont, Illinois 60439
Current Affiliations
(June 2013 – Present)
2D Crystals – Future of Innovative Devices
Division of High Energy Physics

## Slide 2
Overview of 2D Crystals
Bandgap Engineering for Innovative Electronics
Flexible and Transparent Electronics
Conclusion
Division of High Energy Physics

## Slide 3
Overview of 2D Crystals
Bandgap Engineering for Innovative Electronics
Flexible and Transparent Electronics
Conclusion
Division of High Energy Physics

## Slide 4
Graphene
h-BN
Transition Metal Dichalcogenides
Excellent Conductor
Excellent Insulator
Natural 2D Crystals
Division of High Energy Physics

## Slide 5
Metals: ScTe2 ,TaS2 , etc.
Semiconductors: WSe2 , MoS2, etc.
Insulators: PtSe2 ,PdS2 , etc.
Superconductors: VS2 , NbSe2 , etc.
88 TMDs have been explored since 1960s
Periodic Table of Elements
Transition Metal Dichalcogenides
MX2
M = Transition Metal
X = Chalcogen
Natural 2D Crystals
Division of High Energy Physics

## Slide 6
Graphene
h-BN
Transition Metal Dichalcogenides
Excellent Conductor
Excellent Insulator
Phosphorene
Natural 2D Crystals
Division of High Energy Physics

## Slide 7
Liu, K. et al. Nano Letters, 12, 2012
Patel, P. R., et al. J.Adv.Dev.Res. 3, 2012
Physical Vapor Deposition
Hydrothermal Synthesis
Electrochemical Synthesis
Large Scale Growth
Exfoliation
Division of High Energy Physics

## Slide 8
Layered Compounds
Division of High Energy Physics
Notes: .

## Slide 9
Mo: [Kr]. 5d5.6s1
W: [Xe].4f14.5d4.6s2
For the first time we have Semiconductors with conduction electrons contributed by d-orbital
The d-orbital electronics
Periodic Table of Elements
MX2
M = Transition Metal
X = Chalcogen
Significant Change in Band-structure due to :
Charge
Strain
Heat
Light
Division of High Energy Physics

## Slide 10
Overview of 2D Crystals
Bandgap Engineering for Innovative Electronics
Flexible and Transparent Electronics
Conclusion
Division of High Energy Physics

## Slide 11
Metal Insulator Transition in TMDs
Electric Field
Mechanical Force
Thermal Gradient
Thickness Scaling
Swastibrata Bhattacharyya, et al. Physical Review B, 86, 075454, 2012
Ashok Kumar, et al. Modeling and Simulation in Material Science and Engineering, 21, 065015, 2012
Source
Drain
Gate
Substrate
Dielectric
Piezoelectric
Thermoelectric
Green Devices
Gate Tunable Electrical, Mechanical, Thermal and Optical Properties
Advanced Electronics Components
Detectors
Amplifiers
Filters
Modulators
Resonators
Ultra Low Power
High Performance
Division of High Energy Physics

## Slide 12
2 Layers
4 Layers
6 Layers
10 Layers
25 Layers
T = 300K
VDS = -0.2 V
Phosphorene
Ni
Contact
Ni
Contact
Phosphorene
5 µm
Saptarshi Das, et al. Tunable Transport Gap in Phosphorene.
under review, 2014.
Division of High Energy Physics

## Slide 13
Overview of 2D Crystals
Bandgap Engineering for Innovative Electronics
Flexible and Transparent Electronics
Conclusion
Division of High Energy Physics

## Slide 14
Exfoliation and identification of WSe2 flakes
Transfer of CVD grown graphene
All 2D Thin Film Transistor
WSe2
Graphene
20nm SiO2: Back Gate Oxide
Highly Doped Si: Back Gate Electrode
Al
Al
Electron beam lithography followed by Al evaporation to create mask for graphene etch
Oxygen plasma etch of graphene from the channel area
Division of High Energy Physics

## Slide 15
Removal of Al from the graphene-WSe2 contact interface
20nm SiO2: Back Gate Oxide
Highly Doped Si: Back Gate Electrode
Al
Al
Al
Al
Transfer of few layer h-BN
h-BN
WSe2
Graphene
Transfer of CVD grown graphene
Al
Electron beam lithography of Al etch mask for patterning graphene top gate electrode
Oxygen plasma etch of graphene
All 2D Thin Film Transistor
Division of High Energy Physics

## Slide 16
Removal of Al etch mask
20nm SiO2: Back Gate Oxide
Highly Doped Si: Back Gate Electrode
Al
Al
h-BN
Al
WSe2
Graphene
All 2D Thin Film Transistor
Division of High Energy Physics

## Slide 17
Graphene
Source
Graphene / h-BN Top Gate
Bi-Layer
WSe2
Graphene
Drain
5µm
VDS = -1.0 V
Bi-Layer WSe2 Flake
Graphene Contact
20nm SiO2 Gate Dielectric
Back Gate Transfer Characteristics
Electron Branch
Hole Branch
Mobility: 24 cm2/V.s
ON/OFF : 2x107
Mobility: 45 cm2/V.s
ON/OFF : 7x107
Ambipolar Conduction
All 2D Thin Film Transistor
Saptarshi Das, et al. All Two Dimensional, Flexible, Transparent and Thinnest Thin Film Transistor.
Nano Letters 14 (5), 2014.
Division of High Energy Physics

## Slide 18
Output Characteristics
VGS = -0.6V:0.1V:-0.3V
Transfer
Characteristics
VDS = -1.0 V
VDS = -0.1 V
Bi-Layer WSe2 Flake
Graphene Contact
h-BN Gate Dielectric
(f)
Flexible TFT on PET
Division of High Energy Physics

## Slide 19
Top Gate Transfer Characteristics
Without Strain
With Strain
3-Layer WSe2 Flake
Graphene Contact
(f)
Effect of Strain
van der Walls epitaxy compensates for strain
Division of High Energy Physics

## Slide 20
Active Device on Flexible Substrate
WSe2 Flakes
(f)
Optical Transparency
Active device was found to be 88% Transparent
Division of High Energy Physics

## Slide 21
Center for Nanoscale Materials
Thinnest Transistor Ever
All Two Dimensional
High Mobility
(100x better than a-Si)
High ON-OFF current ratio
Ambipolar
Flexible and
Transparent
Thinnest Thin Film Transistor
(3-4nm)
Saptarshi Das, et al. All Two Dimensional, Flexible, Transparent and Thinnest Thin Film Transistor.
Nano Letters 14 (5), 2014.
Wireless Detectors
Energy Efficient
Cost Effective
High Performance

## Slide 22
Overview of 2D Crystals
Bandgap Engineering for Innovative Electronics
Flexible and Transparent Electronics
Conclusion
Division of High Energy Physics

## Slide 23
Conclusion
Saptarshi Das. et al. High Performance Multi-layer MoS2 Transistor with Sc Contacts.
Nano Letters, 13(1), 2013.
Nano Letters Top 20 Cited Article of 2013
Saptarshi Das. et al. WSe2 FET with Enhanced Ambipolar Characteristics.
Applied Physics Letters, 103, 2013.
Saptarshi Das, et al., Screening and Interlayer Coupling in Multilayer MoS2
Physica Status Solidi, RRL, 7 (4), 2013.
Cover Article of the Journal
Saptarshi Das, et al. Where does the Current Flow in the Two Dimensional Layered Systems.
Nano Letters, 13 (7), 2013.
Saptarshi Das. et al. Towards Low Power Electronics: Tunneling Phenomenon in TMDs ACS Nano, 8(2), 2014.
Division of High Energy Physics

## Slide 24
Extreme Sensitivity and Tunability of 2D Crystals make them viable for Energy Efficient, High Performance and Low Cost Detector Designs
Conclusion
Division of High Energy Physics

## Slide 25
Acknowledgement
PhD Advisor
Dr. Joerg Appenzeller
Scientific Director of Birck nanotechnology Center &
Professor of Electrical and Computer Engineering
Purdue University
West Lafayette, Indiana, 47907
Collaborators
Marcel Demarteau
Wei Zhang
Richard Gulotty
Abhijith Prakash
Postdoc Advisor
Dr. Andreas Roelofs
Director of Nanoscience and Technology Division
Argonne National Laboratory
Lemont, Illinois, 60439
Use of the Center for Nanoscale Materials was supported by the U. S. Department of Energy, Office of Science, Office of Basic Energy Sciences, under Contract No. DE-AC02-06CH11357.
This work is supported by the DOE Office of High Energy Physics under DoE contract number DE-AC02-06CH11357
Division of High Energy Physics